## Slide 1
Conceptual Design Review of R2D2
4
- Engineering design -
https://indico.cern.ch/event/1003865/
CEA: M. Durante, E. Rochepault, V. Calvelli, H. Felice, P. Mallon, P. Manil, G. Minier, G. Maitre, B. Prevet, S. Perraud, F. Rondeaux
CERN: S. Izquierdo Bermudez, J.C. Perez, D. Tommasini, J. Fleiter, H. Felice
09/03/2021

## Slide 2: F2D2 ↔ R2D2
F2D2 dipole
Ltot = 1400 mm
Lss = 566 mm
4 coils = 4 graded double-pancakes
8 sub-coils (HF/LF)
Double layer
Flared ends
Layer jump + Exit jumps
External joints
R2D2 dipole
Ltot = 1300 mm without leads
Lss = 243 mm
2 coils = 2 graded single layer
4 sub-coils (HF/LF)
Single layer
Racetrack
Exit jumps
External joints
1m
F2D2_v8.A
(see 1, E. Rochepault
& 2, V. Calvelli)

## Slide 3: R2D2 engineering stakes
How to handle cables in graded coils?
How to ensure longitudinal support?
→ (Unfortunately) R2D2 is not a ‘simplified F2D2’ in all matters (see 2, V. Calvelli)

## Slide 4: Cable dimensions
HF
LF
12.58 x 1.97
Virgin, bare
12.58 x 1.25
12.88 x 2.27
Virgin, insulated
12.88 x 1.55
13.04 x 2.36
Heat Treated Insulated
13.04 x 1.61
CAD Cable
Section
(margin included)
0.15
Expansion during reaction :
+ 4.6 % thickness
+ 1.3% width
No changes in insulation

## Slide 5: Coil detailed geometry 1/3
Each coil {HF+LF, single-pancake} is designed and fabricated as one impregnated object
1 coil = 2 sub-coils = 2 unit lengths
Splicing is external → Exit jump
F2D2 layer jump design similar to FRESCA2
  HW-bend ‘S-shape’ with EW offset for clamping
  R2D2 has no layer jump but « forerunners »
Straight exit LF
Exit jump HF
(replace internal splice)
Layer jump forerunners
~336mm
FRESCA2
(see 2, V. Calvelli)

## Slide 6: Coil detailed geometry 2/3
Insulated/reacted cables dimensions (wHF = wLF = =wcbl)
Magnetic design (see 2, V. Calvelli)

## Slide 7: Coil detailed geometry 3/3
Straight section 243 mm
Extended straight section 474 mm
Minimum bending radius : (see 5, M. Durante, for experimental validation)
Magnetic design (see 2, V. Calvelli)  long lead ends!
Mechanical/geometrical contraint
Project spec. (see 1, E. Rochepault)

## Slide 8: Cable lengths
From CAD: for one {HF+LF} coil, without margins:
Overall demand including margins and additional lengths:
Cable type | Coil cable length (Lex = 200)
HF | 22,8 m
LF | 55,9 m
HF | 34 m
LF | 67 m

## Slide 9: Coil components overview
Preliminary design: details not included
Even with one pancake, each coil has two layers
  → accomodates exit jumps
  → iron filler is used to have a flat coil surface
  → iron fillers contribute to magnetic field
Titanium
Stainless steel (SS)
Iron
Insulation filler
Insulation

## Slide 10: Coil components: closeup on details
Post:
  10mm-split (tbc) for HT contraction
  Thickness variation to accomodate exits
Components insulation
  No coating
  Wrapped insulation
MQXF
HT test

## Slide 11: Coil components: splices & joints
Splicing procedure similar to FRESCA2’s
  At least 200mm extra length compatible with furnace
  Option: increasing distance between exits (see later)
Layer jump LF forerunner
Layer jump HF
forerunner
Exit jump HF
Straight exit LF
(see 5, M. Durante, for experimental qualification)

## Slide 12: Preliminary winding tooling 1/3
R2D2 winding will be performed at Saclay
Fabrication procedure is inspired from SMC and FRESCA2 feedback
R2D2 is not strictly a fabrication demonstrator for F2D2!

## Slide 13: Preliminary winding tooling 2/3
Winding of each sub-coil starts at the layer jump
Mica sheets save space for trace (on lower side)

## Slide 14: Preliminary winding tooling 3/3
Warning: this animation is based on F2D2 design (double-pancake coil)
Clamping of the jumps/exit will be similar for R2D2

## Slide 15: Heat treatment tooling concepts
Reaction performed at Saclay
Coil should be able to slide as much as possible sliding
  Mica sheets all around
  Minimal guiding features, one fix point (LE)

## Slide 16: R2D2 reaction configuration
Mold
Mold
Rail
Post
HF
LF
Y
Coil / Mold insulation
0.6
Post aligned with the insulated reacted coil
Coil / Mold insulation
(mica)
0.6
Coil / Rail insulation (mica)
0.6
Titanium (components)
SS (tooling)
Post / Coil insulation
(mica + fiberglass)
0.6
Cavity for reaction

## Slide 17: R2D2 impregnation configuration
Z
Y-Filler (during impregnation ? To be decided with a 3D CAO)
Rail
Post
HF
LF
X
Y
Mold / Y-Filler insulation
0.5
Coil / Y-Filler insulation
6+0.5
Post aligned with the insulated reacted coil
Trace + insulation
0.3+0.2
Midshim insulation
2
Coil / Rail insulation
4
Rail / Mold insulation
1
Titanium (components)
Iron (components)
Post / Coil insulation
0.6
Mold
Mold
SS (tooling)
Impregnation performed at Saclay
  2-layers coil pack integrates SS rails and iron filler that contribute to magnetic field
Impregnation process should be demonstrated on SMC

## Slide 18: R2D2 final configuration
Y-Pad
X-Pad
Y-Filler
Rail
Post
HF
LF
Midplane
X
Y
Y-Pad / Y-Filler insulation
0.5
Coil / Y-Filler insulation
6+0.5
Post aligned with the insulated reacted coil
Trace + insulation
0.3+0.2
Midshim insulation
2
Coil / Rail insulation
4
Rail / X-Pad insulation
1
Post / Coil insulation
0.6
Titanium (components)
SS (tooling & components)
Iron (components)

## Slide 19: Coil interface with structure
Coil pack integrates iron filler that contribute to magnetic field
Iron yoke
Rails
Endshoe
Fillers (iron + ins.)
Titanium post
& spacers
Pads (iron)

## Slide 20
Break for questions?

## Slide 21: R2D2: longitudinal support concepts
Goals of the longitudinal support:
  No separation in coil-ends
  Safe stress zone (<200 MPa)
External joint  small support area (red surfaces)
Long spacers  difficult to reach coil-pole contact*
« Anything you do to reduce the tails will reduce the risk » (this review, yesterday session)
Is longitudinal support required?
New concept ?
Three approaches
  Conventional
  Rigid wall support
  Internal pre-load

## Slide 22: Option 1: conventional 1/2
a) Rods + Endplates (baseline: FRESCA2c)
Pros:
Well-known
Cons:
High forces in Rods
Coil-pole separation at ultimate current
Lead end needs redesign
Asymmetric configuration of exits

## Slide 23: Option 1: conventional 2/2
b) Exit cables can be moved outwards to allow more space for Endplate contact and symmetry
c) Rods pressure is applied directly to the Horseshoe (mechanical bypass or sliding interfaces)

## Slide 24: Option 2: Hard wall support
Pros:
Simple and compact
Can benefit from Al structure contraction
No longitudinal pre-stress
Cons:
Little pre-stress at warm, only via bullets
Coil-pole separation

## Slide 25: Option 3: internal pre-load
Benefits from split Post
Pros:
« internal » pre-load, via the pole
No coil-pole separation (potentially), no overload of the conductor
Scalable
Cons:
Still requires an external structure to counter-act the force
Need for a detailed engineering study (split Rods)
Need for R&D
Risks for the project

## Slide 26: Other open questions
Cable glued on components?
Split post value?
Insulation detailed configuration
Need for additional preliminary tests?
(see 5, M. Durante)

## Slide 27: R2D2 Simplified schedule
RD-2.1 Conceptual design report F2D2/R2D2
Internal review conceptual design R2D2
Engineering Design Review EDR R2D2
Conceptual Design Review CDR R2D2
Coil Fabrication Readiness Review FRR
RD-3.1
R2D2 Cu coil
RD-4.1
R2D2 Magnet
Assembly Readiness Review ARR
RD-3.2
R2D2 Nb3Sn coils
RD-4.2b
Test reports
RD-4.2a
Manufacturing folder
 | 2020 | 2021 |  |  |  | 2022 |  |  |  | 2023 |  |  | 
 | T4 | T1 | T2 | T3 | T4 | T1 | T2 | T3 | T4 | T1 | T2 | T3 | T4
Conceptual Design | 3D mecha +quench |  |  |  |  |  |  |  |  |  |  |  | 
Engineering Design | Components + tooling |  |  |  | Other |  |  |  |  |  |  |  | 
R&D and tests |  |  | Splices | winding | heat treat. | Cu coil |  |  |  |  |  |  | 
Coil Manufacturing |  | Fabrication SMC |  |  |  | Cu coil | Nb3Sn coils |  |  |  |  |  | 
Magnet Assembly |  |  | R&D struct. | R&D struct. |  |  | Cold tests |  |  | Assembly |  |  | 
Protection |  |  | Design QH |  |  | Implementation SG | Implementation QH |  |  |  |  |  | 
Magnet Test |  |  |  |  |  |  |  |  |  | Mecha Analysis | Mecha+Magn+quench Analysis |  | 
today
RD-2.2a
SMC coil
RD-2.2b
Engineering design report R2D2

## Slide 28
Thank you

## Slide 29: References
HD1: P. Ferracin, IEEE TAS, 2005
SQ: P. Ferracin, IEEE TAS, 2007+2008
SD: H. Felice, IEEE TAS, 2007
SMC: E. Fornasiere, IEEE TAS, 2013 + other SMC ref
RMC: J.C. Perez, IEEE TAS, 2016 + CERN conv.
MQXF: E. Takala, IEEE TAS, 2021 + other MQXF ref + G. Vallone priv. conv.
FRESCA2: E. Rochepault, IEEE TAS, 2018 + G. Willering, IEEE TAS, 2019
ERMC: M. Garcia, IEEE TAS, 2020
More info: US MDP-FCC 05

## Slide 30
Spare

## Slide 31: Cable dimensions: spare
Parameter | Unit | Proposed |  |  |  | 
 |  | HF |  | LF |  | Reason of uncertainty
 |  | Value | Uncertainty | Value | Uncertainty | 
Strand diameter | mm | 1.1 | 0 | 0.7 | 0 | -
Number of strands | - | 21 | +/-1 | 34 | +/-1 | Cabling stability
Unreacted width | mm | 12.446 | +/-0.030 | 12.446 | +/-0.030 | Cabling stability +Ic degradation
Unreacted thickness | mm | 1.969 | +/-0.030 | 1.253 | +/-0.020 | 
Bare cable compaction | % | 10.5 | +/-1.5 | 10.5 | +/-2.5 | 
Packing factor | % | 84.9 | ? | 87.5 | ? | 
Pitch angle | ° | 16.5 | +/-1 | 16.5 | +/-1 | 
Transposition pitch | mm | 84.0 | +/-5 | 84.0 | +/-5 | 
Width Reaction expansion | % | 1.0 | +0.5/-1.0 | 1.0 | +0.5/-1.0 | Conductor properties
Thickness Reaction expansion | % | 3.0 | +/-0.5 | 3.0 | +/-0.5 | 
Reacted width | mm | 12.570 | +0.090 -0.150 | 12.570 | +0.090 -0.150 | Cabling+Ic degr.+Conductor
Reacted thickness | mm | 2.028 | +/-0.040 | 1.291 | +/-0.030 | 
Insulation thickness | mm | 0.15 | +/-0.01 | 0.15 | +/-0.01 | Braiding
Cable does not exist yet
ECC Baseline + Uncertainties management  F2D2/R2D2 Cable Baseline

## Slide 32: Concepts for longitudinal support
8x Exits
2x Endplate
FRESCAc could serve as baseline: « conventional approach » = 4 Rods + 2 Endplates
FRESCA2c RT load applied by symmetric Endplates on Horseshoes = 40% Fz,mag
FRESCA2c resulting load at CD = 68% Fz,mag
4x Rods

## Slide 33: Longitudinal support: benchmark
Magnet | % EMF, RT | % EMF, cold | Coil-pole | Quench behavior in ends
HD1a | 260 Mpa | ? | 85 µm | Quenches in coil-ends
HD1b | 300 MPa | ? | 35 µm | improved
SQ02a | 40 % | 70 % |  | Improvement of Iss
SQ02b | 80 % | 115% |  | 
SQ02c | 0 | 0 |  | Detraining
SD01a | 180 MPa | ? |  | Detraining
SD01b | 0 | 0 |  | 
SMC | Usually low |  |  | Quenches in coil-ends
RMC-FR2 | 5 % | 32 % | -25 MPa | Quenches in coil-ends
RMC-QXF | 24 % | 52 % | 0 MPa | Quenches in coil-ends
MQXFS1a/b, 3a |  | 50 % | -10 MPa | No clear impact
MQXFS1c, 3b/c, 4, 5 |  | 93 % | 10 MPa | 
FRESCA2a,b | 28 % | 68 % | 75 µm | No quench in the ends
FRESCA2c | 40 % | 68 % | 160 µm | 
ERMC | 64 % tbc | 89 % tbc |  | No quench in the ends

## Slide 34: Goal of the longitudinal support
No separation here
While keeping the conductor in its safe stresse zone (<200 MPa)

## Slide 35: R2D2: expected effect of longitudinal preload
Von Mises stresses < 150 MPa at nominal; < 200 MPa at ultimate (high stresses in ends)
No separation at nominal
(183 % Fz,mag)
but separation occurs with higher X pre-stress… …or at ultimate
→ Even 174% Fz,mag at CD doesn’t guarantee contact criterion at ultimate
(see 3, E. Rochepault)