## Slide 1: TD18 post-mortem SEM observation: Update
Markus Aicheler
10. Nov. 2010

## Slide 2
North sign!

## Slide 3
Contents:
Joining gap everywhere?
“To break down and not to break down”
Breakdown distributions between cells
Breakdown distributions in cell
What comes next

## Slide 4
Joining gap everywhere?

## Slide 6
Only accumulation, no pit below
Molten accumulation with molten pit below

## Slide 7
Gap is everywhere along the waveguides
Accumulation of chips visible in gaps?

## Slide 8
“To break down and not to break down”

## Slide 10
Fatigued surface
Splashes on fatigued surface
=> No breakdown!

## Slide 11
Breakdown distributions between cells

## Slide 12
Facts for part C down-stream side:
6 of 8 highest magnetic field regions exhibit this “B-Field arc”
numerous breakdown sites are located around this feature expanding in direction to the waveguide entry
wall
waveguide
waveguide
iris
Hs/Ea
REMEMBER:

## Slide 13
Part D – down stream
(Cell 18 – up stream)
6 out of 8 sites with B-Arcs
Excellent link between B-Arc and secondary craters
No symmetry in BD distribution detectable
Part E – down stream
(Cell 17 – up stream)
?
3 out of 8 sites with B-Arc initiations!
Poor link between B-Arc and secondary craters
No symmetry in BD distribution detectable

## Slide 14
Part D – down stream
(Cell 18 – up stream)
Part E – down stream
(Cell 17 – up stream)

## Slide 15
Part D – down stream
(Cell 18 – up stream)
Part E – down stream
(Cell 17 – up stream)

## Slide 16
Breakdown distributions in cell

## Slide 17
Part D -- up stream
(Cell 17 – down stream)
Part E – down stream
(Cell 17 – up stream)
No good correlation!
Orientation correct?

## Slide 18
What comes next:
Breakdown distribution on iris
Cross section through gap and B-Arc in order to assess where the gab is coming from
Breakdown distribution of Part C in order to compare both cell walls of cell 18
Strange waveguide features…