## Slide 1
Authors would like to acknowledge the support provided by European Union’s ARIES collaboration H2020 Research and Innovation Programme under Grant Agreement no. 730871.
ARIES Update – Small samples
Stewart Leith, Bing Bai, Michael Vogel

## Slide 2
Chart: Nitrogen Percentage (%)
| 8 | 10 | 14 | 18 | 22
300W | 21.7673 | 13.8777 | 13.8623 | 10.8293 | 11.7563
400W | 17.1553 | 8.6407 | 9.6973 | 8.424 | 9.67 | 6.0213
Chart: Deposition Pressure (mbar)
| 2.1999999999999999E-2 | 1.7999999999999999E-2 | 1.4E-2 | 2.4E-2
300W-8% | 21.7673 | 14.2763 | 9.632 | 20.8137
400W-10% | 6.4697 | 7.4607 | 8.6407 | 9.927
Specific trends observable in surface roughness. Decrease seen with:
  Increased Cathode Power
  Increased N2%
  Decreased deposition pressure
Related to NbN phase formation and subsequent grain morphology
HiPIMS NbN

## Slide 3
300W
HiPIMS NbN

## Slide 4
300W
400W
HiPIMS NbN

## Slide 5
300W
400W
Substrate Bias
HiPIMS NbN

## Slide 6
HiPIMS NbN
Chart: Lattice Parameter (Å)
| 4.4004136406933378 | 4.3972786287316383
5% 400W - Pressure V | 16.5 | 15.5
8% 400W - Pressure V | 15.5
8% 400W 2200mPa - Bias V | 14.6 | 9.5 | 15.5 | 11
10% 400W - Pressure V | 13 | 14.6 | 14.6
400W 2200mPa - N2% V | 13.5 | 14 | 12.3 | 11.5
300W 2200mPa - N2% V | 11.5 | 11.5 | 11.5 | 8.9
Stat Check | 14 | 8.8 | 16 | 12.8 | 11 | 15.6
Reliance of Transition temperature on Lattice Parameter. Shown by many authors.
  Large variability
  Maximum apparent at ca, 4.4Å

## Slide 7
SIS Films
Final series of HiPIMS SIS films deposited
  AlN thickness of 8nm (4off) and 30nm (3off)
  NbN thickness varied as before (100 to 200nm)
Original
SIS – 8nm AlN
SIS – 30nm AlN

## Slide 8
(1)
(3)
(2)
(4)
1
3
2
4
SIS film morphology dominated by underlying HiPIMS Structure
  NbN “superimposed” on top of Nb + AlN
SIS Films

## Slide 9
SIMS analysis completed in positive mode for a selection of ML samples
Presence of O identified with NbO, in NbN layer. Not in Nb
  Significant decrease in O content for HiPIMS NbN vs DC MS NbN film
SIS Films
Chart: Sputter Time (s)
Chart: Sputter Time (s)
DC MS NbN
HiPIMS NbN

## Slide 10
Chart: NbN Film Thickness (µm)
| 0.20401249999999999 | 0.15736249999999999 | 0.2324285714285714 | 0.10198 | 7.4896666666666653E-2
Transition Temperature | 12.58 | 11.68 | 12.88 | 12.78 | 11.98
Entry Flux | 88 | 57 | 80 | 52 | 63
SIS Films
Previous DC MS NbN SIS films
HiPIMS NbN SIS films
Coated Separately
NbN Transition temp increases with increasing film thickness
  Decreased Tc with HiPIMS NbN SIS films vs original
  DC MS NbN SIS films display equal Tc to originals.
Entry field reaches specific maximums due to film thickness depending on recipe
  Matches Kubo’s theory – Cleaner films = Thicker layer
Increased entry field for HiPIMS SIS films vs DC MS SIS films.
Chart: NbN Film Thickness (µm)
| 0.20666666666666667 | 0.15461249999999999 | 9.9449999999999997E-2 | 0.25370000000000004
TT - 899 | 15.9 | 15.8 | 15.5 | 16.1
TT - 790 | 15.2 | 15 | 15.3
TT - 927 | 14.7
EF - 899 | 39 | 38 | 34 | 33
EF - 790 | 61 | 61.5 | 59
EF - 927 | 64.5

## Slide 11
SIS Films
Chart: Applied Field (mT)
Chart: Applied Field (mT)
Best performing Hen
Best performing Htr
DC MS SIS films display smallest magnetisation loop
Highest Hen samples not necessarily smallest loop
HiPIMS NbN shows more pronounced “dip” but earlier separation. Decreased BL barrier?

## Slide 12
Next Steps
Superconducting analysis of final HiPIMS NbN and HiPIMS SIS samples

## Slide 13
Thanks for your Attention!
Authors would like to acknowledge the support provided by European Union’s ARIES collaboration H2020 Research and Innovation Programme under Grant Agreement no. 730871.

## Slide 14
Extra Slides

## Slide 15
Chart: Time (µs)
Waveform general trend indicates decreasing peak current with increasing N2%
Aging target leads to increased peak current
  Aging target similar effect to increased pressure (Iosad et al, 2011)
HiPIMS NbN

## Slide 16
0V
100V
Substrate Bias
HiPIMS NbN

## Slide 17
0V
100V
22%
5%
Substrate Bias
Nitrogen Percentage
HiPIMS NbN

## Slide 18
Chart: Substrate Bias (V)
| 50 | 75 | 60 | 30 | 0
Lattice Parameter | 4.3907 | 4.4229 | 4.3934 | 4.3802 | 4.3715
Crystallite Size | 31.4 | 11.2 | 62.7 | 27 | 20.6
Lattice Parameter dependent on specific deposition parameters. Increases with:
  Increasing substrate bias
  Decreasing Pressure
  Increasing Cathode Power
Reaches a specific minimum for N2% - related to phase formation
  Crystallite size increases with:
    Decreasing cathode power
    Decreasing N2%
    Increasing substrate bias. Except at high values due to phase change.
    Increasing deposition pressure
HiPIMS NbN
Chart: Nitrogen Percentage (%)
| 8 | 10 | 14 | 18 | 22
300W LP | 4.3907 | 4.3876 | 4.3894 | 4.39 | 4.391
400W LP | 4.4004 | 4.3959 | 4.3978 | 4.3953 | 4.3982 | 4.4013
300W CS | 31.4 | 30.1 | 17.7 | 13.4 | 9.8
400W CS | 53.6 | 20.4 | 17.1 | 18.7 | 8 | 6.9

## Slide 19
HiPIMS NbN Films