## Slide 1: Field penetration experiment
Daniel Turner
Lancaster University
Daresbury Laboratory
Notes: Working title

## Slide 2
Field penetration concept
DC magnetic field parallel to the surface
Field local to the sample surface
  Avoid edge effect.
  Allow possibility if sample scanning.
Magnetic field applied from one side of the sample to the opposing side, similar to an SRF cavity.
Applied and penetrated field measured by Hall probe sensors
HP1
HP2
Sample

## Slide 3: New Thermal radiation shields
Larger mass compared to Al radiation shields gives a better thermal stability.

## Slide 4: Table
 |  |  |  |  |  | Bratislava VSM |  |  | Laser RTU |  | STFC Field penetration |  |  | 
 |  | Sample | Substrate Treatment |  |  | B Perp (mT) | B para (mT) | Tc (K) | B Perp (mT) | B para (mT) | Tc (K) | Hfp(0) (mT) | Hfp(4.2K) | Hfp(4.5K) (mT)
Code | Origin | Material |  |  |  |  |  |  |  |  |  |  |  | 
C7 | STFC | Nb | 10µm |  | SUBU CERN | 24.1 | 150.1 | 9.35 | 0 | 0 | 9.43 | 228.82 | 183.4291 | 186.405
L13 | STFC | Nb | 10µm |  | EP | 22 | 100.3 | 9.35 | 0 | 0 | 9.42 | 219.53 | 175.816 | 0
L18 | STFC | Nb | 10µm |  | EP + SUBU | 17.7 | 61 | 9.3 | 0 | 0 | 9.87 | 190.03 | 155.6199 | 154.606
L19 | STFC | Nb | 10µm |  | SUBU | 17.3 | 73.2 | 9.2 | 0 | 0 | 9.91 | 208.15 | 170.7624 | 164.562
C1 | Siegen | Nb | 3µm |  | SUBU CERN | 15.5 | 49.6 | 9.5 | 0 | 0 | 8.25 | 160.7 | 101.6734 | 
L1 | Siegen | Nb | 3µm |  | SUBU INFN | 14.5 | 38 | 9.6 | 0 | 0 | 9.37 | 163.98 | 133.368 | 0
L9 | Siegen | Nb | 3µm |  | Tumbling | 16 | 38.6 | 9.38 | 0 | 0 | 9.03 | 148.04 | 113.059 | 0
L10 | Siegen | Nb | 3µm |  | EP | 15.5 | 32.7 | 9.38 | 0 | 0 | 8.97 | 154.55 | 122.007 | 0
L23 | Siegen | Nb | 3µm |  | EP + SUBU | 15 | 24.5 | 9.38 | 0 | 0 | 8.74 | 128.62 | 98.244 | 0
C10 | INFN | Nb | 3µm |  | SUBU5 CERN | 12 | 0 | 9.37 | 17 | 50.2 | 9.38 | 173.39 | 138.627 | 137.629
L8 | INFN | Nb | 3µm |  | Tumbling | 18 | 0 | 9.48 | 19.1 | 42.5 | 9.01 | 187.46 | 113.059 | 0
L16 | INFN | Nb | 3µm |  | EP + SUBU5 | 14 | 0 | 9.37 | 15.5 | 47.2 | 8.77 | 106.03 | 81.71198 | 72.332
L20 | INFN | Nb | 3µm |  | SUBU5 INFN | 20 | 0 | 9.58 | 23.7 | 45 | 10.36 | 179.65 | 150.1239 | 143.805
L21 | INFN | Nb | 3µm |  | EP | 18 | 0 | 9.28 | 18.8 | 45.2 | 0 | 0 | 0 | 0

## Slide 5
Notes: All the samples, hard to distinguish data like this, but can see there is a difference between each institution

## Slide 9: Best surface treatment determined by Hvp
STFC | Siegen | INFN with laser treatment
SUBU CERN | SUBU INFN | SUBU INFN
EP | SUBU CERN | Tumbling
SUBU INFN | EP | SUBU CERN
EP + SUBU | Tumbling | EP + SUBU
 | EP + SUBU | 
Notes: SUBU seems to give the best results, outlier with the STFC SUBU from INFN. Same with INFN SUBU CERN. EP seems slightly worse than SUBU for Siegen, but is better than SUBU INFN for STFC?
EP+SUBU is the worst for each institution.

## Slide 12
Notes: Increasing Hfp for each sample, but not increasing Hll

## Slide 13
Notes: Not a strong correlation between HFPE and Hll with a big jump in VSM for EP and SUBU CERN from STFC
But there is a clear correlation for thick STFC samples

## Slide 14
Notes: Some kind of correlation with Hperp and Hfp

## Slide 15: Next steps
Test how the field of full flux penetration varies with varying thickness’
Laser treated QPR disk
Move onto multilayer samples
Notes: Should I mention that the system is now fully automated?

## Slide 16: Superconducting joins

## Slide 17
Chart: T
| 2.8734359999999999 | 4.2119330000000001 | 4.997096 | 5.9991960000000004 | 7.9928520000000001 | 10.008649999999999 | 11.997669999999999
 | 232.866 | 219.76 | 213.479 | 193.145 | 156.591 | 97.991 | 26.304
Tcheck
L14 – Nb3Sn initial - 2µm
Hvp(0) = 250.37 mT
Tc = 12.76 K

## Slide 18
Chart: L14 - Nb3Sn - Repeat
| 2.7229570000000001 | 4.2057460000000004 | 4.9916429999999998 | 5.999371 | 8.0013799999999993 | 10 | 12.00009
 | 218.395 | 207.737 | 199.429 | 184.436 | 138.555 | 83.691 | 29.678
Tcheck
Nb3Sn – Repeat - 2µm
Hvp(0) = 232.2 mT
Tc = 12.72 K

## Slide 19
Chart: L15
| 2.781072 | 3.0069720000000002 | 4.2028100000000004 | 5.0021100000000001 | 6.0026020000000004 | 7.0020600000000002 | 8.0010739999999991
New method | 186.249 | 188.093 | 165.779 | 147.92 | 123.32 | 94.527 | 56.381
Tcheck
L 15 Nb3Sn - 2µm
Hvp(0) = 206.82 mT
Tc = 9.42 K