## Slide 1: Epoxy composites for application in superconducting magnets
Pascal Studer
Laboratory for Soft Materials

## Slide 2: Structure of the presentation
  Motivation
  Engineering approaches
  Examples / research
  Experimental tools for preparing SENB samples
  Conclusion & Outlook

## Slide 3: Superconducting electromagnets
Particles guided by magnetic fields
  Electromagnets, Lorentz force
  Operated in the superconducting state at very low temperatures
  Superconductor: NbTi / Nb3Sn
CHART
  CH-Accelerator Research & Technology
  Collaboration CERN,ETH, EPFL
resulting B-field direction
Particle trajectory
1 Motivation

## Slide 4: Requirements for epoxy application in superconducting magnets
Aluminum bronze
Epoxy (or other)
Superconductor
T = 4.2 Kelvin
Function of the epoxy:
  Keeping the superconductors in place  high modulus, high fracture toughness
  Electrical insulation  Electrical insulator
1 Motivation
Processing requirements
  No outgassing  Cross-linking without emission of volatiles & low volume change
  Long pot-life  Low initial viscosity, slow reaction
Other requirements
  Radiation stability
  Operation at cryogenic temp. (~4 K)  matching of thermal expansion coefficients

## Slide 5: The causal chain of why research is needed
Cooling to cryogenic temperature leads to thermal stresses
Strong magnetic fields exert forces on conductors
Above a critical stress, the material releases elastic energy by cracking or localized yielding
The released energy is dissipated as heat
Approaching 0 K, heat capacity of almost all materials vanishses
Thus, cracks and yielding result in significant local temperature increases at 4 K
Superconductor becomes resistive above a critical temperature and given current density
Shutdown of the magnet
Significant cost factor
1 - Motivation

## Slide 6: Possible approaches to solve the problem
Prevent thermal stresses
 matching of thermal expansion coefficient to superconductor and metal (outside)
Increase KIc
 prevention of cracking
Control yielding behaviour
Increase heat capacity
 prevent temperature increase to above critical temperature
Increase thermal conductivity
 reduce the peak temperature
Finding new superconductors with higher critical temperature
 not part of my work
2 – Engineering approach

## Slide 7: Definition of fracture thoughness
2 – Engineering handles
Many engineering materials fail well below their theoretical strength.
Irwin found an approximation for the solution near the crack tip:
Thus, the stresses at a specific location near the crack tip defined by θ and r depend on the factor defined as the stress intensity KI:
The singularity at r=0 suggests that all materials fail for a > 0 and σꝏ > 0. However, every material some plasticity or microcracking at the crack tip.
The critical value of KI at which failure occurs is an intrinsic material property, the so-called „fracture thoughness“ KIC.
Plastic zone size, dugdale model
CTD-101K (LN2): 3.07 microns
r
θ

## Slide 8: Different ideas of epoxy composites for increasing K1c
Rubber toughening
Incorporate soft but tough particles in epoxy matrix
Different mechanisms
  Matrix crazing (Formation of many small crazes increases energy-release rate, adhesion dependent, low modulus required to prevent debonding particle/matrix)
  Shear yielding: Interaction between stress fields around particles leads to shear bands, acting as an energy-dissipative mechanism, facilitated by cavitation of the rubber (increasing von Mises stress)
Not applicable! Below Tg, rubber is not soft anymore
3 Examples & Research
Matrix crazing
Rubber
Epoxy
Particle toughening
Incorporate hard particles (micro/nano)
  Yielding of epoxy around particles
  Crack deflection  increase in crack surface area
Possible sedimentation (microfillers)
Possible aggregation (nanofillers/particles)
Plane stress – tensile  yielding
Shear yielding
Ceramic

## Slide 9: Epoxy with TiO2 nanoparticles
Preparation procedure
1. Nanoparticle suspension
Oleylamine
TiO2
CHCl3
2. Mix particle suspension with hardener or resin
3. Remove CHCl3 with roto-evap
4. Mix hardener & resin  curing
Epoxy resin:
Some hardeners:
HY 5922
CTD-101K Part B
3 Examples & Research

## Slide 10: Epoxy with TiO2 nanoparticles (MY750 resin)
STEM images: Tecnai F30, FEG, 300 kV (ScopeM)
TEM samples prepared by ultramicrotomy
Agglomeration
Bright Field
Bright Field, zoom in
STEM mode HAADF
3.9, 3.7, 3.4 nm
FFT of BF img
3 Examples & Research
Thanks to Fabian Gramm (ScopeM, ETHZ)

## Slide 11: Different ideas of epoxy composites for increasing K1c
Crack bridging
Epoxy-aramide nanofiber composite
Toughening by fiber bridging over crac
Process:
  1. Dissolution of aramide in DMSO/KOH/(H2O) polyanion solution
  2. Precipitation by adding proton donor (H2O
  3. Filtration / Drying / Characterization
  4. Incorporation into epoxy
Jung et al., 2020 (Polymer)
Epoxy
3 Examples & Research
Aramide fiber / DMSO / KOH solution
After stirring for 5 days
OH-
OH-
OH-
Interactions:
Electrostatic
Van der Waals
Aromatic
1
2
H+
1 um
10 nm
Jung et al., 2020 (Polymer)
Notes: Graph vergrössern

## Slide 12: Results on preparing aramide nanofiber colloidal solutions
0.2% solution
0.2% aramide in DMSO/KOH
KOH pellets
Stirred 7 days
Precipitated with proton donor H2O (added 0.5 mL/mg of aramide)
Formation of a colloidal gel
3 Examples & Research
2% solution
2.3% aramide in DMSO/H2O (1:25)
KOH pellets crushed
Stirred 9 hours
Precipitated with proton donor H2O (added 0.5 mL/mg of aramide)
Forms clumps
Problem: Not fully dissolved (next slide) & concentration
Notes: Graph vergrössern

## Slide 13: Preparation times for aramide polyanion solutions
3 Examples & Research
Composition (1:25 H2O/DMSO), KOH | Preparation method (RT) | 6h | 24h | 
1 % aramide sol. | Stirred, 400 rpm |  |  | 
1 % aramide sol. | Tumbler, ~80 rpm |  |  | 
2 % aramide sol. | Tumbler, ~50 rpm |  |  | 
Notes: Graph vergrössern

## Slide 14: Aramide nanofibers, open questions
3 Examples & Research
Preparation of dried nanofibers for application from higher concentrated solutions (1%, 2%, 4%,…)
  What happens when the concentration of proton donor is slowly increased instead of instantaneous mixing?
  Dilution necessary before precipitation? Influence on microstructure?
  What would be an appropriate diluent? (aprotic, polar, basic)
    Acetone, EtOH+KOH, H2O+KOH, ?
What is the influence of temperature on both aramide dissolution and precipitation?
Effect of nanofibers in epoxy on pot-life viscosity?
How do the fibers align during infusion of dense structures?
Notes: Graph vergrössern

## Slide 15: Different ideas of epoxy composites for increasing KIc
Pre-stressing (internal pressure)
Idea: incorporate nascent UHMWPE (highly crystalline) particles into epoxy
After curing, melt the UHMWPE  lower crystallinity  specific volume goes up  pre-stress closes cracks
Chain explosion  improved adhesion?
Melting
UHMWPE
Epoxy
Pre-stressed
material
3 Examples & Research
Notes: Graph vergrössern

## Slide 16: UHMWPE in Epoxy (CTD-101K)
First trial
  Simply mixing GUR 4120 (commercial UHMWPE grade) with epoxy, degassing according to standard protocol & curing
    White layer on top
    Probably due to trapped air
3 Examples & Research
Second trial
  Mixing GUR with liquid hardener (part B)
  Degassed 10 mBar, 60 °C, 30 min  bubbling
  Mixed with other components, degassed, cured, ultrasonic bath 2 min
  Similar result
  Air is entrapped since top level sank
Third trial
  Suspending GUR in ether (lower density  sediments)
  Centrifugated, tip sonicated & centrifugated again
  Now cured
Notes: Bild einfügen

## Slide 17: Possible approaches to solve the problem
Prevent thermal stresses
 matching of thermal expansion coefficient to superconductor and metal (outside)
Increase K1c
 prevention of cracking
Increase heat capacity
 prevent temperature increase to above critical temperature
Increase thermal conductivity
 reduce the peak temperature
Finding new superconductors with higher critical temperature
 not part of my work
3 – Examples & Research

## Slide 18: Combined approach: heat capacity & thermal expansion match.
Zirconium tungstate (ZrW2O8)
negative coefficient of thermal expansion (α = ⎼7.2 * 10-6 K-1) of ZRW2O8
 overall reduction in thermal expansion coefficient
 thermal stresses are distributed throughout epoxy rather than on interface superconductor/epoxy/metal
Schematics of Zirconium Tungstate and the
RUM mechanism
10.1007/s10853-009-3692-4
+ Gadolinium Oxide (Gd2O3) composite
Gadolinium oxide has anomaly in heat capacity at ~3K  where the magnet is operated
Cracking and yielding would result in lower local temperature rise
Heat capacity of GD2O3
10.1016/j.jct.2005.02.014
3 Examples & Research

## Slide 19: Measuring KIc for filled epoxy composites
Single-etch notch bend samples (SENB)  difficult preparation
F
The test setup
Sample
Sample
Tapping on blade
Sample preparation
Sample
Pressurized area
Controlled force
Stopping the crack
4 – Experimental tools

## Slide 20: Measuring KIc for filled epoxy composites
Device design
  Controlled force
  Most parts 3D printed
  Except force transmitter (CNC)
In progress…
4 – Experimental tools

## Slide 21: Conclusion & Outlook, questions
Further research
  Explore toughening of epoxy composite with nascent UHMWPE and PTFE
  Fabricate aramide nanofiber epoxy composite
  Finish the sample notching device, obtain reliable KIc values
Thanks
  André Brem, Bernhard Auchmann and Theo Tervoort for their support
  Fabian Gramm (ScopeM) for support with TEM imaging
  Chris for helping with the design of the improved sample notcher
5 - Conclusion