## Slide 1: DETERMINATION OF PHOTONEUTRON PRODUCTION FROM DIFFERENT TARGETS IRRADIATED BY ELECTRON BEAM
Elmira Melyan
23th June 2021

## Slide 2: Contents
Introduction
Experiment
Methodology
Experimental results
Simulations
Results comparison
Conclusion

## Slide 3: Introduction
neutron activation analysis
ADS
LINAC technology is attractive for ADS
Commercially available
Are in common use
Physically small
radioisotope production
nuclear waste assay

## Slide 4: Experiment
A.I. Alikhanyan National Laboratory, YerPhi, Yerevan, Armenia
LUE-75 Linear Accelerator Facility
Energy: 70 MeV
Photoneutron converters: BeO, D2O
Samples were irradiated 3.8 h and 3.05 h respectively

## Slide 5: Materials Irradiated Thicknesses and weights of the sample
Material | Molar Mass | Thickness (mm) | Weight (g)
Al | 26.98 | 0.5 | 0.2150
Y | 88.91 | 0.25 | 0.1641
In | 114.82 | 0.1 | 0.1060
Co | 58.93 | 0.5 | 0.7174
Cu | 63.55 | 0.125 | 0.4019
Bi | 208.98 | 0.5 | 0.7276
Ta | 180.95 | 0.125 | 0.3069
Au | 196.97 | 0.0125 | 0.0401
Nb | 92.91 | 0.5 | 0.3341
Mn | 54.94 | 0.05 | 0.0982

## Slide 6: Experimental Setup
W
Al-Cylinder
Al-Monitor
Converter
Foils
4.4 cm
0
15.4 cm

## Slide 7: Methodology
Induced activity method was used (Off-line analysis).
Advantages:
Lower boundary of the element recording, involves the activation of the material by n, γ or charged particles.
Allows to investigate the production mechanism of the residual nuclei in a wide mass range.
Characteristic γ ray spectra of emitted residual nuclei in the target are measured by HPGe detectors.
Obtained gamma ray spectra were analyzed by DEIMOS software

## Slide 8: Experimental Results
Sample | Reaction | BeO | D2O
Nb | (n,2n) | 4.24E-28 | 2.12E-28
Ta | (n,a) | 9.77E-29 | 3.56E-30
 | (n,2n) | 9.49E-28 | 7.52E-28
Y | (n,a) | 1.12E-29 | 8.84E-30
 | (n,2n) | 8.90E-28 | 7.05E-28
 | (n,3n) | 7.32E-29 | 5.80E-29
Al | (n,a) | 1.11E-30 | 1.64E-30
Cu | (n,g) | 2.11E-30 | 1.67E-30
 | (n,3n) | 2.21E-29 | 6.24E-30
Mn | (n,g) | 6.01E-31 | 6.01E-31
 | (n,2n) | 6.42E-31 | 1.35E-30
Sample | Reaction | BeO | D2O
Co | (n,a) | 8.91E-31 | 9.39E-31
 | (n,2n) | 2.91E-28 | 3.84E-28
 | (n,3n) | 5.93E-29 | 6.97E-29
Bi | (n,a) | 7.36E-29 | 6.65E-29
In | (n,a) | 1.95E-30 | 1.62E-30
 | (n,p) | 1.67E-30 | 1.32E-30
 | (n,g) | 1.64E-29 | 2.88E-29
 | (n,3n) | 1.53E-29 | 1.21E-29
Au | (n,a) | 5.59E-29 | 6.63E-29
 | (n,g) | 1.97E-29 | 2.16E-29
 | (n,2n) | 2.27E-27 | 2.89E-27

## Slide 9: MCNP Simulation

## Slide 10: Neutron Flux Visualisation

## Slide 11: Photoneutron energy distribution

## Slide 12: Neutron energy distribution

## Slide 13: Neutron energy distribution

## Slide 14: Reaction Rate

## Slide 15: Comparison (n, 2n)

## Slide 16: Comparison (n, g)

## Slide 17: Comparison (n, a)

## Slide 18: Conclusion
A set of targets were irradiated by electron beam using two different neutron converters
Reaction Rates were calculated as a result of experiments
Simulations were done by MCNP software, where neutron fluxes and reaction rates were calculated for each sample. Both cases results were similar, however neutron fluxes for BeO-converter case are slightly higher
Reaction rates which are common for all cases were compared showing overall agreement between experimental and theoretical investigations

## Slide 19
Thank You
for Your Attention