## Slide 1
LXXI International Conference «Nucleus-2021»
CARBON NANOMATERIALS APPLICATION FOR ISOL-METHOD OF HEAVY ION FUSION REACTION PRODUCTS
Joint Institute for Nuclear Research
Flerov Laboratory of Nuclear Reactions
Presenter: Viacheslav Vedeneev

## Slide 2
Separation of heavy ion fusion reaction products
Catchers: Solid Liquid Gas
Main requirements:
Enough separation efficiency;
Separation time – in order of SHE isotopes lifetime.
Catcher material characteristics:
1. High temperature stability (D=D0exp(-Q/RT)). D0 – diffusion factor, Q – activation energy.
2. High porosity.
Porous graphite – polygraphene

## Slide 3
Two well-known volatile superheavy elements: Cn (Z=112) and Fl (Z=114).
Some isotopes have long enough decay time:
283Cn – 3.8 s, 285Cn – 29 s, 289Fl – 2.6 s.
Favorable reactions: 242, 244Pu+48Ca
Solid ISOL method application for Superheavy nuclei
mass measurements
Separation time –
order of seconds
Separation efficiency – quite enough
Notes: The experiments performed at FLNR JINR showed that some of the nuclei with Z=112 and 114 have long enough half-lives, e.g., 3.8 s for 283Cn, 29 s for 285Cn, and 2.6 s for 289Fl.These elements are volatile. It means that the ISOL method can be applied for investigation of these elements
There are special requirements for the hot catcher in studies of short-lived superheavy nuclei that have low production cross-sections. The necessary separation time should be about ~ 1 s and the necessary efficiency must be higher than 10 %.

## Slide 4
Setup | Catcher | Target thickness | Transport temperature | Separation time, s | Separation efficiency, %
ISOLDE-SC | Liquid lead | 170 g/cm2 | ≤ 1000 K | 30 | 7.8
MASHA | Polygraphene paper | 0.06 g/cm2 | 293 K | 1.8 | 0.07
Comparison of ISOL systems at ISOLDE-SC and MASHA
ISOLDE-SC: p+ + natPb
MASHA: reaction 40Ar+144Sm
Application of ISOL method for heavy ion induced reaction
Main characteristics of ISOL systems are:
1. Separation efficiency;
2. Separation time.
Notes: Представлена твердотельная ИЗОЛ система, использующаяся на масс-сепараторе МАША для сепарации продуктов полного слияния под действием тяжелых ионов. В качестве горячего поглотителя продуктов реакций применяется полиграфеновая фольга.
The use of porous graphite as the hot catcher improves the time characteristics and the efficiency of extraction. At ISOLDE a liquid lead target is used as the hot catcher to provide a better diffusion of particles. At MASHA the extraction time was 1.8 s as compared with 30 s at ISOLDE. A separation time of 1.8 c of the MASHA setup seems to be a convenient value for the experiments on measuring the masses of superheavy elements. Since the production cross-sections of superheavy elements are of a few picobarns, the total efficiency of separation have to be more than 10 %.

## Slide 5
MASHA (Mass Analyser of Super Heavy Atoms)
MASHA setup is a combination of ISOL method of synthesis and separation of radioactive nuclei with the classical method of magnetic mass analysis, allowing identification of the synthesized nuclides in the wide mass range (A = 1 – 450 a.m.u.).
Poly-graphene paper, density of 0.5 g/cm3 (porosity – 75%). It is possible to produce as a paperboard with thickness 0.6 mm
Operating temperature of hot catcher – 1800-2000оС.
Delivery time of nuclides to the ECR ion source ~ 1.8 s.
ECR ion source: ionization efficiency – up to 90% for noble gas.
Operation pressure – 10-5 mbar
Middle
Notes: Установка MASHA представляет собой ..
В качестве горячего поглотителя продуктов реакций применяется полиграфеновая фольга.
The hot catcher is a very important component for the set-ups that use the ISOL method since the efficiencies of extraction of nuclides depend on its properties. The analysis of different materials shows that a good choice for the hot catcher is porous graphite due to its time characteristics and the efficiency of extraction.

## Slide 6
Separation efficiency of MASHA setup as a function of measurement time.
During the experiment, a detailed study of efficiency and reliability of all systems was carried out. It was observed that the separation efficiency of MASHA setup is not stable during the experiment in the case of high beam intensity (typically 10 mA of 48Ca). The high beam intensity corrupts the Hot Catcher and the separation efficiency of the Hot Catcher decreases by almost ten times during a few days.
Limitations of the method for experiments with heavy ion beams
First attempt of determination of mass of Cn and Fl elements as daughter products of the reaction 48Ca+242Pu (2015)
Target: 242Pu (0.49 mg/cm2) with an admixture
of Nd isotopes (~ 1%).
Poly-graphene paper after irradiation (300 h).
Beam current (48Ca) ~ 0.5 pmA.
Electrical volume power density – 2 kW/cm3
Ion irradiation power density – 8 kW/cm3
(ion beam intensity 0.5 pmA)
Notes: Выполнены измерения зависимости эффективности от времени облучения при интенсивностях пучков тяжелых ионов вплоть до 0,5 pmkA.
Измерения эффективности проводились в реакции Ca+Nd благодаря специальной конструкции мишени.The target of 242Pu (0.49 mg/cm2) had an admixture of Nd isotopes (~ 1 %). During the experiment the yields of mercury isotopes produced in the reaction 48Ca+natNd were measured. The yield of 185Hg was tested each day.
Обнаружено, что снижение эффективности сепарации связано с изменением структуры горячего поглотителя из полиграфена. Предложена новая конструкция горячего поглотителя.

## Slide 7
New design of the hot catcher: “Separated” graphite heater + catcher made of 1,1 mg/cm2 graphene foil or carbon nanotube paper 6,4 mg/cm2 thicknesses.
Installation of 16-strip silicon detector at the middle plane F1 (permanent control of the separation system by measurement of Hg yield).
New design ECR ion source and the vacuum chambers for ECR ion source, catcher and transport line: chemical inert covering of the inner part of the vacuum chambers; heating of the vacuum chamber at the temperature 300C.
Modernization of the MASHA setup
Notes: Была выполнена модернизация установки MASHA которая включает в себя …

## Slide 8
New materials: graphene and carbon nanotubes
Graphene/nanotube paper foil
Polygraphene heater
Shield

## Slide 9
New arrangement of rotating target and separation system
Target for test experiment: irradiation stability of the new design hot catcher and synchronous measurement of products of the reactions 40Ar+144Sm and 40Ar+166Er
Rotating target wheel
144Sm
(6 sectors)
166Er
(6 sectors)
Polygraphene Heater
Graphene/Carbon nanotube catcher foil
Ion
beam
To ECRIS
Target
Notes: The new version of the hot catcher was designed. It includes now a poly-graphene heater and a thin catcher made of 2 mg/cm2 graphene foil or carbon nanotube paper. This construction has to prevent the catcher from heating and radiation destruction.
The ECR ion source with a special ceramic coating was developed and tested.
A special construction of a rotating target wheel was developed. The target wheel consists of the 6 identical sectors: 3 of 144Sm and 3 of 166Er. This target construction allows us to measure simultaneously in the test experiment the reaction 40Ar+144Sm at the intermediate plane F1 of spectrometer and the reaction 40Ar+166Er at the focal plane F2.

## Slide 10
40Ar + 144Sm → 184Hg
40Ar + 166Er → 206Rn
Strip detector at the intermediate focal plane F1
for control of the separation system
Test experiment:
F1: 40Ar+144Sm184Hg
F2: 40Ar+166Er206Rn
Experiment with superheavy elements:
F1:48Ca+142Nd184Hg
F2:48Ca+242Pu290Fl
Middle
M/ΔM=1600-3000
M/ΔM=40-70
Notes: The additional strip detector was placed at the intermediate focal plane F1 to control the separation efficiency during the experiment. It registers permanently the products of the complete fusion reaction 48Ca+natNd which takes place due to the admixture of Nd in the target, providing the Cn nuclei have to be detected in the focal plane detector.
In the test experiment we carried out simultaneously the reaction 40Ar+144Sm at the intermediate plane F1 and the reaction 40Ar+166Er at the focal plane F2.

## Slide 11
Separation efficiency of isotope 185Hg as a function of time measured with polygraphene catcher in two different reactions. 185Hg was measured at the middle plane of MASHA separator in the reaction 48Ca with natNd admixture in both targets.
Separation efficiency of Rn and Hg isotopes as a function of time measured simultaneously with graphite nanotube catcher for beam energy in the middle of the target 218 MeV. Rn isotopes – at the focal plane (F2), Hg isotopes – at the middle plane (F1) of MASHA separator.
Efficiency stability of the hot catcher from carbon nanotubes

## Slide 12
Time response of MASHA separator for two different solid hot catcher designs. Blue line – new design with nanotube paper. Green line – old design with polygraphene.

## Slide 13
New design of the hot catcher: test on the ion beam shows the perspective of the new materials
Installation of the strip detector at the middle plane F1 gives the permanent control
New design ECR ion source and the vacuum chambers for ECR ion source, catcher and transport line
Chemical inert covering of the inner part of the vacuum chambers – test experiment started
Conclusion: current status of modification of MASHA spectrometer
Notes: For the MASHA mass-spectrometer a series of improvements of setup parameters was performed…

## Slide 14
Staff and the acknowledgements
A.M. Rodin, L. Krupa, E.V. Chernysheva, A.V. Gulyaev, A.V. Gulyaeva, M. Holik, J. Kliman, P. Kohout, A. Kohoutova, A.B. Komarov,
A.S. Novoselov, A. Opichal, J. Pechousek, A.V. Podshibyakin,
V.S. Salamatin, S.V. Stepantsov, V.Yu. Vedeneev, S.A. Yukhimchuk.
Sincere gratitude to:
FLNR U-400M acceleration complex for a qualitative ion beam;
FLNR engineering staff for the experiment support;
Saint-Petersburg University and NUCLEUS-2021 for organizing the online conference;
listeners – for your attention!
LXXI International Conference «Nucleus-2021».