## Slide 1
Status of coated conductor cables for high field magnets
D. Uglietti
Ecole Polytechnique Fédérale de Lausanne (EPFL), Swiss Plasma Center (SPC), CH-5232 Villigen PSI, Switzerland
Background – magnets and HTS materials
Cables: fusion magnets and dipoles
Achievements
Non-twisted stack concepts
Summary
Based on:
2019 A review of commercial high temperature superconducting materials for large magnets: from wires and tapes to cables and conductors https://dx.doi.org/10.1088/1361-6668/ab06a2
2020 Non-twisted stacks of coated conductors for magnets: Analysis of inductance and AC losses https://doi.org/10.1016/j.cryogenics.2020.103118

## Slide 2
 Je must be high
Small bore
R/r >> 1
Bpeak/B0 ~ 1
Thick winding
r
B0
R
Bpeak
High field dipoles (and solenoids)
Fusion magnets
 Je is not so important
R/r ~ 1
Bpeak/B0 > 1
Thin winding
Large bore
r
R
B0
Bpeak
Operating current
about 30–100 kA
(50-300 tapes)
About 5–30 kA
(10-50 tapes)
Background – magnets
Magnet type influences the cable design
High field and/or large size  large stresses

## Slide 3
1
1
>5
Bi2212
Bi2223
REBCO
Round, twisted, fine filaments are not requirements.
In fact, the first HTS commercial magnets (NMR) was made with coated conductor (non-round, non-multifil., non-twisted).
REBCO is the youngest  largest margin of improvement
Production capacity and Je are still growing fast
Background – technical HTS
Je(4.2 K, 15 T) Long. ten. stress Trans. comp. stress
Table 1 in https://dx.doi.org/10.1088/1361-6668/ab06a2
N. of manufacturers
REBCO is the weakest in some directions (peeling, …)
What will be the commercial application? MRI for NbTi (3000 t/y), NMR for Nb3Sn (50 t/y?)
REBCO: wind turbines, NMR, compact high-field tokamak?
https://doi.org/10.1038/s41598-021-81559-z

## Slide 4
Stacked slotted matrix (ENEA)
Cables for fusion magnets
Twisted stacked, round or flat (SPC)
Twisted stacked, round (KIT)
VIPER (Commonwealth Fusion)
CORC multi-stage (CERN)
Operating current: 30–100 kA
Two cabling stages

## Slide 5
Cables for high field dipoles
CORC cable – Canted Cosine Theta (Berkeley)
Tapes in layer 4 had not homogeneous properties.
Ic reduction in layer 4 (too tight bending); more flexible cable in development
Field quality affected by screening current (as usual)
Quench detection is not an issue, but one cable was damaged after thermal runaway (perhaps too high contact resistance between tapes?)
2.9 T at 4.2 K, 6290 A, 100 m of CORC
CORC: 30 tapes (2 mm wide),
3.8 mm , Cu/nonCu=1
https://doi.org/10.1088/1361-6668/abc2a5
Operating current: 5–30 kA
One cabling stages
CORC ha relatively low Je (0.55 x tape Je)
Stress concentration (CCT avoid it)
45%
4
2.5

## Slide 6
Cables for high field dipoles
REBCO Roebel cable - aligned block (CERN)
Ends were re-designed to account for Roebel cable characteristics
Magnetic field almost aligned to the wide face of the tape: Ic increment and lower magnetization
REBCO Roebel cable - Cos theta (CEA)
https://doi.org/10.1109/TASC.2020.2978788
Roebel cable trajectories are different from Rutherford cable ones
Insulated with glass sleeve
https://doi.org/10.1088/1361-6668/aab887
https://doi.org/10.1109/TASC.2018.2820177
Roebel Je>0.9 tape Je
Large critical compressive stress

## Slide 7
Roebel Je>0.9 tape Je
Large critical compressive stress
Material waste during punching (could be avoided)
CORC ha relatively low Je (0.4–0.6 x tape Je)
Stress concentration (CCT avoid it)
Achievements
Roebel and CORC were intensively investigated.
Both are very flexible.
Both can be produced in long length (hundreds of meters).
Various tests have shown that quench detection in coated conductor cables is not critical: non-inductive voltage taps are sensitive enough to detect early voltage development (current sharing among tapes).

## Slide 8
REBCO Twisted stacked – block coil (University of Grenoble/NEEL/Ge2LAB)
Why twisting once per turn?
How much twisting needs a stack?
https://doi.org/10.1109/TASC.2017.2677470
Roebel and CORC are the best way to assemble tapes in cables?
Anything else?
Achievements

## Slide 9
Achievements
HTS can withstand large transient perturbations (flux jumps, AC losses, current redistribution, …)
Twisting a stack has modest impact on stability, losses and inductance mismatch among tapes. https://doi.org/10.1016/j.cryogenics.2020.103118
LTS
HTS
Jc
T
Jc
T
Coated conductor cable designs were mostly copied from LTS cables.
LTS strand and cable requirements and designs (1960-1980) based on physics.
Strand microstructure and cable design driven by stability
Tapes and wire characteristics are driven by manufacturability and maximising Jc
How much twisting needs a stack? Probably no twisting is fine.

## Slide 10
AC losses background
Twisting a stack provides a modest (<35%) reduction of losses.
Bac>>Bp
Coupling loss
Hysteretic loss
Saturated coupling loss
D/d100
D
d
Bac>>Bp , for a given dB/dt
D/d3
/21.6
dB/dt
dB/dt
dB/dt
Large loss means large magnetization loops, affecting field quality.
D
d

## Slide 11
AC losses background
Three necessary conditions to achieve loss reduction (needed for LTS stability):
Twisting 
Twist pitch < 
Fine filaments (50–200 smaller than wire/cable size) 
In coated conductors stacks and cables :
Twisting 
Twist pitch < Usually not investigated ?
Fine filaments (tapes and stack have roughly the same size) X
Only twisting was copied. Why?
Twisting has advantages:
twisting provides cable flexibility (CORC, VIPER)
In multistage cable, twisting the stacks (1st stage elements) could provide a moderate AC loss reduction

## Slide 12
Brookhaven Technology Group Inc. ExoCable™
Stacked, non twisted
Y. Yanagi,NIFS, 2014
Short piece length, originally proposed to simplify construction of helical coils. It can works also on long length
2.4 mm
1.2 mm
https://doi.org/10.1088/1361-6668/ab0b9c
https://doi.org/10.1109/TASC.2019.2902420
8 REBCO layers
Department of Electrical Engineering Shanghai Jiao Tong University
Non-twisted concepts
S. Lelekov
ASC2014 and ASC2020
Of course, any Bi2223 magnet: …
https://doi.org/10.1109/TASC.2013.2239342
https://doi.org/10.1109/TASC.2016.2524466
3 T MRI
3.6 T +21 T NMR
https://doi.org/10.1109/TASC.2017.2657689
https://doi.org/10.1088/1361-6668/aa6676
10 T + 25 T LTS
Any significate difference?
https://doi.org/10.1016/j.cryogenics.2016.06.011

## Slide 13
Non-twisted concepts
T. Painter, NHFML
Perhaps better suited for dipoles:
Co-wound tapes
Non-insulated (turn-to-turn)
Coaxial formers
Formers reinforce previous layer (no-gap insertion)
Co-wound tapes
Non-insulated
O1B.2-1 Thomas Painter, First test results of the integrated coil form technology, TOFE 2020
Paul Scherrer Institute (PSI) has acquired Tokamak Energy’s proprietary magnet technology for use in PSI’s accelerator and beam line applications.
https://www.tokamakenergy.co.uk/tokamak-energy-and-switzerlands-paul-scherrer-institute-sign-collaboration-and-license-agreement-for-magnet-technology/

## Slide 14
12 mm
CuBe tape, 100 μm
CEA dipole, 2016
2 tapes per stack
4 tapes per stack
8 tapes per stack
Non-twisted stack for dipole
It is allowed to stack more than 2 tapes…
2 tapes per stack
Applied to Bi-2223:
https://doi.org/10.1109/TASC.2003.812398
https://doi.org/10.1016/S0921-4534(02)01133-4
Campbell, 1982: “… a thin conductor … in the direction perpendicular to the field”.
https://doi.org/10.1016/0011-2275(82)90015-7
Block dipole with non-twisted stack https://doi.org/10.1016/j.cryogenics.2020.103118 section 5.2
https://doi.org/10.1109/TASC.2018.2796063
https://doi.org/10.1109/TASC.2018.2809780
Screening currents deteriorate field quality
Perhaps magnetisation is reduced

## Slide 15
Perhaps replacing CORC with a stack?
from 2.9 T to >6 T
Non-twisted stack for dipole
Relaxing twisting/transposition requirements enlarge the design space.
Non-twisted concept opportunities:
Simple geometries and manufacturing
The highest current density (same as tape Je)
Critical transverse stress similar to the tape value
Sometimes, moderate increase in Jc (field almost paralle to ab plane)
CORC cable – Canted Cosine Theta (Berkeley)
https://doi.org/10.1088/1361-6668/abc2a5
2.3 x Iop
How to generate higher field?
Iop
22%
35%
43%
100%

## Slide 16
About project management: requirements and design choices (twisting, impregnation, …) for HTS should be based on rigorous physical analysis and motivations.
LTS have completely different requirements and characteristics than HTS.
Why copying technical solutions from LTS to HTS?
Summary
Non-twisted concepts enlarge the space design, simplify manufacturing and have outstanding electrical and mechanical performances.
Roebel cables and CORC have been used successfully for prototype dipoles.
Make a difference?
Status and
achievements