## Slide 1: Results from the EU HTS program
Lucio Rossi (CERN, now INFN-Milano) on behalf of EU FP7-EuCARD2 & H2020-ARIES
L. Bottura, G. de Rijk, G. Kirby J. van Nugteren, J. Murtomaki, A. Ballarino, J. Fleiter, H. Bajas, G. Willering (CERN)
M. Durante, C. Lorin, Ph, Fazilleau, Th. Lecrevisse (CEA), A. Kario, W. Goldacker (KIT), A. Usoskin and U. Betz (BHTS), C. Senatore, M Bonurs (UniGE), M. Dhallé, P. Gao (U Twente), T. Salmi (U.Tampere)

## Slide 2: The Partners
BHTS: A. Usoskin
CEA: M Durante, Ph. Fazilleau, C. Lorin (F. Borgnolutti)
CERN: A. Ballarino, M. Bajko, L. Bottura, J. Fleiter, G. Kirby, J. van Nugteren, L. Rossi
DTI: N. Zangenberg
INFN: G. Volpini (M. Sorbi)
INPG: A. Badel, P. Tixador
KIT: W. Goldacker, A. Kario
SOTON: Y. Yang
TUT: E. Härö, T. Salmi, A. Stenvall
UniGE: C. Senatore
UT: M. Dhallé

## Slide 3: Scope of FP7-Eucard2
CONDUCTOR
5-20 kA cable @4.2K 5-20T ten kAmps-class cable
For accelerator dipoles:
Joverall  400 A/mm2
  80-85% filling factor
  Jeng strand  400 A/mm2 min.
  Jeng strand  600 A/mm2 enhan.
Accelerator type
  Transposed
Not too many joints  high current – 100 m long tape
Demonstrator MAGNET – accelerator type
Aperture  40 mm (Rmin cable  20 mm!)
5 T standalone with 20% margin (> 6 T ss limit)
Insertable in High Field  outer Diam < 100 mm (including mech. structure)
Length < 1m (Lstraight  200mm)
Must reach 16-17 T in 13 T background (Fresca2)

## Slide 4: Selection of HTS: REBCO  cable type: ROEBEL
Choice in favor of REBCO tapes assembled in Roebel cable
  REBCO: continuing the route of EuCARD
  EU Industry. Other EU programs (FP7-Eurotapes)
  High current density (use// orientation) & Transposition!
  “Easy” start: conductor in final form, no need high temperature heat treatment of whole coil.
Other types of cable like stacked tape cable with twist on the curvature ends have been investigated. Eyes on CORC®!
Activity on Bi-2212 have been pursued in the collaboration CERN-ASC(Fl) on advanced powder from Nexans with mesurements by Univ. of Geneva on strand and in future U.Twente on cable
W. Goldacker et al., 2006 J Phys. Conf. Ser. 43 901

## Slide 5: EuCARD2 conductor
Good in term of Je
Even better in terms of Jlayer YBCO
C. Senatore

## Slide 6: We procured and tested tapes form various suppliers
C. Senatore

## Slide 7: New line for CERN (w=12mm) at Bruker
A.Usoskin & U. Betz - BHTS
2014
2015
2016

## Slide 8: H2020-ARIES
Scope: reduce substrate
100 µm 50 µm
To – almost – double Je
Idea behind:
Reduce cost of kA-m
Possible use of extra current density to increase Cu stabilizer
After a successful start … 
2018
C. Senatore

## Slide 9: …did not work at all; low yield; severe bow of the tape. attempt to correct the bow decreased Je

## Slide 10: Roebel cable - cont.

## Slide 11: New line for the Roebel
Anna Kario, Simon Otten, Andrea Kling, et al.

## Slide 12: Ic vs. transv. stress
J. Fleiter et al. SUST 26.6 (2013)
Demonstrated that above 100 MPa bare cable is severely damaged: but we will work at 150-200 MPa...
P. Gao and M. Dhallé
showed that impregnated cable works at 400 MPa

## Slide 13: Achievements (closing on 31 April 2017)
parameter | units | target
JE (20 T, 4.2 K) | (A/mm2) | 600
s (IC) within a unit length | (%) | 10
M(1.5 T, 10 mT/s) | (mT) | 300
Range of stransverse | (MPa) | 100
Range of elongitudinal | (%) | ±0.3
Unit length | (m) | 100
parameter | units | target
IC (20T, 4.2 K) | (kA) | 10
Width | (mm) | 12 ± 0.1
Thickness | (mm) | 1.0 ± 0.1
Effective contact resistance | (mW) | 5
Tape
Cable
✔
✔
✔
✔
✔
✔
L. Bottura, CERN
Plus direct order form CERN (about 500 kE) doubling the Eucard finacing to BHTS and other purchase

## Slide 14: Aligned Block lay-out by J. van Nugteren
Magnetic Field [T]
Percentage on Loadline [%]
The two plots present flux path variation for insert magnet:
(left) standalone in Iron ,
(right) in 13T ideal background field
Yellow area is the region more near to short sample.
Very different from std. LTS magnets.
e.m. model and e.m. design by J. Van Nugteren @ CERN

## Slide 15: e.m. model by J. van Nugteren (CERN& U.T.)
Dynamic E.M. cable model J. van Nugteren, EUCAS 2015
Hysteretic losses are dominant but how much coupling do we have in impr. Roeble?
Measurements at U. Twente have validated the e.m. model with a contact resistance in the orders of 10 ;
These values are not too different to measurements done in KIT (A. Kario): 20-30 
Good news: we expect current sharing in our cable.
Courtesy of M. Dhallé, U.T.

## Slide 16: AB dipole magnet (FeatherM2)
Quench CU bars
G. Kirby, CERN
J. Murtomaki, CERN
Design: minimal precompression: the coil are leaning against a rigid wall

## Slide 17: Going in steps:FeatherM0 flat racetrack, 5 m cable
G. Kirby, J. van Nugteren, CERN

## Slide 18: Magnet technology issues… design & protection issues…
Winding (un)stability : small tension
Impregnation  delamination
QD & QP Studies with strongly anistotropic th. Cond.
and with strong TCS variation inside tape/cable
Current redistribution
e.m. model of J. Van Nugteren, U.T. & CERN
Tampere TUT. J. Ruuskannen

## Slide 19: FeatherM0.4 – cable behaved as “expected”
Computation showed little time to react to a quench: 20-30 ms:
Quench detection.
Improved voltage taps ( 1 mV)
Array of temp. sensors
Pick-up coil array
Fiberglass in Bragg grating
12.8 kA, cable qualified
Way too much diagnostics
Too many wires!

## Slide 20: FeatherM2 construction: a complex assembly

## Slide 21: Manufacturing the Eucard2 first AB dipole FeatherM2
Courtesy of Glyn Kirby

## Slide 22: FeatherM2 AB block dipole construction

## Slide 23: Fin Joints by G. Kirby
Classical butlap joint in FM0.4:
>100 n!  40 n
New design, called Fin block joint (G. Kirby).
Improvement by a factor 2, no need of overcooling: do we need it? Certainly it helps to transfer current more uniformly…

## Slide 24
First accelerator-type magnet before going to test:
The Eucard2 FeatherM2.1-2 dipole
April 2017.
FeatherM2.1-2
Is special cable:
Tape from SUNAM
Cable by SuperOx
Low current

## Slide 25
Quench detected by protection
1 mV
3 mV
Minute to react
High resolution low frequency acquisition

## Slide 26: FeatherM2 first excitation cycle
Courtesy H.Bajas and J. van Nugteren, CERN
The copper ring works
The transition is soft, Contact resistance is in the 10 µΩ range!!
Coupling current decay in 80 s
But very little persistent current!
Only 60 unit of b3 foreseen
(model with no iron).
Measured about 20 unit!
Recalculated wth iron (L. Bortot et al.): agreement with 20 units!

## Slide 27: Degradation due to the cycle? Cold down also a little suspicious. But happened other times
FeatherM2_1-2
3.1 T
FeatherM2_3-4
(Eucard2 cable) 4.5 T (expected > 5 T)
G. Willering, CERN

## Slide 28: Cos design with Roebel at CEA-Saclay
Design A - « thick » cable : 12 x 1.2 mm² bare, 13 tapes 140-µm thick
Design B - « thin » cable : 12 x 1.0 mm² bare, 15 tapes 100 µm-thick
Cos-θ B : 1.0 mm + 2x125µm insulation, 17 turns
Layout | Unit | Cosϑ A | Cosϑ B
Iop | kA | 11.68 | 10.06
Bop | T | 5 | 5
Bpeak | T | 5.7 | 5.8
Ic | kA | 14.4 | 15.2
LL margin | (%) | 20 | 34
T margin | K | 20 | 30
Sd. inductance | mH/m | 0.49 | 0.73
coil inner radius | mm | 22 | 24
yoke inner raidus | mm | 50 | 50
yoke outer raidus | mm | 112 | 110
Nb. of turns | - | 14 | 17
Unit len. of cond. | m | 20 | 24
Cos-θ A : 1.2 mm + 2x100µm insulation, 14 turns
C. Lorin, M. Durante & Ph. Fazilleau

## Slide 29: Cos Theta coil at CEA: one layer; Technological test to compare with Ruth. cable
Finished. At CEA
To be tested
Very good quality winding and careful control of all process
C. Lorin, M. Durante & Ph. Fazilleau, CEA

## Slide 30: (some) Technical lessons
Working with tape and Roebel is difficult but possible. But do we need transpostition?
  Relatively smooth process in the period when effort was sufficient
  Too many uncertainty open. Main is the degradation. Is it intrinsic? Due to resin-induced delamination ? (CT101K is already suspected for NbSn…). Compatibility with resin is to be assessed more systematically. Or need to avoid liquid?
Persistent Currents are reasonable for FQ, not as bad as one could expect (b3 about 20 units).
  This point need more study. Could be canceled by intrinsic correction (magix magnet? See experiment of L. Bortot , C. Petrone et al. on a SC shield).
  Because of current anisotropy in the tape, and – see presentation of D. Uglietti, we do not need transposition. Simple stacked tape can do the job? WHAT IS IMPORTANT IS TO HAVE GOOD CURRENT SHARING. Robel even impregnated shows that current sharing is there.
The large enthalpy margin really pays off but must be coupled with a current sharing mechanism. Defect needs to be “bypassed”. Current sharing plays the role of “stabilizer” to shunt defects. The large enthalpy margin allows for the small inherent dissipation.
We had about 3.5 km of tapes and 150 of Roebel.  Luca Bottura excel file Some unit lengths is still there. It is possible to have a final FeatherM2_5-6 built in more controlled condition.

## Slide 31: General lesson learnt
Knowledge of tape behaviour is of course the first thing
Knowledge of the cable, i.e of the “conductor” is as well critical and is much more difficult. Depends also on the coil technology.
Taking more steps with intermediate mock-up is important
But a program cannot be done all in series: some parallelism must be introduced, otherwise you risk to see certain problem too late.
Foresee test and multiple retesting.
Difficult to do the program if has not some stable priority (which it had in 2016-17).
Long term program with company (HTS manufacturer) may suffer form company change of strategy.
We spent in Eucard2 (plus conductor and tooling) about 4 M€ (1.4 from EU) including salary and 0.5 M€ in ARIES (all from EU).

## Slide 32: Spares

## Slide 33: Situation in 2011-12
Forming the EU strategy aiming at 80-100 km VLHC, then FCC.
Dipoles of 15-16 T, ultimate 20T
Noticing the activity in USA (stimulus program, NHMFL/ASC Bi-2212 performance jump)
Decision to use EuCARD2 (2013-2017) to explore accelerator quality HTS.
Application aimed at Bi-2212 Rutherford, but open to consider also YBCO based conductor(s)
FP7 EuCARD – WP7 technology R&D 2008-2013
  FRESCA2 dipole 13 T,  100 mm facility Tested in July 2017: 13 T!
  HTS insert + 6 T (no bore) Tested in Juy 2017: 4.52 T @4.2K (power supply limit, no quench)
Fresca2
EuCARD HTS Insert
Conductor procured by CERN
Magnet designed and manufatcured by CEA

## Slide 34: Choice of Supercondutor: REBCO
REBCO | characteristics | Bi-2212
High, steadily improving | Critical current | High, more stagnant
Roebel cable (waste), ready to use, 50-200 m unit length | Cabling and general | Easy Rutherford cable, but need special H.T., very long length possible
Very bad (tape). | Magnetization | Worst than NbSn but manageable
Excellent, better than Nb3Sn | Mechanical prop. | Weak vs. transv. stress
Difficult bend in non-easy way, joints not easy, good insulation and handling | Coil technology | Very complex HT, large scale coils may be difficult. Easy joints
Various suppliers and projects everywhere | Supply | Limited number

## Slide 35
This corresponds to 800 A/mm2
 =  10%
Test in Tallahasse NHMFL

## Slide 36: Conductor characterization at CERN (MSC-SCD)
Elaboration of Jc(B,T,θ) scaling for REBCO materials
Magnetization measurements with VSM +/-10.5 T, 1.9-100 K
Residual Resistivity Ratio (RRR) measurements of the copper stabilizer
Splice resistance measurements at 4 K in the field range 0-12 T and at 77 K
  Type 0: Lowest resistance (13-40 n cm2 )
  Type 1: High resistance (98-570 n cm2 )
  Type 2: Very High resistance (150-884 ncm2)
J. Fleiter
Geometrical rules for Roebel; stacking factor important

## Slide 37: Measurements of losses in Univ. of Twente (NL) and Univ. of Southampton (UK)
Losses are dominated by the hysteresis of superconductor assemblies in Roebel.
Simple assemblies of isolated tapes are coupled, i.e. as a monolithic conductor, but not quite fully.
The 15 tape Roebel samples with/without epoxy impregnation behave as two in-line coupled stacks, each stack of 7-8 tapes. The saturation fields of the stacks increases linearly with the number of tapes, as expected.
Epoxy impregnated Roebel is less coupled and the strand in transposition seemed uncoupled.

## Slide 38: Back to Eucard2 : from tape to cable
A. Kario & W. Goldacker

## Slide 39: F_M0.1,2,3,4
StSt dummy ctd101K
test instrumentation tests, electrical short
Test dummy filled resin CTD101G test failed
HTS , 1st real test coil FeatherM0.4 Bruker tape , KIT cable
Fiber optics development for temperature onset detection
G. Kirby, CERN

## Slide 40
Quench detection
> 1 s
Zoom of the last 50 ms
Protection 10 mV, 20 ms
Low resolution high frequency acquisition

## Slide 41: Soft transition and easy detection: FeatherM0.4 coil
Heater pulse:
I_SH=30 A, U_SH= 40 V, t_pulse= 1.3 s
Quench detection
Stability is huge: hundred of Joules to quench

## Slide 42: FeatherM2.1-2
Sc until here
Current sharing
Runaway above 3 mV
Courtesy H.Bajas, CERN

## Slide 46: Not so easy but almost ready to wind (Nov 2018)
Courtesy of C. Lorin

## Slide 47: Stacked cable based magnet design (Grenoble)
But very high Filling factor easy cable to do, no waste…
Mechanics at the ends is difficult but probably manageable….
To avoid huge redistribuition: partial insulated tape inside the cable
P. Tixador, A. Badel & J. Himbele