## Slide 1: The Japanese HTS (High Field Magnet) programs for accelerators
T. Ogitsu, M. Sugano, T. Nakamoto, K. Suzuki, M. Iio, M. Dhakarwal; KEK,
N. Amemiya, Y. Sogabe, X. Luo; Kyoto U.
T. Shen, X. Wang, L.G. Fajardo, C. Myers; LBNL, C. Reis; UC Berkeley,
R. Gupta, P. Joshi, J. Schmalzle, G. Jochen, S. Joshi; BNL
S. Awaji; Tohoku Univ., H. Oguro; Tokai Univ., N. Banno; NIMS
A. Ballarino, S. Hopkins; CERN, D. Larbalestier; NHMFL, G.Velev, X. Xu; FNAL
S. Kawashima, T. Kawarada, Y. Murakami, K. Saito; Kobe Steel and JASTEC
Asami, H. Ii, H. Sakamoto, T. Kato; Furukawa Electric

## Slide 2: R&D for High Field Magnet for Accelerator in Japan
Based on international collaboration
  HTS: US-Japan collaboration framework
    KEK, Kyoto U., LBNL, BNL, UC Berkeley
  Nb3Sn: CERN-KEK collaboration
    KEK, Tohoku U., Tokai U., NIMS, JASTEC, Furukawa, CERN, NHFML, FNAL

## Slide 3: R&D for High Field Magnet for Accelerator in Japan
Based on international collaboration
  HTS: US-Japan collaboration framework
    KEK, Kyoto U., LBNL, BNL, UC Berkeley
  Nb3Sn: CERN-KEK collaboration
    KEK, Tohoku U., Tokai U., NIMS, JASTEC, Furukawa, CERN, NHFML, FNAL

## Slide 4
UC Berkeley
Dept of Nuclear Engineering
Experimental material science for nuclear applications
Kyoto Univ.
Graduate School of Engineering Department of Electrical Engineering
Advanced Technologies on
AC-Loss and Field Quality Analysis on HTS magnets
LBNL
Member of US-MDP
Developing 20 T HTS Accelerator Magnets
Advanced Technologies for
High Field Accelerator Magnet
BNL
Member of US-MDP
Developing Various HTS Magnets
Advanced Technologies for
HTS Magnet
KEK
Developing HTS Magnets for High Radiation Environments
Advanced Technologies for HTS Magnet with Radiation Hardness
Advanced
HTS Magnet
Technologies
for
Future
Accelerator
Sciences
US-Japan
Framework

## Slide 5
Task1: HTS magnet technologies for high-radiation environment
  Gamma ray irradiation to organic materials
  Neutron irradiation at the IMR Oarai and preform Ic test.
  Microscopic analysis of irradiation damage.
Task 2: Stability, quench protection, and magnet safety
Quench experiments of various spiral conductors.
Task 3: Measuring and modeling AC loss and field quality of HTS accelerator magnets
  Analyses of mechanical effect of shielding current, and CCT wound with CORC wires.
Field measurement of various HTS magnets.
Task 4: HTS/LTS high field hybrid accelerator dipole technology
Non-organic insulation technology R&D for HTS and Nb3Sn conductor.
Develop rad-hard racetrack coils that can be tested at BNL 10T test stand.
Prepare test stand, complete quench protection system design. Device a detailed test program including magnetization measurement.
Task and Target
J-PARC 2nd Target
FCC Interaction Region Magnets
Muon Collider Production Solenoid

## Slide 6: Task 1: Irradiation of a novel epoxy developed at QST gamma-ray facility (KEK + LBNL)
CTD-101 k, used by US LARP, after one thermal cycle to 77 K
Extensive cracks
NHMFL-mix61, an amine-based epoxy after one thermal cycle to 77 K
No crack
25 MGy, 50 MGy, 100 MGy irradiated
  Samples shipped to LBNL.
  Mechanical tests pending.
RT tensile test
CTD 101K
NHMFL mix61
ATLAS ECT
Yin, Shen et al., IEEE Trans. Appl. Supercond., 2019

## Slide 7: Current status of neutron irradiation
Task 1 Neutron irradiation to HTS conductors
PIE of GdBCO samples with neutron flux of 1.80, 2.58x1022 n/m2
D. X. Fischer, et al., Supercond. Sci. Technol. 31 (2018) 044006
Neutron irradiation effect on Tc
*influence of Cd foil for SuperPower SCS4050
No significant degradation in shielded HTS tape at 0.6 x 1022 n/m2.
But, reduction of Tc by 5 K in unshielded sample.
Vanishment of superconductivity is confirmed
PIE of GdBCO samples of target fluence 1x1021, 5x1021 n/m2
Fast neutron irradiation by shielding of samples with Cd foil
Irradiation of EuBCO samples to confirm the contribution of Gd
Materials analysis of irradiated samples by X-ray diffraction
Further study
X-ray diffraction patterns of the unirradiated GdBCO tape as a preliminary study.

## Slide 8: Task 2: Quench experiments of CORC and other spiral conductors
As of January 27, 2021
Quench experiments using CORC samples provided by LBL
Quench experiments using
short “home-made” spiral samples
Copper core looks helping protection.
Normal voltage appeared but not quenched

## Slide 9: Task 2. Stability and quench protection of HTS magnets – LBNL delivered samples and sample holder for quench experiment at Kyoto Uni.
Samples provided by Advanced Conductor Technologies
The multi-REBCO-tape CORC® wire is promising for HEP magnet applications
The collaboration under US-Japan will enable us to fully understand the stability and quench behavior of CORC® wires in conditions relevant for applications
The multi-REBCO-tape CORC® wire is promising for HEP magnet applications
The collaboration under US-Japan will enable us to fully understand the stability and quench behavior of CORC® wires in conditions relevant for applications
Ic 149 A at 1 µV/cm criterion, 91% of expected Ic
After multiple times of winding and unwinding during the development of sample holder
Reproducible VI transition

## Slide 10: Task 2. Stability and quench protection of HTS magnets: LBNL developed a method to minimize damages during a quench of REBCO tapes
Methods to determine peeling and shear stress during a quench established. Simple analytical model also cross-checked with FEM models.
Delamination by thermal stress.
Removal of damages using a simple and scalable method.
C276
Cu
Ag + REBCO
4 K to 300 K,
shear stress >23 MPa

## Slide 11: Task 3: Simple calculation and analyses of field quality of CORC magnets
Calculated current distribution
Coaxial three layers with
uniform current distribution
Simple field calculation
(quasi-3D model for RTC)
A simple calculation method was developed in order to
evaluate influence of CORC wires’ geometry and
shielding currents on field distribution along z-axis.
As of January 27, 2021

## Slide 12: Task 3. Field quality of LBNL C2 magnet based on a new round REBCO CORC wire (65 mm aperture, 2.9 T dipole field at 4 K) accessed at LBNL and provided to Kyoto University for analysis.
current
Dipole field
C2
magnet
The 65 mm-aperture C2 magnet generated a dipole field of 2.9 T at 4.2 K, providing the unique opportunity to measure and understand the field quality of a REBCO dipole magnet using CORC® wires
Measurements agree with the calculation for the dipole field
Strong magnetization effects in b3 – too large due to the high Jc and tape width

## Slide 13
C2 (aperture 65 mm)
on aluminum bronze mandrel
C1 (aperture – 70 mm) on
bluestone mandrel
Task 3. Field quality of LBNL C2 magnet. A ramp-rate dependence was observed in non-allowed skew terms. A similar behavior was seen in C1 with the plastic printed mandrel
3.1 mm diameter CORC wire that contains
16 REBCO tapes in 8 layers.
C1 before assembly
3.8 mm diameter CORC wire that contains
30 REBCO tapes in 12 layers.
Xiaorong Wang et al 2021 Supercond. Sci. Technol. 34 015012
C2 before
assembly
Xiaorong Wang et al 2019 Supercond. Sci. Technol. 32 075002

## Slide 14: Task 4 Inorganic Insulation HTS coil
Cu tape (t=0.1mm)
Coated Layer
Cu-Stabilizer
Substrate
Superconductor
Cu-Stabilizer
REBCO #1
Cu-Stabilizer
Superconductor
Substrate
Cu-Stabilizer
Coated Layer
REBCO #2
R&D of continuous coating on long tapes by real to real insulation machine is in progress.
Although continuous coating is successful, difference in thickness of ~16 mm in the width direction is confirmed.
Preparing the winding of the circular test coil #2 with co-winding 2 REBCO and Cu tape
(same shape as Test coil #1)
  Wires identified and shipped from LBNL to KEK for testing KEK’s new ceramic coating insulation on Nb3Sn and Bi-2212 wires.

## Slide 15: Task 4. High Field Test with Common Coil Configuration @BNL
323.2
335
31
R&D on High Field Accelerator Dipole (Highest Field and Field Quality Studies)
R5.5
Two tests in one go:
Two HTS insert coils in two apertures of the common coil dipole:
Upper Bore: field primarily parallel
Lower bore: field primarily perpendicular
Background
field :~10 T
30
30
Design study in progress
Power Supply Acquired

## Slide 16
Task1: HTS magnet technologies for high-radiation environment
Gamma ray irradiation at QST Takasaki up to 100 MGy: DONE, preparing for mechanical testing.
Initial PIE performed, For GdBCO complete degradation confirmed with 1.8x1022 n/m2.
X-ray diffraction study on non-irradiated GdBCO, prepare for irradiated GdBCO
Task 2: Stability, quench protection, and magnet safety
Initial quench experiments using CORC sample and short spiral sample.
Task 3: Measuring and modeling AC loss and field quality of HTS accelerator magnets
Development of calculation method to evaluate field quality of CORC magnets.
  Field measurement of C1 and C2 including ramp rate dependence.
Task 4: HTS/LTS high field hybrid accelerator dipole technology
R&D of continuous coating on long tapes by real to real insulation machine is in progress.
Testing inorganic insulation with Nb3Sn and Bi-2212 conductors is in progress.
Design study of racetrack coil in progress.
Preparing test stand, acquired power supply.
Achievement so far

## Slide 17: R&D for High Field Magnet for Accelerator in Japan
Based on international collaboration
  HTS: US-Japan collaboration framework
    KEK, Kyoto U., LBNL, BNL, UC Berkeley
  Nb3Sn: CERN-KEK collaboration
    KEK, Tohoku U., Tokai U., NIMS, JASTEC, Furukawa, CERN, NHFML, FNAL

## Slide 18: Conductor Development Programme
The programme now includes 10 active partners and 3 new agreements awaiting signature
First workshop held 5-6 March 2018 at CERN
MOU btw KEK and CERN

## Slide 19
Kobe Steel / JASTEC
Furukawa Electric
Fabrication
• Optimization of HT condition
• Microstructure observation
• Compositional analysis
• High field magnet facility
• Evaluation of deff
• Evaluation of Jc, Bc2
• Mechanical property
Design and Characterization
28 T HM
• In-depth characterization
HT, Jc, composition, deff ...
• Program coordination
• Defining specification
• Conceptual design
Tohoku University
R&D billets
Spec,
design
CERN
Tokai University
KEK
R&D structure

## Slide 20: Status of Nb3Sn conductor R&D
DT wire
  non Cu Jc @16T 1,100 A/mm2
  reasonable results in deff (~50µm)
  and rolling test (Ic/Ic0>95%, RRR>100 @ 10% roll)
  Further improvement and mass production R&D in progress
Nb tube wire
  Non-Cu Jc of 580 A/mm2 @16 T
  Further improvement in progress

## Slide 21: R&D Plan modified
Task1
Review past technologies and select.
First review meeting in Feb. 2016
Task2
Design wire layout and composition
Procure material (possible trial billets)
Task3
Production of R&D billets
W; 1~5kg * N=8
Task 5
Select candidate
Produce 2*5km wire
Heat treatment study
5 Years Plan
Task 4
Production of R&D billets with Advanced Technologies
W; 1~5kg * N=8
Change Task 4 and 5 to accommodate further R&D with Nb-Ta-Hf: collaboration with NHFML (2020-2022 within CERN-KEK Collaboration)
Also
Collaboration with NIMS for Cu-Zn matrix technology for possible enhancement of Jc and mechanical strength
preliminary
Collaborator
Dr. Banno
(NIMS)
Collaborator
Prof. Larbalestier
(NHMFL; FSU)
MOU btw KEK and CERN

## Slide 22: Magnet Development (Dream)
HL-LHC D1
FCC D1
Design study
Subscale coil
12T model magnet
2024-2026 EXF
16-20T magnet R&D
2026-2028 EXF
2016-2025
2018-2020
2022-2024 EXF
HL-LHC D1 Magnet Development
  Ongoing project
  1 Prototype: 2020-2021
  6 Production 2022-2025
    ↓
FCC D1 magnet design study (2018-2020 done)
  FCC Collaboration
  ↓
  Development of high strength Nb3Sn conductors (2021-2023)
  ↓
Nb3Sn subscale coil R&D (2022-2024)
  Establish Coil fabrication technology
↓
12 T Large Aperture Dipole (2024-2026)
  Model of FCC D1 with the bore of f100 mm (Nb3Sn)
  Can be used as Test stand
  ↓
16-20 T Dipole Magnet (2026-2028)
  Nb3Sn 4 T insert
  HTS 8 T insert?