## Slide 1
Progress of the High Field Magnet R&D
with IBS
Qingjin Xu
(IHEP, CAS)
In collaboration with Yanwei Ma’s group at IEE-CAS
Team members: Zhan Zhang, Chunyan Li, Ershuai Kong, Yingzhe Wang, Chengtao Wang (IHEP)
Dongliang Wang, Xianping Zhang,… (IEE)
中国科学院高能物理研究所
Institute of High Energy Physics, CAS
中国科学院电工研究所
Institute of Electrical Engineering, CAS

## Slide 2
Je of Practical Superconductors Presently
Chart: Applied Magnetic Field (T)
| 5 | 10 | 15 | 20
REBCO: B ∥ Tape plane | 4599.7996 | 4264.0246 | 3416.6751 | 3085.9004
REBCO: B ⊥ Tape Plane | 3664.9998 | 2919.9995 | 2379.9996 | 1796.1537 | 1447.6924 | 1188.462 | 1034.3652 | 956.923 | 851.8301 | 780.8449 | 719.9995 | 679.4359 | 626.087 | 593.2388 | 563.4783 | 535.3843 | 516.5215 | 469.5647 | 433.0766 | 406.956 | 391.3041 | 367.6926 | 360.0003 | 344.3473 | 328.6954 | 322.3077
Bi-2212: 50 bar OP | 2187.8458 | 2018.5437 | 1897.0961 | 1799.3564 | 1729.1673 | 1666.7736 | 1608.1837 | 1558.7923 | 1516.4066 | 1473.2906 | 1436.5687 | 1398.9095 | 1365.3787
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: High Field MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar | 1379.4097 | 1269.0093 | 1128.2455 | 1107.3276
YBCO B perp ln extrap | 322.2305 | 315.4585 | 296.3443 | 267.862 | 242.7389
YBCO par ln extrap | 3024.7539 | 2573.1471 | 2188.967 | 2051.8662
IBS 2016
(short sample)
500A/mm2
IBS
100-m tape

## Slide 3
He Huang, et al., SuST, 31 (2018) 015017
At 4.2K, 10 T, Jc~1500A/mm2，I=437 A
At 4.2K, 14 T, Jc~1400A/mm2
At 4.2K, 27 T, Jc~550A/mm2
The anisotropy of Jc at 10T is 1.37
Performance of Hot-Pressed Ba122/Ag Tapes

## Slide 4
4.2 K, 10 T: Jc=1100 A/mm2
Performance of HIP Ba122 Tapes with Cu/Ag Sheath
Size of the grains was around 0.5 um, smaller than that in the Hot-pressed samples.
The Jc may be improved with the increase the grain size.
Science China-Materials, Accepted

## Slide 5
100-m Long Ba122 Tapes by Rolling Process
In 2020, Jc of a 100-m 7-core tape using the new fabrication technique reached 500 A/mm2 @ 4.2 K, 10 T.
Tape width 4.8 mm, tape thickness 0.3 mm. Ic > 200 A.
In 2018, Jc of such tape is 300 A/mm2 @ 4.2 K, 10 T.

## Slide 6
Φ30mm
Thickness
0.8mm
Hoop
Epoxy impregnating
Fixed on the winding plane
Φ2mm Screw & nuts
Fake
Leader
Heat
treatment
Current leader soldering
YBCO
Leader A Leader B
YBCO
Cu
First Performance Test of IBS Solenoid Coil under 24 T
Wang, et al., SuST,. 2019(32) 04LT01
The transport Ic of the single pancake IBS coil reach 40% of that at zero external magnetic field.

## Slide 7
At 30 T @ 4.2 K, the Ic of the double pancake IBS coil was reached 48A (56% of short sample)
Qian, et al., Physica C 580 (2021) 1353787
D30 coil :
inner diameter: 30mm
Performance Test of IBS Solenoid Coil under 30 T

## Slide 8
Preparition of bent IBS tape
Jc of Bent IBS Tapes
Cracks appear regularly in part of the superconducting cores under tensile stress !
Ic of bent IBS tapes decreases with smaller bending diameters.
OMI of D10 bent tape
Sample results by ASIPP in 2018
Sample results by IHEP in 2021

## Slide 9
< 绕制线圈 > < 布置抽头 > < 绕制完毕 > <组装钽箔> < 组装热处理> < 热处理>
< 热处理后> < 内侧接头> <外侧接头> < 光栅与抽头 > <环氧浸渍后制备完成>
Development of Racetrack Coils with 100-m Long IBS Tapes

## Slide 10
IBS
Nb3Sn
IBS coil was inserted in the center
and assembled together with
the 10-T model dipole magnet
NbTi and Nb3Sn background coils
10-T background mode dipole
Assembly completed and ready for test
Under test at 4.2 K
Performance of the model dipole
Development of Racetrack Coils with 100-m Long IBS Tapes
NbTi

## Slide 11
Parameter | Value
Background field | 0-10 T
Rate | 1 A/s
Maximum pressure on IBS | 120 MPa
Development of Racetrack Coils with 100-m Long IBS Tapes

## Slide 12
Zhang, et al., SuST,. 34 (2021) 035021
Two racetrack coils have been made using the 100 m length IBS tapes.
The coils reached 86.7% of critical current of the short sample at 4.2 K and 10 T, and 81.25% of the quench current under self-field,
with highest compressive stess over 100 MPa.
Development of Racetrack Coils with 100-m Long IBS Tapes

## Slide 13
OD 640 mm
AP 2*30 mm
Nb3Sn
ReBCOor
IBS
ReBCO
Or
IBS
Nb3Sn
Nb3Sn
Ongoing: Development of the 16-T Hybrid Dipole Magnet
Nb3Sn 12~13 T + HTS 3~4 T

## Slide 14
Yoke OD
500mm
Strand | diam. | cu/sc | RRR | Tref | Bref | Jc@ BrTr | dJc/dB
IBS | 0.802 | 1 | 200 | 4.2 | 10 | 4000 | 111
Target cost of IBS: 20 RMB /kAm @12 T
Next in future: the 12-T IBS Dipole Magnet

## Slide 15
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
Challenges and Outlook
Tc reached 55K
1st IBS solenoid at 24 T
1st IBS Racetrack at 8 T
2nd IBS Racetrack at 10 T
The engineering current density of the long-length IBS still needs a significant improvement, to reach the similar level as ReBCO or Bi-2212 conductors.
The materials of stabilizer should be shifted to copper or any other low-cost metals to realize the low cost of IBS.
Structure and fabrication methods of IBS and corresponding coils should be further optimized to minimize the Jc degradation at high field and high stress.
And many other issues like detailed magnetic and mechanical properties study of IBS, quench detection and protection of the IBS coils / magnets and etc.
We are expecting a IBS-only 12-T dipole magnet in 10 years…

## Slide 16
Thanks for your attention!