## Slide 1
Lucas Brouwer
Accelerator Technology and Applied Physics Division
Lawrence Berkeley National Laboratory
4/15/2021
Modeling tools for HFM R&D

## Slide 2: Scope of the Presentation
modeling strain induced margin reduction (strand to magnet level)
improved modeling of interfaces
high performance computing for efficient solution of large 3D models
Mechanical modeling
Multiphysics codes for magnets
HTS cable and magnets
mechanical and electromagnetic models guiding cable design
evaluation of screening induced fields in HTS accelerator magnets
diverse set of codes for simulating strongly coupled (EM-thermal-circuit) behavior of magnets enable accurate modeling of CLIQ and other challenging scenarios
Focus on recent advances (representative examples) and key challenges for each

## Slide 3: Modeling critical current degradation of Nb3Sn at the strand and cable level
FEM Modelling reproduces Ic degradation as a function of transverse pressure for 10-stack cable compression test
G. Vallone, et al., IEEE Trans. Appl. Supercond., 28, 4, 2018
B. Bordini et al., IEEE Trans. Appl. Supercond., 20, 3, 2010
Strand sub-modeling
(includes insulation and resin)
Ic measurement on wire inside cable
Rutherford cable stack
Structural FEM analysis in Ansys APDL
Pre-stress evaluation from heat treatment (950K to 300K)
Cool down of sample from 300K to 4.2K + Ramped external load
𝐉𝐜 evaluation for each element using Ekin’s law
Numerical integration on the strand cross section → Ic degradation for the entire strand
as a function of external load
Simulation of Ic sensitivity to uniaxial transverse pressure
Ic Reduction @15 T vs. Pressure
Courtesy of Emanuela Barzi

## Slide 4: Margin maps including stress at the magnet level
Example 2: blended cable properties in 3D (CCT)
Example 1: Individual strands and insulation included in 2D (MQXF)
G Vallone et al 2021 Supercond. Sci. Technol. 34 025002
Ic(B,T,strain) calculated on mesh using (B, strain) from FEM models gives margin as a function of position and evolution vs. magnet current (min. margin can move)
Many uncertainties, but is proving to be a valuable tool for comparison with test diagnostics
Overlay of margin and quench location from acoustic sensors

## Slide 5: Improved Modeling of Interfaces
See detailed talk on interface modeling from Giorgio Vallone
Summary of recent developments
pole debonding modeled for MQXF
implementation on 2D CCT models shows initial debonding location and evolution
quantitative results are challenged by uncertainty in interface material properties
Strong non-linearity of interface contact models are computationally challenging in 2D and 3D

## Slide 6: Use of high performance computing reduces run times for large 3D mechanical models, allowing for 3D design and optimization
Example: CCT4 3D ANSYS mechanical model
Solid186, 7M DOFs
3 load steps: assembly, cooldown, Lorentz forces
PCG (iterative) solver
Solution time is reduced from overnight to less than one hour
L. Brouwer et al. IEEE Trans. Appl. Supercond. 4001006, 28.3, 2017
*http://scs.lbl.gov/
using the Lawrencium cluster*
Not yet implemented for multiphysics or interface de-bonding models

## Slide 7: Summary of Mechanical Modeling
Recent advances
7
Key challenges
  uncertainty in material properties of conductor and interfaces
  implementing energy release and thermal effects leading to quench for debonding models
  extending the use of HPC resources as needed (for highly non-linear interface debonding, margin analysis, etc.)
  sub-strand and cable level modeling predicts Ic reduction
  magnet-level margin maps show distribution and evolution of margin during powering
  development of interface debonding models and their initial application to Nb3Sn accelerator magnets
  high performance computing (HPC) resources enable efficient solution of large 3D mechanical models

## Slide 8
modeling strain induced margin reduction (strand to magnet level)
improved modeling of interfaces
high performance computing for efficient solution of large 3D models
Mechanical modeling
Multiphysics codes for magnets
HTS cable and magnets
mechanical and electromagnetic models guiding cable design
evaluation of screening induced fields in HTS accelerator magnets
diverse set of codes for simulating strongly coupled (EM-thermal-circuit) behavior of magnets enable accurate modeling of CLIQ and other challenging scenarios

## Slide 9: A diverse set of codes are now available for simulating strongly coupled, multiphysics behavior of magnets
Challenge: multiphysics coupling of EM, thermal, and circuit effects in magnets over large variations in time and length (for CLIQ[1] etc.)
STEAM: co-simulation approach (FEM, network models, …)
Supported simulation tools
In-house developed: LEDET, ProteCCT, SIGMA, BBQ
Developed in other institutions: QLASA
Commercial: PSPICE, LTSpice, COMSOL, ANSYS, PSIM
Automated model generators (supported for PSPICE, SIGMA, LEDET, COSIM)
“Meta-methods” (requiring tool adapter APIs), i.e. cooperative simulation
“Front-ends”: Jupyter notebooks and scripts to make it easier to use the above-mentioned and run simulations
ANSYS user elements (self-contained FEM)
L. Brouwer et al 2019 SUST 32 095011
STEAM References
For BBQ: M. Mentink, et al., IEEE Trans. on Appl. Supercond., 28, 4004806, 2018
For COSIM: L. Bortot, et al., IEEE Trans. on Appl. Supercond., 28.3, 1-6, 2017
For ProteCCT: M. Mentink et al., IEEE Trans. on Appl. Supercond., 28, 4004806, 2018
For SIGMA: L. Bortot, et al., IEEE Transactions on Magnetics, 54.3, 7000404, 2017
For LEDET: E. Ravaioli, et al., Cryogenics, 80.3, 346-356, 2016.
For any software [in addition]: https://espace.cern.ch/steam/
[1] E. Ravaioli, PhD thesis, 2015

## Slide 10: These codes are benchmarked and are now routinely used for high-field Nb3Sn accelerator magnet studies
Quench protection of the Nb3Sn CCT magnet CD1
J. Gao, et al. IEEE Trans. Appl. Supercond. 30.4 (2020). 4701505
CLIQ and EE simulated with ANSYS UDE’s, including eddy current effects in CCT structure (FEM)
E. Ravaioli, et al. IEEE Trans. Appl. Supercond. 29.5 (2019). 4701405
Quench Protection of the First 4-m-Long Prototype of the HL-LHC Nb3Sn Quadrupole Magnet
STEAM-LEDET simulations of CLIQ, energy extraction, and heaters show good agreement with test results

## Slide 11: STEAM tools applied to quench protection of multi-filamentary Bi-2212 HTS accelerator magnets
CLIQ design optimized using STEAM-LEDET modeling, 1st low current test at 77 K
Silver Mid-Tap
Common Coil RC7+RC8
Bladder
Key
Joint
Strain
Gauges
Double Pancake Windings
~5 T, Bi-2212 common coil magnet

## Slide 12: Summary of Multiphysics Magnet Modeling
Recent advances
Key challenges
  extension to REBCO and HTS cables (magnetization models/approaches)
  extension to 3D
  management and sharing of codes
  a diverse set of tools can model CLIQ and other strongly coupled EM, thermal, and circuit behavior of magnets
  these codes are being extended to multi-filamentary HTS (important for future hybrid LTS/HTS testing)

## Slide 13
modeling strain induced margin reduction (strand to magnet level)
improved modeling of interfaces
high performance computing for efficient solution of large 3D models
Mechanical modeling
Multiphysics codes for magnets
HTS cable and magnets
mechanical and electromagnetic models guiding cable design
evaluation of screening induced fields in HTS accelerator magnets
diverse set of codes for simulating strongly coupled (EM-thermal-circuit) behavior of magnets enable accurate modeling of CLIQ and other challenging scenarios

## Slide 14: 3D mechanical modeling of HTS cables guiding design (representative example for CORC)
V A Anvar et al 2018 Supercond. Sci. Technol. 31 115006
FEM models predict degree of Ic degradation during bending of CORC cable as a function of: winding angle, tape width, friction, copper thickness, substrate thickness, # of layers, and core diameter

## Slide 15: Different approaches to 3D modeling of HTS cables can relate cable design parameters to magnetization and AC loss
EM-thermal network models
AC loss and coupling time constants evaluated for SCSC cable concept
Current vector potential with thin-strip approximation
3D T-A formulation (FEM)
Magnetization loss as a function of CORC cable parameters: winding direction, layer structure, and striation
Y. Sogabe, et. al., SUST, 33, 055008, 2020
Yawei Wang et al, SUST, 33, 025003, 2019
Magnetization, hysteresis, and loss for Roebel, CORC, and twisted stack cables
J. van Nugteren, HTS accelerator magnets, PhD thesis, 2016

## Slide 16: Simulated screening currents for the Feather-M2 HTS Magnet
[1] Bortot, L., et al. "A Coupled A–H Formulation for Magneto-Thermal Transients in High-Temperature Superconducting Magnets." IEEE Transactions on Applied Superconductivity 30.5 (2020): 1-11.
[2] Bortot, L,, et al. "Numerical analysis of the screening current-induced magnetic field in the HTS insert dipole magnet Feather-M2. 1-2." Superconductor Science and Technology 33.12 (2020): 125008.
Backup slide contains details on the A-H FEM formulation
Field multipoles compared to measurements at different temp [2]
A coupled A-H, 2D FEM formulation allows for numerical modeling of REBCO screen currents in accelerator magnets [1]

## Slide 17: AC losses and shielding current induced fields can be evaluated in 3D for accelerator magnets wound with single coated conductors
Large-scale electromagnetic field analysis tool for HTS magnets [1-2] using T-formulation and thin-strip approximation with applying hierarchical matrices and preconditioning by Algebraic Multi-Grid method
1.5 M of degree of freedoms or more, enabling us to model almost whole part of a magnet wound with single coated conductor.
17
Courtesy of Dr. Amemiya and Dr. Gosabe of Kyoto University
[2] Y. Sogabe, et. al., IEEE-TAS, 29, 5900505, 2019
[1] T. Mifune, et. al., SUST, 32, 094002, 2019
Achieved: evaluation of ac losses and shielding current induced fields (SCIFs) of magnets wound with single HTS tape
Not achieved: detailed analysis of ac losses and SCIFs of magnets wound with cables, considering their detailed structures

## Slide 18: Summary of HTS Cable and Accelerator Magnet Modeling
Recent advances
several different 3D numerical approaches can relate HTS cable design parameters to bending limits, magnetization, and AC loss
large-scale electromagnetic field analysis tools enable modeling of screening current induced fields and AC loss in HTS accelerator magnets (2D and 3D)
Key challenges
  current sharing around defects in detailed cable geometries
  including effects due to detailed cable structure in magnet models
  increase in the degrees of freedom (tens of million?)
  more parallel computation

## Slide 19
Acknowledgements
LBNL: Giorgio Vallone, Xiaorong Wang, Qing Ji, Zoe Webb-Mack, Tengming Shen
FSU-MAGLAB: Daniel Davis
CERN: Emmanuele Ravaioli, Lorenzo Bortot, Mariusz Wozniak, Glyn Kirby, Jeroen van Nugteren
FNAL: Emanuela Barzi
Kyoto University: Yasuke Sogabe, Naoyuki Amemiya
Thank you for your attention

## Slide 20: There is a large HTS modeling community worldwide, many relevant developments for power, fusion, NMR, and other applications not included in this presentation
20
http://www.htsmodelling.com/

## Slide 21: A coupled field formulation for HTS Magnets [1]
[1] Bortot, L., et al. "A Coupled A–H Formulation for Magneto-Thermal Transients in High-Temperature Superconducting Magnets." IEEE Transactions on Applied Superconductivity 30.5 (2020): 1-11.

## Slide 22: Network Model for RECBO Pancakes with Heat Transfer
Courtesy of Zoe Webb-Mack, Qing Ji, and Xiaorong Wang

## Slide 23: Network Model for RECBO Pancakes with Heat Transfer
Courtesy of Zoe Webb-Mack, Qing Ji, and Xiaorong Wang

## Slide 24: Network Model for RECBO Pancakes with Heat Transfer
Courtesy of Zoe Webb-Mack, Qing Ji, and Xiaorong Wang
State of the art:
- Experimental results on current sharing between stacks of tapes and NI pancake coil can be reproduced with a ngspice network model. Current sharing in NI pancake coils can be counter-intuitive.
Lessons learned:
- Simple electrical network model can explain the observed experimental results.
- Electrical and thermal aspects need to be coupled to fully understand the current sharing behavior.
Key challenges:
- More high-quality experimental results
- Improved modeling

## Slide 25: RESULTS: There are no preferred locations for the high-Cp subelements for thermal efficiency, i.e. the Gd2O3 tubes DO NOT HAVE TO BE EXTERNAL to the superconducting elements. It is the total cross sectional area of the high-Cp tubes that matters.
MQE Thermal Modeling of Nb3Sn Wires with N High-Cp subelements
6 at corners
6 central
24 external
24 (w/18 central)
Standard
60/61 RRP wire
“Heat Diffusion in high-Cp Nb3Sn Composite Superconducting Wires”, Invited paper, Instruments 2020, 4, 28
Courtesy of Emanuela Barzi