## Slide 1: Warm Magnets
Gijs de Rijk
CERN
CAS
Chavannes de Bogis, Switzerland
28th September 2021

## Slide 3: Contents
Introduction: magnetic field and warm magnet principles
Field description and magnet types
Practical magnet design & manufacturing
Permanent magnets
Examples of accelerator magnets from the early times until the present
Literature on warm Magnets
3

## Slide 4: Magnet types, technological view
iron dominated
electromagnet
permanent magnet
coil dominated
superconducting
normal conducting (resistive)
static
cycled / ramped slow pulsed
fast pulsed
We can also classify magnets based on their technology
Notes: In electromagnets the field is produced by electrical currents going through the windings. In permanent magnets, on the other hand, the field is produced by hard magnetic material, such as NdFeB or SmCo.
Iron dominated magnets use a yoke (usually in electrical steel or iron) to guide, shape and reinforce the field; the position of the coils (or permanent magnets) is of minor importance for the strength and homogeneity of the field. Coil dominated magnets use the flux directly generated by the electric current flowing in the windings to shape the field; the position of the iron yoke (if any) is of minor importance for the strength and homogeneity of the field.
Normal conducting (or resistive) magnets have resistive coils, in copper or aluminum, and they are operated around room temperature. Joule heating has to be taken into consideration; when air cooling (natural convection) is not enough, typically a forced flow of demineralized water is added.
Superconducting magnets have superconducting coils, with no Joule heating. The known technical superconductors need to be cooled at cryogenic temperatures to work.
The mode of operation can be static (dc, ex. main magnets in a collider or synchrotron light source), cycled / ramped / slow pulsed (ex. main magnets in a synchrotron for hadron therapy) or fast pulsed (ex. kickers).
In some cases, there might be some hybrids, e.g. an electromagnet with some permanent magnet.

## Slide 5: Earth magnetic field
In Geneva, on 06/09/2021, the (estimated) magnetic field (flux density) is
|B| = 47672 nT = 0.047672 mT = 4.7672·10-5 T ≈ 0.5 Gauss. Bhorizontal = 22259 nT
Notes: The Earth’s field at our latitudes is about 0.5 Gauss, that is, 5·10-5 T.
The value above was computed using the World Magnetic Model (WMM) and the latitude / longitude / elevation of Archamps. The date also matters, because the Earth’s magnetic field changes (in direction and amplitude) with time.
You can check that out at www.ngdc.noaa.gov/geomag/WMM.

## Slide 6: Maxwell equations
Integral form Differential form
With:
Ampere’s law
Faraday’s equation
Gauss’s law for magnetism
Gauss’s law

## Slide 7: Magnetostatics
Let’s have a closer look at the 3 equations that describe magnetostatics
always holds
holds for linear materials
holds for magnetostatics
(1)
(3)
(2)
Gauss law of magnetism
Ampere’s law with no time dependencies
Relation between field and the flux density
Notes: In magnetostatics, as there are no time dependent fields, the equations for the electric and the magnetic parts become uncoupled.
We give these equations a number as we will use them much during this introduction.

## Slide 8: Magnetic fields
From Ampere’s law with no time dependencies
We can derive the law of Biot and Savart
(Integral form)
If you wanted to make a B = 1.5 T magnet with just two infinitely thin wires placed at 100 mm distance in air one needs : I = 187500 A
To get reasonable fields ( B > 1 T) one needs large currents
Moreover, the field homogeneity will be poor

## Slide 9: Iron dominated magnets
Yoke
coil
This is valid as mr >> 1 in the iron : limited to B < 2 T
With the help of an iron yoke we can get fields with less current
Example: C shaped dipole for accelerators
B = 1.5 T
Gap = 50 mm
N . I = 59683 A
2 x 30 turn coil
I = 994 A
@5 A/mm2, 200 mm2
14 x 14 mm Cu

## Slide 10: Comparison : iron magnet and air coil
These two curves are the transfer functions – B field vs. current – for the two cases
Imagine a magnet with a 50 mm vertical gap ( horizontal width ~100 mm)
Iron magnet wrt to an air coil:
  Up to 1.5 T we get ~6 times the field
  Between 1.5 T and 2 T the gain flattens of : the iron saturates
  Above 2 T the slope is like for an air-coil: currents become too large to use resistive coils
Courtesy A. Milanese, CERN
Notes: The different behavior of the two cases (with / without iron) can be seen also in the transfer function curves, where the central B field is plotted as a function of the Ampere-turns.
An iron yoke introduces a non-linearity – the B-H response of the yoke material – though it greatly enhances the field up to about 2 T. After this, the saturation becomes predominant and additional field becomes (much) more expensive in terms of current. This is why resistive dipoles in the great majority of cases are meant to work till about 1.8 – 2.0 T. For example, the SPS MBB dipole (52 mm full vertical gap) has 5750 A x 16 turns for a nominal field of 2.0 T, that is, 92 kA (for a current density of about 6.2 A/mm2).
At low field the permeability of the material is not well behaved and very low field magnets are special in their own way too.
Above 2 T, since many Ampere-turns are needed, it is interesting to pack a lot of current in a compact space close to the gap and to make the Ampere-turns cheap: this is when superconducting magnets are used. For example, in the LHC there are 40 cables per pole (per aperture), for a nominal current of 11850 A to get to 8.3 T: that makes 40 x 2 x 11850 = 948 kA (for an average current density of about 400 A/mm2).
There is also a hybrid family of super-ferric magnets: these are iron-dominated, but they have superconducting coils to magnetize the iron. We will not cover this category.

## Slide 11: Magnetic field quality: multipole description
The “wanted” or is equal to 1
In a ring-shaped accelerator, where the beam does multiple passes, one typically demands :

## Slide 12: Magnetic Length
In 3D, the longitudinal dimension of the magnet is described by a magnetic length
magnetic length Lmag as a first approximation:
For dipoles Lmag = Lyoke + d d = pole distance
For quadrupoles: Lmag = Lyoke + r r = radius of the inscribed circle between the 4 poles
Courtesy A. Milanese, CERN
Notes: Looking along the longitudinal (z) direction, the field B is maximum at the centre (z = 0) of the magnet, it is more or less constant till reaching the ends, where it rolls off to reach a 0 value outside. The magnetic length lm is defined as that length which – multiplied by the central field value B0 – returns the same integrated field.
The same holds substituting the field B with the gradient G, or with any multipoles Bn, An. In this case, the integrals have to be performed on the not-normalized (upper case) coefficients, and the normalized terms (lower case) are then obtained by dividing by the integral of the fundamental harmonic.
For long magnets – where the longitudinal dimension is much larger than the gap – the behavior is dominated by the (long) central part, so taking the values of 2D simulations and multiplying by a length yields good results. For short magnets, the behavior is intrinsically 3D.

## Slide 13: Magnets in an accelerator: power convertor and circuit
B field stability in time: ~10-5 - 10-6
Typical R of a magnet ~20mW - 60mW
Typical L of a magnet ~20mH – 200mH
Powering cable (for 500A): Cu 250 mm2 (Cu: 17 nW.m) R = 70 mW/m, for 200m: R= 13mW
Take a typical rise time 1s
power
Convertor (current source)
Cu (or Al) cables or busbars
Cu or Al coil
Steel yoke
Vacuum chamber
beam
B (flux density)
Then the Power Convertor has to Supply : 0-500 A with a stability of a few ppm.
Voltage up to 40 V (resitive)
And 100 V (inductive)

## Slide 14: Types of magnetic fields for accelerators
Courtesy D. Tommasini, CERN

## Slide 15: fluxlines in magnets
Dipole Quadrupole sextupole
0
0.8 T
1.6 T
0
0.8 T
1.6 T
0
0.5 T
1.0 T

## Slide 16: Symmetry and allowed harmonics
In a fully symmetric magnet certain field harmonics are natural.
Magnet type | Allowed harmonics bn
n=1 Dipole | n=3,5,7,...
n=2 Quadrupole | n=6,10,14
n=3 Sextupole | n=9,15,21
n=4 Octupole | n=12,20,28
Non-symmetric designs and fabrication errors give rise to non allowed harmonics: bn with n other than listed above and an with any n
NB: For “skew” magnets this logic is inverted !

## Slide 17: Basic magnet types
Courtesy D. Tommasini, CERN

## Slide 18: Practical magnet design & manufacturing
Steps in the process:
Specification
Conceptual design
Detailed design
  Yoke: yoke size, pole shape, FE model optimization
  Coils: cross-section, geometry, cooling
  Raw material choice
  Yoke ends, coil ends design
Yoke manufacturing, tolerances, alignment, structure
Coil manufacturing, insulation, impregnation type
Magnetic field measurements

## Slide 19: Specification
Before you start designing you need to get from the accelerator designers:
B(T) or G (T/m) (higher orders: G3(T/m2), etc)
Magnet type: C-type, H-type, DC (slow ramp) or AC (fast ramp)
Aperture:
  Dipole : “good field region“  airgap height and width
  Quads and higher order: “good field region“  aperture inscribed circle
Magnetic length and estimated real length
Current range of the power convertor (and the voltage range: watch out for the cables )
Field quality:
Cooling type: air, water (Pmax , Dpmax and Qmax (l/min))
Jacks and Alignment features
Vacuum chamber to be used  fixations, bake-out specifics
These need careful negotiation and often iteration after conceptual (and detailed) design, and will probably be a compromise.

## Slide 20: Conceptual design
From B and l you get NI (A)
From NI (A) and the power convertor Imax you get N
Then you decide on a coil X-section using:
This defines the coil cavity in the yoke (you add 0.5 mm insulation around each conductor and 1 mm ground insulation around the coil) and select the best fitting rectangular
You can the draw the draft X-section using:
Decide on the coil ends: racetrack, bedstead
You now have the rough magnet cross section and envelope

## Slide 21: Power generated
Power generated by coil
DC: from the length of the conductor N∙Lturn , the cross-section s and the specific resistivity r of the material one gets the spent Power in the coil
For AC: take the average I2 for the duty cycle
Power losses due to hysteresis in the yoke: (Steinmetz law up to 1.5 T)
Power losses due to eddy currents in the yoke
Courtesy D. Tommasini, CERN

## Slide 22: Cooling circuit parameters
Aim: to design dcooling , Pwater[bar], DP[bar], Q[l/min]
Choose a desired DT (20ºC or 30ºC depending on the Tcooling water )
with the heat capacity of water (4.186 kJ/kgºC) we now know the required water flow rate: Q(l/min)
The cooling water needs to be in moderately turbulent regime (with laminar flow the flow speed is zero on the wall !): Reynolds > 2000
A good approximation for the pressure drop in smooth pipes can be derived from the Blasius law, giving:
Courtesy D. Tommasini, CERN

## Slide 23: Theoretical pole shapes
The ideal poles for dipole, quadrupole, sextupole, etc. are lines of constant scalar potential
straight line
hyperbola
Dipole
quadrupole
sextupole
Notes: It can be shown that the ideal pole profiles are curves of constant scalar potential. This follows from the definition of the scalar potential itself (not covered here) and from the fact that the flux lines are perpendicular to the iron pole, if the iron permeability is infinite.
The expressions are quite neat in polar coordinates, though they become cumbersome – already for a sextupole – in Cartesian coordinates.
The ideal pole profile for a dipole is simply a straight line.
The ideal pole profile for a quadrupole is a hyperbola.
In my opinion, these formulae are more of academic interest, as anyway the pole is of finite width and its profile is optimized using some simulation tools. My preference is for simple profiles – i.e., profiles that can be described with line segments and circular arcs. This is often possible without any detrimental effect on field quality, especially when the pole is not very wide.
All these profiles can be derived also using conformal mapping. There is quite a bit of elegant complex mathematics in it, details can be found in some of the references.

## Slide 24: Practical pole shapes: shims and alignment features
Dipole example: below a lamination of the LEP main bending magnets, with the pole shims well visible
Quadrupoles: at the edge of the pole one can put a combination a shim and alignment feature (examples: LHC-MQW, SESAME quads, etc)
This then also allows to measure the pole distances : special instrumentation can be made for this
Notes: The ideal poles for a dipole are two infinite parallel lines. Wide poles indeed help for field quality – though they need to be terminated somewhere. At the extremes, shims are then introduced. For long magnets, their size and shape can be simulated in 2D to optimize the on paper field quality (basically, the expected allowed harmonics). The real field quality will depend also on the mechanical tolerances and the possible asymmetry in the magnetic properties of the material.
Here the lamination for the LEP magnets is shown, where about ¼ of the pole width is actually used for shims.
These magnets were rather particular – see the right picture. Since the top field was only 110 mT, the yoke was made in steel / concrete, with the steel being 30% in volume. This is referred to as dilution. We say that the stacking factor is 0.30. In the great majority of cases, the stacking factor is above 97%; the few % unoccupied by iron is taken up by insulation in within the laminations and voids.

## Slide 25: Finite Element electromagnetic models
Aim of the electromagnetic FE models:
  The exact shape of the yoke needs to be designed
    Optimize field quality: adjust pole shape, minimize high saturation zones
    Minimize the total steel amount ( magnet weight, raw material cost )
  Calculate the field: needed for the optics and dynamic aperture modelling
    transfer function Bxsection(I) , , magnetic length
    multipoles (in the centre of the magnet and integrated) bn and an
Some Electromagnetic FE software packages that are often used:
  Opera from Cobham: 2D and 3D commercial software see: http://operafea.com/
  “Good old” Poisson, 2D: now distributed by LANL-LAACG see: http://laacg.lanl.gov/laacg/services/download_sf.phtml
  ROXIE (CERN) 2D and 3D, specialized for accelerator magnets; single fee license for labs & universities see: ttps://espace.cern.ch/roxie/default.aspx
  ANSYS Maxwell: 2D and 3D commercial software see: http://www.ansys.com/Products/Electronics/ANSYS-Maxwell

## Slide 26: FE models: steel curves
You can use a close ‘generic’ B(H) curve for a first cut design
    You HAVE to use a measured, and smoothed, curve to properly calculate Bxsection(I) , , bn and an
    As illustration the curves for several types of steel:
slope is mrm0
End slope is m0

## Slide 27: Yoke shape, pole shape: FE model optimization
Use symmetry and the thus appropriate boundary conditions to model only ¼th (dipoles, quadrupoles ) or even 1/6th sextupoles.
Meshing needs attention in the detailed areas like poles, slits, etc

## Slide 28: Yoke manufacturing
Yokes are nearly always laminated to reduce eddy currents during ramping
Laminations can be coated with an inorganic (oxidation, phosphating, Carlite) or organic (epoxy) layer to increase the resistance
Magnetic properties: depend on chemical composition + temperature and mechanical history
Important parameters: coercive field Hc and the saturation induction.
  Hc has an impact on the remnant field at low current
    Hc < 80 A/m typical
    Hc < 20 A/m for magnets ranging down also to low field B < 0.05 T
  low carbon steel (C content < 0.006%) is best for higher fields B > 1 T
Yoke laminations can be glued together (small to medium size magnets), bolted or welded into stacks
Field Strength H [A/m] | Minimum Induction B [T]
100 | 0.07
300 | 1.05
500 | 1.35
1000 | 1.50
2500 | 1.62
5000 | 1.72
10000 | 1.82
Example specification for 0.5 mm thick epoxy coated steel for LHC transfer line corrector magnet
Bmax=0.3 T
Example specification for 1.5 mm thick oxide coated steel for the LHC warm separation magnets, Bmax= 1.53 T
Field Strength [A/m] | Minimum Induction [T]
40 | 0.20
60 | 0.50
120 | 0.95
500 | 1.4
1 200 | 1.5
2 500 | 1.62
5 000 | 1.71
10 000 | 1.81
24 000 | 2.00

## Slide 29: Yoke manufacturing
Stacking an MBW dipole yoke stack Stacking an MQW quadrupole yoke stack
MQW yoke assembly

## Slide 30: Yoke stack manufacturing
Double aperture LHC quadrupole MQW
Stacking on a precision table
Welding the structural plates
Finished stack

## Slide 31: Yokes: holding a laminated stack together
Yokes are either
  Glued , using epoxy coated laminations
  Welded, full length plates are welded on the outside
  Compressed by tie rods in holes
  or a combination of all these
To be able to keep the yoke (or yoke stack) stable you probably need end plates (can range from ± 1 cm to 5 cm depending on the size)
The end plates have pole chamfers and often carry end shims
Tie rod
Welded stack
Glued yoke (MCIA LHC TL)

## Slide 32: Coil manufacturing, insulation, impregnation type
Winding Cu conductors is an well established technique
When the Cu conductor is thick it is best to use “dead soft” Cu (T treatment)
Insulation of the coil
  Glass fibre – epoxy impregnated
    Individual conductor 0.5 mm glass fibre, 0.25 mm tape wound half lapped
    Impregnated with radiation resistant epoxy, total glass volume ratio >50%
  For thin conductors: Cu emanel coated, possibly epoxy impregnated afterwards

## Slide 33: Coil ends
For dipoles some main types are racetrack of bedstead
Quadrupoles

## Slide 34: Coil manufacturing
MQW Glass fibre tape wrapping.
Winding the hollow Cu conductor

## Slide 35: Coil manufacturing
MBXW Coil winding
Finished MBXW coil
Mounted coil coil electrical test (under water !)
Dipoles racetrack coil

## Slide 36: Magnetic field measurements
Several Magnetic Measurements techniques can be applied, e.g.:
  Rotating coils: multipoles and integrated field or gradient in all magnets
  Stretched wire: magnetic centre and integrated gradient for n > 1 magnets
  Hall probes: field map
  Pickup coils: field on a current ramp
Example below : MQW : double aperture quadrupole for the LHC.
Rotating radial coil

## Slide 37: Sextupoles
These are sextupoles (with embedded correctors) of the main ring of the SESAME light source
Courtesy A. Milanese, CERN
Notes: This is an example of a common design found in synchrotron light sources, where the (short) sextupoles have additional windings so that they can be used as corrector magnets. In this case, the correctors are a horizontal / vertical dipole – providing up to 0.5 mrad kick at 2.5 GeV – and a skew quadrupole.

## Slide 38: Permanent magnets
Linac4 @ CERN permanent magnets , quadrupoles
Courtesy D. Tommasini, CERN
Sextupole Hallback Array

## Slide 39: Hybrid magnets
CLIC final focus,
Courtesy D. Tommasini, CERN

## Slide 40
Examples;
Some history, some modern regular magnets and some special cases

## Slide 41: The 184’’ (4.7 m) cyclotron at Berkeley (1942)
Courtesy A. Milanese, CERN
Notes: This cyclotron magnet was built with 4000 tons of iron and 300 tons of copper. It provided a maximum field of 2.34 T, for a dissipated power of 2.5 MW.
We will not look into this kind of accelerator magnets, sticking to the ones found in synchrotron and related transfer lines.

## Slide 42: Cyclotrons
Harvard 1948
1974

## Slide 43: Some early magnets (early 1950-ies)
Bevatron
(Berkeley)
1954, 6.2 GeV
Cosmotron
(Brookhaven)
1953, 3.3 GeV
Aperture:
20 cm x 60 cm

## Slide 44: PS combined function dipole
Gradient @1.2 T : 5 T/m
Equipped with pole-face windings for higher order corrections
Water cooled Al race-track coils
Courtesy D. Tommasini, CERN

## Slide 45: CPS booster
4 accelerator rings in a common yoke. (increase total beam intensity by 4 in presence of space charge limitation at low energy): B=1.48 T @ 2 GeV
Was originaly designed for 0.8 GeV !
Courtesy D. Tommasini, CERN

## Slide 46: dipole magnet : SPS dipole
H magnet type MBB
B = 2.05 T
Coil : 16 turns
I max = 4900 A
Aperture = 52 × 92 mm2
L = 6.26 m
Weight = 17 t

## Slide 47: Quadrupole magnet : SPS quadrupole
type MQ
G = 20.7 T/m
Coil : 16 turns
I max = 1938 A
Aperture inscribed radius = 44 mm
Lcoil = 3.2 m
Weight = 8.4 t

## Slide 48: MBW LHC warm separation dipole (1)

## Slide 49: MQW: LHC warm double aperture quadrupole

## Slide 50: Elena, anti proton decelerator
.

## Slide 51: Soleil, synchrotron light-source
Courtesy A. Dael, CEA

## Slide 52: Literature on warm accelerator magnets
Books
  G.E.Fisher, “Iron Dominated Magnets” AIP Conf. Proc., 1987 -- Volume 153, pp. 1120-1227
  J. Tanabe, “Iron Dominated Electromagnets”, World Scientific, ISBN 978-981-256-381-1, May 2005
  P. Campbell, Permanent Magnet Materials and their Application, ISBN-13: 978-0521566889
  S. Russenschuck, Field computation for accelerator magnets : analytical and numerical methods for electromagnetic design and optimization / Weinheim : Wiley, 2010. - 757 p.
Schools
  CAS Bruges, 2009, specialized course on magnets, 2009, CERN-2010-004
  CAS Frascati 2008, Magnets (Warm) by D. Einfeld
  CAS Varna 2010, Magnets (Warm) by D. Tommasini
Papers and reports
  D. Tommasini, “Practical definitions and formulae for magnets,” CERN,Tech. Rep. EDMS 1162401, 2011

## Slide 53: Acknowledgements
For this lecture I used material from lectures, seminars, reports, etc. from the many colleagues. Special thanks goes to:
Davide Tommasini, Attilio Milanese, Antoine Dael, Stephan Russenschuck, Thomas Zickler
And to the people who taught me, years ago, all the fine details about magnets !