## Slide 1
WP8 – Innovative Superconducting Magnets
Lucio Rossi – INFN-Milano –LASA for WP8 collaboration members
I.FAST kick off meeting – 4 May 2021 - remote

## Slide 2: WP8 Listing (only part of Magnets)
INFN-LASA
Gabriele.Ceruti@mail.polimi.it

## Slide 3: WP8 duration: from M1 to M48 !! Scope of our WP8 (Magnet part)
Here we want to develop technologies supporting the EU Industry that wish to learn about the CCT developed by CERN.
We aim at something useful for advanced HatronTherapy (SEEIIST)
 1 HTS CCT preceeded by 1 NbTi of same dimension as “gauge”
  2 HTS CCT ideal: need additional effort for budget (HTS tapes -> CERN)
Straight!, since we consider that HTS is already difficult enough!
CCT dipole
4 T operative
5 T target; Ø =60-90 mm;
500mm < L < 1000 mm
Baseline
Dream

## Slide 4: Nb-Ti CCT: p-gantry and HiLumi LHC
LBNL: CCT coil prototype for large acceptance proton gantry  = 400 mm: Successfully tested to 3.5 T; segmented former.
HiLumi LHC: CERN has designed, built and tested a dual 3 T, 2 m long -  = 105 mm, straight CCT. Now IHEP Beijing producing 2x13 units
Short circuit at 3.5T!!
Proto 2m 2.9 T 105 mm very successful at CERN. However, learning and transfer not easy (China…, SE)…

## Slide 5: We build on HTS in Eucard2 – ARIES programs
Courtesy of Glyn Kirby

## Slide 6: Degradation due to the cycle? Cold down also a little suspicious. But happened other times
FeatherM2_1-2
3.1 T in ss - 3.5 T in overshooting mode
FeatherM2_3-4
(Eucard2 cable) 4.5 T (expected > 5 T)
G. Willering, CERN

## Slide 7: LBNL effort on HTS accelerator magnets
Program based on CORC and CCT layout led by X. Wang & S. Prestemon
Program on use of Bi-2212 Rutherford cable with race track and CCT layout led by T. Shen and S. Prestremon
Inner layer
Outer layer
By Advanced Conductor Technologies
Courtesy of Tengming Shen
Courtesy of Xiaorong Wang

## Slide 8: MgB2, instead? It maybe convenient for 3 T
Maybe using MgB2 instead of the first NbTi…
If we can afford the conductor - depending on CERN mainly and on Ic degradation vs curvature radius, we can get some field (3T) with MgB2?
Alternative : explore low losses Nb3Sn, like the one for ITER, as possible alternative to Nb-Ti. Probably it works but is also expensive… Depending also on our Industry partner.
MgB2 cable from HiLumi LHC – WP6 – Courtesy A. Ballarino - CERN

## Slide 9: Program in short

## Slide 10: Program in short – cont.
See next talk by Timeo Winkler

## Slide 11: Timeline
Task 8.1
Task 8.2
Task 8.3
Task 8.4
Task 8.5
Task 8.6

## Slide 12: WP8 Risk & Mitigation Actions
See next talk by Timeo Winkler

## Slide 13: I.FAST WP8 Innovative SC Magnet. Budget for the program.
CERN is Project Coordinator
INFN is the WP8 – Magnet Coordinator (CEA is the deputy) START: 1 May 2021
17.5 94,300 121,200 215,500
22.5 89,900 115,600 205,500

## Slide 14: The amount of personnel paid by EC must be complemented by the matching resources by Institutes. We MUST MEET Deliverables!!

## Slide 15: HITR+ WP8 (Magnet Design) and I.FAST WP8 (Innovative Magnets) will work closely together …
&

## Slide 16: Thanks!
(reserve slides follow)

## Slide 21: Last task led by GSI – see next talk!