## Slide 1: Inverted and thin NEG, where we are M.Taborelli, L.Lain Amador, P.Costa Pinto, L.Ferreira, P.Chiggiato TE-VSC

## Slide 2
Inverted NEG scheme
Performance of inverted NEG
Performance of thin NEG < 1μm
Summary

## Slide 3: Inverted NEG (Non Evaporable Getter) scheme
Additional NEG layer on the Al mandrel

## Slide 4
Control of the NEG thickness
Analysis in XRF after cutting the chamber:
The thickness is uniform
Composition is uniform and correct
A. E. Prodromides et al. Vacuum 60 (2001) 35, 41

## Slide 5: Crystalline Structure
All samples show the small crystal size (estimated around 3 nm)
XRD analysis
5
Ref. prepared by the conventional coating process

## Slide 6: Pumping performance: transmission method
Cold trap to remove “parasitic” CH4 (not pumped by NEG)
Steady state upon H2 injection:
P2/P1 + Monte Carlo calculation (Molflow) : enable to get the sticking coefficient for hydrogen

## Slide 7: Pumping performance: what can be measured
Φ 5 mm
We expect a sticking of 10-3 10-2 and can easily measure a pressure ratio of 0.5-0.005: not for too slim chambers!
Φ 16 mm x 0.4 m
Φ 12 mm x 0.3 m
L/R=50
L/R=120
L/R=480
L/R=666
2 m
Φ4 mm
L/R=1000
0.3 m

## Slide 8: Pumping performance: sticking factor and speed
Reproducible
Reaches reference sticking and pumping speed (Ex: For a chamber of 6 mm diam. the pumping speed for H2 will be 5.6 l/s/m)
Activation is delayed in temperature compared to standard reference
Sticking factor for H2
0.4
0.3
0.2
0.1
Pumping speed l/s/cm2

## Slide 9: Pumping performance: aging
Expected for standard NEG
Aluminium mandrel 0.5 mm

## Slide 10
The expected capacity( as reference) is reached
Also in this case there is a delay in the temperature
Saturated surface: 1 Monolayer ML CO (defined as 5x1014 -1x1015)
CO is adsorbed on the surface
C=O
C=O
C=O
Pumping performance: CO capacity
1ML

## Slide 11: Hypotheses for the origin of delay
Impurities incorporated during the process?
transferred to the NEG from the electroplated copper substrate
coming from the chemical baths
The active surface of the film is the part deposited initially on the Al mandrel
Does it oxidize more than for the usual air exposure?
Is the structure of the very first layer of coating different?

## Slide 12: Origin of delay: comparison of substrates
Electroformed copper has in general few more impurities than OFE:
Still there is no evidence that O related impurities those play a role for the activation
Measured in Thermal Desorption Spectroscopy on 10x10x1 mm samples

## Slide 13: Orgin of delay: different plating recipes?
Not much statistics, but ...no marked difference with electroforming in pulse mode or DC (with brightener)
In spite of the different purity of the copper the performance of NEG is similar and delayed with respect to the reference NEG
Sticking factor for H2

## Slide 14: Origin of delay: etching and mandrel thickness
Thickness of aluminium mandrel
0.5 mm, 7h etching
1.5 mm, 24 h etching
This was on cut the chambers? See PhD
Decrease of O in XPS
Better activation with thin mandrel
2 Al(s) + 2 NaOH(aq) + 2 H2O(aq) → 2 NaAlO2(aq) + 3 H2(g)
100
80
60
40
20
0
O1s peak area % (rel. units)
Sticking factor for H2

## Slide 15: Making the NEG thin (if necessary for impedance)
For a film with much lower conductivity (σf NEG) than the substrate (σs Cu) the impedance is only governed by film thickness d
E.Belli et al
PR Accel Beams 21 111002 (2018)
d
d
σf
σs
σf
σs
s
s

## Slide 16: How much cycles for thin NEG?
The expected effect is a higher sentitivity to venting/activation cycles for thin NEG: indeed……
After 4 cylces of venting /activation the activation of thinner films requires more time
→It is more difficult for the surface oxygen to diffuse into the film

## Slide 17
How much cycles for thin NEG?
As expected after some cycles the concentration of dissolved oxygen is higher in thinner films
The lower concentration gradient slows down the further diffusion and activation
XPS
depth profiles
30 nm
203 nm
1100 nm

## Slide 18: How much cycles for thin NEG?
Reduction of the surface oxides
(X-ray Photoelectron Spectroscopy)
For film thickness ≥100 nm the activation after few (4) cycles can be recovered for 21h of activation at 250C
250C activation
O1s peak area % (rel. units)
80
70
60
50
40
30

## Slide 19: Photon stimulated Desorption on thin NEG
Critical energy:4keV
Incidentangle:10mrad
Powerdensity:20W/m
150 nm thick NEG
Cycles 1-4: PSD decrease with venting/activation(250C x 4h)/irradiation cycles
Cycle 10: slight increase when venting/activating without further irradiationn, but conditions quickly (irradiation helps to reduce H content)
Cycle 11: venting without activation
For PSD the thin NEG is robust upon cycling
StSt
Y.Tanimoto et al.

## Slide 20: What do we know on thin and inverted NEG
Property/NEG | Standard NEG | Thin NEG | Inverted NEG
1st activation O decrease | 250C x 1h | Lowest thickness 30nm | 250C x 1h
N cycles: O decrease | (see pumping) | >100 nm 250C x 24h N ≤ 4 | ?
1st activation pumping speed | 180-200C x 24h | Reduced for 200 nm | 275C x 24h
pumping speed: N cycles | Sticking 1/N , N≤ 20 200C x 24h | ? | Sticking as expected 1/N, N≤ 3 , 275Cx24h
PSD | Ec = 20keV, 250C x 24h | 150 nm, Ec=4KeV, 250C x 4h, N=10 | ?
SEY | 1.1 for 250 C x 1h | >30 nm 1.2, 250C x 24h | 1.2 for 250C x 1h
SEY, N cycles | 1.2 , 250C x 1h for N=3 recovers at 300 x 1h for N=10 | 200 nm 1.2, 250C x 24h , N = 4 | ?

## Slide 21: Thank you!

## Slide 23: Pumping speed and H2 saturation of NEG
For 1000 nm the pumping speed is as expected: after saturation a regeneration (no venting) of 24h x 250C, recovers only half of the initial pumping speed.
For 200 nm the pumping speed is about half of reference: after saturation and regeneration (no venting) it recovers the same value for several saturation (no venting) cycles
Atomic concentration of H in the film is similar for both thicknesses (~4% at. H in the film): did we reach equilibrium of H dissolved and H2 pressure during activation?
Chart: H2 pumped moleculs [mol/cm2]
| 15370063030453.057 | 21835678367577.133 | 589681846105791.88 | 2849691966716791 | 1.1907019784086634E+16 | 2.2734904265400984E+16 | 2.2734904265400984E+16 | 2.5839736927554156E+16 | 3.0192321781224992E+16 | 3.2349364431573368E+16 | 3.7645735597377216E+16 | 4.9081481641474032E+16 | 5.2141351057410968E+16 | 5.5470505068710688E+16 | 5.7106982002367944E+16 | 7.20408104179522E+16 | 7.8958433113476576E+16 | 9.876475725825176E+16
1000 nm 1st saturation | 742.9028 | 726.5405 | 709.6905 | 680.3259 | 571.4134 | 415.1623 | 377.0304 | 370.5824 | 341.0825 | 315.5161 | 255.8616 | 168.8693 | 147.742 | 135.243 | 125.3738 | 69.4508 | 57.3603 | 33.1025
1000 nm 2nd saturation | 392.9097 | 392.0988 | 381.6832 | 357.7942 | 363.3439 | 369.0108 | 400.0558 | 384.6508 | 377.0304 | 377.0304 | 344.7652 | 293.1456 | 135.243 | 120.8393 | 79.6191 | 73.3077 | 69.4517 | 49.1168
200 nm 1st saturation | 354.3161 | 354.3161 | 321.2476 | 293.2679 | 293.2637 | 270.8814 | 251.2973 | 251.2973 | 176.4925 | 125.4117 | 87.2696 | 69.4706 | 51.373 | 34.5098
200 nm 2nd saturation | 350.413 | 326.8379 | 293.2582 | 267.4329 | 245.2977 | 226.1144 | 181.3553 | 175.7595 | 132.1229 | 104.4315 | 78.0753 | 58.2819 | 37.9557 | 21.6696 | 13.5338
200 nm 3rd saturation | 417.8916 | 426.968 | 410.76 | 424.9507 | 391.957 | 400.1992 | 323.7426 | 321.198 | 230.2922 | 187.2331 | 158.9687 | 125.406 | 85.4511 | 60.4475 | 36.7881
Chart: recovery of the pumping speed after saturation with H2 (200 nm film)
| 24
Initial pumping speed | 376
after 3rd saturation | 316 | 316 | 378 | 377 | 430

## Slide 24
Inverted NEG:
Shows a decrease of SEY which is not delayed

## Slide 25
4th activation cycle at 250 oC
Reduction of the surface oxides
(X-ray Photoelectron Spectroscopy)
Maximal secondary electron yield
3 – Studies on “very thin” NEG films