## Slide 1: Large volume GEM production Rui De Oliveira TE/MPE/EM

## Slide 2: Summary
GEM Single mask production process in details
Production at CERN
  New equipments
  New building

## Slide 3: Process step by step

## Slide 4
5um Copper
5um Copper
50um Polyimide
Base material
50um adhesiveless copper clad Polyimide
Rolls of 100m x 600mm
Polyimide : APICAL NP or AV
2 suppliers :
Sheldhal (US)
Nippon steel (Jp)
CR layer 10nm

## Slide 5
Photoresist deposition
Optimized process
15um dry resist (KL 1015 – Korea)
15um resist
15um resist
Maximum size 100m x 600mm
Dupont manual laminators

## Slide 6
Photoresist holes patterning
Optimized process
15um resist
15um resist
70um
hole
UV exposure
2.2m x 0.6m
Continuous
Development
0.65m

## Slide 7
Top copper etching
Optimized process
Add some test patterns for fast check?
Continuous spray copper etching
0.65m width

## Slide 8
Resist stripping 10GEM/day
Should be improved to strip 5 to 10 GEM / hour
Dead bath : alcohol

## Slide 9
Polyimide anisotropic etching
5 GEMs/day
Not optimized process
Dead bath
70um
30um

## Slide 10: Tooling for polyimide etching
Previous tool
2m x 0.6m
Risky handling
Heavy
3 GEMs/day
Present tool
1m x 0.6m
Less risky
Light
5 to 6 GEMs/day
Future
No tool
100m x 0.65m
30 to 40 GEMs/Day
Optimized process
Poliymide etch , rinse and dry

## Slide 11
15um resist
Bottom resist protection deposition
Optimized process
We have moved from liquid resist to solid
STD lamination
0.65m width

## Slide 12
Bottom copper etch by chemical reaction
Top copper protected by galvanic connection
etchant

## Slide 13
Tooling for electro-copper etching
Lots of manual operation
Limiting to 4 to 5 GEMs/day
Need to be improved
FR4 frame
Copper on both sides
Electrically isolated
Top and bottom GEM
connection to frame
1 to 2 cm needed
to make the
connection

## Slide 14
Resist stripping
Not optimized process
Will move from 10 GEM/day to 30 GEM/day
Dead bath : alcohol

## Slide 15
Soft Polyimide etching
The hole become double conical
Not optimized process : 6 to 7 GEM/day
Will move to more than 30 GEM/day

## Slide 16: cross section pictures

## Slide 17: Top and bottom aspect
TOP
BOTTOM
With solid resist in
last productions It’s hard
to make a difference
With liquid resist during
Copper electro etching

## Slide 18: Comparison with std GEM from external supplier
70um copper hole diameter target
Polyimide hole above 50um

## Slide 19: Defects (CMS GEM)
-Copper remains in between some sectors
-We have introduced
a HV test between sectors before delivery
-Previously only an isolating test was performed
-Oxide traces
-No electrical effect
-But we try to avoid them
-Defects due to dust during photoresist patterning.
-Improve cleanliness during image transfer
-No incidence in sparks

## Slide 20: Examples
Large GEM already produced:
ILC Dhcal: 1m x 33cm (5 pieces)
Kloe: 750mm x 40cm (30pieces)
CMS: 1m x 45cm (6 pieces)
CMS
KLOE

## Slide 21: GEM single mask processes needed to be optimized
Chemical Polyimide etching
Second Polyimide etching
Copper electro etching
Stripping
Reality

## Slide 22: Production at CERN
GEM size
  With existing equipments 1.5m x 0.5m active area
  Mid 2011: 2m x 0.5m active area
Volumes
  With existing equipment: 10 GEMs/month.technician
    We can hire one more technician
  Mid 2011: 24GEMs/month.technician (240GEM/year)

## Slide 23: GEM equipment investment in the existing CERN premises early 2011
  -1 continuous polyimide etch machine 100 kCHF
    Existing equipment limits us to 5 GEM/day (polyimide etch step) with heavy tooling and big handling risks (for the GEM)
    The new equipment will do 1 GEM every 5mins without tooling and no handling risk
  -1 Cu electro etch line 140 kCHF
    Existing equipment is limited to 1m x 0.6m with baths in different places
    The new equipment will be able to treat 2m x 0.6m GEM in the same line
  total: 240 kCHF

## Slide 24: New building
PCB workshop
-1400 m2 (now 1000m2)
-Modern Chemical zone
-Modern Water/air treatment
-Room for new processes
-laser
-plasma
-MPGD
-Replacement of old equipment
-Ergonomic layout

## Slide 26: Cross section
Timing:
Nov 2010 Market survey results for consulting
Design 3 months
Market survey for construction
March 2011 call for tender for construction
Mid 2011 construction start
Mid 2013 construction end

## Slide 27: Other GEM possibilities
Copper hole diameter down to 30um
Hole pitch down to 50um
Polyimide thickness 12.5 , 25 or 50 um
Sectors down to 1mm
Possibility to add holes in the gluing regions

## Slide 28: Outsourcing
Micrometal (Germany)
New Flex (Korea)
Keerthi industries (India)
Tech-etch (US)
With some offers for large volume production
we start to see the limit price of the GEMs : in
the range of 600 CHF/sqr.meter

## Slide 29: Summary
We have some possibilities to make GEM outside CERN
Still need work to find the best choice
  We are now interesting for industry.
TE-MPE-EM can increase its capacity to face GEM productions up to 500 pieces/ year (1m x 0.5m)
Should we propose std 100 x 100 single side GEMs at CERN store (50% cost reduction)?