## Slide 1: Discussion Defect Characterization

## Slide 2
Collaboration on “acceptor removal” in p-type Si: Bucharest, CERN, Minsk, Hamburg, CiS formed (TSC, DLTS, HRTEM, PL)
project: Schottky diodes on Epitaxial Silicon for Radiation Damage Characterization of CMOS MAPS : (RAL, Giulio Villani)
Defect and Material Characterization

## Slide 3: Defect and Material Characterization
Main activities
  Detection and microscopic characterization of standard and material engineered silicon via dedicated techniques (DLTS, TSC, TDRC, SIMS, ICP-MS, PITS, FTIR, TCT, EPR, HRTEM, PL, fluorescent centers ?)
  Identification of electrically active defects induced by irradiation responsible for trapping, leakage current, change of Neff , change of E-Field
  Studying possible application for radiation hardening
  Deliver input for device simulations (e.g. TCAD) to predict detector performance under various conditions
Milestones [2018-2022]
    WP 1.1 Electrically active defects in p-type silicon [7 MS]
    WP 1.2 Microstructural Investigations on extended and clustered defects [4 MS]
    WP 1.3 Theory of defects and defect kinetics modeling [5 MS]

## Slide 4
Status: As irradiated – several type of diodes (FZ, CZ, EPI), several type of irradiations (e, n, p)
  High fluences (CV, IV, TSC and HRTEM):
  - STFZ PiN diodes and LGADs (CNM) in Bucharest (2019), CV/IV, TSC and HRTEM
  - EPI PiN diodes of different resistivity at Hamburg and CERN, CV/IV, TSC (ongoing)
  - HRTEM on highly neutron irradiated samples (1017cm-2 and 1019) (done in Bucharest)
  Low fluences (CV/IV and DLTS):
    - electron irradiated EPI PiN diodes (Minsk, CERN and Hamburg) (ongoing)
    - neutron and proton irradiated EPI, CZ and FZ PiN diodes (CERN, Hamburg and Bucharest)
Annealing studies (DLTS, TSC, HRTEM)
at 60 / 800 C – TSC, partly done for hadron irradiation (EPI 50 ohmcm at Hamburg), DLTS (Bucharest and CERN); at T > 150 C – done on electron irradiated samples (DLTS, Minsk), started at Hamburg on some hadron irradiated samples (TSC) and it will start soon in Bucharest (DLTS, TSC)
HRTEM on highly neutron irradiated PiN samples (ongoing in Bucharest)
WP 1.1. Electrically active defects in p-type silicon
M2: Determine defect annealing behaviour in STFZ and engineered silicon. Correlation with device performances (Q4/2019)
M3: Determine defect transformations and kinetics in STFZ and engineered silicon after treatments at high temperatures (between 150 °C and 350 °C). Correlation with the device performance (Q3/2020)
  M4: Identify the role of impurities in the formation of defects impacting on device performance (Q1/2021)
  M5: Detection/characterization of radiation induced defects in LGAD and HV-CMOS sensors based on STFZ and defect engineered p-type silicon, establish the annealing behavior (annealing at 80°C), correlation with electrical performance of the devices (Q3/2021)

## Slide 5
  WP 1.2. Microstructural Investigations on extended and clustered defects M1: Microstructural characterization of the radiation induced clustered defects (fluences between 1015 and 1017 neq cm-2) and monitoring of the evolution of clusters at 80 °C (Q3/2019)
  M2: In situ- annealing studies at 5 temperatures (between 150 °C and 350 °C) in order to determine the structural transformations of the extended and clustered defects (Q3/2020)
  M3: Microstructural characterization of the oxide semiconductor interface in irradiated LGADs and HV CMOS devices, time evolution at 80 °C (Q3/2021)
  M4: Microstructural characterization of the oxide semiconductor interface in irradiated optimized LGADs and HV CMOS devices (Q3/2022)
Status:
  - HRTEM on STFZ PiN diodes and LGADs (CNM), fluence 1015 n/cm2, and annealing up to 240 C, in Bucharest (2019)
  HRTEM on LGADs (fluence ~1019cm-2 ) in Bucharest
- finished
- started
- not yet started

## Slide 6
WP 1.3 Theory of defects and defect kinetics modelling
M1: Modelling of the detected defect generation/kinetics and of the impact on the device performance corresponding to annealing treatments at 80 °C (Q3/2020)
M2 : Modelling of the detected defect generation/kinetics and of the impact on the device performance corresponding to annealing at temperatures between 150 °C and 350 °C and final assessment of the role of the intentional added impurities (Q1/2021)
M3 : Identification of the optimal impurity concentrations for pads, LGADs and HV CMOSs as input for production. (Q3/2021)
Status:
– ongoing with the BiOi generation rate “puzzle”, A&B configurations, C content
- finished
- started
- not yet started

## Slide 7: Thoughts
Acceptor removal
  Need to clarify and parametrize, if possible, the multiple reasons for the strong variations of gBiOi. Combine the “macroscopic” acceptor removal models (i.e. parameterization of the c parameter) with the formation of defects (i.e. BiOi formation rates) – can C can be accounted too?
    gBi=2gABiOi +gBBiOi, where gBBiOi is unkown yet!
    Carbon content, still not accounted
  Need to have all the information about the samples (producer, process, size, macroscopic behaviour –when sent for DLTS/TSC investigations)
  Need to clarify the impurity content by SIMS (especially C) in the samples and by LA-ICPMS (B and P) to determine the actual doping process (how much of B doping is compensated by P in the different samples)
  Need DLTS/TSC on CMOS sensors (some LGADs are measured in Bucharest)
  Need to link observations (acceptor removal) on LGADs, CMOS and p-type pad sensors with the defect formation (TSC, DLTS,..) measurements
  Try to measure [BiBs]
  Find effective capture parameters of BiOi for different electric fields to be used in TCAD simulations
  Try to measure [Bs] in irradiated samples

## Slide 8: RD50 Working Plan -Defect and Material Characterization
M1: Detection and characterization of all radiation induced defects in STFZ and engineered silicon (Q3/2019) – (done on neutron irrad. STFZ, PiN and LGADs produced by CNM, on electron irradiated EPI diodes
M2: Determine defect annealing behaviour in STFZ and engineered silicon. Correlation with device performances (Q4/2019) (done on STFZ, PiN and LGADs produced by CNM, started on EPI of different resistivities and CZ samples)
  M3: Determine defect transformations and kinetics in STFZ and engineered silicon after treatments at high temperatures (between 150 °C and 350 °C). Correlation with the device performance (Q3/2020)
  M4: Identify the role of impurities in the formation of the defects impacting on the device performance (Q1/2021)
  M5: Detection/characterization of radiation induced defects in LGAD and HV-CMOS sensors based on STFZ and defect engineered p-type silicon, establish the annealing behavior (annealing at 80°C), correlation with electrical performance of the devices (Q3/2021)
  M6: Validity tests on optimized material engineered sensors (pads, LGADs and HV CMOSs). Comparison between prediction and experiments (Q1/2022)
  M7: Validity tests on finally optimized material engineered sensors (pads, LGADs and HV CMOSs) (Q3/2023)
- finished
- started
- not yet started
WP 1.1. Electrically active defects in p-type silicon
Analysis of electrically active defects and of the radiation induced changes in the electrical characteristics of devices built on p-type silicon.

## Slide 9
  M1: Microstructural characterization of the radiation induced clustered defects (fluences between 1015 and 1017 neq cm-2) and monitoring of the evolution of clusters at 80 °C (Q3/2019)
  M2: In situ- annealing studies at 5 temperatures (between 150 °C and 350 °C) in order to determine the structural transformations of the extended and clustered defects (Q3/2020)
  M3: Microstructural characterization of the oxide semiconductor interface in irradiated LGADs and HV CMOS devices, time evolution at 80 °C (Q3/2021)
  M4 : Microstructural characterization of the oxide semiconductor interface in irradiated optimized LGADs and HV CMOS devices (Q3/2022)
- finished
- started
- not started yet
WP 1.2. Microstructural Investigations on extended and clustered defects This work targets microstructural investigations of extended and clustered defects by electron microscopy:

## Slide 10
M1: Modelling of the detected defect generation/kinetics and of the impact on the device performance corresponding to annealing treatments at 80 °C (Q3/2020)
M2 : Modelling of the detected defect generation/kinetics and of the impact on the device performance corresponding to annealing at temperatures between 150 °C and 350 °C and final assessment of the role of the intentional added impurities (Q1/2021)
M3 : Identification of the optimal impurity concentrations for pads, LGADs and HV CMOSs as input for production. (Q3/2021)
M4 : Improvements of the developed models according to validity test foreseen at WP.1.1 - M6 and provide new optimization solutions for WP.1.1-M7 (Q3/2022)
M5 : Validity test for the developed theoretical models based on the results obtained on WP.1.1 - M7 optimized sensors (Q3/2023)
- finished
- started
- not started yet
WP 1.3 Theory of defects and defect kinetics modelling