## Slide 1
Soleil: update on status of pumping property testing facility, SR beamline and capabilities in thin film characterization
C. Herbeaux
On behalf of Vacuum group
IFAST Task 10.5 Kick-off Meeting
May 12, 2021

## Slide 2: Contents
Reminder on NEG coating capabilities at SOLEIL
  Sticking factor and sorption capacity characterisation
  PSD beamline
Possible evolution of the PSB beamline
Last results for PSD measurement
Conclusion

## Slide 3
NEG coating Characterization
2 Transmission Method Test Benches for NEG coating characterization
P2
P1
Pinj
Gas inlet
C <<
Turbo
Sticking factor
Sorption capacity
Activation optimization
@ Vacuum LAB
Transmission Method
P. Costa Pinto, P. Chiggiato, A. Sapountzis, T. Sinkovits, M. Taborelli,
CERN 80th IUVSTA Workshop, NSRRC, Hsinchu, Taiwan (2016)
is calibrated with MOLFLOW+ to find
See Nicolas Béchu presentation for more details

## Slide 4
NEG coating Characterization
Typical
Sorption Capacity curves of NEG coating
for Increasing activation T°
Evolution of the ratio
( ‘pumping speed ’)
is a function of the number of injected molecules
When the NEG starts to saturate the ratio start to decrease
When the activation T° is higher the NEG can pump more molecules
Threshold ~ 180°C
Optimum ~ 250°C
for a standard TiZrV 1µm NEG
@ Vacuum LAB

## Slide 5
NEG coating Characterization
C [l.s-1]
S [l.s-1]
PT [mbar]
S.R
Q [mbar.l.s-1]
η
Q ~ C x PT
C << S
Photon to molecule yield η
(gas load)
TEST Chamber
beam collimation
SIP
SIP
 photon exit D08-1 but inside the Storage Ring
Evolution of the PSD yield with the photon dose
Activation of the NEG with RS?
‘Have an insight’ into the NEG
« dynamic pumping »
« dynamic saturation »
In operation since October 2020
@ PSD Beamline on D08-1

## Slide 7
NEG-coated,
Water cooled chambers
from SAES
Cu-OFS
DN63
NEG coating Characterization
Ongoing ‘TEST PLAN’
[ april 2021 ]

## Slide 8
Possible evolution of PSD Beamline
C [l.s-1]
S [l.s-1]
PT [mbar]
S.R
Q [mbar.l.s-1]
(gas load)
TEST Chamber
beam collimation
SIP
SIP
Adapt the PSD beamline for 3 gauge method
Turbo molecular pump
+ gauge+RGA
Turbo molecular pump
+ gauge+RGA
gauge+RGA

## Slide 9
NEG coating Characterization
@ PSD Beamline on D08-1
Very first experiment / Oct-Nov 2020
DN63
chamber
Representative
Data
1 m

## Slide 10: Last PSD Measurements
Red curve : DN20 SS chamber showing bad results maybe consequence of problems occuring during bake out and activation
Green curve : DN20 Cu OFS chamber showing good results before and after activation

## Slide 11
After PSD measurement the sorption capacity of the bad DN20 SS chamber has been measured : The NEG coating is not efficient.

## Slide 12: Comparison od DN60 and DN20 chambers
Slopes after activation are different : geometry effect?

## Slide 13: Conclusion
The characterization of NEG coating are going on with sorption and PSD measurement
Evolution of the PSD beamline in considered for 3 gauges method measurement
Recent experience indicates that sorption characterization must be done before PSD measurement in order to validate the coating quality.