## Slide 1: MCBXF Magnet production at CIEMAT
Series Production kick-off meeting – 23rd April 2021
Carla Martins (CIEMAT)
On behalf of MCBXF CERN-CIEMAT Collaboration

## Slide 2: MCBXF Cable Revision
Position
Defect
Reparation

## Slide 3: MCBXF Coil Winding
    Split cable for Inner and Outer Layer
End spacers: 3D printing in stainless steel. Insulated with glass fiber tape impregnated with binder (acetone as solvent)
Copper wedges: insulated with glass fiber sleeves glued with binder at both ends
Winding tension is decreasing while the turns are increasing (from 4.5 kg to 3.5 kg).
Measurement of last cable at both ends on every turn registered.

## Slide 4: MCBXFB Coil Binding (I)
    We use binder (CTD 1.1) with butanone as solvent. Curing at 120ºC during 18 hours with slow cooling.
It is necessary to apply binder on both layers (inner and outer). For the inner layer, we use the same mould with fillers replacing the outer layer.
    Binder is applied with a brush, controlling applied weight by zones.
Binding mould is assembled at the winding machine. Delicate process to avoid cables loosening

## Slide 5: MCBXFB Coil Binding (II)
    Heating using resistors. The complete mould is thermally insulated with several layers of aluminium foil.
    Resistors (4 at each side of the mould and up)
    Aluminium foil insulation
    Temperature control system

## Slide 6: MCBXFB Coil Binding (III)
    Important to avoid wrinkles in kapton protective sheets during mould assembly. During the curing cycle, more and bigger wrinkles could appear and the cable insulation could be damaged.
    The coil length increases due to the pressure applied by the mould. Elongation usually is larger in the inner layer (winding over kapton foil) than in the outer one (winding over Nomex, less smooth).
    The coil is now rigid enough to be manipulated during the next steps of the fabrication.
    After the binding of each layer, the final end spacers must be adapted to the last cable block at each end of the coil.

## Slide 7: MCBXFB Coil Impregnation (I)
    The tasks needed to prepare the coil for impregnation take place in a custom table

## Slide 8: MCBXFB Coil Impregnation (II)
    Lifting of the winding mandrel is very delicate operation. It is important to be very careful with the previous steps to avoid damaging the coil

## Slide 9: MCBXFB Coil Impregnation (III)
    Tinning mould used to stabilize the current leads of the coil
    Intermediate measurements between impregnation mould parts and adjustments needed to ensure that everything is in place (to avoid/minimize leaks).
Stabilized and insulated current lead

## Slide 10: MCBXFB Coil Impregnation (IV)
    Transversal mould closing with silicone seals is also very delicate. To avoid the expansion of the resin entrance (& exit) holes, a new design has been implemented.
The hole in the silicone seal must be placed far from the closing sheet (to avoid ripping)
Hole
Closing sheet
  A first leak test of the mould with He gas take place outside the vacuum chamber
  A second leak test at warm conditions before starting each impregnation process is established to check that the mould is properly sealed

## Slide 11: MCBXFB Coil Impregnation (V)
    The mould is introduced in a custom vacuum chamber to ease vacuum processing. The heating of the mould is also made by resistors (up & down the mould).
    The coils are impregnated with CTD-101K resin at 60ºC (mould and resin). Curing for 16 hours at 125ºC.
    Vacuum chamber

## Slide 12: MCBXFB Coil Impregnation (VI)
    Impregnation mould opening

## Slide 13: MCBXFB Coil Quality Control
Dimensional measurements with CMM to control principal dimensions of the coil (length, pole window, midplane). The coil is measured clamped onto the winding mandrel.
Electrical measurements: resistance, self-inductance and insulation. The self-inductance is measured with a frequency sweep to detect short-circuits, due to the large number of turns
Chart: L (H)

## Slide 14: MCBXF Components: Collaring Shoes & GI
Ground insulation (kapton foils) pre-formed at 140ºC heating during 6 hours.
Collaring shoes are laser-cut and pre-formed with a custom tooling (0,5mm stainless steel sheet).

## Slide 15: MCBXF Components: Collars
Prototype collars manufactured by EDM wire-cut
Collar sets assembled using a custom tooling
Instrumentation done at CERN

## Slide 16: MCBXF Components: Iron Yoke laminations
Iron laminations for the prototypes manufacturing process:
  Laser cut
  EDM wire cut
  Black oxide for surface protection

## Slide 17: MCBXF Components: End Plates & Rods
Two 70mm thickness endplates (stainless steel), with eight rods (also stainless steel) compress the iron laminations

## Slide 18: MCBXF Components: Connection Plate
Duratron and G10 parts (radiation resistant)

## Slide 19
Summary (I)
    Cable revision (and reparation of insulation defects if any).
    Coil winding:
      Decreasing tension (from 4,5kg to 3,5kg). Cable position at both heads monitoring (compare with nominal values, and other coil data).
      Insulate (glass fiber tape) all components in touch with cable.
    Coil binding:
      CTD 1.1 with butanone. Control quantity applied by weight.
      Avoid kapton wrinkles.
    Coil impregnation:
      CTD 101K resin.
      Lifting of the winding mandrel and closing of the impregnation mould is a delicate operation.
      Leak test of the mould at room temperature + leak test (in vacuum chamber) at warm temperature.

## Slide 20
Summary (II)
    Coil quality control:
      Dimensional measurements with CMM.
      Electrical measurements (resistance, self-inductance and insulation).
    Other magnet components:
      Ground insulation (GI).
      Collaring shoes.
      Collars.
      Iron Yoke laminations.
      End Plates and Rods.
      Connection Plate.

## Slide 21: Thanks for your attention