## Slide 1
NbTi Round Busbars for Powering the HL-LHC Inner Triplets: a Study Analysis
G. Succi, B. Bordini, D. Baffari

## Slide 2
Contents
Introduction
The 2 kA and 18 kA busbars
THEA model
Results
Current dump and validation time
Quench stoppers
To resume and conclusions

## Slide 3
Contents
Introduction
The 2 kA and 18 kA busbars
THEA model
Results
Current dump and validation time
Quench stoppers
To resume and conclusions

## Slide 4
Introduction
The Inner Triplet (IT) magnets are powered by the following set of subsystems: Sc link, DFX (Distribution FeedBoX), DCM (D1 to DFX Connection Module), N lines, and the NbTi magnet leads.
λ plate
Courtesy: Y. Leclercq
19 busbars are routed through the DFX.
The λ-plate (plug) assures electrical continuity for the powering, but hydraulic discontinuity between the LHe and SFHe volumes of the DFX and of the DCM.

## Slide 5
Introduction
Cases analysed here
Courtesy: E.Todesco

## Slide 6
Contents
Introduction
The 2 kA and 18 kA busbars
THEA model
Results
Current dump and validation time
Quench stoppers
To resume and conclusions

## Slide 7
The 2 kA and 18 kA busbar
The 2 kA and 18 kA circuits in the DFX, DCM, and N lines are made of NbTi round busbars:
Cu core is multifilamentary and void fraction is ~30 % [1]
[1] J. Fleiter and S. Hopkins, Private communication

## Slide 8
Contents
Introduction
The 2 kA and 18 kA busbars
THEA model
Results
Current dump and validation time
Quench stoppers
To resume and conclusions

## Slide 9
THEA Model
We define 1 thermal component coupled to 1 electric component. There is no transverse heat propagation to the surroundings (e.g. a jacket).
We set an initial minimum normal region at the centre of the domain, , to trigger the quench propagation. and elsewhere.
Note: NbTi resistivity is modelled by means of the power law, using and n from the table.
Ex: 18 kA busbar
1.9 K
1.9 K
x=0
x=23 m
Note: the component is represented as a cylinder, but it is treated as a 1-D line by the code
I=18 kA
B=0.55 T

## Slide 10
Results
T(x) profile
ΔV(t) evolution
‘Knees’ define the moments when the region inside the corresponding V taps loses the sc state.

## Slide 11
Results
Knees are useful to derive the QPV
1) Average velocity:
2) Punctual velocity:
The QPV is 1.7 m/s in the 2 kA busbar and roughly 3 times higher in the 18 kA busbar (5.4 m/s).

## Slide 12
Results
The field increase makes the QPV to increase by ~0.1 m/s and 0.5 m/s in the 2 kA and 18 kA busbars, respectively.
Given the same ratio of field increase (2, in this case), an higher absolute field makes the QPV to accelerate more.
QPV as f(B)

## Slide 13
Contents
Introduction
The 2 kA and 18 kA busbars
THEA model
Results
Current dump and validation time
Quench stoppers
To resume and conclusions

## Slide 14
Current dump and validation time
We want to derive the maximum validation time, , to assure that current reduces by 90 % before of a constant current case: .
Once we know and , the detection threshold determines the remaining parameters.
Time scale
depends on the detection threshold, ΔV
τ is the time-constant of a specific circuit

## Slide 15
Current dump and validation time
We express and for each circuit of interest.
2 kA circuit (MCBXF)
18 kA circuit (D1)
18 kA circuit (MQXF)
Taking the 100 mV threshold as reference for quench detection [1], the maximum validation time is at least 8.2 s for the 2 kA circuit of the MCBXFs, 2.8 s for the 18 kA circuit of D1, and 1.4 s for the MQXF.
Note:
D1 and MQXF differ both by (13 kA and 18 kA, respectively) and by the constant for the current decay
[1] R. Denz, Quench Detection Systems for HL-LHC Busbars, 2021

## Slide 16
QPV and validation time as f(I)
We study the dependence of the QPV and validation time on the busbar current (ex. 2 kA busbar).
Transition to normal state slows down as I decreases: , , and , as well.
The maximum validation time, , corresponding to guarantees the proper busbar protection under all operating conditions.

## Slide 17
Contents
Introduction
The 2 kA and 18 kA busbars
THEA model
Results
Current dump and validation time
Quench stoppers
To resume and conclusions

## Slide 18
Quench stoppers
Is it possible that a quench remains confined in a limited busbar region without being detected, while T diverges above 100 K?
Current flows only in copper during quench
Thus, . We start the computations assuming:
To answer this question, we analyse the quench length to have a voltage drop of 10 mV:
Ohm’s law; η is the resistivity
These are the model lengths we study in THEA to freeze the quench in a limited region.

## Slide 19
1.9 K
Quench stoppers
In particular, we analyse the 18 kA busbar, defining a ~20 cm domain (see previous slide).
1.9 K
x=0
x=20.4 cm
I=18 kA ;
B=0.55 T
Voltage extraction
Quench propagates from an initial normal region, but it is forced to stop due to the boundaries at 1.9 K.

## Slide 20
Quench stoppers
is the limit length to have quench, without runaway.
(Similar values for the 2 kA busbar, with )
The actual detection threshold is in the range 20-100 mV [1]. As a result, such a quench stopper would not be detected. However, this would not constitute a problem for the thermal integrity of the busbar, since .
[1] R. Denz, Quench Detection Systems for HL-LHC Busbars, 2021
Indeed: and

## Slide 21
Contents
Introduction
The 2 kA and 18 kA busbars
THEA model
Results
Current dump and validation time
Quench stoppers
To resume and conclusions

## Slide 22
To resume and conclusions
The QPV is 1.7 m/s in the 2 kA busbar and 5.4 m/s in the 18 kA busbar.
The QPV increases as a result of an higher field at the contact point between a feed and a return line in the DCM. The increase in the QPV is more relevant at an higher absolute field (18 kA vs 2 kA busbar).
A 100 mV threshold for quench detection [1] gives a maximum validation time, 8.2 s for the 2 kA circuit of the MCBXF, 2.8 s for D1, and 1.4 s for the MQXF. This agrees with values set in [1].
At current regimes , quench propagation is slower with respect to . As a result, the maximum validation times expressed here assure the proper busbar protection under all operating conditions.

## Slide 23
To resume and conclusions
A quench may occur in a busbar region shorter than 20 cm (for the 18 kA busbar; 50 cm for the 2 kA busbar) without being detected. However, the peak temperature would be around 30 K so that it does not pose a threat for busbar integrity.
Comparison with A. Verweij (asymmetric quench propagation) [2]
[2] A.Verweij, Validation of the busbar protection scheme, 2021
(2 kA) | ΔV=100 mV | ΔV=20 mV | ΔV=10 mV
Verweij (L=12 m) | 36 K | 26 K | 27 K
Me (L=55 m) | 34 K | 23 K | 26 K
Verweij (L=12 m) | 36 K | 26 K | 27 K
Me (L=55 m) | 34 K | 23 K | 26 K
(18 kA) | ΔV=100 mV | ΔV=20 mV | ΔV=10 mV
Verweij (L=12 m) | 34 K | 30 K | 42 K
Me (L=23 m) | 34 K | 30 K | 52 K
Verweij (L=12 m) | 34 K | 30 K | 42 K
Me (L=23 m) | 34 K | 30 K | 52 K

## Slide 24
Next steps: Busbars through the Plug
We are interested in the quench propagation in the 2 kA and 18 kA busbars passing through the λ-plate (‘Plug’).
Plug
The Plug assures electrical continuity of the powering, but hydraulic discontinuity between the LHe and SFHe volumes of the DFX and of the DCM.
Courtesy: Y. Leclercq
3 x 4-in-1 2 kA
round busbars
Courtesy: Y. Leclercq
Ø 7.0
Ø 6.5
Ø 6.5
40
2 kA busbar

## Slide 25
Would the additional PbSn cause a delay in quench detection?
Yes, the PbSn in the Plug actually slows down the quench propagation (due to the PbSn heat capacity) so that detection is delayed, as well.
Results – 2 kA busbar
2) If yes, how to proceed to evaluate this risk?
20 ms
 Be careful to the Cu content !

## Slide 26
Appendix

## Slide 27
Effect of the RRR
The RRR has a clear impact on the T, ΔV, and QPV (ex. 18 kA busbar)

## Slide 28
Asymmetric quench
We define a model with the initial normal region located on one side of the domain: .
The other model parameters are the same of the symmetric case.
Note: NbTi resistivity is modelled by means of the power law using parameters from the table.
Ex: 18 kA busbar
1.9 K
1.9 K
x=0
x=23 m
I=18 kA
B=0.55 T
Note: the component is represented as a cylinder, but it is treated as a 1-D line by the code
By comparison:

## Slide 29
T(x) profile
ΔV(t) evolution
Asymmetric quench
Knees are useful to derive the QPV
‘Knees’ define the moments when the regions inside the corresponding V taps lose the sc state.

## Slide 30
Asymmetric quench
QPV as f(B)
The QPV is ~1.7 m/s and 5.5 m/s in the 2 kA and 18 kA busbars, respectively. This confirms the numbers of the symmetric case shown above.

## Slide 31
Parametric study: what happens to if the busbar operates at ?
Quench stoppers

## Slide 32
Why is almost the same for each combination of domain length and current?
The governing equation and boundary conditions at steady state are:
Steady-state temperature profile
If , . Consequently, while proportionally.
Thus, remains the same.
(k is considered constant and equal to its average value in the T range under study, 1.9-30 K )
Peak temperature :
Quench stoppers