## Slide 1: Focus on: Bipolar Junction Transistors
RadWG Workshop – 8 June, 2021
Rudy Ferraro (BE-CEM-EPR)

## Slide 2: Introduction
Kick-off of the ‘RadWG Component Selection Guideline’ documents!
First one dedicated to Bipolar Junction Transistor(s)
The writing of this document implied a tremendous amount of work:
  (Re-)processing of test data from 39 test campaigns
  Analysis made complex due to various test data format used through the years
  Number of measured parameters increased with time
Guideline & Presentation summary:
  Complete BJT list with characteristics
  Radiation effects on BJTs
  LHC environment and qualification implications
  Test circuit & setup
  Test methodology
  Analysis of BJTs response
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 3: BJT Testing in numbers: when and who?
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors
10 years of BJT Testing
49 Radiation campaigns performed
19 different references tested
Most of the BJT tested for (and by) SY-EPC for LHC power converters

## Slide 4: BJT Testing in numbers: characteristics
Medium Power
Fast Switching
Dual Amplifier
General Purpose
High Power
Transistor Application (from datasheet)
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors
Notes: Modify numbers for component types

## Slide 5: List of tested BJT
Application | Type | Reference | Manufacturer | Characteristics |  |  |  |  |  |  | Radiation Tolerance
 |  |  |  | VCEO [V] | VCBO [V] | VEBO [V] | PD [W] | IC [A] | Hfe | Ft [MHz] | 
General Purpose Transistor | NPN | BC807-25 | NXP | -45 | -50 | -5 | 0.25 | -0.5 | 160-600 | 80 | ***
 | NPN | BC817-25 | NXP | 45 | 50 | 5 | 0.35 | 0.5 | 160-400 | 100 | ***
 |  | BC850CLT1G | ON Semiconductor | 45 | 50 | 6 | 0.23 | 0.1 | 420-800 | 100 | ****
 |  | BC847B,215 | NXP | 45 | 50 | 6 | 0.25 | 0.1 | 200-450 | 100 | ****
Switching Transistor | PNP | 2N2907AUB* | Microsemi | -60 | -60 | -5 | 0.5 | -0.6 | 50- | - | ***
 | NPN | 2N3019 | ON Semiconductor | 80 | 140 | 6 | 0.8 | 1 | 15-300 | 400 | ***
 |  | BC550CTA | ON Semiconductor | 45 | 50 | 5 | 0.5 | 0.1 | 110-800 | 300 | ****
 |  | 2N2222AUB* | Microsemi | 50 | 75 | 6 | 0.5 | 0.8 | 20- | - | ****
Medium Power | PNP | FMMT591 | Diode incorporated | -60 | -80 | -7 | 0.5 | -1 | 100-300 | 150 | *****
 | NPN | FMMT491 | Diode incorporated | 60 | 80 | 7 | 0.5 | 1 | 100-300 | 150 | ****
 |  | ZTX653 | Diode incorporated | 100 | 120 | 5 | 1 | 1 | 30-300 | 140 | **
 |  | PZT2222AT1G | ON Semiconductor | 40 | 75 | 6 | 1.5 | 0.6 | 35-300 | 300 | ****
High Power | NPN | MJD45H11T4G | Fairchild | 80 | - | 5 | 20 | 8 | 40-150 | 50 | *
Dual amplifier | NPN | 2N3810 | Solid State inc. | 60 | 60 | 5 | 0.6 | 0.05 | 75-900 | 100 | *****
High frequency
Higher power dissipation
Higher max collector current
High power dissipation
High max collector current
Characteristics and relative radiation tolerance of all BJTs visible in a single document!
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 6: Radiation Effect on BJT
Current-gain degradation:
Main parameters affected: Vbe and
Bibliography of radiation effects presented in the document
Radiation effects: TID & DD
DD induces a linear increase of -1
TID induces a sublinear increase of -1
TID: Positive charges trapped in oxide (POTCs)
Interface Trap (ITs)
 increase of leakage current
 increase of surface recombination
DD: Bulk defects
 increase of surface recombination
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors
[Ref]
[Ref]

## Slide 7: Radiation Effect on BJT
Current-gain degradation:
Main parameters affected: Vbe and
Bibliography of radiation effects presented in the document
Radiation effects: TID & DD
DD induces a linear increase of -1
TID induces a sublinear increase of -1
TID: Positive charges trapped in oxide (POTCs)
Interface Trap (ITs)
 increase of leakage current
 increase of surface recombination
DD: Bulk defects
 increase of surface recombination
Enhanced Low Dose Rate Sensitivity (ELDRS) effect:
Lower the dose rate  higher the degradation
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors
[Ref]
[Ref]
[Ref]

## Slide 8: LHC environments and qualifications implications
Protons
200 MeV
Neutrons
Electrons (<108)
Wide variety of DDEF/TID Ratio:
  From 109 up to 1011 cm-2.Gy-1
CERN Accelerators fields composed of mixed particles
  Components exposed to both TID & DD
  But with the high neutron dominance DD
  mechanisms tend to dominate
90% of the ratio are above 1010 cm-2.Gy-1
  10 times less TID than 200 MeV protons for the same DD
BJTs in this environment will mainly suffer from DD, even though TID contribution should not be neglected
  (R.Ferraro, IEEE Trans. Nucl. Sci. 66 (2019) 1548 - 1556)
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 9: Test Facilities
CERN Cobalt 60 Facility
Paul Scherrer Institut
PSI-PIF – Switzerland, Viligen
  200 MeV proton  TID + DD
  High TID Contribution wrt LHC fields ‘worst-case’
  No ELDRS or Annealing test possible
  High availability  Qualification ok knowing limitations
CC60 – Switzerland, CERN
  Cobalt 60 Source  TID Only
  Can be used to assess individual TID response
  ELDRS Test possible
  Annealing Test
  Requires a second test for DD
CERN High energy AcceleRator Mixed field
CHARM – Switzerland, CERN
  Representative LHC Radiation mixed-fields  TID+DD
  Representative TID/DD ratio [see Radsaga presentation]
  Some positions ELDRS compatible
  Annealing test possible but not practical
  Lower availability than PSI
Ideal Protocol:
Qualification against TID and DD at PSI
Qualification at CC60 to obtained individual ELDER TID response
Validation at CHARM
In general use of radiation design margin is used instead of performing (2), which combined to the fact that DD dominates should ensure a safe margin before validation at CHARM
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 10: RADW BJT Test Circuit
At PSI only the BJT is placed in beam
At cobalt & CHARM tested radiation tolerant opamps are used
Collector current fixed by the opamp circuit by providing a reference voltage
When the Beta decreases due to radiation the opamp increase the injected base current to keep the collector current to the requested value
Collector and base current monitored and used for beta calculation
Base-to-emitter voltage drift also monitored
Temperature monitored
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 11: Examples of test boards
2N3810
2N3819
2N2222AUB
Test boards made modular for easy change of DUTs:
Boards can be stacked using the same setup to increase number of DUTs
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 12: Examples of test boards
2N3810
2N3819
2N2222AUB
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 13: Test Methodology
If no specific request:
General purpose BJT: Ic = 1 mA
Switch transistor BJT: Ic = 1 mA
Power transistors: Ic = according to system
Beta degradation measured continuously
Beta = f(Ic) measured at different steps
Extraction of beta degradation for different Ic
General rule:
Lower the current, higher the degradation
5 mA
2 mA
1 mA
300 uA
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 14: Test Methodology
If no specific request:
General purpose BJT: Ic = 1 mA
Switch transistor BJT: Ic = 1 mA
Power transistors: Ic = according to system
Beta degradation measured continuouslyc
Beta = f(Ic) measured at different steps
Extraction of beta degradation for different Ic
General rule:
Lower the current, higher the degradation
5 mA
2 mA
1 mA
300 uA
From 2020:
Complete beta characteristics measurement implemented to allow the estimation of the degradation for different collector currents
Before 2020:
Beta degradation only with selected biasing collector current
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 15: Examples of characteristic degradations
2N2907AUB
2N3019
2N3810
BC850
2N2222AUB
BC487
PZT2222
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 16: BJT test results analysis per application
Radiation responses for each lot with:
  Facility
  Particle
  Effects
  EDMS link
Component's characteristics
Obsolete components
Documents contains a comparative analysis per type of application with exhaustive list of performed test
Analysis of lots-to-lots and TID vs DD response discussed when possible
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 17: BJT Response comparisons
Comparison of combined TID-DD responses (mostly from PSI, some from CHARM)
  Only DDEF axis showed since the TID axis is different for CHARM/PSI
Various initial gains
Various sensitivities
Various sensitivities
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 18: BJT Response comparisons
Comparison of combined TID-DD responses (mostly from PSI, some from CHARM)
  Only DDEF axis showed since the TID axis is different for CHARM/PSI
High linearity of the response:
 Strong indication that the DD mechanisms dominates
Various sensitivities
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 19: BJT Sensitivity comparisons
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors
No significant differences between the groups
Good candidates can be found for all the type of applications
Radhard devices are not the best ones (hardened mainly against TID and not DD)
Radhard devices
Quantitative comparison between the devices possible by means of the slopes

## Slide 20: Best candidates
It depends!
Minimum gain acceptable?
Maximum relative degradation?
High speed?
High power?
Target Dose and DD?
You will find all the info in the document to find the candidates that comply with your project requirements..
.. If not, you are very welcome to send us a list of BJT to be tested !
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 21: Conclusions
New ‘RadWG Component Selection Guideline’ documents introduced
One document per type of components will be provided
These documents will help the CERN development to understand the radiation effects, the test methodology and to have access to an exhaustive analysis of the radiation response in a single document
The first document dedicated to BJTs will be released within 2 weeks and link will be sent through the RADWG mailing list
Future reports to be presented during the next RADWG:
  MOSFET
  Regulators
We really hope these documents will be useful to you
R. Ferraro (BE-CEM-EPR) - Focus on: Bipolar Junction Transistors

## Slide 22
Thank you for your attention!

## Slide 23: RADW Test Setup
Testing of electronic components by R. Ferraro (BE-CEM-EPR )

## Slide 24: BJT Testing in numbers: when and who test?
Testing of electronic components by R. Ferraro (BE-CEM-EPR )