## Slide 1
Simulations results
Overview of results collected at ELI-NP and POLITO
Lorenzo Peroni
Martina Scapin and Alberto Morena
Progress meeting for P219 Experiment in PHELIX

## Slide 2: Summary
  ELI-NP simulations (HELIOS)
  POLITO methodology
  Benchmark and calibration
  GSI experiments predictions
  Conclusions and outcomes

## Slide 3: HELIOS code
HELIOS is a 1-D radiation-hydrodynamics code designed to study the hydrodynamic evolution of radiating plasmas. It can be used to study the evolution of planar, cylindrical, or spherical plasmas heated by laser beams.
The code updates energy and momentum conservation equations in a Lagrangian reference frame (i.e., grid moves with fluid).
  The high-power lasers produce a surface plasma condition which acts as high-pressure loading source condition for the material in the rear portion of the sample.
Target  SESAME equation of state, thermal conductivity, and electrical resistivity data.
Laser  Irradiance (W/m2); pulse time history

## Slide 4: ELI-NP preliminary results
Target  material: graphite 1.77 g/cm3; thickness: 1 mm
Laser  energy: 180 J; spot diameter: 1 mm; pulse duration: 5 ns
Velocity
Pressure

## Slide 5: ELI-NP preliminary results
Target  material: graphite 1.77 g/cm3; thickness: 1 mm
Laser  energy: 180 J; spot diameter: 1 mm; pulse duration: 1 ns
ELI-NP Conclusion:
Velocity
Pressure

## Slide 6: The experiment methodology
LS-DYNA
3D/2D axisymmetric simulation of the shock propagation and the target failure
1D simulation for the laser deposition phase
Helios
Comparison of the results and model validation
Target
Thickness
Spot size
Shock
Spall
Bulge Fragmentation
Spatial distribution
time duration
LASER
VISAR,
PDV, (LDV)
High-speed camera
Design of the experiment

## Slide 7: Benchmark
Experimental setup
Shot conditions
Target  material: graphite (r0=1.754 g/cm3)
Laser  spot diameter: 4 mm; pulse duration: 5 ns
Validation and tuning of FE simulations based on CEA experiments
LULI2000

## Slide 8: Helios results
Mass density (g/cm3)
Target
Non-solid region
Temperature (eV)
0.35 eV ≈ 4000 K
graphite melting temperature
Non-solid region
Target
CEA SHOT7
Shockwave
50 mm

## Slide 9: HELIOS results
Pressure
(MPa)
Target
Decay of the pressure peak
LS-DYNA
HELIOS
5 ns
20 ns
40 ns
50 ns
30 ns
At the end deposition time of 5 ns the shock wave front is at 35 microns far from the front surface

## Slide 10: HELIOS results
Velocity
(cm/s)
Target
LS-DYNA
Helios
5 ns
20 ns
40 ns
50 ns
30 ns
Boundary condition for FE simulations

## Slide 11: HELIOS to LS-DYNA
Reduced Thickness
Radius
Solid target
R=0 mm
LS-DYNA
Boundary conditions: velocity time history profiles imposed to the nodes on the surface
Spot radius
R=0.5 mm
R=1 mm
R=1.5 mm
From HELIOS at a chosen depth
Scale factor: spatial characteristic of the laser pulse
Attention to the Timestep!
Velocity

## Slide 12: LS-DYNA material model
EOS: Grüneisen
Compression
Elastic-perfectly plastic model
Porous graphite
data
FAILURE CONDITIONS
sMAX
eMAX
In uniaxial strain case
(Compression)
In tension!!

## Slide 13: LS-DYNA results
0.715 mm
Y-velocity (mm/ms)
Evaluation of the velocity of the back surface
Mesuring spot dimension/position
SHOT 7 @ CEA
Target  material: porous graphite; thickness: 0.75 mm
Laser  energy: 121 J; pulse duration: 5 ns
LASER
vyMAX = 1970 mm/ms
2 mm

## Slide 14: LS-DYNA results
Comparison with experimental results
Range of measurement 0 ≤ R ≤ 1mm
Averaged curve
Range of measurement 0 ≤ R ≤ 0.2 mm
Averaged curve
SHOT 7 @ CEA
Target  material: porous graphite; thickness: 0.75 mm
Laser  energy: 121 J; pulse duration: 5 ns
vyMAX = 1970 mm/ms

## Slide 15: LS-DYNA results
Comparison with experimental results
Post-mortem
LS-DYNA
SHOT 7 @ CEA
Target  material: porous graphite; thickness: 0.75 mm
Laser  energy: 121 J; pulse duration: 5 ns
2.5 mm

## Slide 16: Results analysis: back surface velocity
DAMPING
(model dependent)
SPALL STRENGTH
FAILURE CONDITION
Same order of magnitude of the pulse duration
Damage Evolution/
Energy dissipation
Rayleigh damping coefficient for stiffness weighted damping
(0.06)

## Slide 17: LS-DYNA results
SHOT 15 @ CEA
Target  material: porous graphite; thickness: 0.75 mm
Laser  energy: 259 J; pulse duration: 5 ns
Pressure(MPa)
0.703 mm
LASER
vyMAX = 2754 mm/ms
2 mm
Range of measurement 0 ≤ R ≤ 1 mm
R= 1 mm

## Slide 18: LS-DYNA GSI Prediction 5 ns
SHOT LOW @ GSI
Target  material: porous graphite; thickness: 1 mm
Laser  energy: 180 J; pulse duration: 5 ns
Pressure(MPa)
0.943 mm
LASER
vyMAX = 4000 mm/ms
0.5 mm
Range of measurement 0 ≤ R ≤ 1 mm
R= 1 mm

## Slide 19: LS-DYNA GSI Prediction 5 ns
Range of measurement 0 ≤ R ≤ 1 mm
R
Average
SHOT LOW @ GSI
Target  material: porous graphite; thickness: 0.5 mm
Laser  energy: 180 J; pulse duration: 5
Range of measurement 0 ≤ R ≤ 1 mm
SHOT LOW @ GSI
Target  material: porous graphite; thickness: 0.75 mm
Laser  energy: 180 J; pulse duration: 5
R
Average

## Slide 20: LS-DYNA GSI Prediction 1 ns
SHOT HIGH @ GSI
Target  material: porous graphite; thickness: 1 mm
Laser  energy: 180 J; pulse duration: 1 ns
Range of measurement 0 ≤ R ≤ 1 mm
Average
R
R= 1 mm

## Slide 21: Conclusions and outcomes
Following the preliminary ELI-NP results the laser deposition phase could be simulated with 1D code HELIOS
The obtained velocity at the plasma-solid interface could be used as boundary condition for the LS-DYNA model in order to assess the conditions at the back surface tacking into account the strength and failure model of the material
Different modelling techniques were tested (2D FE, 3D FE, SPH, FE-SPH) and 2D axisymmetric model results as the much effective solution (fast and enough accurate)
The results are strongly dependent from the adopted damping and failure model
Velocity measurements on the back surface could strongly vary in function of the portion of the sample considered and the dimensions of the measuring spot

## Slide 22
Thank you for your attention!