## Slide 1: Superconducting RF at CERN: overview
Walter Venturini Delsolaro,
on behalf of the CERN SRF community
PBC technology mini workshop: superconducting RF, Tuesday 21 Sep 2021, CERN

## Slide 2: Outline
SRF in todays (and future) CERN accelerators
  LHC
  HIE ISOLDE
  HL-LHC
  FCC
SRF infrastructure
R&D
Caveat: I will not be able to cover all CERN SRF in 15 minutes

## Slide 3: The SRF community at CERN…
Group photo at the TTC workshop, CERN, 2020

## Slide 4: Standing on the shoulders of giants
LEP2 cavity

## Slide 5: LHC accelerating systems

## Slide 6: LHC RF Cryomodule
4 cryomodules of 4 cavities
Nb-coated Cu-cavities operating at 4.5 K
8 - 16 MV/beam
400.790 MHz + - 100kHz
1 spare module
1 spare dressed cavity

## Slide 7
LHC ACS cavity (1/2)
Parameters | Value
Frequency [MHz] | 400.79
Operating temperature [K] | 4.5
Nominal Accelerating Voltage Vacc = (Eacc x Lacc) [MV] | 2
Accelerating length Lacc = (ncell.b.l/2) [m] with b = 1 | 0.374
Accelerating gradient Eacc [MV/m] | 5.33
Linac r/Q [W] at b=1 | 85.3
Circuit r/Q [W] at b=1 | 42.7
G [W] | 256.9
Q0 at operating temperature for RBCS=36.4 nW* | 7.109
Q0 at nominal gradient | > 2.109
Cavity dynamic RF heat load [W] | 23.4
Epk/Eacc at b=1 | 2.4
Bpk/Eacc [mT/(MV/m)] at b=1 | 5.08
Max. surface field Epk [MV/m] | 12.85
Max. surface magnetic field Bpk [mT] | 27.11
Stored energy [J] at nominal Eacc and b=1 | 18.5
Qext | 2 to 6.104
RF power [kW] | 300
* : Average values from measurements of LHC cavities in the 90’s, and post-processed by A. Miyazaki (presented at the CERN SRF2018 workshop)
0.58 A protons
CW operation
F. Peauger

## Slide 8
LHC ACS cavity (2/2)
Nb/Cu cavity
Conduction cooling through copper substrate
OFE copper plate shaped by deep drawing or spinning
Electron beam welding and vacuum brazing (flanges)
Stainless steel flanges and helium tank (no bellows)
1 variable FPC
4 x HOM couplers
3 pick-up antenna (2 spares)
Welds
Parameters | Value
Cavity thickness [mm] | 2.5
Beam aperture [mm] | 300
Cavity stiffness [kN/mm] | 20
Tuning sensitivity [kHz/mm] | 240
Pressure sensitivity* [Hz/mbar] | -60
Lorentz Force detuning* [Hz/(MV/m)2] | -12.6
* : measured on bare cavity in vertical test

## Slide 9
MINIBALL
HRS
GPS
HEBT
HIE Linac
REX
SCATTERING
CHAMBER
REXEBIS
REXTRAP
Target
Target
BTY
Radioactive Ion Beams (RIBs) are produced when the protons impact in one of the two targets in the facility
The RIB of interest is selected in one of the separator lines (GPS, HRS) and transported to a low energy experimental station to be studied
Alternatively, the RIB can be accelerated after it is accumulated and transversely cooled in the REX-TRAP and charge bred in the REX-EBIS
Jose Alberto Rodriguez – CERN SRF Workshop – Dec. 1st 2016
ISOLDE COMPLEX:

## Slide 10: HIE ISOLDE post accelerator
XT03
XT02
XT01
ISOLDE Solenoidal Spectrometer (ISS)
Scattering chamber (SEC)
Miniball

## Slide 11
HIE ISOLDE accelerating cavity
QS
QSS
Parameters | QS | QSS
Frequency [MHz] | 101.28 | 
Operating temperature [K] | 4.5 | 
bopt | 0.109 | 0.122
Accelerating gradient Eacc [MV/m] | 6 | 6
r/Q [W] at bopt | 553 | 502
G [W] | 30.3 | 30.1
U/Eacc2 [J/(MV/m)2] | 0.207 | 0.214
Q0 at nominal gradient and 10W losses | 4.7e8 | 4.9e8
Cavity dynamic RF heat load for RS=50nW [W] | 7.7 | 7.9
Epk/Eacc | 5 | 5.3
Bpk/Eacc [mT/(MV/m)] | 9.6 | 9.3
Max. surface field Epk [MV/m] | 30 | 31.8
Max. surface magnetic field Bpk [mT] | 57.6 | 55.8
Stored energy [J] at nominal Eacc | 7.45 | 7.7
Acceleration of heavy ions (A/q=4.5)
Very low beam current
CW operation
E-field
H-field

## Slide 12: HIE ISOLDE cavity
2.5 K
4.6 K
World record surface fields for Nb/Cu!

## Slide 13: HIE ISOLDE cryomodule

## Slide 14: HL-LHC Crab Cavities (WP4)
LHC Point 1 (horizontal)
4 RFD CM to be installed + 1 CM spare
LHC Point 5 (vertical)
4 DQW CM installed + 1 CM spare
SPS BA6
2 Test Prototype (1DQW, 1RFD)
SM18 Area
Cavity cold testing, clean room facilities & cryomodule qualification
*each CM consists 2-cavities

## Slide 15: Prototype Cryomodules
Vertical crossing for ATLAS, first one to go to SPS 2018
Horizontal crossing for CMS
Cavities fabrication starting 2017
Rama Calaga @ the 3rd CERN SRF Workshop, 2018

## Slide 16: SPS test bed for crab cavities
Crab cavities DQW prototype built and tested in horizontal bunker (picture: cavity string assembly)
First crabbing of a proton beam
Crab cavities DQW cryomodule installed in the SPS
0 Deg
90 Deg
180 Deg
R. Calaga, O. Capatina, F. Gerigk, A. Macpherson, M. Therasse, G. Vandoni

## Slide 17: SRF infrastructure
SRF activities span over 3 CERN departments (EN, TE, SY)
Mechanical workshops, metrology, EB welding, chemistry, and sputtering labs, SM18 assembly and test area
Most infrastructures date back from LEP era
New SRF hub under study, to centralize and streamline cavity and cryomodule workflow
SM18: Clean rooms, RF testing, cryogenics infrastructure
252: Clean rooms, coating benches warm RF lab
Cryolab
Main workshop:, metrology, machining, EB welding
Chemistry lab
Vacuum surfaces, coating labs
Material studies labs

## Slide 18: LHC cavity- clean booth and coating bench

## Slide 19: HIE ISOLDE clean room
RF vertical test assembly area

## Slide 20: Surface fields and frequency stability
F. Peauger at the 4th CERN SRF workshop, 2019

## Slide 21: R&D
R&D is focused on new cavity designs, diagnostics tools, innovative tuning techniques, new cooling schemes, new materials (A15)
Typically R&D has lower priority, after support to operations, approved projects and infrastructures
An important fraction is done under the umbrella of the FCC study
General SRF R/D is also pursued in the context of other projects/activities: for instance, LHC spares etc.

## Slide 22: Some examples (or floating ideas)
PERLE: re-use of cryomodule hardware developed for SPL (then stopped) in collaboration with CNRS
Collaboration with SOLEIL on passive Nb/Cu cavities for beam manipulation
Particle discrimination for AMBER in the North Area with RF separation
Muon collider (requires SRF for the proton driver and for the high energy muon acceleration)
Axion detection with SRF cavities
…

## Slide 23: Fast Reactive Tuner
A. Macpherson et al.
Frequency tuned by a coupled voltage-controlled reactance on shorted transmission line, with new ultra fast ferro-electric material
Proof of principle done at CERN on a real SRF cavity, compensation of microphonics
Potential application in HL-LHC

## Slide 24
Problem of the breakdown in components of the surface resistance
SRF material R/D: core tasks and tools
ADVANCE THE FUNDAMENTAL UNDERSTANDING OF THE SURFACE RESISTANCE
Explore estimators of Rs from measurements of DC superconducting properties: Tc, ΔTc, Bc1, Bc2, χ’, χ’’, etc.
Explore estimators of Rs from surface characterizations
Diagnostics tools aimed at disentangling the components of Rs on real cavities: thermometry, magnetic field mapping
Quadrupole resonators
1.3 GHz programs
Sample studies
RF measurements: accuracy and resolving power (i.e. transients)
Magnetic and electric field limitations of SRF materials
Optical inspections of real cavities

## Slide 25: FCCee RF system baseline
800 MHz 5-cell cavities
bulk Nb, 2 K
852 cavities
Eacc=20 MV/m
200 kW/cav.
4 cav./cryom.
Designed for fixed synchrotron radiation power of 50 MW per beam
Elliptical shape
400 MHz 4-cell cavities
Nb/Cu, 4.5 K
408 cavities
Eacc=10 MV/m
1 MW to 200 kW per cav.
4 cav./cryom.
400 MHz 1-cell cavities
Nb/Cu, 4.5 K
104 cavities
Eacc=5 MV/m
1 MW /cav
4 cav./cryom.
Re-used for FCC-hh
Jlab
LHC
LEP
CDR FCC-ee: The Lepton Collider, 2019

## Slide 26
O. Brunner - SRF Summary
Challenging the baseline
Spoke
QWR Ver2
QWR Ver1
Re-entrant
HWR
LHC
F. Peauger
Alternative cavity design study initiated in Nov. 2020
  CLIC expertise applied to SRF -> Slotted Waveguide Elliptical (SWELL) cavity operating at ~ 600 MHz 1
  Beam dynamics studies -> ~ 600 MHz conceivable for Z machine 1-cell UROS1 and 2-cell SWELL cavity types
1 The SWELL cavity concept was published in 2010 by Z.Liu and A. Nassiri (Beijing U., ANL)
I. Karpov
3/7/2021
O. Brunner, FCC week 2021

## Slide 27: Bulk Nb program
FCC 802 MHz 5-cell performance at 2K
Eacc = 31 MV/m & Q0 = 2x1010 Cavity Quench limited (Bpk ~ 130 mT)
HG 704 MHz 5-cell performance at 2K
Eacc = 29.7 MV/m & Q0 = 1.4 x1010 Cavity not quench limited
Frank Marhauser & team @ JLAB
JLAB
CERN

## Slide 28: Performance goals: a moving target
R/D ongoing at CERN (joint effort between groups MME-VSC-RF) during the last years to push performance of Nb/Cu using 1.3 GHz mono cells, which are the international standard for SRF
Preliminary survey of materials and performance goals was done during CDR phase (S. Aull et.al, Report number: CERN-ACC-2018-0019)
Nb/Cu HIPIMS coatings displayed optimized RBCS below 300 nΩ at 4.5 K, 1.3 GHz, and low Q-slope
HIE ISOLDE seamless QWR reached 120 mT at 100 MHz no special field limits for Nb/Cu
By simple scaling and reasonable assumptions on Rres we can aim to Rs=50-90 nΩ (~3-5 109 ) at 400 MHz, 10 MV/m and 4.5 K
Performance targets and breakeven points are being reviewed for all frequencies considered for FCC, including 600 MHz, based on the recent developments of the 1.3 GHz program

## Slide 29: Recent progress in 1.3 GHz Nb/Cu program
Progress slowed in recent years by poor copper substrates
HIPIMS coating on seamless (machined out of the bulk), electro-polished copper cavity
Q slope mitigated, comparable with bulk Nb up to 15 MV/m
Test was stopped by administrative limits at Cryolab
More cavities in the pipeline

## Slide 30: Summary
Great tradition in SRF at CERN
SRF cavities key elements in past and present CERN accelerators
Infrastructure consolidation efforts in recent years, being continued
R/D focused on CERN scenarios for future accelerators
Vital and enthusiastic local SRF community contributing to worldwide efforts