## Slide 1
Joffre Gutierrez Royo*
A. Romanov, G. Telles, N. Lamas, P. Krkotic, J. O’Callaghan, X. Granados, E. Garcia-Tabarés, M. Taborelli, P. Chiggiato, P. González, I. Korolkov, R. Miquel, F. Perez, M. Pont, T. Puig, S. Calatroni
Geneva
PS
SPS
LHC
Future Circular Collider (FCC)
HTS coatings for FCC and beyond
*jgutierrez@icmab.es
PBC technology minworkshop: superconducting RF
Tuesday Sep 21, 2021
Notes: I will present the work developed by a consortium formed by these groups towards providing a solution for the FCC-hh beam-screen chamber issue. The FCC-hh is the most ambitious post LHC scenario envisioned by CERN. At the end of this presentation I will also show another possible application for these novel coatings.

## Slide 2
4 – Potential gain and ¿pitfalls? of CCs below the GHz range
3 – How we coat surfaces with CC
2 – CCs vs Cu: Rs(H) in the GHz range
1 – Coated Conductors in a nutshell
Outline

## Slide 3
4 – Potential gain and ¿pitfalls? of CCs below the GHz range
3 – How we coat surfaces with CC
2 – CCs vs Cu: Rs(H) in the GHz range
1 – Coated Conductors in a nutshell
Outline

## Slide 4
Cu ~ 20 mm
Ag ~ 2 mm
REBCO HTS ~ 1 – 3 mm
Buffers ~ 0.2 – 1 mm
Metallic Substrate ~ 30 – 100 mm
Coated Conductors are commercially available
with different widths in Km length
Tc ≈ 91 K
Hc2 (4.2K) > 100 T
Hirr (4.2K) > 60 T

## Slide 5
CCs as low-impedance coating for the FCC-hh beam-screen chamber
FCC working conditions:
16 T, 40 – 60 K, 1 GHz & 25 A peak
CCs offer excellent opportunities for high-energy physics

## Slide 6
CCs as low-impedance coating for the FCC-hh beam-screen chamber
P  Be2QVG
  High Q T = 4.2K
  &
  High Be
FCC working conditions:
16 T, 40 – 60 K, 1 GHz & 25 A peak
Higher than Cu Q-value RADES halsocopes @ GHz
Opportunities for the BASE detector in the kHz – MHz range
CCs offer excellent opportunities for high-energy physics
CCs as low-impedance coating for cold DM axions

## Slide 7
Zs characterization is done with a 8 GHz cavity Hakki-Coleman resonator
Operating in the mode
Compatible with ICMAB cryostats:
25mm Ø bore 9 T magnet
50mm Ø bore 16 T magnet

## Slide 8
4 – Potential gain and ¿pitfalls? of CCs below the GHz range
3 – How we coat surfaces with CC
2 – CCs vs Cu: Rs(H) in the GHz range
1 – Coated Conductors in a nutshell
Outline

## Slide 9
Rs of state-of-the-art CCs outperforms FCC Cu in the GHz range
FCC working conditions: 16 T, 40 – 60 K, 1 GHz & 25 A peak
Outperform Cu Rs under FCC working conditions
Withstanding induced image currents
Preventing magnetic field disturbance  Segmented REBCO-Cu hybrid coating
FCC Cu
REBCO
T = 50 K, n = 8 GHz
CCs as low-impedance coating for the FCC-hh beam-screen chamber
T. Puig et al, Supercond. Sci. Technol. 32 (2019)

## Slide 10
REBCO CCs support high-currents at high-magnetic fields
REBCO is a HTS and a high-field superconductor
FCC working conditions: 16 T, 40 – 60 K, 1 GHz & 25 A peak
Outperform Cu Rs under FCC working conditions
Withstanding induced image currents
Preventing magnetic field disturbance  Segmented REBCO-Cu hybrid coating
CCs as low-impedance coating for the FCC-hh beam-screen chamber
T. Puig et al, Supercond. Sci. Technol. 32 (2019)

## Slide 11
A segmented REBCO-Cu hybrid coating doesn’t disturb H and keeps good Rs
FCC working conditions: 16 T, 40 – 60 K, 1 GHz & 25 A peak
Outperform Cu Rs under FCC working conditions
Withstanding induced image currents
Preventing magnetic field disturbance  Segmented REBCO-Cu hybrid coating
CCs as low-impedance coating for the FCC-hh beam-screen chamber
G. Telles et al, to be submitted
(G. Telles @ EUCAS 2021, Field Quality and Surface resistance studies for the FCC beam screen. Materials IX, ID: 441)

## Slide 12
The improvement in Rs is higher at lower temperatures
T = 10 K, n = 8 GHz
REBCO
T = 50 K, n = 8 GHz
REBCO
DM Axion detection cavities operate at 4.2K, further benefiting from REBCO

## Slide 13
4 – Potential gain and ¿pitfalls? of CCs below the GHz range
3 – How we coat surfaces with CC
2 – CCs vs Cu: Rs(H) in the GHz range
1 – Coated Conductors in a nutshell
Outline

## Slide 14
Two-step delamination technique for large surface coatings with CCs
Attach
Welding of CC on top of a surface
Delamination
Mechanical peeling
Technology is easily scalable
A. Romanov & G. Telles, to be submitted

## Slide 15
Proof-of-concept:
CC coated RADES haloscope shows a 50% in-field Q improvement
  CC coated Axion cavity Cu only
  Q(0T, 4.2K) ~ 80k
  Q(11T, 4.2K) ~ 60k vs Q(11T, 4.2K) ~ 40k
  Curvature
  R9 mm
With some R&D efforts we made it work on curved surfaces
P  Be2QVG

## Slide 16
Proof-of-concept:
A R9 mm bending radius was a bit too much for the CC used
RADES haloscope Cu
T = 10 K, n = 8 GHz
  CC coated Axion cavity Cu only
  Q(0T, 4.2K) ~ 80k
  Q(11T, 4.2K) ~ 60k vs Q(11T, 4.2K) ~ 40k
RADES haloscope CC
REBCO
  Curvature
  R9 mm
P  Be2QVG

## Slide 17
Proof-of-concept:
Now we can coat R9 mm curvatures with nominal Rs values
  CC coated Axion cavity Cu only
  Q(0T, 4.2K) ~ 80k
  Q(11T, 4.2K) ~ 60k vs Q(11T, 4.2K) ~ 40k
We have learnt a big deal: In a near future we will be able to coat < R9 mm
RADES haloscope Cu
T = 10 K, n = 8 GHz
RADES haloscope CC
REBCO vs REBCO after R9 mm bent
  Curvature
  R9 mm
P  Be2QVG

## Slide 18
4 – Potential gain and ¿pitfalls? of CCs below the GHz range
3 – How we coat surfaces with CC
2 – CCs vs Cu: Rs(H) in the GHz range
1 – Coated Conductors in a nutshell
Outline

## Slide 19
BASE opportunity: Enhanced Q and operating at higher magnetic fields
BASE detector (exploded)
Opportunities
Coat the cavity with CCs  Increase Q
Make a resonant REBCO coil  Work at 100 MHz & high-Q (low-rf loss) in fields up to 10 T
  n0 = 50 kHz- 200 kHz
Resonant NbTi coil

## Slide 20
A. Romanov, et al. Scientific reports 10 (2020)
GR model
At high magnetic fields, vortices dominate Zs
n = 8 GHz
We can reconstruct Zs and make predictions
The vortex resistivity is :
With
Fitting parameter
The G-R model shows excellent agreement with experiments
The Gittleman-Rosenblum model

## Slide 21
The lower we go in frequency, the bigger the Rs gain will be!
But…
Calatroni and Vaglio, IEEE Transactions on Applied Superconductivity, 27 (2017)
Cu
REBCO
FCC Cu
RRR100 Cu
RRR1000 Cu
factor 1250 – 3000
REBCO
Rs REBCO estimation with G-L model
T = 4.2 K, n = 100 MHz
CC’s Rs greatly outperforms that of Cu in the MHz range and below

## Slide 22
We need to take into account the effective surface impedance of a multilayer system
Stack
If kREBCOtREBCO >> 1
ZStack ≈ ZREBCO
RF field penetration depth
Can we fulfil this condition < GHz range?
A. Romanov, et al. Scientific reports 10 (2020)

## Slide 23
It will be advisable to characterize CCs in the MHz range
for :
In the MHz
REBCO @4.2K
n0 = 40 – 60 GHz
rn = 5 – 30 mWcm
Bc2 = 80 – 120 T
tREBCO ≈ 1.5 – 3 mm
Experiment @ B = 10 T
kREBCOtREBCO = 3 – 15
If kREBCOtREBCO >> 1
ZStack ≈ ZREBCO
our experience in the GHz range 3 – 15 is enough as not to see Zmetals
A. Romanov, et al. Scientific reports 10 (2020)

## Slide 24
Conclusions
CCs are very appealing materials for high-frequency & high-field applications due to their low Rs , high “Hc2” and high currents under magnetic field.
REBCO CCs coatings provide a solution for the FCC-hh beam-screen chamber.
We have demonstrated that cavities coated with REBCO have a higher Q-value in the GHz range under magnetic fields up to 11T. Potentially obtaining a factor >5 gain in Q factor as compared to Cu.
In the MHz range (and below) REBCO CC can provide a factor >1000 improvement in Rs(H) as compared to Cu. An in-depth study of REBCO’s microwave response in this range is needed.

## Slide 25
A word on Copper’s Rs
https://www.copper.org/resources/properties/cryogenic/

## Slide 26
Copper
OFH Copper
VP Copper
Copper
OFH Copper
VP Copper
A word on Copper’s Rs
Going beyond RRR ~ 100 for Cu coatings is hard

## Slide 27
Copper
OFH Copper
VP Copper
Copper
OFH Copper
VP Copper
A word on Copper’s Rs
For accelerator components RRR ~ 100 Cu coatings should be achievable

## Slide 28
Copper
OFH Copper
VP Copper
A word on Copper’s Rs
Rs of state-of-the-art CCs outperforms even OFH Cu in the GHz range
T = 10 K, n = 8 GHz

## Slide 29
The vortex resistivity is :
The Gittleman-Rosenblum model in a nutshell
Flux tube lattice
Equation of motion for fluxons:
Not considering thermal contributions
Assuming
The Gittleman-Rosenblum model
describes the microwave response of the mixed state
With
Fitting parameter