## Slide 2: SRF Coatings at CERN
PBC technology mini workshop: superconducting RF – 21st September 2021
G. Rosaz (TE-VSC), on behalf of FCC SRF WP3

## Slide 3: Outline
Infrastructures
Processes
R&D activities
Achievements
Beyond

## Slide 4: Mandate
Develop superconducting thin films – focus on low Tc (s-wave) for SRF cavities
Investigate alternative materials – Nb3Sn, V3Si …
Design coating devices for complex geometries
Develop suitable surface treatments in view of high performance
Coat SRF cavities for CERN accelerator complex (LHC, HIE-ISOLDE) and for external collaboration.

## Slide 5: Infrastructures

## Slide 6: Surface Preparation
118
107

## Slide 7: Coatings
101
252

## Slide 8: Processes

## Slide 9: B.118 (surface preparation)
Nb and Cu surface treatments
Cu
  SUBU (chemical polishing)
  Electropolishing
  High Pressure Water Rinsing
SUBU

## Slide 10: B.107 (surface preparation)
Degreasing
Pickling
Passivation
Electroplating
Electroplating
Pickling
Degreasing

## Slide 11: Coating techniques
Physical Vapor Deposition
  Pure Material Target / Alloyed targets
  UHV
  Temperature: from 100°C up to 800°C
Diode Sputtering
Ar (10-1 mbar)

## Slide 12: Coating techniques
Physical Vapor Deposition
  Pure Material Target / Alloyed targets
  UHV
  Temperature: from 100°C up to 800°C
Diode Sputtering
Ar (10-1 mbar)

## Slide 13: Coating techniques
Physical Vapor Deposition
  Pure Material Target / Alloyed targets
  UHV
  Temperature: from 100°C up to 800°C
Diode Sputtering
Ar (10-1 mbar)

## Slide 14: Coating techniques
Physical Vapor Deposition
  Pure Material Target / Alloyed targets
  UHV
  Temperature: from 100°C up to 800°C
Diode Sputtering
Ar (10-1 mbar)
Simple set-up
High working pressure

## Slide 15: Coating techniques
Physical Vapor Deposition
  Pure Material Target / Alloyed targets
  UHV
  Temperature: from 100°C up to 800°C
Diode Sputtering
Ar (10-1 mbar)
Simple set-up
High working pressure
Magnetron Sputtering
Ar (10-4/-3 mbar))

## Slide 16: Coating techniques
Physical Vapor Deposition
  Pure Material Target / Alloyed targets
  UHV
  Temperature: from 100°C up to 800°C
Diode Sputtering
Ar (10-1 mbar)
Simple set-up
High working pressure
Magnetron Sputtering
Ar (10-4/-3 mbar))
e-

## Slide 17: Coating techniques
Physical Vapor Deposition
  Pure Material Target / Alloyed targets
  UHV
  Temperature: from 100°C up to 800°C
Diode Sputtering
Ar (10-1 mbar)
Simple set-up
High working pressure
Magnetron Sputtering
Ar (10-4/-3 mbar))
e-

## Slide 18: Coating techniques
Physical Vapor Deposition
  Pure Material Target / Alloyed targets
  UHV
  Temperature: from 100°C up to 800°C
Diode Sputtering
Ar (10-1 mbar)
Simple set-up
High working pressure
Magnetron Sputtering
Ar (10-4/-3 mbar))
e-
More complex set-up
Temperature control required on cathode
Higher coating rate
Lower contamination

## Slide 19: B.101 (coating)
3 coating setups
  2 for samples R&D
  1 for 1.3GHz / 800 MHz cavities

## Slide 20: B.252 (coating)
2 coating setups
Dedicated to Cavities production
  HIE-ISOLDE
  LHC

## Slide 21: B.252 (coating)
2 coating setups
Dedicated to Cavities production
  HIE-ISOLDE
  LHC
Cathode
Magnet
Coating apparatus schematic

## Slide 22: R&D Activities

## Slide 23: Surface treatments
Electropolishing
12 V, 1 rpm
Horizontal EP
10 V, 0 rpm
Vertical EP
12 V, 0.5 rpm
Horizontal EP
Process optimization on 1.3GHz cavities
Scale-up to larger objects (400MHz)
Velocity magnitude distribution (m/s)
TE/VSC seminar on EP

## Slide 24: Surface treatments
Electropolishing
Electroforming
12 V, 1 rpm
Horizontal EP
10 V, 0 rpm
Vertical EP
12 V, 0.5 rpm
Horizontal EP
Process optimization on 1.3GHz cavities
Scale-up to larger objects (400MHz)
Velocity magnitude distribution (m/s)
L. Lain Amador et al, Electrodeposition of copper applied to the manufacture of seamless superconducting rf cavities, Phys. Rev. Accel. Beams 24, 082002
TE/VSC seminar on EP

## Slide 25: Coatings
1.3GHz cavities
Samples
Investigation of High Power Impulse Magnetron Sputtering
DCMS : Direct Current Magnetron Sputtering
HiPIMS: High Power Impulse Magnetron Sputtering
Time
Voltage/ Current
Voltage/ Current
DCMS
HiPIMS
Parameter (unit) | Range
Pulse duration (us) | 1-200
Frequency (Hz) | 20-500
Power (kW) | 100 peak, 2 avg
Gas | Ar, Kr
Pressure (mbar) | 8.10-4-5.10-2

## Slide 26: Coatings
1.3GHz cavities
Samples
Investigation of High Power Impulse Magnetron Sputtering

## Slide 27: Coatings
1.3GHz cavities
Samples
Investigation of High Power Impulse Magnetron Sputtering

## Slide 28: Coatings
1.3GHz cavities
Samples
Investigation of High Power Impulse Magnetron Sputtering
Modulation of the critical current density = Modification of pinning strength in the layers

## Slide 29: Coatings
1.3GHz cavities
Samples
Simulations
Investigation of High Power Impulse Magnetron Sputtering
Magnetostatic for source design

## Slide 30: Coatings
1.3GHz cavities
Samples
Simulations
Investigation of High Power Impulse Magnetron Sputtering
Magnetostatic for source design
PIC-MC + KMC simulations
Plasma discharge
Transport
T. Richard PhD thesis

## Slide 31: Coatings
1.3GHz cavities
Samples
Simulations
Alternative Materials (Nb3Sn)
Investigation of High Power Impulse Magnetron Sputtering
Growth temperature and annealing effect

## Slide 32: Coatings
1.3GHz cavities
Samples
Simulations
Alternative Materials (Nb3Sn)
Investigation of High Power Impulse Magnetron Sputtering
Growth temperature and annealing effect
Use of diffusion barrier layer enhancing Tc
E. A. Ilyina et al, Development of sputtered Nb3Sn films on copper substrates for superconducting radiofrequency applications, SUST, 32, 3 2019

## Slide 33: Achievements

## Slide 34: Achievements
HIE-ISOLDE
Bres= 50 mG
Highest field ever reached by a Nb/Cu cavity
(~30MV/m in elliptical shape)

## Slide 35: Achievements
HIE-ISOLDE
LHC
Bres= 50 mG
Highest field ever reached by a Nb/Cu cavity
(~30MV/m in elliptical shape)
T= 4.5 K
Spare program has shown improved performance vs baseline

## Slide 36: Achievements
A15 (Nb3Sn)
1.3GHz

## Slide 37: Achievements
A15 (Nb3Sn)
1.3GHz
STATE OF THE ART Nb/Cu

## Slide 38: Achievements
A15 (Nb3Sn)
1.3GHz
STATE OF THE ART Nb/Cu

## Slide 39: Achievements
A15 (Nb3Sn)
1.3GHz
STATE OF THE ART Nb/Cu
VERY PROMISING STARTING POINT
OPTIMIZATION ON-GOING

## Slide 40: Beyond

## Slide 41: Beyond
RADES Cavity coating with Nb3Sn
Customized holder and heater.
Cf: J. Golm presentation
Other materials?

## Slide 42: Conclusion
Strong know-how gained regarding surface treatments dedicated to SRF surfaces
Coating techniques capable of providing very low surface resistance materials
Expertise in coating systems/processes design
On-demand customization (e.g. RADES cavity)
Current application targets low Jc
Pinning efficiency can be tuned (ions energy, impurities etc.)

## Slide 43: Thank you for your attention (interested by a lab tour? give a call)