## Slide 2: SRF for axion haloscopes
Sergio Calatroni - CERN

## Slide 3: Exclusion plots
1
Photon frequency (E=h) (GHz)
10
E must be parallel to B
Source: The Review of Particle Physics

## Slide 4: Summary
Where and how could SRF be used for axion detection?
  “Sikivie” like RF cavities: axion + (B) photon  (RF) photon
    (ADMX), RADES (previous talk by J. Golm), QUAX, BASE (see last talk by S. Ulmer)
  “Light shining through a wall”: (RF) photon  axion  (RF) photon
    DarkSRF, (Multimode pumping, Bogorad et al.)
  “Heterodyne” type experiments: axion + (RF) photon  (RF) photon
    See next talk, D’Agnolo et al.
I will then focus on two aspects, relevant for all these experiments: SRF in a magnetic field, and nonlinearities

## Slide 5: Axion conversion in an RF cavity I
Note:
no need for cavity QL to be larger than Qa ~106
Pa
See talk by J. Golm earlier today
Source: Particle Dark Matter, G. Bertone ed.

## Slide 6: Axion conversion in an RF cavity II
CAPP: Patras Workshop 2021
7 GHz
REBCO tape glued on Al segmented cavity @ 7 GHz
2.3 GHz
2.3 GHz
JRF parallel to B

## Slide 7: Axion conversion in an RF cavity III
QUAX a- (KLASH), arXiv:1903.06547v1 and IEEE TAS 29 (2019) 3500605
NbTi / NbTiN – Cu cavity @ 14.46 GHz
Fit of depinning frequency: NbTi = 44 GHz, NbTiN = 26 GHz
(Nb3Sn from literature : 3-4 GHz)
(REBCO from literature = 20-100 GHz)

## Slide 8: One slide on FermiLab
Axion conversion in Nb3Sn cavity
DarkSRF: light through wall
A. Romanenko: ECFA meeting
1.3 GHz cavity (650 MHz)

## Slide 9: One slide on heterodyne, intermodulation
See talk by R. T. D’Agnolo!
A. Berlin et al.: arXiv:2007.15656v1
(Use the RF resonance as a “pump mode”, coupling with a small-mass axion would generate a “signal” within the resonance bandwidth)
(Needs an SRF cavity with high-field, high-Q)
Intermodulation
Axions create nonlinearities in Maxwell’s equations.
Pumping two different modes of a cavity, will generate a signal third mode by intermodulation
(Needs an SRF cavity with high-field, high-Q)
Z. Bogorad et al.: arXiv:1902.01418v2

## Slide 10: Superconductivity and SRF relevant to axion searches
SRF in a magnetic field

## Slide 11: Superconductors in a magnetic field
Meissner effect. Flux expulsion Type I superconductors (some pure metals) Type II superconductors
Mixed state. Abrikosov flux lattice Type II superconductors
Normal conducting state
Image source: wikipedia

## Slide 12: Flux lines
Image source: link
Flux lines arrange in a hexagonal pattern of flux quanta (), minimizing the free energy.
The number density N [m-2] of flux quanta is such that . They repel each other.
A material defect reduces locally the superconductivity. The flux quantum tends to occupy this region to further minimize energy, distorting the lattice, at the expense of a slight increase of elastic energy of the flux lattice. This phenomenon is called flux pinning

## Slide 13: Some theory background: fluxon motion in RF
The motion of the rigid fluxon lattice behaves as a harmonic damped oscillator with quadratic potential
The “depinning frequency”
Gittleman and Rosenblum: Phys Rev. Lett. 16, 734 (1966)
Calatroni and Vaglio, IEEE Trans. Appl. Supercond. 27 (2017) 3500506
Coffey, Clem PRL 67, 386 (1991)
Brandt PRL 67 2219 (1991)
Silva et al, PRB 78, 094503 (2008)
Chart: 
Simplified model, neglecting thermally activated flux creep.
B field is normal to the surface
The RF current JRF is parallel to the surface
An oscillating Lorentz force F is generated on the flux lattice
k  pinning

## Slide 14: Effect of magnetic field: fluxon losses in RF
Surface resistance, reactance due to vortex motion
The total surface resistance scales as f2
Fluxon losses dominate, thus we should choose fresonance < fdepinning

## Slide 15: To use an SRF cavity in a magnetic field
Materials must have a high Jc, i.e. strong pinning (strongly dependent on fabrication process)
Image source: National High Magnetic Field Laboratory

## Slide 16: Frequency dependance
At low enough frequency (compared to depinning frequency), SRF has an advantage compared to (cold) copper
The crossing point is experiment-dependent and field-dependent
HTS for the FCC beam screen studies: reduction of beam coupling impedance

## Slide 17: Superconductivity and SRF relevant to axion searches
Non-linearities

## Slide 18: Q factor of SRF cavities
Q0 vs E curve is nonlinear even in best cavities
(“quadratic losses”)
(“nonquadratic losses”)

## Slide 19: Example of RLC circuit
Standard series RLC circuit
Nonlinearity in R(I) creates distortion  “harmonics”, intermodulation
Not to forget same happens (+ noise) in the measurement hardware…

## Slide 20
Questions ?

## Slide 21
Type I superconductors
(a few pure metals)

## Slide 22
Type II superconductors
(most superconductors)

## Slide 23: Nb/Cu at 1.3 GHz