## Slide 1
New hybrid organic-inorganic ferrophotovoltaic perovskites nanoparticles for high voltage solar cells and IoT
R. Ndioukane, F. Baldé, N. C. Y. Fall, A. K. Diallo, D. Kobor, M. Touré
Email: r.ndioukane1532@zig.univ.sn

## Slide 2
Outlines
Results and discussion
Conclusion and perspectives
Context and problematics
Material and method

## Slide 3
Context and problematics
Energy is considered as one of the primary challenges for the sustainable development of human societies.
Environmentally friendly renewable energy sources, as an alternative to conventional fossil fuels, have witnessed extensive development during past decades because of their potential to provide energy without greenhouse gas emissions and hence mitigate climate change through global warming.
Among a variety of renewable energy sources, PV technologies which enable direct conversion of solar energy to electricity account for a substantial and growing proportion of alternative energy electricity generation capacity globally.
Silicon solar cells are one of the most reliable and efficient technology for renewable energy production.

## Slide 4
In addition, the prevalent silicon PVs generally have poor performance under ambient light conditions, are also costly when operated at much lower levels of energy conversion than the capability of Si and difficult to integrate into small, lightweight, and portable systems for the IoT.
However, because of time consuming production processes and high costs production, researchers tried to develop other technologies for solar energy production.
Context and problematics
Certified record efficiency according to NREL now exceeds 25 %.
Perovskite solar cells seem to be a good alternative.
For indoor applications, the power supply of billions of independent electronic devices and equipment, with the advent of the IoT, is a huge energy requirement that risks compromising reduction decisions of the impact of energy consumption on the climate.
One of the solutions would be the use of photovoltaic cells capable of efficiently converting low intensity light in the indoor environment into megawatt to microwatt class electrical power.

## Slide 5
Context and problematics

## Slide 6
However, despite their excellent properties, one of the greatest difficulties to integrate widely such materials in electronic and photovoltaic devices is to achieve them in thin films form because of their incongruent melting property.
In our previous study, we have successfully fabricate the nanoparticles thin film of such materials, which will facilitate their integration for electronic and photovoltaic devices.
Context and problematics
Despite this breakthrough, OPV are known to degrade due to moisture and heat, upon prolonged exposure to light and are prone to ion or halide vacancy migration, leading to unstable operation of photovoltaic devices.
To overcome such difficulties, we oriented our research to inorganic PZN-PT oxide perovskite materials with excellent and stable properties compared to the organic ones.
The objective of this work is to initiate an innovative photovoltaic technology based on novel inorganic in biopolymer matrix with suitable bandgap widths, more friendly environment use.

## Slide 7
Material and method
Grinding
Biopolymer CC
glass
ITO
TiO2
PZN-4.5PT-np-biopolymer
Pentacene
Dipersion of the perovskite nanoparticles inside the biopolymer matrix
Stirring for homogenization
R. Ndioukane et al. 2020
PZN-4.5PT powder
PZN-4.5PT monocrystal

## Slide 8
Results and discussion
Nanoparticles characterization
Transmission Electron Microscopy
Chart: Diameter (nm)
Spherical shape
Diameter : 30 – 100 nm
It reveals that the average size of ferroelectric nanoparticles is around 78 nm
Conclusion: This proves the nanometric character of the powders produced
Size distribution
Dynamic Light Scattering DLS
R. Ndioukane et al. 2018

## Slide 9
Results and discussion
Surface characterization
A slightly nonhomogeneous distribution of nanoparticles inside the device, which certainly explain the low current density.
One can see the accumulation of perovskites nanoparticles on the biopolymer surface.
This reduces a better extraction of charges while increasing recombination kinetics at the interface.
SEM images

## Slide 10
Results and discussion
SEM image in transverse mode
ITO
Pentacene
PZN-4.5PT-np-biopolymèr
TiO2
Thicknesse (µm) | ITO | TiO2 | PZN-4.5PT-np-biopolymer | Pentacene
DKFB-PD2 | 1,60 | 1,71 | 1,68 | 1,43
Observation in scanning electron microscope in transverse mode, allowed us to see the disposition of the various deposited layers but also to determine their thickness.
R. Ndioukane et al. 2019

## Slide 11
Results and discusion
I-V characteristics
30 min
15 min
Time (min) | PCE (%) | VCO (V) | JSC (A/cm2) | FF | Pmax (mW/cm2)
15 | 21,83 | 5,17 | 3,125x10-4 | 0,27 | 0,43
30 | 31,62 | 5,86 | 3,125x10-4 | 0,34 | 0,63
We find that the open circuit voltage increases over time with a max value of 5.86 V.
This is due to the fact that Ferroelectric perovskites have the ability to accumulate electrical charges on the surface of the sample thus can increase the open circuit voltage over time of exposure to light
The Pmax result shows a promising photovoltaic property for indoor application
V(V)
I(A)
I(A)
V(V)
Chart: 
Chart: 

## Slide 12
Conclusion and perspectives
We can note that long exposure to light from a solar cell containing ferroelectric perovskites increase the open circuit voltage but has no effect on the short circuit current of the device.
The yield is proportional to Vco and Isc, will have a direct impact.
Investigations are in progress particularly for the stability in time and the temperature effect.
We successfully fabricated and demonstrated the large improvement of the photovoltaic performance due to the presence of the PZN-PT-np+biopolymer+pentacene layer.
Perspective
Pmax shows a promising photovoltaic property for indoor application.

## Slide 13
THANK YOU FOR
YOUR ATTENTION