## Slide 1: Superconductors and Superconducting Magnets
Luca.Bottura@cern.ch
2 June 2022

## Slide 2: Overview
Why superconductors ? A motivation
A superconductor physics primer
Superconducting materials and cables
The making of a superconducting magnet
Examples of superconducting magnet systems

## Slide 3: Overview
Why superconductors ? A motivation
A superconductor physics primer
Superconducting materials and cables
The making of a superconducting magnet
Examples of superconducting magnet systems

## Slide 4: Why superconductivity anyhow ?
Conventional iron electromagnets
Nb-Ti
Abolish Ohm’s law !
  no power consumption (although need refrigeration power)
  high current density
  ampere turns are cheap, so don’t need iron (although often use it for shielding)
Consequences
  lower running cost  new commercial possibilities
  energy savings
  high current density  smaller, lighter, cheaper magnets  reduced capital cost
  higher magnetic fields economically feasible  new research possibilities
Graphics by courtesy of M.N. Wilson

## Slide 5: Cost of energy (electricity)
Source: Bundesministerium fuer Wirtschaft und Technologie
Evolution of energy prices in Germany
Private customers
Corporate customers
Energy efficiency is an inevitable design constraint !

## Slide 6: NC vs. SC Magnets - 1/2
Normal conducting accelerator magnets
  Magnetization ampere-turns are cheap
  Field is generated by the iron yoke (but limited by saturation, e.g. ≈ 2 T for iron)
  Low current density in the coils to limit electric power and cooling needs
  Bulky and heavy, large mass of iron (cost driver)
One of the dipole magnets of the PS, in operation at CERN since 1959

## Slide 7: NC vs. SC Magnets - 2/2
Superconducting accelerator magnets
  Superconducting ampere-turns are cheap
  Field generated by the coil current (but limited by critical current, e.g. ≈ 10 T for NbTi)
  High current density, compact, low mass of high-tech SC material (cost driver)
  Requires efficient and reliable cryogenics cooling for operation (availability driver)
A superconducting dipole magnet of the Tevatron at FNAL, the first superconducting synchrotron, 1983

## Slide 8: High current density: solenoids
B
a
t
Je
The field produced by an infinitely long solenoid is:
In solenoids of finite length the central field is:
where f < 1, typically ~ 0.8
The thickness (volume and cost) for a given field is inversely proportional to the engineering current density Je
all-SC solenoid record field: 24 T (NIMS, 2011)

## Slide 9: High current density - dipoles
JE = 375 Amm-2
120mm
≈ 1x106 MA-turn
LHC dipole
660mm
The field produced by an ideal dipole (see later) is:
JE = 37.5 Amm-2
JE
-JE
Graphics by courtesy of M.N. Wilson
≈ 5x106 MA-turn
≈ 6 MW/m
all-SC dipole record field:
16 T (LBNL, 2003)

## Slide 10: The Hall of Fame of SC colliders
 |  | Tevatron | HERA | RHIC | LHC
Maximum energy | (GeV) | 980 | 920(1) | 250(2) 100/n(3) | 7000
Injection energy | (GeV) | 151 | 45 | 12 | 450
Ring length | (km) | 6.3 | 6.3 | 3.8 | 26.7
Dipole field | (T) | 4.3 | 5.0 | 3.5 | 8.3
Aperture | (mm) | 76 | 75 | 80 | 56
Configuration |  | Single bore | Single bore | Single bore | Twin bore
Operating temperature | (K) | 4.2 | 4.5 | 4.3-4.6 | 1.9
First beam |  | 7-1983 | 4-1991 | 6-2000 | 9-2008
(1) energy of the proton beam, colliding with the 27.5 GeV electron beam
(2) energy for proton beams
(3) energy per nucleon, for ion beams (Au)

## Slide 11: Champion dipoles cross sections
HERA
Bore: 75 mm
Field: 5.0 T
Tevatron
Bore: 76 mm
Field: 4.3 T
RHIC
Bore: 80 mm
Field: 3.5 T
LHC
Bore: 56 mm
Field: 8.3 T

## Slide 12: Tevatron at FNAL (Chicago, IL, USA)
Injection | (GeV) | 151
Flat-top | (GeV) | 980
Length | (km) | 6.3
Dipole field | (T) | 4.3
Aperture | (mm) | 76
Temperature | (K) | 4.2
Commisioned |  | 1983
Image by courtesy of Fermi National Accelerator Laboratory

## Slide 13: HERA at DESY (Hamburg, D)
Injection | (GeV) | 45
Flat-top | (GeV) | 920
Length | (km) | 6.3
Dipole field | (T) | 4.7
Aperture | (mm) | 75
Temperature | (K) | 4.5
Commisioned |  | 1991
Closed |  | 2007
Image by courtesy of Deutsches Elektronen Synchrotron

## Slide 14: RHIC at BNL (Upton, NY, USA)
Injection | (GeV) | 12/n
Flat-top | (GeV) | 100/n
Length | (km) | 3.8
Dipole field | (T) | 3.5
Aperture | (mm) | 80
Temperature | (K) | 4.3-4.6
Commisioned |  | 2000
Image by courtesy of BrookhavenAccelerator Laboratory

## Slide 15: LHC at CERN (Geneva, CH)
Injection | (GeV) | 450
Flat-top | (TeV) | 7
Length | (km) | 26.7
Dipole field | (T) | 8.3
Aperture | (mm) | 56
Temperature | (K) | 1.9
Commisioned |  | 2008

## Slide 16: Motivation - Re-cap
Superconductors are used to abolish Ohm’s law, either to:
  Decrease power consumption, and thus improve the performance and operation balance (cost + efficiency) replacing existing technology  technology displacer
  Allow to reach higher magnetic field, over larger bore and for longer time, allowing new physics or technological opportunities  technology enabler

## Slide 17: Overview
Why superconductors ? A motivation
A superconductor physics primer
Superconducting materials and cables
The making of a superconducting magnet
Examples of superconducting magnet systems

## Slide 18: A great physics problem in 1900
What is the limit of electrical resistivity at the absolute zero ?
… electrons flowing through a conductor would come to a complete halt or, in other words, metal resistivity will become infinity at absolute zero.
“X-rays are an hoax”
“I have not the smallest molecule of faith in aerial navigation other than ballooning or of expectation of good results from any of the trials we hear of”
"There is nothing new to be discovered in physics now. All that remains is more and more precise measurement”
W. Thomson (Lord Kelvin)
T


## Slide 19: Superconductors Pre-history
… thus the mercury at 4.2 K has entered a new state, which, owing to its particular electrical properties, can be called the state of superconductivity…
H. Kamerlingh-Onnes (1911)

## Slide 20: Cooper Pairs
Superconductor
    paired electrons forming a quasi particle in condensed state
    zero resistance because the scattering does not excite the quasi-particle
Normal conductor
    scattering of e-
    finite resistance due to energy dissipation
Bardeen, Cooper and Schrieffer
Proper physics: a gas of Fermions. The conduction electrons at the Fermi surface have large energy (few eV) and interact with lattice defects, displacements or thermal excitations (hence (T))
Proper physics: paired electrons in the vicinity of the Fermi surface, with opposite momentum and spin (bosons with zero spin). The binding energy introduces a small energy gap between paired and unpaired state. An external electric field makes the pair drift.

## Slide 21: Pairing mechanism
Lattice displacement

phonons (sound)

coupling of charge carriers
Only works at low
temperature
Bardeen, Cooper, Schrieffer (BCS) - 1957
t1
t2
100-1000 nm
Proper physics: the binding energy is small, of the order of 10-3 eV. Pairs can be broken easily by thermal energy. The interaction is long range, and Cooper pairs overlap and can exchange electrons

## Slide 22: First (not last) superconducting magnet project cancelled
Solvay conference (1914)
The 10 T magnet project was stopped when it was observed that superconductivity in Hg and Pb was destroyed by the presence of an external magnetic field as small as 500 Gauss (0.05 T)
A 100 kGauss magnet ! (H. K. Onnes)
Third International Congress of Refrigeration, Chicago (1913)
Superconductivity languished for 40 years…

## Slide 23: 1986 - A Big Surprise
One Thousand and One Superconductors
B. Matthias (1918-1980)
Bednorz and Mueller
IBM Zuerich, 1986
Theoretical limit around 30 K

## Slide 24: 1987 - The prize !

## Slide 25: High-Tc timeline
Critical Temperature TC (K)
0
10
20
30
40
50
100
150
200
250
300
1900
1940
1980
1985
1990
1995
2000
2005
2010
2015
2020
Year of Discovery (-)
Liquid He
Liquid H2
Liquid N2
Room
Temperature
High-p
IBS
HTS
LTS
NbTi

## Slide 26: Hey, what about field ?
Cool
down
B
B
Raise field
Meissner & Ochsenfeld, 1933
Type I ( < 1/√2)
Pure metals
BC ≈ 10-3…10-2 T
Complete field exclusion
superconducting
normal-conducting
Levitated magnet
Superconducting disk
Example of magnetic levitation
W. Meissner, R. Ochsenfeld

## Slide 27: Free energy and critical field
Let us define the Gibbs free energy of a material in a magnetic field:
A system in equilibrium will tend to a minimum of G
In zero applied field, the SC phase (being in a condensed state) has lower free energy than the normal phase:
The field expulsion (M=-H) corresponds to a magnetic energy density:
The material prefers to expel the magnetic field (Meissner effect) until the free energy of the SC phase in field equals the free energy of the normal state:
Thermal energy
Magnetic energy
G = U - TS - 0 M · H
0/2 Hc2= Gnormal- Gsup(H=0)
Gsup(H=0) < Gnormal(H=0)
-0 M · H = 0/2 H2
Thermodynamic critical field

## Slide 28: Type I – critical field
The difference in free energy DG among the SC and normal state is small
The corresponding values of the thermodynamic critical field are also small, i.e. in the range of few mT to barely above 100 mT
0/2 Hc2= DG
Not very useful for magnet engineers !

## Slide 29: Energy efficient fluxons
Meissner & Ochsenfeld, 1933
Type I ( < 1/√2)
Pure metals
BC ≈ 10-3…10-2 T
Complete field exclusion
Type II ( > 1/√2)
Dirty materials: alloys intermetallic, ceramic
BC ≈ 10…102 T
Ginsburg, Landau, Abrikosov, Gor’kov, 1950…1957
Partial field exclusion
Lattice of fluxons
Landau, Ginzburg and Abrikosov

## Slide 30: Values of L ,  and 
Material | L (nm) | (B=0) (nm) |  (-)
Al | 16 | 1600 | 0.01
Pb | 32 | 510 | 0.06
In | 24 | 360 | 0.07
Cd | 110 | 760 | 0.15
Sn | 30 | 170 | 0.18
Nb | 40 | 39 | 1
Nb3Sn | 200 | 12 | ≈ 20
MgB2 | 185 | 5 | ≈ 40
YBCO | 200 | 1.5 | ≈ 75
Type I
Type II

## Slide 31: Lattice of quantum flux lines
Observation on Pb-4at% In magnetised by a field of 3000 Oe and decorated by Co particles
Essmann & Träuble, 1967
0 = h/2e = 2.07 x 10-15 Wb
Flux quantum
Supercurrent
Graphics by courtesy of Superconductor Lab, Oslo

## Slide 32: Type II – critical field
Tc(K)
NOTE: of all the metallic superconductors, only NbTi is ductile.
All other are brittle inter-metallic compounds
The upper critical field BC2 and temperature TC of metallic superconductors are mutually related
Both BC2 and TC are determined by the chemistry of the material
HTS
Graphics by courtesy of M.N. Wilson

## Slide 33: Hey, what about current ?
A current flowing in a magnetic field is subject to the Lorentz force that deviates the charge carriers:
F = J x B
This translates into a motion of the fluxoids across the superconductor  energy dissipation  loss of superconductivity
To carry a significant current we need to lock the fluxoids so to resist the Lorentz force. For this we mess-up the material and create pinning centers that exert a pinning force FP

## Slide 34: Type II Superconductors (x < l)
B
Normal state cores
Superconducting region

## Slide 35: Pinning centers
Microstructure of Nb-Ti
Graphics by courtesy of Applied Superconductivity Center at NHMFL
Precipitates in alloys
Grain boundaries in
inter-metallic compounds
Microstructure of Nb3Sn
grain

## Slide 36: Jc(B,T,…)
B [T]
T [K]
Jc [A/mm2]
5
5
100
1,000
10,000
100,000
10
10
15
B = 5 [T]
T=1.9 K
T=4.2 K
The maximum current that can be carried by the superconductor is the current at which:
|J x B| = FP
The above expression defines a critical surface:
JC(B,T,…) = FP / B
Critical surface of a LHC NbTi wire
Jc (5 T, 4.2 K) ≈ 3000 A/mm2

## Slide 37: Superconductors physics - Re-cap
Superconducting materials are only useful if they are dirty (type II - high critical field) and messy (strong pinning centers)
A superconductor is such only in conditions of temperature, field and current density within the critical surface, and it is a normal-conductor above these conditions. The transition is defined by a critical current density JC(B,T,…)
The maximum current that can be carried is the IC = ASC x JC

## Slide 38: Superconductor types – 1/2
Magnetic field exclusion:
  Type I – full exclusion of field lines from the material bulk up to lower critical field BC1
  Type II – full exclusion of field lines from the material bulk up to BC1 followed by partial flux penetration (vortices) up to upper critical field BC2
Underlying theory:
  Conventional – explained by BCS theory (usually applying to LTS)
  Unconventional – needs theory different from BCS (usually applying to HTS)

## Slide 39: Superconductor types – 2/2
Critical temperature:
  LTS – low-temperature superconductors, critical temperature TC up to (about) 30 K
  HTS – high-temperature superconductors, critical temperature TC above 30 K, in the range of liquid nitrogen (77K) and higher
  NOTE: MgB2 is a special case: TC ≈ 40 K but explained by LTS theory
Material class:
  Elements (e.g. Pb, Hg)
  Alloys (e.g. Nb-Ti, Nb-Zr)
  Compounds (e.g. Nb3Sn)
  Ceramics (e.g. REBCO)
  Pnictides (e.g. IBS)
  Organic, Sulfides, …

## Slide 40: Overview
Why superconductors ? A motivation
A superconductor physics primer
Superconducting materials and cables
The making of a superconducting magnet
Examples of superconducting magnet systems

## Slide 41: Superconducting magnet cook-book
Devise the desired magnetic configuration for the specified field, bore homogeneity and duty cycle
Analyze mechanically and thermally
Design a cable to fit the winding, by choosing cross sections and cable configuration with:
  Superconductor ASC to carry the current with sufficient margin
  Stabilizer AST sufficient for stability and protection
  Sufficiently low AC loss
Insulate cable, wind coils, mount in a supporting and magnetic structure, insert in a cryostat
Top-off with current leads and instrumentation as desired
Cool properly to cryogenic temperatures
Power up, shake with quenches
Enjoy the field according to your taste
Science in the Kitchen, P. Artusi, 1891

## Slide 42: From materials to magnets
Materials must be made in high-current wires, tapes and cables for use in magnets
The manufacturing route depends, among others on:
  The material (e.g. alloy or chemical compound),
  The material synthesis (e.g. reaction conditions or a crystal growth method)
  The material mechanical properties (e.g. ductile or fragile)
  The compatibility with other materials involved (e.g. precursors or mechanical supports)

## Slide 43: A summary of technical materials
 | LTS |  |  |  | HTS |  | 
 | Nb-Ti | Nb3Sn | Nb3Al | MgB2 | YBCO | BSCCO | IBS
 | 1961 | 1954 | 1958 | 2001 | 1987 | 1988 | 2006
Tc (K) | 9.2 | 18.2 | 19.1 | 39 | ≈93 | 95(5) 108(6) | 16(7) 38(8) 55(9)
Bc (T) | 14.5 | ≈30 | 33 | 18(1) 36…74(2) | ≈120(3) ≈250(4) | ≈200 | 40(7) 80(8) 100(9)
Notes:
(1) wires and tapes
(2) thin layers
(3) B parallel to c-axis
(4) B in the ab-plane
(5) BSCCO-2212
(6) BSCCO-2223
(7) IBS-11
(8) IBS-122
(9) IBS-1111
HTS are not only superconducting at high temperature, they also have an exceptional critical field ! (important for high magnetic field applications)

## Slide 44: Nb-Ti manufacturing route
extrusion
cold drawing
heat
treatments
NbTi is a ductile alloy that can sustain large deformations
IC(5 T, 4.2 K) ≈ 1 kA
NbTi billet
Graphics by courtesy of Applied Superconductivity Center at NHMFL
1 mm
LHC wire

## Slide 45: NbTi: an industrial process

## Slide 46: The trick to high Jc in NbTi
Intermediate heat treatment is necessary to form precipitates (pinning centers) and improve draw-ability. Subsequent drawing elongates the precipitates to the desired spacing

## Slide 47: Nb3Sn synthesis
Initial Nb3Sn synthesis routes (Kunzler) required high-temperature heat treatment (> 950 °C)
Breakthrough achieved by three groups in 1969-1970:
  K. Tachikawa at the National Research Institute for Metals in Japan
  A. R. Kaufman at the Whittaker Corporation in the USA
  E . W. Howlett at the Atomic Energy Research Establishment at Harwell in Great Britain.
A15 compound layers (V3Ga and Nb3Sn) could be formed by solid diffusion at the interface of Nb/V and Cu-Sn/Ga at modest temperatures, of the order of 700 °C
In addition, Cu de-stabilizes Sn-rich compounds

## Slide 48: Nb3Sn manufacturing routes
Nb3Sn is brittle and cannot be drawn in final form. The precursors are drawn and only later the wire is heat-treated to ≈650 C for several hrs, to form the Nb3Sn phase
Graphics by courtesy of Applied Superconductivity Center at NHMFL
IC(12 T, 4.2 K) ≈ 1.5 kA

## Slide 49: MgB2 manufacturing routes
Technical MgB2 is manufactured wires and tapes
  Powder-in-Tube
    In-situ
    Ex-situ
  Mg diffusion
The precursor (Mg/B or MgB2 powders) requires a high-temperature heat treatment to form the brittle superconducting phase
The MgB2 must be clad in Fe/Nb/Ni to protect Cu
Critical manufacturing issues:
  Powder quality, granulometry, mixing, final porosity
Doping with impurities the Mg/B powder is beneficial to JC:
  SiC, C, B4C, C nanotubes, Hydrocarbons
  C substitutes B MgB2-xCx

## Slide 50: BSCCO manufacturing routes
Oxide powder in tube OPIT
1) draw down BSCCO powder in a silver tube
2) stack many drawn wires in another silver tube and draw down again
3) roll the final wire to tape and heat treat at about 900C in oxygen to melt the B2212
BSCCO is also brittle: a special sequence of rolling and sintering heat treatments must used. Silver has the important feature that it is transparent to Oxygen at high temperature, but does not react with it
BSCCO wire and tape
Graphics by courtesy of M.N. Wilson and
Applied Superconductivity Center at NHMFL

## Slide 51: REBCO manufacturing routes
1) produce a tape with an aligned texture
2) coat the tape with a buffer layer
3) coat the buffer with a layer RE-Ba2Cu3O7 such that the texture of the RE-BCO follows that of the buffer and substrate
REBCO has better critical properties than BSCCO but, unlike BSCCO, grains do not align during processing. If grains are not aligned the supercurrent cannot jump between the grains. The manufacturing processes are all forcing a certain degree of alignment in the microstructure
1 m
≈0.1 mm
IC(20 T, 4.2 K) ≈ 1 kA

## Slide 52: YBCO production: high-tech
Work in clean-room conditions, costly processing of long lengths

## Slide 53: Practical conductors: high JE
Multifilamentary wires have current carrying capability of 100… 1000 A
Insulated with varnish or glass-braids they can be used to make all kind of small size magnets
Large size magnets (e.g. LHC dipoles) require invariably large operating currents (10 to 100 kA) to:
  Decrease inductance,
  Lower the operating voltage,
  Ease magnet protection (?)
Rutherford cables are ideally suited for this task
JE ≈ 500 A/mm2
LHC cable prototype

## Slide 54: Rutherford cable machine @ CERN
Strand spools on rotating tables
Strands fed through a cabling tongue to shaping rollers

## Slide 55: Practical conductors: low JE
Super-stabilized conductor, a superconducting cable (e.g. Rutherford) backed by a large amount of good normal conductor (e.g. Al)
JE ≈ 50 A/mm2
Internally-cooled conductor, e.g. Cable-In-Conduit Conductor (CICC), a rope of wires inserted in a robust conduit that provides a channel for cooling

## Slide 56: Superconducting wires and tapes for all taste…
NbTi
Nb3Sn, Nb3Al
BSCCO
YBCO
MgB2

## Slide 57: … and superconducting cables
CICC
Braids for
power transmission
Rutherford
Super-stabilized
Internally cooled

## Slide 58: Overview
Why superconductors ? A motivation
A superconductor physics primer
Superconducting materials and cables
The making of a superconducting magnet
Examples of superconducting magnet systems

## Slide 59: LHC dipole
Bnominal 8.3 (T)
current 11850 (A)
stored energy  10 (MJ)
cold mass  35 (tonnes)

## Slide 60: Superconducting dipole magnet coil
Ideal current distribution that generates a perfect dipole
Practical approximation of the ideal distribution using Rutherford cables
+J
J
+J
J

## Slide 61: Twin coil principle
Combine two magnets in one
Save volume, material, cost

## Slide 62: LHC dipole coils
B
B

## Slide 63: Fine cables
LHC Nb-Ti strand
LHC inner cable
LHC outer cable cross section
7500 km of superconducting cables with tightly controlled properties (state-of-the-art production)

## Slide 64: Coil winding
B
B
Cable insulation
Coil winding machine
Stored coils
10 m precision !

## Slide 65: Ends
Inner layer
Layer jump
Ends, transitions, and any deviation from the regular structure are the most delicate part of the magnet

## Slide 66: Collaring and yoking
yoking
collaring

## Slide 67: Magnet assembly
Alstom
Noell
Ansaldo

## Slide 68: Cold mass

## Slide 69: Cryostat
Vacuum enclosure
Low conduction foot
Thermal screens

## Slide 70: Cryo-magnets and tests
Magnet reception, cryostating, preparation for cold test and “stripping” for installation
Magnet powering tests and magnetic measurements

## Slide 71: Magnet installation
Descent in the tunnel
Magnet transport and installation

## Slide 72: Interconnection
65’000 electrical joints
Induction-heated soldering
Ultrasonic welding
Very low resistance
HV electrical insulation
40’000 cryogenic junctions
Orbital TIG welding
Weld quality
Helium leaktightness

## Slide 73: Large scale use of HTS
BSCCO
2223
Warm end (300K)
50 K
4.2 K

## Slide 74: Finally, in the tunnel !

## Slide 75: Overview
Why superconductors ? A motivation
A superconductor physics primer
Superconducting materials and cables
The making of a superconducting magnet
Examples of superconducting magnet systems

## Slide 76: Magnetic Resonance Imaging (MRI)
Superconducting magnet manufacturing at Siemens Magnet Technology
MRI basic components

## Slide 77: Nuclear Magnetic Resonance (NMR)
28.2 T
HTS
sample
SC solenoid
SC solenoid

## Slide 78: Motors and generators
Superconductors offer higher power and torque density

## Slide 79: Motors & generators
3.6 MW generator
HTS coils

## Slide 80: ASCEND
Advanced Superconducting and Cryogenic Experimental powertraiN Demonstrator
High power density (motor) and lossless power transmission (cables and leads) to aviation increase efficiency and reduce emissions

## Slide 81: Energy storage by technology
Power Rating
Discharge Time
Seconds
Days
10 kW
10 MW
10 GW

## Slide 82: SC Magnetic Energy Storage
Nb-Ti torus 200 kJ / 160 kW
(B = 4 T, diameter = 1.1 m)
HTS solenoid 814 kJ
(B = 5 T, diameter = 814 mm

## Slide 83: Transformers & FCL
SC Fault Current Limiter
3.4 kA / 220 kV
SuperOx
HTS Transformer 630 kVA, 18.7kV to 0.42 kV

## Slide 84: Magnetic separation
superconducting solenoid, enclosed within iron shield
stainless steel canister containing ferromagnetic mesh
pipes feeding the kaolin slurry for separation

## Slide 85: Thermonuclear fusion
PF1
PF2
PF3
PF4
PF5
PF6
ITER
International Thermonuclear Experimental Reactor
CS
TF

## Slide 86: HEP detectors of the past...
Omega
BEBC

## Slide 87: … and HEP of the present (CMS and ATLAS)
CMS
ATLAS

## Slide 88: Other uses of superconductivity
Letter to Prof. Main, University of Nottingham, 14 April 1997
The Church of the Latter Day Snakes
founded 1905, revived 1950
We have a big interest in this machine…
How big is this magnet, and can it be concealed beneath a floor…
Does it make much noise…
Does it hurt… because it will be me doing the levitating.
…we pull back the curtain in the Snake Chamber and I start to rise up from the ground…
Tsonaoumi, 202 Kg
I put in five pounds for you… This is only the start.
…the Natural Law Party… please do not sell them a machine… they are very bonkers…

## Slide 89: A word of closing
Superconducting magnet design is a lot about superconductors (materials, wires, cables, and their electric and thermal properties)…
… but not only !
  High field & forces bear mechanical problems that are tough to solve (B=10 T  pmag=400 bar !)
  Materials at low temperature are not what we are used to (mechanical and magnetic properties, thermal expansion, electrical insulation)
  Cooling is an applied science by itself

## Slide 90: Where to find out more - 1/3
Superconducting magnets:
  Case Studies in Superconducting Magnets: Y. Iwasa, Plenum Press, New York (1994), ISBN 0-306-44881-5.
  Superconducting Magnets: M.N. Wilson, Oxford University Press (1983) ISBN 0-019-854805-2
  High Field Superconducting Magnets: F.M. Asner, Oxford University Press (1999) ISBN 0 19 851764 5
  Superconducting Accelerator Magnets: K.H. Mess, P. Schmuser, S. Wolf, World Scientific, (1996) ISBN 981-02-2790-6
  Stability of Superconductors: L. Dresner, Plenum Press, New York (1994), ISBN 0-306-45030-5
  Handbook of Applied Superconductivity ed. B. Seeber, UK Institute Physics 1998
  Proc Applied Superconductivity Conference: IEEE Trans Magnetics, 1975 to 1991, and IEEE Trans Applied Superconductivity, 1993 to 2012,
  Proc European Conference on Applied Superconductivity EUCAS, UK Institute Physics
  Proc International Conference on Magnet Technology; MT-1 to MT-20 (2007) mainly as IEEE Trans Applied Superconductivity and IEEE Trans Magnetics

## Slide 91: Where to find out more - 2/3
Cryogenics
  Helium Cryogenics S.W. Van Sciver, Plenum Press, 86 ISBN 0-0306-42335-9
  Cryogenic Engineering, B.A. Hands, Academic Press 86 ISBN 0-012-322991-X
  Cryogenics: published monthly by Elsevier
Materials - Superconducting properties
  Superconductor Science and Technology, published monthly by Institute of Physics (UK).
  IEEE Trans Applied Superconductivity, published quarterly
  Superconductivity of metals and Cuprates, J.R. Waldram, Institute of Physics Publishing (1996) ISBN 0 85274 337 8
  High Temperature Superconductors: Processing and Science, A. Bourdillon and N.X. Tan Bourdillon, Academic Press, ISBN 0 12 117680 0

## Slide 92: Where to find out more - 3/3
Materials - Mechanical properties
  Materials at Low Temperature, Ed. R.P. Reed and A.F. Clark, Am. Soc. Metals 1983. ISBN 0-87170-146-4
  Handbook on Materials for Superconducting Machinery, Batelle Columbus Laboratories, 1977.
  Nonmetallic materials and composites at low temperatures, Ed. A.F. Clark, R.P. Reed, G. Hartwig, Plenum Press
  Nonmetallic materials and composites at low temperatures 2, Ed. G. Hartwig, D. Evans, Plenum Press, 1982