## Slide 1: RF tests of 1.3 GHz Nb/Cu elliptical cavities
L. Vega-Cid, S. Atieh, A. Bianchi, G. Favre, L. Ferreira, L. Lain-Amador, S. Leith, C. Pereira, M. Redondas, G. Rosaz, K. Scibor, W. Venturini Delsolaro, P. Vidal-Garcia
FCC Week 2022
31th of May 2022

## Slide 2: Contents
FCC Framework:
  SRF requirements
  Timeline
Overview of 1.3 GHz cavities program:
  Workflow
  Tested cavities
RF tests results
  Towards FCC: At 4.2 K
  Towards high gradient, high energy machines: At 1.85 K
Summary and conclusions

## Slide 3: FCC FRAMEWORK

## Slide 4: SRF System requirements
Evolved scenario from the CDR (Input from WP1):
Frequency | 400 MHz
Eacc [MV/m] | 
# cell/ cav | 
Toperation [K] | 
Q0 | 
Most demanding scenario:
Frequency | 400 MHz
Eacc [MV/m] | 12
# cell/ cav | 
Toperation [K] | 
Q0 | 
Frequency | 400 MHz
Eacc [MV/m] | 12
# cell/ cav | 2
Toperation [K] | 
Q0 | 
Frequency | 400 MHz
Eacc [MV/m] | 12
# cell/ cav | 2
Toperation [K] | 4.5
Q0 | 
Frequency | 400 MHz
Eacc [MV/m] | 12
# cell/ cav | 2
Toperation [K] | 4.5
Q0 | 3E9
Notes: To give context to the RD program within the FCC, let’s see the requirements of the SRF system.

## Slide 5: Timeline
@400 MHz:
Eacc~12 MV/m Q0~3E9
T= 4.5 K
1.3 GHz elliptical cavities
400 MHz elliptical cavities
2021
2022
2023
2024
2025
Delivery of FCC Feasibility Study
Provide an optimized recipe for 400 MHz cavities fabrication
@1.3 GHz:
Eacc~12 MV/m Q0~4E8
T= 4.2 K
Thin film of low Rs
Good bonding
High quality substrate
Synergy (and co-funding) with general SRF R&D project
Notes: Looking at the timeline, two milestones within the FCC framework:
At the end of 2025 an elliptical cavity of 400 MHz needs to be provided meeting FCC requirements.
At the end of this year, we need to provide an optimized recipe as input for producing the bigger 400 MHz cavities. We have targeted the optimization in each of the steps

## Slide 6: overview of 1.3 GHz cavities program

## Slide 7: Workflow
Substrates manufacturing
RF testing
Cleanroom assembly
EN-MME, TE-VSC, collaborations with INFN/LNL, JLab…
Surface treatments + Coating
TE-VSC-SCC
SY-RF-SRF
SY-RF-SRF, TE-CRG
1 day
1.5 week
1 week

## Slide 8: Workflow
Substrates manufacturing
RF testing
Cleanroom assembly
EN-MME, TE-VSC, collaborations with INFN/LNL, JLab…
Surface treatments + Coating
TE-VSC-SCC
SY-RF-SRF
SY-RF-SRF, TE-CRG
1 day
1.5 week
Regular meetings to comment results and establish a plan of action accordingly.
1 week

## Slide 9: Tested cavities
2021
BM1.1
L1.2
BM1.2
W1.3
BM1.3a
W1.4
L1.5
BM2.1
W1.5
BM1.3b
Jan
Feb
Mar
Apr
May
Jun
Jul
Aug
Sep
Oct
Nov
Dec
BM2.2
N4.1
BM4.1
2022
Jan
Feb
BM3.1
18 tests performed in the last 15 months thanks to the fruitful collaboration!
Mar
Apr
May
BM2.3
BM3.2a
BM3.2b
BM4.2
BM2.4
R&D 1.3 GHz elliptical cavities

## Slide 10: Tested cavities
Seamless
Welded
BM
Machined from bulk billet
L
Electroformed
W
E-beam welded

## Slide 11: Tested cavities: Welded
IRIS: Welded from inside by firing at a tilted angle from outside the cavity.
EQUATOR: E-beam welded from inside using a deflector

## Slide 12: Tested cavities
Seamless
Welded
BM
Machined from bulk billet
L
Electroformed
W
E-beam welded

## Slide 13: Tested cavities: Machined from bulk billet
Bulk Cu billet
Machining of first half cell
Courtesy: K. Scibor
Machined cell
E-beam welded to cut-offs
Machining of second half cell

## Slide 14: Tested cavities
Seamless
Welded
BM
Machined from bulk billet
L
Electroformed
W
E-beam welded

## Slide 15: Tested cavities: Electroformed
“L. Laín Amador. et al., “Electrodeposition of copper applied to the manufacture of seamless superconducting rf cavities ”, Phys. Rev. Accel. Beams 24, 082002 ,2021
Notes: https://journals.aps.org/prab/abstract/10.1103/PhysRevAccelBeams.24.082002

## Slide 16: rf tests results

## Slide 17: RF tests
1.3 GHz cavity testing campaign:
  Q vs Eacc at 1.85K and 4.2 K
  Q vs Temperature
  Frequency vs Temperature

## Slide 18: RF performance at 4.2 K
Welded
W
Internal e-beam welding
Remarks:
W: 1 substrate tested. No big impact of weld on 4.5 K (BCS) performance, likely the higher probability of defects only affects Rresidual.
Notes: Why study at 1.85 K?
To determine the superconducting parameters we test at 1.85K.
Besides, interest goes beyond FCC, to study potential application of this technology in other machines: high gradient and high energy

## Slide 19: RF performance at 4.2 K
Seamless
BM
Machined from bulk billet
Remarks:
BM: 4 substrates from different billets.
  BM1: Last coating has record performance. Test stopped at low field at 4.2 K for safety.
Notes: Why study at 1.85 K?
To determine the superconducting parameters we test at 1.85K.
Besides, interest goes beyond FCC, to study potential application of this technology in other machines: high gradient and high energy

## Slide 20: RF performance at 4.2 K
Seamless
BM
Machined from bulk billet
Remarks:
BM: 4 substrates from different billets.
  BM1: Last coating has record performance. Test stopped at low field at 4.2 K for safety.
  BM2: Very similar performance achieved after re-coating.
Notes: Why study at 1.85 K?
To determine the superconducting parameters we test at 1.85K.
Besides, interest goes beyond FCC, to study potential application of this technology in other machines: high gradient and high energy

## Slide 21: RF performance at 4.2 K
Seamless
BM
Machined from bulk billet
Remarks:
BM: 4 substrates from different billets.
  BM1: Last coating has record performance. Test stopped at low field at 4.2 K for safety.
  BM2: Very similar performance achieved after re-coating.
  BM3: Very similar performance achieved after re-coating.
Notes: Why study at 1.85 K?
To determine the superconducting parameters we test at 1.85K.
Besides, interest goes beyond FCC, to study potential application of this technology in other machines: high gradient and high energy

## Slide 22: RF performance at 4.2 K
Seamless
BM
Machined from bulk billet
Remarks:
BM: 4 substrates from different billets.
  BM1: Last coating has record performance. Test stopped at low field at 4.2 K for safety.
  BM2: Very similar performance achieved after re-coating.
  BM3: Very similar performance achieved after re-coating.
  BM4: Second coating worse due to issues during assembly.
Notes: Why study at 1.85 K?
To determine the superconducting parameters we test at 1.85K.
Besides, interest goes beyond FCC, to study potential application of this technology in other machines: high gradient and high energy

## Slide 23: RF performance at 4.2 K
Seamless
L
Electroformed
Remarks:
L: 1 substrate produced. Peel-off during 1st coating. Very promising results of 2nd and 3rd coatings at 4.5 K.
Notes: Why study at 1.85 K?
To determine the superconducting parameters we test at 1.85K.
Besides, interest goes beyond FCC, to study potential application of this technology in other machines: high gradient and high energy

## Slide 24: RF performance at 4.2 K
Conclusions:
BCS resistance has been optimized.
FCC SRF requirements in terms of material properties are are potentially met with high repeatability using Nb/Cu technology.
Next steps:
Scale HIPIMs on 400 MHz cavity substrates (starting now)
Continue the R&D for optimizing this technology to use it in high energy, high gradient accelerators (applications including FCC)

## Slide 25: RF performance at 1.85 K
Welded
W
Internal e-beam welding
Remarks:
W: Remarkable Q slope.
Notes: Why study at 1.85 K?
To determine the superconducting parameters we test at 1.85K.
Besides, interest goes beyond FCC, to study potential application of this technology in other machines: high gradient and high energy

## Slide 26: RF performance at 1.85 K
Seamless
BM
Machined from bulk billet
Remarks:
W: Remarkable Q slope.
BM: Very promising results, with BM1.3 showing record performance. Although same recipe has been followed to coat the cavities, this performance has not been achieved again. Currently under investigation.
Notes: Why study at 1.85 K?
To determine the superconducting parameters we test at 1.85K.
Besides, interest goes beyond FCC, to study potential application of this technology in other machines: high gradient and high energy

## Slide 27: RF performance at 1.85 K
Seamless
L
Electroformed
Remarks:
W: Remarkable Q slope.
BM: Very promising results, with BM1.3 showing record performance. Although same recipe has been followed to coat the cavities, this performance has not been achieved again. Currently under investigation.
L: Promising results obtained. More substrates are being produced.

## Slide 28: RF performance at 1.85 K
Superconducting parameters
 | BM1.1 | BM1.2 | BM1.3 | BM2.1 | BM2.2 | BM2.3 | BM3.1 | BM3.2 | BM4.1 | BM4.2 | W1.4 | W1.5 | N4.1 | L1.1 | L1.2 | L1.5
[n] |  | 19.99 | 4.48 | 14.4 | 7.34 | 15.09 | 26.4 | 22.45 | 7.82 |  | 19.53 | 16.4 | 10.4 | 33.27 | 23.9 | 8.7
/ [K] |  | 20.11 | 20.33 | 19.96 | 20.1 | 20.3 | 19.8 | 19.8 | 20.6 |  | 20.38 | 21.23 | 19.1 | 19.75 | 19.8 | 20.27
[n·K] |  | 1.56E+05 | 1.46E+05 | 1.34E+05 | 1.55E+05 | 1.69E+05 | 1.52E+05 | 1.59E+05 | 1.71E+05 |  | 1.75E+05 | 1.98E+05 | 1.11E+05 | 1.40E+05 | 1.68E+05 | 1.74E+05
[K] | 9.31 | 9.31 | 9.31 | 9.36 | 9.36 | 9.4 | 9.38 | 9.41 | 9.37 | 9.41 | 9.38 | 9.3579 | 9.35 | 9.3602 | 9.34 | 9.35
[nm] | 55.58 | 51.73 | 51.08 | 49.31 | 48.04 | 47.75 | 48.98 | 46.99 | 55.44 | 50.86 | 49.56 | 49.33 | 48.57 | 51.54 | 56.8 | 48.01
 | BM1.1 | BM1.2 | BM1.3 | BM2.1 | BM2.2 | BM2.3 | BM3.1 | BM3.2 | BM4.1 | BM4.2 | W1.4 | W1.5 | N4.1 | L1.1 | L1.2 | L1.5
 |  | 19.99 | 4.48 | 14.4 | 7.34 | 15.09 | 26.4 | 22.45 | 7.82 |  | 19.53 | 16.4 | 10.4 | 33.27 | 23.9 | 8.7
 |  | 20.11 | 20.33 | 19.96 | 20.1 | 20.3 | 19.8 | 19.8 | 20.6 |  | 20.38 | 21.23 | 19.1 | 19.75 | 19.8 | 20.27
 |  | 1.56E+05 | 1.46E+05 | 1.34E+05 | 1.55E+05 | 1.69E+05 | 1.52E+05 | 1.59E+05 | 1.71E+05 |  | 1.75E+05 | 1.98E+05 | 1.11E+05 | 1.40E+05 | 1.68E+05 | 1.74E+05
 | 9.31 | 9.31 | 9.31 | 9.36 | 9.36 | 9.4 | 9.38 | 9.41 | 9.37 | 9.41 | 9.38 | 9.3579 | 9.35 | 9.3602 | 9.34 | 9.35
 | 55.58 | 51.73 | 51.08 | 49.31 | 48.04 | 47.75 | 48.98 | 46.99 | 55.44 | 50.86 | 49.56 | 49.33 | 48.57 | 51.54 | 56.8 | 48.01

## Slide 29: RF performance at 1.85 K
Superconducting parameters
Remarks:
Standard deviation of superconducting parameters is low: Reproducible coatings, process well under control.
Residual resistance is more variable, which is expected as this parameter is influenced even by tiny defects.
Correlation observed between Q slope and residual resistance.
 | Average | Standard deviation
[n] | 16.44 | 8.01
/ [K] | 20.11 | 0.47
[n·K] | 1.58E5 | 2.04E4
[K] | 9.36 | 0.03
[nm] | 50.60 | 2.90
 | Average | Standard deviation
 | 16.44 | 8.01
 | 20.11 | 0.47
 | 1.58E5 | 2.04E4
 | 9.36 | 0.03
 | 50.60 | 2.90

## Slide 30: RF performance at 1.85 K
Superconducting parameters
Chart: 𝑇𝑐 [K]
| 9.31 | 9.31 | 9.31 | 9.36 | 9.36 | 9.4 | 9.3800000000000008 | 9.41 | 9.3700000000000028 | 9.41 | 9.3800000000000008 | 9.3579000000000008 | 9.35 | 9.3602000000000007 | 9.34 | 9.35
 | 55.58 | 51.73 | 51.08 | 49.31 | 48.04 | 47.75 | 48.98 | 46.99 | 55.44 | 50.86 | 49.56 | 49.33 | 48.57 | 51.54 | 56.8 | 48.01
Chart: 𝑅𝑟𝑒𝑠 [nΩ]
| 19.989999999999991 | 4.4800000000000004 | 14.4 | 7.34 | 15.09 | 26.4 | 22.45 | 7.8199999999999994 | 19.53 | 16.399999999999999 | 10.4 | 33.270000000000003 | 23.9 | 8.7000000000000011
Abcs | 156000 | 146000 | 134000 | 155000 | 169000 | 152000 | 159000 | 171000 | 175000 | 198000 | 111000 | 140000 | 168000 | 174000
Lambda | 55.58 | 51.73 | 51.08 | 49.31 | 48.04 | 47.75 | 48.98 | 46.99 | 55.44 | 50.86 | 49.56 | 49.33 | 48.57 | 51.54 | 56.8 | 48.01
ABCS and λL are not dependent on the residual resistance.
λL is not correlated to the transition temperature.

## Slide 31: SUMMARY AND CONCLUSIONS

## Slide 32: Summary and conclusions
The R&D program on 1.3 GHz cavities is exploring the potential of the Nb/Cu technology on a high turnaround cavity substrate, which is recognized as international standard in the SRF community.
An important goal is to provide a coating recipe for producing 400 MHz cavities that meet the FCC SRF system requirements.
Different recipes have been investigated with a total of 18 cavities tested since 2021.
The performance at 4.2 K (“BCS” resistance) has been optimized with high repeatability.
RF results at 1.85 K are encouraging and ensure the potential application of this technology to high energy, high gradient accelerators.
Repeatability of results at 1.85 K is however not yet achieved. Further investigations are ongoing to optimize the still occasionally occurring high residual resistance at 1.85 K, which includes a non linear component (Q-slope)

## Slide 33: Thank you for your attention
Questions ?
Acknowledgements
Laetitia Dufay-Chanat, Zoran Jankovic, Serge Forel, Agostino Vacca, Torsten Koettig, Gabriel Pechaud, Sebastien Prunet