## Slide 1: Progress with bipolar HiPIMS-deposited Nb3Sn films on Cu for SRF applications
S. Leith, C.P.A. Carlos, G. Rosaz, M. Himmerlich, M. Taborelli, D. Fonnesu, E. Reches, T. Koettig, A. Baris, B. Ruiz Palenzuela, S. Pfeiffer, A. -T. P. Fontenla

## Slide 2
[1] J. Charlesworth, I. MacPhail, and P. Madsen, J. Mater. Sci. 5, 580 (1970).
Binary phase diagram of the Nb-Sn system [1]
Nb3Sn
Tc | Nb ~ 9.2 K
 | Nb3Sn ~ 18.3 K
Challenges
A15 phase formation (typically high temperature)
Stoichiometry control (Sn at. % 18 - 26 at. %)
Copper substrate influence
Motivation
Nb3Sn: Q0 at 4.2 K ~ bulk Nb at 2 K
RBCS @4.2K and 500MHz | Nb ~ 45nΩ
 | Nb3Sn ~ 0.4nΩ

## Slide 3
1 µm
1 µm
[2] K. Ilyina et al. Supercond. Sci. Technol., 32 (2019)
[3] M. Arzeo et al. FCC Week 2018
Film porosities and Cu inclusions/interdiffusion
DC MS Coatings @ CERN
Impressive Tc
  Sn dependent (increased with Kr)
  Increased with Ta interlayer
Surface cracking
  Mitigated with Kr
Formation of A15 phase
  High temperatures required!
Cu Diffusion
  Interlayer required (Ta/Nb)
Q-slope
Pronounced Q-slope
T=2.5K
T=4.5K
Ta barrier layer (high T growth)

## Slide 4
Bipolar HiPIMS Nb3Sn/Ta/Cu
Improved density required for RF performance
  Proven with Nb/Cu
Lessons learnt dictate starting coating parameters
Coating parameters:
Gas: Kr
Ts: 650 … 750°C
P: 7·10-4 … 5·10-2 mbar
PP: 35 … 100 V
Post anneal: 0 … 72 hrs
Cu
Ta
Cu
Nb3Sn

## Slide 5
Crystallinity and Morphology
Correct A15 phase within studied parameter regime
  Further analysis ongoing
1μm
Nb3Sn
Ta
Cu
Pt
2μm
Morphology mainly affected by pressure and positive pulse
  Dense, crack free, porous surface
  Dense cross section. Grainy Nb3Sn
100 V
1μm
2μm
2.5.10-2 mbar
1μm
2μm
50 V
7.0e-4 mbar

## Slide 6
Compositional Analysis
Correct stoichiometry range
  Sn % = 19.8 to 26.4 at. % (EDS)
Chart: EDS Scanning Voltage (kV)
| 5 | 7 | 10 | 15 | 20
7.0e-4 mbar | 23.27 | 26.18 | 25.26 | 24.3 | 24.23
2.5e-2 mbar | 25.635 | 27.46 | 26.38 | 25.52 | 24.94
1μm
No Anneal
Post Anneal
Sn depleted near surface region
1μm
Chart: Annealing Time (hrs)
| 0 | 24 | 48 | 72
5kV | 23.47 | 21.74 | 22.24 | 21.75
10kV | 23.74 | 23.65 | 24.11 | 23.7
Sn reduction with annealing
    Near surface only
35V PP
7.0e-4 mbar
50V PP

## Slide 7
Surface Contamination
10μm
Reduction methods
  Decreased Ta coating temp
  Stainless steel substrate holder
20μm
5μm
Evident
Unclear
XPS only
XPS and EDS
72h, 750°C Anneal
Presence of Cu on film surface
  Evident/unclear in SEM (XPS vs. EDS)
    Evaporation from uncoated Cu surfaces
    Diffusion through Ta
  Annealing
    Sublimation? (3.9e16 / m2s @ 750°C)
  Further investigations ongoing

## Slide 8
Superconducting Performance
Inductive Tc measurement
[5] D. Fonnesu - PhD Thesis (to be published)
Chart: Positive Pulse (V)
| 50 | 100 | 100 | 65 | 80 | 80 | 35 | 35
7.0e-4 mbar | 12.8703 | 6.6534 | 5.9071 | 10.8696 | 12.1092 | 10.9938 | 14.2396 | 14.3938
2.5e-2 mbar | 14.6961 | 14.8241 | 12.7785 | 14.3833 | 14.4281 | 15.37 | 13.7605 | 14.1804
Chart: Positive Pulse (V)
| 50 | 100 | 65 | 80 | 35
7.0e-4 mbar - 10kV | 23.74 | 19.97 | 22.91 | 23.24 | 25.26
2.5e-2 mbar - 10kV | 25.92 | 23.12 | 23.11 | 26.38 | 22.475

## Slide 9
[7]
Chart: Sn Content (At. %)
| 24.13 | 23.74 | 23.65 | 23.65 | 24.11 | 24.11 | 19.97 | 19.97 | 23.7 | 19.78 | 22.91 | 20.420000000000002 | 23.24 | 23.24 | 23.12 | 23.12 | 24.94 | 24.94 | 20.65 | 20.65 | 22.44 | 22.44 | 20.97 | 20.97 | 25.07 | 25.07 | 24.38 | 24.38 | 24.27 | 24.27 | 24.77 | 24.77 | 25.71 | 25.71 | 24.344999999999999 | 24.344999999999999 | 25.92 | 25.92 | 21.88 | 25.26 | 25.26 | 26.38 | 25.907499999999999 | 25.907499999999999 | 24.582500000000003 | 24.582500000000003 | 23.6175 | 23.6175 | 25.887499999999999 | 25.192499999999999 | 25.192499999999999
Tc Sides Removed | 13.2893 | 12.8703 | 14.2862 | 13.949 | 13.9134 | 13.5069 | 6.6534 | 5.9071 | 12.3426 | 5.6536 | 10.8696 | 5.995 | 12.1092 | 10.9938 | 13.735 | 13.4659 | 14.6861 | 15.2569 | 7.2103 | 6.1923 | 10.9491 | 8.0878 | 10.1163 | 7.9644 | 13.9329 | 13.997 | 13.9405 | 13.8652 | 13.7012 | 13.7123 | 14.0161 | 13.9936 | 14.5972 | 15.2572 | 13.438 | 13.7523 | 14.6961 | 14.8241 | 15.0005 | 14.2396 | 14.3938 | 15.37 | 14.8495 | 15.1536 | 13.0037 | 13.0161 | 10.3253 | 11.1145 | 14.7392 | 13.5379 | 14.198
[6] A. Godeke. Supercond. Sci. Technol., 19 (2006)
[7] G. De Marzi et al. J. Phys.: Condens. Matter 25 (2013)
Godeke Trend [6]
Superconducting Performance
Chart: Positive Pulse (V)
| 50 | 100
7.0e-4 mbar - annealed | -0.712 | -0.8862
2.5e-2 mbar | -1.5456 | -1.3632 | -1.5963
low temp | -0.7817
7.0e-4 mbar - unannealed | -1.1237 | -1.3987
Compressive residual stress

## Slide 10
Superconducting Performance
QPR Coating for RF measurements
  Targeting High Tc
Ta Coating
Nb3Sn Coating
Ta Coating:
P = 1.0.10-3mbar
No heating
PP = 50V
Nb3Sn Coating:
P = 2.5.10-2 mbar
Ts = 750°C
PP = 35 V
No anneal

## Slide 11: Summary and Future Work
A15 phase deposited
  Sn % within required stoichiometric range
  Encouraging 15.4 K Tc soft limit
Surface Cu contamination
  Lower coating temperature
  Interlayer optimisation
Minimisation of residual stress
  Film thickness optimisation
  Post coating annealing
Deposition of further QPR samples

## Slide 12: Thank you for your attention!

## Slide 13
Extra Slides

## Slide 14: Thermal expansion Coefficients
Element | α (x 10-6) K-1
Cu | 16.8
Ta | 7.64
Nb | 7.02
Nb3Sn | 6.3

## Slide 15: SIMS Results

## Slide 16
DCMS
HiPIMS
700 MHz b=0.65 Single Cell Cavity profile