## Slide 1: The Ell Cavities program at CERN: Atomic layer deposition
Thomas Proslier, Yasmine Kalboussi
FCC Week 2022
31th of May 2022

## Slide 2: Contents
Atomic Layer deposition
Secondary electron yield
Multilayers
Perspectives

## Slide 3: Atomic Layer Deposition
Al2O3 = TMA(Al(CH3)3) + H2O
Thin films (≤ 1 µm) synthesis technique based on self-limiting surface chemical reactions. Sequential injection of vapor phase precursors . Layer by layer growth. Cycles.
Advantages:
Thickness and composition control down to the atomic level.
Pin-hole free films.
Excellent conformality on complex-shaped and large area substrates.
Large palette of materials.
Low temperatures (RT-450°C)
Limits:
Slow deposition (0.3 to 10 Å/min).
New materials require new chemistry.
Applications:
Micro-electronic, Photovoltaic, Catalysis, Batteries, Detectors…
Electronique flexible

## Slide 4: Atomic Layer Deposition – Materials

## Slide 5: Secondary electron yield – Mitigate Multipacting
Control thickness and chemical composition – uniformity
Tune SEY and electrical conductivity
Wide variety of substrates (Nb, Cu…)
TiN on Al2O3 (10 nm)
λ = 12 cy = 0.45 nm
Other dep. ~ 10 nm
CEA-ONERA
SEY MAX
R [Ω]

## Slide 6: Multilayers – increase SRF cavities performances (Q and Emax)
Motivation: NbTiN has good superconducting performance (Tc = 17 K)
AlN as an insulating layer.
Chemistry: Combination of TiN and NbN cycles:
n (TiCl4 + NH3) + m (NbCl5 +NH3) = Nb1-xTixN
Tune chemical composition
Good superconducting properties
Compatible with SRF cavities treatments
All conditions are met to apply/test this theory on SRF cavities.
Superconducting alloys – NbTiN/AlN

## Slide 7: From coupons to Cavities…
B
Before
After
Optimized deposition parameters on RF cavities.
Homogeneous deposition (thickness, Tc and structure) over 1,3 GHz Nb and Cu test cavity.

## Slide 8: Cavity dedicated ALD apparatus
High vacuum oven:
- 650°C – 10-6 mbar / 900°C 1bar N2
- Volume retort: Φ = 49 cm, L= 110 cm
(Cavities sizes > 0.6 GHz)
ALD system:
- 9 precursor lines (2 gases, 2 liquids, 4 solids, 1 Ultra high temp.).
- RGA synthesis monitoring.
Interface and control:
- Labview program of ALD system and Oven.
- Automatic synthesis parameter
control and monitoring.
Status:
Deposition tests on samples
Future: Deposition on cavities
49 cm
retort
Program interface
ALD system

## Slide 9: Conclusion-Perspectives:
  SEY: ALD of TiN film is promising to reduce multipacting inside RF cavities.
  Growth of NbTiN and the multilayers AlN/NbTiN by ALD with good superconducting properties, homogeneous composition and thickness control over large surface areas (RF cavities).
  Control doping and surface engineering -> no post treatment chemistry.
  Future Goals :
  SEY: Test the Al2O3-TiN structure on Niobium RF cavities.
  Multilayer: Test the NbTiN-AlN structure on Niobium RF cavities.
  Doping: Test ALD doping procedure on SRF cavityies
  New directions:
  - ALD on Copper complementary to HIPIMS: insulating barrier - Nucleation and thermo- currents.
  - ALD for detectors/optics.

## Slide 10: Thank you for your attention
Questions ?
Acknowledgements
Yasmine Kalboussi1, Baptiste Delatte1, Claire Antoine1, David Longuevergne2, Diana Dragoe3, Jocelyne Leroy4, Sandrine Tusseau-Nenez5, Aurélie Gentils2, Stéphanie Jublot Leclerc2, Fréderic Miserque6, Mohamed Belhaj7, Junling Zheng8, David Hrabovsky9, G. Rosaz10, Thomas Proslier1.
1IRFU, CEA Saclay, 91191 Gif-sur-Yvette Cedex, France ; 2 Université Paris-Saclay, CNRS/IN2P3, IJCLab, 91405 Orsay, France ; 3 Plateforme ICMMO, Rue du doyen Georges Poitou, Bât 410 ,91400 Orsay France ; 4 Laboratoire d’Innovation en Chimie des Surfaces et Nanosciences, 91191 Gif sur Yvette, Cedex, France ; 5 Plateforme de Diffraction des Rayons X, Ecole Polytechnique, Route de Saclay, 91128 Palaiseau. 6 DEN, Service de la Corrosion et du Comportement des Matériaux dans leur Environnement (SCCME), CEA Saclay, 91191 Gif-sur-Yvette Cedex, France, 7 Physics instrumentation environnement space department, coupling of spacecraft and environnement unit, ONERA. 8 Institut des nanosciences de Paris, UPMC, Jussieu 75005 Paris, 9 Université Pierre et Marie Curie, Jussieu 75005 Paris. 10 CERN, Geneva, Switzerland.