## Slide 1: Characterization of the random electrode sectorization in the GEM-foils
M. Bianco1, F. Fallavollita1, R. De Oliveira1, L. F. Ramirez Garcia2, N. Rosi3
1CERN - European Organization for Nuclear Research, Espl. des Particules 1, 1211 Geneva, Switzerland
2Department of Physics, University of Pavia and INFN Pavia, Via Bassi 6, 27100 Pavia, Italy
3Institute of Physics, University of Antioquia, Calle 67 No. 53, 108 Medellín, Colombia
RD51 collaboration meeting

## Slide 2: THE ME0 STATION POSES A TECHNOLOGICAL CHALLENGE FOR THE TRIPLE-GEM TECHNOLOGY
we have evaluated the rate capability of triple-GEM detectors designed for covering large areas and found it inadequate for the high-flux environment of the ME0 station in the CMS experiment [1], [2], [3]
the rate capability of large-area triple-GEM detector is limited by the presence of resistive protection circuits and lowers at increasing
total irradiated detector area
the original gas gain of the detector can be restored through an electrode-by-electrode voltage compensation
in the original design of the ME0 detector at CMS, the triple-GEM detectors would be subjected under irradiation to a gain drop higher than 40%, with a sector-by-sector gain disuniformity of 50%
Segmentation of ME0 foils along transversal direction to beam line (inherited from GE1/1 and GE2/1) as a discharge mitigation strategy
Each GEM electrode is divided in 29 sectors of 100 cm2 surface, all powered independently
Simulated background particle flux in each ME0 detector under irradiation in CMS
Simulated background particle rate per sector in each ME0 detector
1 order of magnitude rate difference
between high-η and low-η sectors: high
gain drop, > 50% gain disuniformity

## Slide 3
Simulated background rate and gain drop in ME0 detector with azimuthal segmentation
adopting an azimuthal segmentation with respect to the LHC beam line is expected to reduce the gain loss and its disuniformity, minimizing the need for a gain compensation[1],[2],[3]
(almost) radially symmetric: high gain uniformity
gain drop can be minimized by increasing number of sectors
simulation-agnostic: independent from knowledge of bkg. flux
Changing in prospective: a rotation in sectorization

## Slide 4
Limits of traditional blank electrode sectorization
However, from a manufacturing technique point of view …
The azimuthal segmentation will require fine precision in photolithographic mask alignment for sector (insulating) gaps
As the holes pattern do not match the ME0 trapezoidal shape and each sector will have slightly different inclination with respect to the vertical line (+/- 10 deg), holes can fall partially on the segmentation area, this require the removal of the hole, as a consequence the dead area, from the standard 200 µm, could rise up to about 600 m, with effects on the detector performances
Proposed solution: resume quite old idea of Sauli, Rui and R&D51 [4], [5], [6] team, random electrode sectorization, i.e. a random alignment between the hole pattern and the sector gap, such idea was also recently resumed by the R&D51 team [7]
such alternative design is a promising solution in terms of manufacturing of large area foils, as this technique does not require a precise alignment of the sector gap with the hole pattern (see next slides)
Up to 600 µm

## Slide 5
Limits of traditional blank electrode sectorization
~ 600 µm

## Slide 6: Random segmentation idea
microscope pictures of blank strip pattern[7]
microscope pictures of random strip pattern[7]
purpose of the electrode sectorization: protect the sectors from the effect of the discharge on the other sectors by reducing the energy of each discharge
electrode sectorization is typically manufactured by introducing an insulating region without GEM-holes between two adjacent electrode sectors
traditional electrode sectorization results in a distortion of the electric field and
consequently a potential degradation of the detection efficiency in the sector gap
to recover the potential efficiency loss at the sector gaps, we have resumed the alternative design concept of the ”random electrode sectorization”
introduced by Sauli about two decades ago, the idea was definitively abandoned
due to the very local copper delamination in the vicinity of the insulating gap
the design foresees a unique surface covered by GEM-holes, while the electrode
sectorization is preserved by removing the copper layer along a strip
the electrode sectorization is manufactured with a random alignment between the
hole pattern and the sector gap
possibility to have holes also in the insulating gap and rims only partially covered by
copper for the holes in the vicinity of the insulating region between adjacent sectors
this layout could result in some electric field lines passing through the holes in the
sector gap, by allowing some electrons to undergo multiplication process
recent studies on random electrode segmentation:
F.M. Brunbauer, “Minimizing distortions with sectored GEM electrodes[7]”

## Slide 7: Detector prototype configuration
microscope pictures of the random electrode sectorization
Triple-GEM detector prototype
active area: 10 cm × 20 cm
gas configuration: 3/1/2/1 mm
double-sided random segmented GEM-foils
single-mask photolithography technique
200 µm width copper free gaps produced at an angle
of ~ 100 µm w.r.t. the hole pattern
1MΩ prot. resist. on top, 100kΩ prot. resist. on bottom
operating gas mixture: Ar/CO2 (70/30) - 5 l/h
double-sided random segmented GEM-foils
top - side
bottom - side
optical inspection results:
optical inspection by backlight → good
holes uniformity → good
holes diameter → good
copper rings diameter: ØCu ~ 74 µm
(required specs 70±5 µm)
polyimide rings diameter: ØPI ~ 53 µm
(required specs 50±5 µm)
20 cm
10 cm
HV sector 1
HV sector 2
HV sector 3
HV sector 4
RO sector
gas
outlet
gas
inlet
high voltage distribution
200 µm

## Slide 8: double-sided random segmented GEM-foils
GEM-foil specs
active area: 200 cm2
double-sided random segmented GEM-foils
single-mask photolithography technique
(CERN PCB Workshop – Rui’s Lab.)
200 µm width copper free gaps produced at an angle of inclination of ~ 100 µm w.r.t. the hole pattern
Hypothesis to be verified:
Hp1: possible copper delamination risk in the vicinity of
the insulating region between adjacent sectors
Hp2: minimize the electric field distortion and recover
the potential efficiency loss at the sector gaps
zoom view
200 µm

## Slide 9: Detector prototype assembly
step 4: installation of the 3mm insternal frame + drift cathode
step 5: connectivity + leakage current test with megger
step 6: installation of the external frames with the O-rings
step 7: installation of the external Kapton window
step 3: installation of the 1mm internal frame + GEM1 foil
step 2: installation of the 2mm internal frame + GEM2 foil
step 1: installation of the 1mm internal frame + GEM3 foil
major assembly steps of the 10 cm × 20 cm detector prototype in clean room

## Slide 10: GEM foils Leakage Current Test in N2
Leakage current test aims to determine the quality of a GEM-foil by measuring the maximum leakage current flowing on the surface of the GEM-holes
When a voltage is applied across the GEM-foil, a current flows from its top to bottom due to the surface conductivity of the Kapton which is known as leakage current
The leakage current flowing through the polyimide of the GEM foil could be affected by the presence of impurities or defects in the holes
moreover, in the random segmentation case, some holes will be partially surrounded by the copper layer, which could adverse effect on the stability of the GEM-foils
The quality of the GEM foils is assessed by monitoring the leakage current and the possible presence of discharges using the NDT1471H Caen Power Supply (50 pA resolution)
The test is performed during 12 hr in pure N2 at 600 V; the maximum accepted values are: 3 nA of leakage and a total number of trips of the HV board lower then 3
GEM1 foil
GEM2 foil
GEM3 foil
zoom view
discharges
discharges
discharges
discharges
leakage current
~ 0.36 ± 0.09 nA
leakage current
~ 0.45 ± 0.10 nA
leakage current
~ 0.42 ± 0.10 nA
No difference is noticed when compared with the results of foils with traditional blank sectorization[8]

## Slide 11: Quality Control and testing
example of standard QA/QC on the detector prototype
High Voltage and Linearity Test in pure N2
high voltage and linearity test aims to determine the current voltage curve in order to identify possible malfunctions, defects in the HV circuit and intrinsic noise rate
high voltage test includes the operating of the chamber at HV values leading to electric current values exceeding 40% the nominal ones as required by a final experiment
NO trips of the power supply or disruptive events were recorded
Measurement of the Effective Gas Gain in Ar/CO2 (70/30)
effective gas gain for the prototype with random electrode sectoritation comparable to the gas gain measured in other triple-GEM detector with standard sectoritazion
effective gas gain in Ar/CO2 (70/30) of about 2×104 at 680 µA
of equivalent divider current (i.e. drift voltage 3.2 kV)
Energy Spectrum in Ar/CO2 (70/30)
typically energy spectrum of 55Fe source: clean separation of the main photopeak and the Ar-escape peak is achieved
energy resolution in Ar/CO2 (70/30):
the detector successfully passed all standard quality controls

## Slide 12: Detector response in the case of short circuit
High Voltage Stability in Ar/CO2 (70/30)
when one sector of the GEM-foils is in short-circuit, the current flowing through the top and bottom side of the foil increases
a short circuit is introduced in the sector 2 of GEM1 (or GEM2, or GEM3). Considering the protection resistors, 1 MΩ (top) + 100 kΩ(bot), and the applied voltage (~375 V), the expected current is ~340 µA for the sector in short-circuit
the current flowing through the other sectors and foils is proved to be stable despite a short-circuit in one of the sectors of the detector prototype
No abnormal leakage current or discharges were detected
during several hours of measurement
the test confirms that the double-sided random segmented foils is stable even under short-circuit in one of the sectors
sector 1
sector 2
sector 3
sector 4
zoom view
short circuit on GEM2
short circuit on GEM3
short circuit on GEM1

## Slide 13: Detector response in the case of short circuit
High Voltage Stability in Ar/CO2 (70/30)
when one sector of the GEM-foils is in short-circuit, the current flowing through the top and bottom side of the foil increases
a short circuit is introduced in the sector 2 of GEM1 (or GEM2, or GEM3). Considering the protection resistors, 1 MΩ (top) + 100 kΩ(bot), and the applied voltage (~375 V), the expected current is ~340 µA for the sector in short-circuit
the current flowing through the other sectors and foils is proved to be stable. No abnormal leakage current or discharges were detected during several hours of measurement
Energy Spectrum in Ar/CO2 (70/30)
the energy spectra measured after positioning a 55Fe source over a sectors adjacent (e.g. sector 3) to the short-circuited one are not affected by the presence of the short
sector 1
sector 2
sector 3
sector 4
55Fe source
short circuit on GEM2
short circuit on all stack
zoom view

## Slide 14: GAS GAIN Uniformity
stepper motors and collimated 5.9 keV 55Fe source (~ 2 mm2) used to scan the 10 cm × 20 cm area at a 3 mm (x-coord.) × 4 mm (y-coord.) grid (~ 2000 «pixels» of equal area)
linear stepper XY positioning stage uses a stepper motor with 50 µm resolution for the x-coord. and a stepper motor with 1 mm resolution for the y-coord.
automated testing system based on Raspberry Pi & LabView controller
for each pixel, sum-up signals from four associated readout connectors have been recorded to compute the effective gas gain and energy spectra
LabVIEW-software interface for the KEITHLEY 6487 picoammeters
to control and monitor the anode current
Raspberry Pi microcontroller
stepper motor
(50 µm resolution)
stepper motor
(1 mm resolution)
source collimator
55Fe source

## Slide 15: GAS GAIN Uniformity
Gas gain map of the triple-GEM detector. Collimated 5.9 keV 55Fe source (~ 2 mm2) used to scan the 10 cm × 20 cm area at a 3 mm (x-coord.) × 4 mm (y-coord.) grid
Projected relative gain for random holes pattern in the sectorized GEM
drop in the gain intensity (~ 30%) is observed at the sector gap
source collimator
3 mm - thick copper collimator with
1.5 mm hole diameter
15 mm
15 mm
Ø ~1.5 mm

## Slide 16: GAS GAIN Uniformity
residual
P/T flactuation
drop in the gain intensity (~ 30%) is observed at the sector gap
projected relative gain for random holes pattern in the sectorized GEM
scan duration: ~ 72 hours of data-taking
gas gain varies with ambient conditions
correcting triple-GEM chamber for temperature and pressure[8]:
percentage variation (i.e. gas gain drop):
fitting model:
Lorentzian + polynomial
Gas gain map of the triple-GEM detector. Collimated 5.9 keV 55Fe source (~ 2 mm2) used to scan the 2 cm × 2 cm area at a 50 µm (x-coord.) × 2 mm (y-coord.) grid
source collimator
6 mm - thick copper collimator with
1.5 mm hole diameter
15 mm
15 mm
Ø ~1.5 mm

## Slide 17: GAS GAIN Uniformity
Gas gain map of the triple-GEM detector. Collimated 5.9 keV 55Fe source (~ 1 mm2) used to scan the 2 cm × 2 cm area at a 50 µm (x-coord.) × 3 mm (y-coord.) grid
projected relative gain for random holes pattern in the sectorized GEM
drop in the gain intensity (~ 33%) is observed at the sector gap
residual
P/T flactuation
source collimator
6 mm - thick copper collimator with
1 mm hole diameter
15 mm
15 mm
Ø ~1 mm
scan duration: ~ 72 hours of data-taking
gas gain varies with ambient conditions
correcting triple-GEM chamber for temperature and pressure[8]:
percentage variation (i.e. gas gain drop):
fitting model:
Lorentzian + polynomial

## Slide 18: Future plan
repeat the measurement of the gas gain uniformity on the double-sided segmented GEM-foils with traditional black electrode sectorization and compare the results with the random sectorization
quantify the effect in reducing distortions and partially restoring the gas gain in the vicinity of the
insulating region between adjacent sectors
improve the measurement of the gas gain uniformity in order to better quantify the gas gain drop in the vicinity of the insulating region between adjacent sectors
it could be affected by the smearing of the source cone
it could be affected by the reciprocal misalignment of the foils within the GEM-stack
repeat the quality control and testing on double-sided random segmented GEM-foils based on the double-mask photolithography technique
considering Rui's experience on random hole pattern: foil production with double-mask technique has
high delamination risk in the vicinity of the insulating region between adjacent sectors
repeat the quality control and testing on large-size, O(~ 3000 cm2), double-sided random segmented GEM-foils area (consistent with a real experiment)

## Slide 19: Conclusion
random electrode segmentation is an alternative design concept, which could minimize the electric field distortion and recover the potential efficiency loss at the sector gaps
some electric field lines passing through the holes in the insulating region will allow some electrons to
follow their initial trajectories and undergo multiplication process
such alternative design is a promising solution also in terms of manufacturing of large-area foils
this technique does not require a precise alignment of the sector gap with the hole pattern
manufacturing technology used for the production of GEM-foils is now sufficiently mature to be able to
implement the random electrode segmentation on large-size GEM-foils
the recent R&D phase currently ongoing on a triple-GEM detector prototype demonstrated the high quality and stability of the GEM-foil manufacturing with random electrode sectorization
although the random segmentation case results in some holes which are partially surrounded by the
copper layer, no adverse effect on the operation and stability of the GEM-foils was observed
an intense testing campaign (laboratory characterization and test-beam) is currently underway to study the response of the detector in the vicinity of the insulating region between adjacent sectors

## Slide 20: bibliography
[1] F. Fallavollita, ‘High-rate capability studies of triple-GEM detectors for the ME0 upgrade of the CMS muon spectrometer’. Proceedings of the iWoRiD2021: 22nd International Workshop on Radiation Imaging Detectors,
27 June - 1 July 2021, Virtual (Belgium) Conference Proceeding submitted to Proceeding Section of Journal of Instrumentation (JINST).
[2] A. Pellecchia, 2021 IEEE NUCLEAR SCIENCE SYMPOSIUM AND MEDICAL IMAGING CONFERENCE. Talk: ‘Rate capability of large-area triple-GEM detectors and new foil design for the innermost station, ME0, of the CMS endcap muon system’, 16 October – 23 October 2021, Virtual.
[3] F. G. Ramirez, PSD12: 12th International Conference on Position Sensitive Detectors. Talk: ‘High-rate capability studies of triple-GEM detectors for the ME0 upgrade of the CMS muon spectrometer’. 12 Sept. - 17 Sept. 2021, University of Birmingham, Birmingham (United Kingdom)
[4] C. Altunbaset al, NIMA 490(2002)177
[5] F. Brunbaueret al, NIMA 875 (2017) 16
[6] https://cds.cern.ch/record/705790 (fig 10.11)
[7] A.P. Marques, F.M. Brunbauer, H. Müller, R. de Oliveira, E. Oliveri, D. Pfeiffer, L. Ropelewski, J. Samarati, F. Sauli, L. Scharenberg, L. Shang, M. van Stenis, S. Williams, Y. Zhou, ‘Minimizing distortions with sectored GEM electrodes’, Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment,Volume 961,2020,163673,ISSN 0168-9002,
https://doi.org/10.1016/j.nima.2020.163673.
[8] F. Fallavollita, ‘Triple-Gas Electron Multiplier technology for future upgrades of the CMS experiment: construction and certification of the CMS GE1/1 detector and longevity studies’, CERN Ph.D. thesis,
CERN-THESIS-2018-349, (2018).

## Slide 21: acknowledge
We would like to thanks the CMS-GEM team for the possibility to join and collect data from beam at H4