## Slide 1
Development of 2D GaN and 3D SiC detectors
Hongwei Liang1, Xin Shi2, Xiaochuan Xia1, Zhenzhong Zhang1
17-11-2021
1 Dalian University of Technology
2 Institute of High Energy Physics Chinese Academy of Sciences

## Slide 2
Outline
Motivation
2D GaN partical detector
3D SiC radiation detector
Prospect

## Slide 3
Advantages of semiconductor radiation detectors
Gas detector
w~30eV
Fano factor (0.2~0.5)
Scintillator detector
w~300eV
Fano factor (~1)
Narrow band gap
semiconductor detector
w~3eV
Fano factor (~0.1)
VS
Energy resolution
Detection efficiency
Pulse rise time
Energy linear range
Integrated
  Small size
  Radiation damage
  High temperature
  Protect from light
  Energy resolution
  Detection efficiency
  Detection efficiency
    Energy resolution
    Carrier collection
Wide bandgap semiconductor based detector
can met the demand

## Slide 4
Table 1: Basic physical parameters of semiconductor materials

## Slide 5
Main research units of GaN-based  particle detectors：
Motivation for the development of 2D(planer) GaN radiation detector
1. The band gap of GaN is 3.4 eV, suggesting excellent high temperature resistance
2. High breakdown field strength, suggesting better carrier collection efficiency
3. Mature process technology, suggesting large-scale integration
4. Industrialized epitaxial growth, suggesting low device cost
High temperature resistance
and radiation resistance

## Slide 6
GaN  particle detector structure:
(a) Double-Schottky contact structure：
(b) Sandwich Structure ( schottky structure)：
J. Vaitkus, W. Cunningham, E. Gaubas, M. Rahman, S. Sakai, K. M. Smith, and T. Wang, Nucl. Instrum. Methods Phys. Res., Sect. A 509(1–3), 60–64 (2003).
P. Mulligan, J. H. Wang, and L. Cao, “Evaluation of freestanding GaN as an alpha and neutron detector,” Nucl. Instrum. Methods Phys. Res. A, vol. 719, pp. 13-16, Apr. 2013.
Q. Xu, P. Mulligan, J. H. Wang, W. Chuirazzi, and L. Cao, “Bulk GaN alpha-particle detector with large depletion region and improved energy resolution,” Nucl. Instrum. Methods Phys. Res. A, vol. 849, pp. 11-15, Dec. 2016.
Z. F. Zhu, H. Q. Zhang, H. W. Liang, B. Tang, X. C. Peng, and J. X. Liu et al., “High-temperature performance of gallium-nitride-based pin alpha-particle detectors grown on sapphire substrates,” Nucl. Instrum. Methods Phys. Res. A, vol. 893, pp. 39–42, Mar. 2018.
(c) p-i-n structure
Lower leakage current noise

## Slide 7
The main problems in the development of Mesa pin detectors
Sapphire Substrate
Buffer layer
GaN sensitive area
The mismatch between GaN and sapphire reaches16%
High dislocation density
High background carrier concentration
Thick films
Leakage mechanism

## Slide 8
SIMS Results
Sample A: undoped i-GaN
Sample B: Al-doped i-GaN
Al concentration：0.214%
AlxGa1-xN
AlxGa1-xN tends to grow
J. H. Lee, and J. H. Lee, J. Appl. Phys., vol. 105, p. 064508, Mar. 2009.
 | Si | O | C
Ga | (12-17 meV) donor | (30-33 meV) donor | (200 meV) donor
N | —— | —— | (900 meV) acceptor
CN
[Si]≈[C], Nd=[Si]+[O]-[C]
≈1016 cm-3
The role of Si, O, C impurities in different positions in the GaN lattice：
[Si]<[C], Nd≠[Si]+[O]-[C]
<[Si] or [C], 1014 cm-3
CN
CN and CGa
Self-compensation
Our solution: Aluminum Isoelectronic doping technique
Decrease in electron concentration
Epitaxial layer structure
SIMS Results
CGa to CN transitions
PL
test

## Slide 9
Clean
DepositionSiO2
Photolithography
Etch SiO2
Lift off
ICP
Etch steps
TMAH
Deposition SiO2
Photolithography
Etch
Annealing
Metal deposition
Lift off
Process flow

## Slide 10
Dead zone includes: 1mm Air、Ni/Au electrode and p-GaN
p-GaN
i-GaN
n-GaN
buffer layer
Sapphire substrate
Ni/Au
Ti/Al/Ni/Au
αPartical
Schematic diagram of particle irradiation detection system
（239Pu+241Am）
Spectra acquired by detector
at varied Vr from 0 to -50 V
FWHM and peak centroid datas
for detector with the varied Vr
CCE datas of detector
under different Vr.
Resolution comparisons with
GaN alpha-particle detectors

## Slide 11
3D-SiC simulation – time resolution：
Motivation for the development of 3D SiC radiation detector
1. Wide band gap (3.2 eV), High breakdown field strength, Mature process technology
2. Narrow electrode spacing – good time resolution and charge collection
3. Good singlecrystal quality – Thick thickness – larger charge collection and signal
4. More radiation resistant than 2D SiC
SiC structure. Electrode radius 5,
electrode spacing 40and 100thick
Drift path: blue electrons and red holes in Fig.a
Electric field xy plane at z=50 in Fig.b
Device structure
Detector scan: 10000 events. Step: 1X1
Fig.a: Time resolution is 38 ps at 350V with electrode spacing 20
Fig.b: Time resolution vs voltage
TOA[ns]
Vertical incidence
Device performance

## Slide 12
Method of making 3D structure
1. ICP etching (Inductive Coupled Plasma Emission Spectrometer Etch)
2. Chemical or electrochemical etching
3. Laser drilling
Auger drilling Pulse drilling
Advantage of laser drilling technology
1. Suitable for a variety of materials
2. Few steps and parameters
3. Short process time
Giulio Pellegrini and P. Roy et al., “Technology development of 3D detectors for high-energy physics and imaging” Nuclear Instruments and Methods in Physics Research A 487 (2002) 19–26.
Byunggi Kim and Ryoichi Iida et al., “Mechanism of nanosecond laser drilling process of 4H-SiC for through substrate vias” Appl. Phys. A (2017) 123:392.
Lukang Wang and You Zhao et al., “Design and Fabrication of Bulk Micromachined 4H-SiC Piezoresistive Pressure Chips Based on Femtosecond Laser Technology” Micromachines 2021, 12, 56.

## Slide 13
Process flow of making 3D SiC structure
Diameter of the cylinder at the top and bottom of the sample
Hole | Diameter（μm）
Entrance | 103
Exit | 81
Exit hole
Entrance hole
SEM image
Semi-insulating SiC single crystal
350 μm thickness
Image of the filled metal indium electrode
Cross-sectional image
Device model | FM-UVPM3A
Laser wavelength | 355nm
Processing power | 3W
Pulse Width | 12ps
Processing speed | 100mm/s
Processing time | 30min/pcs

## Slide 14
Electrical characteristics of 3D SiC structure
1
+
2
3
4
5
6
Label the electrode
The test process diagram and electrode number
White LED excitation
Protect from light
I-V curve of the 3D SiC device under dark and light status
 | Voltage(V) | Current(pA) | 
Light | -100 | 139 | 32.55
Dark | -100 | 4.27 | 
 | Voltage(V) | Current(pA) | 
Light | -100 | 139 | 32.55
Dark | -100 | 4.27 | 
Parameters extracted from the IV test
The device exhibits light response characteristics, indicating that radiation detection is possible!

## Slide 15
Prospect
Study the damage caused by laser drilling.
Investigate the effect of contact type on device performance.
Making terminal protection structuure.
Package the device to improve the reliability of the device.
Study radiation detection performance.
Carry out multi-device integration research

## Slide 16
Thanks！