## Slide 1
Soft X-Ray Low Gain Avalanche Detectors with 55 µm pitch for Imaging Applications using the Timepix4 ASIC.
N. Moffat, J. Villegas, S. Hidalgo, G. Pellegrini
The 39th RD50 Workshop
19th November 2021

## Slide 2: Introduction
Why small pixel LGAD’s?
Issue with Small Pixel LGADs
AC-LGAD – Solving the problem of small pixel LGAD’s
P-SPICE Model
TCAD Model
Conclusion

## Slide 3: Why Small Pixel LGAD’s?
Small pixels provide a very good spatial resolution.
We want to benefit from the excellent capabilities of the Timepix3/Timepix4 ASIC.
Synchrotron Applications
  Timepix4 timing bin of 195 ps is well below the typical interbunch spacing of synchrotron electron bunches of a few ns.
  Material Science -to look at the absorption edges of transition metals, important for magnetic domain studies in the context of storage media. This would be in the 700 - 900 eV range
  Biological samples studies: LGADs with a charge gain somewhat higher than 20 would be needed to reach the so-called “water window”, between the Carbon and Oxygen edges (282 eV to 533 eV – Carbon and Oxygen being present in all biological samples).
  For all these studies, at photon energies below 1 keV the insensitive layer at the photon entrance side of the LGAD must be minimized.
High energy Physics
  LHCb –Velopix
Medical Physics
  Analysing biopsy's –typically thin, more information gathered by using “soft” Xrays

## Slide 4: LGAD Basic Structure
Impact ionisation region
Electrons traveling at their saturation velocity (good for signal uniformity)

## Slide 5: Small Pixel Problem
https://doi.org/10.1016/j.nima.2021.165746

## Slide 6: AC-LGAD Basics
AC-LGAD replaces the segmentation of the pad implants into continuous sheets of multiplication layer and n+ layer and only segments the metal connected to the readout
The signal is AC-coupled into the metal pads by another continuous sheet of coupling oxide.

## Slide 7: P-SPICE Model

## Slide 8: PSPICE Model
Timepix3 LGAD Standard values | 
w(μm) | 32
p(μm) | 55
g=w-p(μm) | 23
d(μm) | 50
25 square pixels
256x256 square pixels
d
w
g

## Slide 9: The injected pulse

## Slide 10: PSPICE - Resistances
i
A
Ri=ρL/A=(ρ/tn)g/w=RS(g/w)
Rdiag=√2Ri
g
g
√2g
g

## Slide 11: PSPICE - Capacitances
Cdet=ϵsw/d Cox=ϵoxw/tox
Cs=[0.23(d/w)0.75/(g/d+0.18)-0.07d/w]Cd
Cdiag=(0.1)w/d[1-1.15(g/w)(7/(g/d+3)-1]Cd
A.Cerdeira, IEEE Transactions on Nuclear Science 44(1): 63-66, 1997

## Slide 12: PSPICE - Noise
Pspice calculates the noise spectral distribution in every part of the circuit due to all contributions of the entire device
Flicker noise
Shot noise
Thermal noise
v2(f)
[v2]=V2/Hz

## Slide 13: PSPICE - Noise
v2(f)
[v2]=V2/Hz
N=VRMS=√(∫BWv2(f)df)=√(∑Nv2(f)Δf)
BW=1GHz; Δf=1MHz;N=1000

## Slide 14: PSPICE - Signal
H=Vmax
Jitter : σjitter (g(w),tox,Rs) ≈ Tr/(S/N)  To be minimized
Signal Height to noise ratio S/N=H/N(g(w), tox,Rs)
N=VRMS=√(∫BWv2(f)df)=√(∑Nv2(f)Δf)
RiseTime : Tr=T(V=90%H)-T(V=10%H)

## Slide 15: PSPICE – Some Results
TCAD:
Decreasing oxide thickness tox improves S/N.
Decreasing pad size w (increasing interpixel gap=p-w) improves S/N.
Rs=696Ω
d=50um
woptimal≈27.5um
wstandard=32um

## Slide 16: PSPICE – Some Results
TCAD:
Increasing sheet resistance Rs improves S/N.
Decreasing pad size w (increasing interpixel gap=p-w) improves S/N.
tox=75nm
d=50um
woptimal≈27.5um
wstandard=32um

## Slide 17
Neighboring pixels  General trend of H(w) (tox=75nm and Rs=696Ω)

## Slide 18: PSPICE preliminary Results
Increasing sheet resistance Rs improves S/N.
Decreasing oxide thickness tox improves S/N.
PSPICE model optimised to reduce charge sharing between pixels.

## Slide 19: TCAD Model

## Slide 20: AC-LGAD structure for TCAD.
55um Pitch Pixels
Pixel size of 27.5um
5 pixels.
High resistive N+ Implant.
Implant doping profiles generated in sprocess.
Distance from edge of the device [um]
Depth [um]
JTE
5 Pixels

## Slide 21: Doping Profiles
Low resistive implant – Lower doping concentration of junction implant.
Doping profiles generated using an analytical function with SDE

## Slide 22: Efield at 180V of AC-LGAD
Distance from edge of the device [um]
Depth [um]
High field seen at the junction –Multiplication
Bulk does not deplete as expected.
Depletion region extends into the bulk only in the region below the N++ region.
Bulk does not deplete below the multiplication region
N++ Resisitive implant too resisitive
Multiplication Region
HV contact

## Slide 23: Efield Across device at a depth of 25um at 180V.
JTE
Bulk un-depleted

## Slide 24: TCAD Results – Waveforms – 80nm Oxide
Rs=696Ω
Pitch=55um

## Slide 25: TCAD Results – Peak at each channel as a function of injection position – 80nm Oxide
Rs=696Ω
Pitch=55um

## Slide 26: Doping Profiles - Irradiated
PowerPoint Presentation (cern.ch)
AIDA Deliverable (cern.ch)
Microsoft PowerPoint - 2017Mandurrino_30thRD50.pptx (cern.ch)
Radiation Model based on the AIDA deliverable for Radiation models and the RD50 talk given by Marco Mandurrino

## Slide 27: Efield Across device at a depth of 25um
Increasing Fluence
JTE
Bulk un-depleted

## Slide 28: TCAD Results – Peak at each channel as a function of injection position – 80nm Oxide – 1e14
Rs=696Ω
Pitch=55um
Collection is not symmetric- due to slope in the electric field

## Slide 29: TCAD Results – Peak at each channel as a function of injection position – 80nm Oxide – 1e15
Rs=696Ω
Pitch=55um
Collection is symmetric- due to slope in the electric field

## Slide 30: Gain of Irradiated AC-LGAD
Not Radiation Hard

## Slide 31: Main Points to Takeaway from TCAD
Design not Radiation Hard
  Implement deep multiplication junction, higher dose boron.
Detector does not deplete
  Modify high resistive (n+) implant, i.e less resistive.
At high fluence, the AC-LGAD works well, we see a uniform charge collection at the neighbouring pixels.
Not much charge is shared between neighbouring pixels. Good for HEP?

## Slide 32: Conclusion
Look at adapting profiles to make them more radiation hard –deep junction.
Junction implant may be to high resistivity, need to study the effect of reducing this resistivity.
The effect of the oxide thickness was also studied but the same effect was seen, this will be optimized after the Resistance is changed.
PSPICE modelled developed to optimize AC-LGAD to reduce charge sharing between pixels.
Can also model the detector to optimize for charge sharing ( Good for position resolution)
Next steps to optimize design for Soft-Xrays

## Slide 33
Thanks for your attention!
Acknowledgements
This work has been financed by the Spanish Ministry of Science and Innovation (MCIN/AEI/10.13039/501100011033/)
Project references: SPID202000X118404SV1