1Helsinki Institute of Physics and Department of Physics, University of Helsinki, Finland
2Institute of Technology, University of Tartu, Estonia
Jyri Kimari1, Ye Wang2, Andreas Kyritsakis2, Ekaterina Baibuz1, Veronika Zadin2, Flyura Djurabekova1
Field enhancer sharpening mechanism
via biased surface diffusion
Theory: electric field gradient biases diffusion
Breakdown mechanism on Cu surface.
Sharpening of initial protrusions lead to runaway?
- -
- -
%DELTA E_{ nitalic m } prop font fixed M %gamma + font fixed A %gamma F
Molecular dynamics simulations with E field
Result: Diffusion bias agrees with theory & DFT
Surface	M (eÅ)		A (eÅ2/V)
	MD	DFT	MD	DFT
Cu {100}	2 ± 1	0.106 ± 0.003	0.0 ± 0.5	0.27 ± 0.02
Cu {110}	0.7 ± 0.1	0.094 ± 0.006	0.24 ± 0.08	0.30 ± 0.04
Cu {111}	0.61 ± 0.06	0.162 ± 0.003	0.27 ± 0.05	0.23 ± 0.02
Field enhancers
facet and sharpen
MD coupled with finite elements method Laplace equation solver
-

---
1Helsinki Institute of Physics and Department of Physics, University of Helsinki, Finland
2Institute of Technology, University of Tartu, Estonia
Jyri Kimari1, Ye Wang2, Andreas Kyritsakis2, Ekaterina Baibuz1, Veronika Zadin2, Flyura Djurabekova1
Field enhancer sharpening mechanism
via biased surface diffusion
Breakdown mechanism on Cu surface.
Sharpening of initial protrusions lead to runaway?
A. Kyritsakis et al. Journal of
Physics D: Applied Physics
51.22 (2018):225203.
Theory
Results
Timko, Helga, et al. Contributions to Plasma Physics 55.4 (2015): 299-314.
e-
e-
e-
e-
e-
e-

---
Theory: electric field gradient biases diffusion
Tsong, Kellogg (1975):
electric field gradient perpendicular to surface biases diffusion
- -
- -
Field enhancer
sharpening
Change in migration energy barrier:
dipole moment
polarizability
Simulations
F =	electric field
γ =	electric field gradient
A. Kyritsakis et al. Physical Review B 99.20 (2019): 205418

---
Molecular dynamics simulations with E field
{100} surface
accelerated with
collective variable
hyperdynamics (CVHD)
K. M. Bal and E. C. Neyts.
Journal of chemical theory and
Computation 11.10 (2015):
4545–4554
MD coupled with finite elements method Laplace equation solver
Veske, Mihkel, et al. Journal of Computational Physics 367 (2018): 279-294.
Kimari, Jyri, et al. In preparation.

---
dipole moment
polarizability
F =	electric field,	γ =	electric field gradient
Simulations
Result: Diffusion bias agrees with theory & DFT
“Drift velocity” ~ bias as function of gradient
Cu {110}	0.7 ± 0.1	0.094 ± 0.006	0.24 ± 0.08	0.30 ± 0.04
Cu {111}	0.61 ± 0.06	0.162 ± 0.003	0.27 ± 0.05	0.23 ± 0.02
Field enhancers
facet and sharpen
Electric properties sanity check from DFT