## Slide 1: Coil 101 cross section analysis and feedback for 2nd generation coils
Susana Izquierdo Bermudez
Images from Ana Teresa Perez Fontenla (CERN EN-MME)

## Slide 2: Coil 101: Overview
CERN practice coil
Conductor: Low grade Nb3Sn. RRP 132/169
Reacted three times to optimize oven parameters:
  First full heat treatment
  2nd heat treatment done with short plateaus
  3rd heat treatment done only with first plateau
Longitudinal contraction after winding (release of the winding tension) . ΔlW = 1.5 mm
Longitudinal contraction after heat treatment: ΔlHT = 0.4 mm

## Slide 3: Cable dimensions
 |  | Cable before reaction | Cable after reaction (2.0 % growth in width, 4.5 % growth in thickness) | Δ
Bare width | mm | 18.150 | 18.513 | 0.363
Bare thickness in | mm | 1.438 | 1.505 | 0.067
Bare thickness out | mm | 1.612 | 1.682 | 0.070
Bare mid-thickness | mm | 1.525 | 1.594 | 0.069
Keystone angle |  | 0.550 | 0.550 | 0.000
According to the studied cross section:
4.5 % growth in thickness seems to be a good assumption
2.0 % in width seems to overestimate the growth in width

## Slide 4: Cable growth - width
Turn 9
Turn 30
Turn 44
Turn 22
 |  | Turn 9 | Turn 22 | Turn 30 | Turn 44
Expected growth | % | 2 |  |  | 
Expected growth | µm | 363 |  |  | 
Measured growth | % | 0.26 | 0.28 | 0.02 | 0.35
Measured growth | µ | 47 | 50 | 4 | 64

## Slide 5: Cable dimensions for the 2nd iteration
1st ITERATION CABLE |  | Cable before reaction | Cable after reaction (2.0 % growth in width, 4.5 % growth in thickness) | Δ
Bare width | mm | 18.150 | 18.513 | 0.363
Bare thickness in | mm | 1.438 | 1.505 | 0.067
Bare thickness out | mm | 1.612 | 1.682 | 0.070
Bare mid-thickness | mm | 1.525 | 1.594 | 0.069
Keystone angle |  | 0.550 | 0.550 | 0.000
Based on this analysis, our suggestion for the second iteration cable is:
2nd ITERATION CABLE |  | Cable before reaction | Cable after reaction (1.17 % growth in width, 4.5 % growth in thickness) | Δ
Bare width | mm | 18.150 | 18.363 | 0.213
Bare thickness in | mm | 1.462 | 1.530 | 0.068
Bare thickness out | mm | 1.588 | 1.658 | 0.069
Bare mid-thickness | mm | 1.525 | 1.594 | 0.069
Keystone angle |  | 0.400 | 0.400 | 0.000
Consequence: 150 µm to be compensated radially in the tooling.

## Slide 6: Radial compensation
Outer radius:
150 µm S2 Glass 
2 x 150 = 300 µm S2 Glass
Inter layer:
500 µm S2 Glass
 650 µm S2 Glass
We can compensate for the differences in cable width, keeping the same tooling and coil inner/outer diameters:

## Slide 7: Coil insulation
1
2
# |  | Nominal (µm) | Measured (µm) | Δ (µm)
1 | IL IR pole | 250 | 200 | -50
2 | IL OL pole | 500 | 460 | -40
3 | OL OR pole | 250 | 250 | 0
4 | IL PT | 500 | 445 | -55
5 | OL PT | 500 | 480 | -20
6 | MP IL | 275 | 290 | 15
7 | MP OL | 275 | 260 | -15
8 | IL IR MP | 400 | 900 | 500
9 | IL OL MP | 800 | 930 | 130
10 | OL OR MP | 400 | 350-590 | 
3
4
5
6
7
8
10
9
A
B
C
A
B
C

## Slide 8: Coil – Some observations
We have about 600 µm of “free radial space”, that seems to be taken by the inter-layer insulation in the pole, and by the inner radius in the mid-plane.

## Slide 9
Roxie non-insulated conductors

## Slide 10
Block 1

## Slide 11
Block 2

## Slide 12
Block 3

## Slide 13
Block 4

## Slide 15: Keystone angle
Keystone evaluation
Inner layer, bock 1
(17 conductors):
  -170 µm thin edge
  (-10 µm/cond.)
  +410 µm thick edge
  (+25 µm/cond.)
Outer layer, bock 3
(16 conductors):
  -490 µm thin edge
  (-30 µm/cond.)
  +320 µm thick edge
  (+20 µm/cond.)

## Slide 16: Ends: Return

## Slide 17: Return end: Comparison CERN-ROXIE

## Slide 18: Return end: Comparison CERN-LARP
CERN
CERN
LARP

## Slide 19: Ends: Lead

## Slide 20: Lead End

## Slide 21: Layer jump

## Slide 22: Additional studies…
For the moment, we only looked at one coil cross section:
To have more statistics we will look at:
CERN: coil 101, different cross section
LARP coil

## Slide 23: 2nd Coil Cross Section Assumptions/Considerations/Guidelines
Cable
  Keystone 0.55 0.40
  Growth in width 2.00 %  1.17 %
Cable insulation
  150 µm, with the possibility to go for 145 µm if needed
Coil insulation
  Inter layer thickness 500 µm  650 µm
  Outer radius S2 glass 150 µm  300 µm
Gradient = 130 T/m at 7 TeV
Field quality:
  b6 = 2 units at 6.5 TeV
  Possibility to add/remove 125 µm shim thickness from the mid-plane and pole for fine tuning field quality during production
    Pole insulation:
      OPTION 1: 2x175 µm  4 x 125 µm (pole-turn insulation 375-500-625 µm)
      OPTION 2:2x175 µm  3 x 125 µm (pole-turn insulation 250-375-500 µm)
    Mid-plane shim: 125 µm  250 µm
  The thin edge of the outer layer wedge should not be smaller than the one for the first cross section
  Same concept for the layer jump.

## Slide 24: Additional slides

## Slide 25
Inner layer, pole turn,
turn2pole
Outer layer, pole turn,
turn2pole

## Slide 27
Outer layer,
pole turn,
Turn2outer D
Outer layer,
pole turn,
Turn 2 midplane

## Slide 29
Left side of the cross section has also been studied, but we have a problem in the scale of the image that needs to be cross-checked
Mid-plane alignment
Pole alignment

## Slide 32
Characterization of insulation thickness layers on-going

## Slide 33: Insulation layers
Wedge:
  S2 ??TEX-??? Sleeve 0.125 mm thickness
Coil Inter-Layer:
  2 x S2 66TEX-933
  (250 mm width, 0.250 mm thickness)
Splice box Inter-Layer:
  3? x S2 33TEX–493 (is it supposed to be better for impregnation if it is not reacted?)
  (250 mm width, 0.250 mm thickness)
Pole:
  2 x S2 33TEX–493  66TEX-933?
  (19 mm width, 0.175 mm thickness)
  4 or 5 x S2 33TEX–493  66TEX-933?
  (19 mm width, 0.100 mm thickness)
  4 x S2 33TEX–493  66TEX-933?
  (19 mm width, 0.125 mm thickness)
Interface spacers-conductor:
  1 x S2 33TEX–493  66TEX-933?
  (1925 mm width, 0.175 mm thickness)
933  Thermally stable inorganic sizing
493  Sizing compatible with epoxies or polyesters (slightly darker after reaction)
Additional orders
Can we change?
To be cross-checked

## Slide 34: Coil shimming
Flexibility to add/remove ~ 100 µm shim with no impact on coil compaction
How to do it?
Mid-plane:
  1st Generation: 0.125 mm G11 in the mid-plane
  2nd Generation: 2x0.125 mm G11 in the mid-plane?
Pole: modify insulation layout around the pole
  1st Generation: 2 x 0.175 mm.
  2nd Generation: 3 x 0.125 mm?
    In case we remove one layer, we will have a pole insulation thickness of 0.250 mm. Is it enough?