## Slide 1: Spatial and temporal resolution of FBK RSD2 sensors
N. Cartiglia
UFSD group
Image courtesy of M. Tornago

## Slide 2: TREDI and resistive silicon detectors
Resistive silicon detectors (aka AC-LGAD) were presented at TREDI 2015
At TREDI 2020, we presented the first results on the properties of silicon sensors with resistive read-out
Now, at TREDI 2022, we present the results obtained with the second FBK RSD production, RSD2.
Physicist
gain implant
AC coupling dielectric
Resistive n++ electrode (sheet resistance)
p++ electrode
Electrodes
AC-RSD building blocks:

## Slide 3: Digress: nomenclature
RSD (also AC-LGAD),
==> AC-RSD
FBK RSD1, RSD2 are AC-RSDs
New design: DC – RSD
(see L. Menzio, Thursday afternoon)
LGAD (also UFSD)
p bulk
p++
Gain implant
metal
oxide

## Slide 4: Aide memoire: RSD principle of operation
4
2
1
3
The signal sees several impedances Zi in parallel, and it is split according to Ohm’s law.
Each pad gets a share Si of the total signal, exactly as in a current divider

## Slide 5: FBK RSD1 lessons learnt
Signal sharing
  allows reaching excellent spatial resolutions,
  does not spoil the temporal resolution proper of the LGAD technology.
Hits on the metal generate (mostly) a signal only in that pad
  ==> no signal sharing if the metal pad is large, the resolution is spoiled
Sharing to many pads leads to signals so small that are not considered in the reconstruction
  ==> reconstruction is biased
Sharing should involve a “fixed” number of pads
  ==> otherwise non-uniform response and performance
Floating pads do not contribute,
==> be aware during testing, you can get to the wrong conclusions
Example of RSD1 structures

## Slide 6: The FBK RSD2 production
Details on RSD2:
M. Mandurrino, “RSD2, the new production of AC-LGADs at FBK”, 39th RD50,
F. Siviero, “First experimental results of the spatial resolution of RSD pad arrays …” VCI2022
2 electrodes
4 electrodes, crosses
3 electrodes,
snowflakes
pois
Optimize the fabrication parameters (resistivity, oxide, gain layer)
Reduce as much as possible the metal area of the pads
Design the electrodes to contain the signal
Split the signal into a well defined set of pads
Goals for RSD2:
Uniform and controlled signal sharing
Focus of this talk

## Slide 7: Experimental set-up
The Particulars TCT laser setup has been used:
  IR laser generates a signal in the RSD,
  simulating the passage of a MIP
  laser spot size ~ 8 μm
  Laser temporal precision: ~ 8 ps
  movable x-y stage provides reference positions of the laser shots, precision: σ Laser~ 2 μm
All pads are read out with an oscilloscope
We used a 16-ch fast analog board, developed at FNAL, with an RMS noise ~ 2 mV.
Minimum signal level ~ 8 mV

## Slide 8: RSD2 sensors with 4 electrodes
Pitch = 1.3 mm
Pitch = 0.45 mm
In this study, the perfomances of sensors with electrodes shaped as crosses are presented.
Two different pitches: 450 mm and 1300 mm
Electrode width: 20 mm
Gap: 80 mm (pitch = 450 mm) and 100 mm (pitch = 1300 mm)
80, 100
20
3
4
1
2
3
4
1
2
Pitch = 0.45 mm

## Slide 9: Signal shape and propagation – 450 mm pitch
The signal is very similar to that of a standard LGAD when the hit is near the pad.
The signal decreases in amplitude and it is shifted in time as the hit position is moved away
Read-out pad
The effects of propagation on the signal shape have been studied by shooting laser signals along the diagonal, and measuring the signals seen in a given read-out pad

## Slide 10: Signal shape and propagation – 1300 mm pitch
The overshoot is smaller in the 1300 mm pitch, as the RC is longer (the capacitance is larger)
When the hit is at the opposite corner of the square, the signal is barely visible ==> distortion in the reconstruction
The signals measured in sensors with pitch either 450 mm or 1300 mm are very similar
The major difference is in the overshoot
Read-out pad

## Slide 11: Signal attenuation in 1300 mm pitch: 2 different sheet resistances
Red = Nomina sheet resistance
Blue = 25% of nominal sheet resistance
No significant difference in signal attenuation.
As expected, the sheet resistance does not influence signal sharing
How does the sheet resistance influence signal attenuation & sharing?
Red = Nomina sheet resistance
Blue = 25% of nominal sheet resistance
On the more resistive sheet, the signal becomes smaller and wider with distance, so the amplitude decreases more rapidly.
Signal amplitude vs distance for two RSDs with different sheet resistance:
Signal area vs distance for two RSDs with different sheet resistance:

## Slide 12: Signal amplitude vs distance for 450 mm and 1300 mm pitch
How signal sharing is affected by the size of the pixel?
450 mm
1300 mm
For the two geometries, compare the signal attenuation seen while shooting along the diagonal.
Read-out pad
Read-out pad
The two pixel sketches are to scale.

## Slide 13: Signal attenuation vs distance for 450 mm and 1300 mm pitch
Example: a pad sees 10% of the signal when the hit is about 1 pitch away along the diagonal
Red = 1300 micron pitch
Blue = 450 micron pitch
The curves “amplitude vs distance” for the two pitches are almost identical if the distance is expressed in unit of pitch
For equal electrode design, sharing is identical, regardless of the pitch size
The absolute distance (450 mm vs 1300 mm) does not matter in the attenuation
Note: the signal is almost contained within a pixel, even if they have very different sizes ==> the cross geometry behaves as envisioned.
Red = 1300 micron pitch
Blue = 450 micron pitch

## Slide 14: Signal sharing among the 4 pads vs run #
450 mm pitch
1300 mm pitch
1
2
0
3
1
2
0
3
2
1
0
3
1
2
0
3
This is the complete signal splits for signals shot along the diagonals

## Slide 15: Position resolution
The main component of the position resolution
is the position jitter, defined as:
100 mV
0 mV
Read-out pad
Imagine a system with a single read-out pad where a hit generates:
A signal of 100 mV when shot near a pad
A signal of 0 mV when shot at the opposite corner
Noise – 2 mV (as in our lab)
500 1000 1500
distance [mm]
Amplitude [mV]
inter-pad: 1300 mm
pitch: 450 mm
100
50
0
0
0.15
0.05
In this simplified system, the signal decreases by:
Pitch 1300 mm: 0.05 mV/mm
Pitch 450 mm: 0.15 mV/mm
So, the jitter is:
Pitch 1300 mm: 2 mV/(0.05 mV/mm) = 40 mm
Pitch 450 mm: 2 mV/(0.15 mV/mm) = 14 mm
Obviously the real reconstruction is more complex, 4 pads are contributing

## Slide 16: Position reconstruction
4 pads are readout, all others connected to gnd
Reconstruction method via charge imbalance (aka charge-weighted position centroid):
This is the simplest alghoritms for position reconstruction.
3
4
1
2

## Slide 17: Simulation results
Shoot in a grid of points, and see where the position is reconstructed:
Red: points where the signals are injected
Green: reconstructed points
The reconstructed points (in green) show a distortion effect called “pincuschion”
(very common in other resistive surfaces)

## Slide 18: Reconstruction results: 450 mm pitch
In the geometry with crosses the “pincuschion” distortion is present, but not very pronounced
The points are “compressed” towards the center.
It is possible to correct this distortion, either with an analytic law or a map.
Laser position red, reconstructed position green

## Slide 19: Position resolution for 450 mm pitch, gain = 10
After correcting for the distortion, the position resolution is about 13 mm
(gain ~10)
Laser position red, reconstructed position green
sx ~ 13 mm
sy ~ 12 mm
Resolution at various positions
Resolution at all positions

## Slide 20: Position resolution for 1300 mm pitch, gain = 10
After correcting for the distortion, the position resolution is about 40 mm
(gain ~10)
Laser position red, reconstructed position green
sx ~ 36 mm
sy ~ 37 mm
Resolution at various positions
Resolution at all positions

## Slide 21: Position resolution vs gain or pitch
For equal gain, the position resolution improves as 1/pitch
Chart: Position resolution vs pitch (0.45 & 1.3 mm), gain = 10
| 2.2222222222222223 | 0.76923076923076916
 | 13 | 36
Chart: Pitch 1.3 mm: position resolution vs gain
| 7.6 | 9.9830508474576263 | 14.169491525423728
Position 1 | 44 | 35 | 19
1/Gain | 50 | 37.5 | 30 | 25 | 21.4286 | 18.75
The position resolution is a strong function of the signal amplitude, reaching about sx ~ 20 mm for a gain ~14
Note:
sx follows quite well the behaviour 1/(dV/dx) (equivalent to 1/gain or 1/pitch)
as predicted by the jitter formula

## Slide 22: Signal delay
The signal delay increases with distance, however, given the shape of the electrodes, the determination of ”distance” it is not straightforward: the vertex? the closest metal?
Along the diagonal, the delay for this specific structure is about 0.3 ps/ mm
  ==> the delay is the same for 450 mm and 1300 mm pitch
  ==> the delay increases in wafer with a higher sheet resistance
Signal delay of the channel with the maximum amplitude for different hit positions
0.3 ps/mm
The time of each pad i is defined as:
Using the laser, a delay map has been created

## Slide 23: Hit time
The time of the hit can be defined in several ways. For examples:
Amplitude-weighted
(leads to uniform precision on the pixel surface):
2) Time of the channel with the maximum amplitude:
(works best when one amplitude is much larger than the other 3, not uniform on the pixel surface)
Chart: Pitch 1.3 mm: temporal jitter vs gain
| 7.6 | 9.9830508474576263 | 14.169491525423728
Position 1 | 41 | 29 | 21
1/Gain | 50 | 37.5 | 30 | 25 | 21.4286 | 18.75
Amplitude weighted temporal resolution (jitter component) vs gain
(laser contribution not subtracted)
The jitter is quite good, similar to that of an LGAD with equivalent gain

## Slide 24: Conclusions
The FBK – AC-RSD2 production has been designed to:
Have uniform signal sharing on the pixel surface
Limit sharing to a well defined set of electrodes
Electrodes shaped as crosses are very effective in reaching both goals
Sharing happens on the whole pixel surface
The signal is mostly contained within 4 electrodes
In our studies, we reached a spatial resolution about 3% of the pitch at gain = 10
Pitch = 450 mm ==> sx ~ 13 mm; sx/pitch ~ 3%
Pitch = 1300 mm ==> sx ~ 37 mm; sx/pitch ~ 3%
Spatial resolution depends upon ~ 1/gain, ~ 1/pitch, and ~noise
Temporal resolution similar to LGAD with equivalent gain

## Slide 25
Acknowledgement
We kindly acknowledge the following funding agencies, collaborations:
RD50 collaboration
INFN - Gruppo V, RSD projects
INFN – FBK agreement on sensor production (convenzione INFN-FBK)
Dipartimenti di Eccellenza, Univ. of Torino (ex L. 232/2016, art. 1, cc. 314, 337)
Ministero della Ricerca, Italia , PRIN 2017, progetto 2017L2XKTJ – 4DinSiDe
Ministero della Ricerca, Italia, FARE, R165xr8frt_fare