Cu Surface Diffusion Bias under Electric Field Gradient
Accelerated Molecular Dynamics, Finite Elements Method,
and Density Functional Theory
Jyri Kimari, Flyura Djurabekova
University of Helsinki
Ye Wang, Andreas Kyritsakis, Veronika Zadin
University of Tartu

---
Outline
- Familar story of vacuum arc
  formation
- Atomistic view of mass
  transport by diffusion
- Molecular dynamics with
  extended time and length scale
- Comparison with density
  functional theory

---
Familiar picture
Anode
Anode
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
Cathode
Cathode
1. Field emission
2. Thermal runaway
Anode
Anode
e-
e-
e-
e-
e-
Cathode
Cathode
3. Breakdown
4. Crater

---
Growth and sharpening of field emitters
- Dislocation slips
- Initial roughness
- Craters of previous breakdowns
- … into huge field emitters?
?
β ≈ 100
Cathode

---
Surface curvature driven mass transport
Competition between minimizing surface energy and electric field energy
Cathode

---
Atomistic view of mass transport
- Biased diffusion in the
  presence of electric field
  gradient
- Strength of the effect
  can be related to
  surface dipole moment
  and polarizability
E_{ nitalic m } approx E_{ nitalic m }( 0 ) - {font fixed M}_{ nitalic sl } F - { {font fixed A}_{nitalic sl} } over 2 F^2 - {font fixed M}_{ nitalic sr } %DELTA F - {font fixed A}_{ nitalic sr } F %DELTA F
A. Kyritsakis et al., Phys. Rev. B 99, 205418 (2019).
T. T. Tsong, P. Cowan, and G. Kellogg, Thin Solid Films 25, 97 (1975).

---
Atomistic simulation of biased diffusion
- Idea 1: implement the effect as modification of migration energy barriers
- Kinetic Monte Carlo model
- Still a lot of uncertainty
  with estimating dipole
  parameters!
tungsten
%GAMMA = %nu exp left( - {E_{nitalic m} } over {k_{nitalic B} T } right)
V. Jansson et al., Nanotechnology 31, 355301 (2020).

---
Something more flexible
- Idea 2: couple field calculation directly to molecular dynamics
- Finite elements
    method field solver
  + Surface charges from
    Gauss’s law
  + Electrostatic forces
    (Lorentz & Coulomb)
  = Femocs
M. Veske et al., Journal of Computational Physics 367, 279 (2018).

---
Simulating diffusion along a field emitter
- Diffusion is slow – a few more tricks are necessary.
- Extending length scale
  - Only 1000–1500 atoms included in molecular dynamics, the rest of the system is a static extension mesh
- Extending time scale
  - Cu {100} surface has relatively high migration energy barriers, ~0.5 eV
  - Accelerated dynamics

---
Extending the electrostatic system
Track movement under gradient

---
Extending the time scale
- We want to promote events of adatoms hopping on the surface
- We can calculate a number that describes how close the system is to an event
At equilibrium, η ≈ 0
Almost at saddle point, η ≈ 1

---
Yanking the system toward events
Total potential energy:
V'(bold R) = V( bold R ) + %DELTA V(%eta )
Timestep stretch:
%DELTA t_{ nitalic CVHD } = %DELTA t_{ nitalic MD } left langle exp left ( {%DELTA V} over {k_{nitalic B } T} right ) right rangle
Bias force acting on atom i:
%DELTA F_{i} = - {{ partial %DELTA V } over { partial %eta } { partial %eta } over { partial %chi_{nitalic global} } sum_j^{nitalic bonds} { { partial %chi_{nitalic global} } over { partial %chi_j } { partial %chi_j } over { partial r_j } } } left ( { { partial r_j } over { partial x_i } } bold hat x + { { partial r_j } over { partial y_i } } bold hat y + { { partial r_j } over { partial z_i } } bold hat z right )
K. M. Bal and E. C. Neyts, J. Chem. Theory Comput. 11, 4545 (2015).

---
Field solutions
Field solutions in different
geometries at applied
field 100 MV/m

---
Trajectories of adatoms
Ten repeats for each
geometry, surface and
applied field

---
All surfaces display biased diffusion
”Drift velocity” = final displacement divided by simulation time
E_{ nitalic m } approx E_{ nitalic m }( 0 ) - {font fixed M}_{ nitalic sl } F - { {font fixed A}_{nitalic sl} } over 2 F^2 - {font fixed M}_{ nitalic sr } %DELTA F - {font fixed A}_{ nitalic sr } F %DELTA F
?
?
polarizability
dipole moment

---
Fitting theoretical prediction
- Drift velocity is connected to migration event rate
- Barrier is modified by the field and its gradient
- Combining these, we can fit Msr and Asr to the MD results
%GAMMA = %nu exp left( - {E_{nitalic m} } over {k_{nitalic B} T } right)
E_{ nitalic m } approx E_{ nitalic m }( 0 ) - {font fixed M}_{ nitalic sl } F - { {font fixed A}_{nitalic sl} } over 2 F^2 - {font fixed M}_{ nitalic sr } %DELTA F - {font fixed A}_{ nitalic sr } F %DELTA F

---
Polarization parameters from density functional theory
Msr and Asr directly ab initio
E. Baibuz et al., 10.48550/arXiv.2201.03460 (2022).

---
MD+electrostatics vs DFT
- Dipole moment Msr error is expected
- Polarizability Asr underestimated in MD, possibly due to different geometry (nanotip in MD, slab in DFT)
Surface	Msr (eÅ)		Asr (eÅ2/V)
	MD	DFT	MD	DFT
{100}	0.0 ± 0.2	0.106 ± 0.003	0.1 ± 0.1	0.27 ± 0.02
{110}	–0.008 ± 0.005	0.094 ± 0.006	0.034 ± 0.008	0.30 ± 0.04
{111}	–0.016 ± 0.006	0.162 ± 0.003	0.02 ± 0.01	0.23 ± 0.02

---
Summary and outlook
- Biased diffusion captured in atomistic simulation
- Polarization physics can be directly compared to density functional theory
- Outlook:
  - Verify results on slab surface
  - Larger scale simulations – actual mass transport
  - Combine accelerated molecular dynamics with plasma formation dynamics in Femocs…?
- All details: J. Kimari et al., J. Phys. D: Appl. Phys. (in press). DOI: 10.1088/1361-6463/ac91dd