## Slide 1: Work Package 10 Task10.2: Ultra-light and 3D-printed structures with integrated cooling
Massimo Angeletti
Collaboration with CERN EP R&D Work Package 4
https://indico.cern.ch/event/1104064/
AIDAInnova 1st Annual meeting
Activities at CERN

## Slide 2: WP10.2: Ultra-light and 3D-printed structures with integrated cooling
Synergy between CERN EP R&D WP4 and AIDA Innova WP10 Task10.2
  AIDA Innova Task10.2 programme focus on the Characterization of Ultra-light and 3D printed structures with integrated cooling for HEP experiments.
  Some studies started during the first year of the CERN EP R&D WP4 programme and they will be shared and further developed within AIDA Innova Task10.2 framework.
  The knowledge acquired with the AIDA Innova Task10.2 characterization studies will be then transferred to the prototype activities of the CERN EP R&D WP4
2020
2021
2022
…..

## Slide 3: WP10.2: Ultra-light and 3D-printed structures with integrated cooling
Outline:
  Ultra-light structures with integrated cooling Carbon cold plate with embedded Kapton pipe
    Purpose,
    2021 Highlights on characterization studies,
    Next and Planning
  3D-printed structures with integrated cooling AM Ceramic & Metal cold plates
    Purpose,
    2021 Highlights on characterization studies,
    Next and Planning
Sensor
Sensor
Sensor
Sensor

## Slide 4: Ultra-light structures with integrated cooling
2 x cold plate
Spaceframe
~1.5m long
ALICE ITS2 OB Stave configuration
Carbon Cold Plate (CP) with embedded Kapton pipes
DI water,
Leak-less mode,
T ambient
Developed by
Also used by
NA61
Used in ALICE in 2 detectors: ITS and MFT (LS2)
MPD, IT (JINR)
Purpose:
Compatible with high-pressure liquid coolants: Two-phase CO2 refrigerant and new coolants (Krypton,…).
Produce extended Carbon CP to cover large surfaces: understand their potentialities and limitations (considering minimum bending radius, pressure drop and pressure resistance limitations).
Collaboration between CERN and Workshape (composite company).
Up to 1.5m

## Slide 5: Ultra-light structures with integrated cooling
2021 Highlights
Kapton pipe characterization:
  Pressure test:
CERN EP R&D WP4
Burst Pressure & Pressure drop test
(Demineralized water)
*3 weeks (2 weeks at T=22°C, p=45 bar; 1 week at T=-28°C, p=15bar, v.quality=0.3)
@CERN TE-VSC-SCC
Samples: Kapton foils (DuPont Kapton HN) of 25 um, 50 um, 75 um and 125 um thickness, glued to CuOFE gaskets (Polymerlab, Scotchweld 2216)
Sample | CO2 Permeation from series fit [l cm/cm2 s]
Kapton 25 um run 1 | 3.20e-12
….. | 
Kapton 125 um run 1 | 2.85e-12
(Preliminary)
(Samples immerged in CO2* prior the test)
  Permeation test with CO2

## Slide 6: Ultra-light structures with integrated cooling
2021 Highlights
ALICE ITS2 IB Cold plate test with two-phase CO2
CERN EP R&D WP4
Vacuum Chamber
Thermal-fluidic test set-up
IR Camera
Proof of concept
Tsat -20°C
q 0.5 W cm-2
G 300 kg m-2 s-1
T mean chip -12°
ΔT across chip 10°C
ΔT fluid-sensor ~ 8°C
Kapton tubes withstand the high pressure (~20 bar) & circulation of CO2 is possible
ALICE ITS2 IB Cold plate
CERN CO2 test facility for mini- and micro-channels
Spray coating
D. Hellenschmidt (CERN EP R&D Fellow)

## Slide 7: Ultra-light structures with integrated cooling
NEXT: High Pressure CPs production for CO2 comparison test
 | Steel | Steel | Kapton | Kapton
ID [mm] | 2.15 | 1 | 1.97 | 1.024
WT [mm] | 0.51 | 0.29 | 0.167 | 0.076
Steel
Kapton
(ATLAS,CMS like configuration)
(ALICE like configuration)
VS
Planning:
2022 |  |  |  |  |  |  |  |  |  |  |  | 
Jan | Feb | Mar | Apr | May | June |  | July | Aug | Sept | Oct | Nov | Dec
… Kapton pipe characterization |  |  |  |  |  |  |  |  |  |  |  | 
CPs Production |  |  | CO2 comparison test |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  | CPs production at WORKSHAPE |  |  |  |  |  | 
NEXT: WORKSHAPE Collaboration
Transfer Know-how for CPs production
Support future samples production
CERN EP R&D WP4
200mm
HP CPs ready for test
(with Kapton pipes)
D. Hellenschmidt

## Slide 8: 3D Printed structures with integrated cooling
Purpose:
Focus on the best attainable features respectively in terms of geometrical features, thermal-fluidic performances and mass minimization; and on the technological processes required to achieve them.
METAL
The studies will be supported by CERN EN-MME (3D printers) and CSEM (Experience with SWaP** - ATTRACT project ).
Within CERN EP R&D, different metal AM technologies are being investigated (3D systems, Microfabrica, …).
CERAMIC
The studies will be supported by Lithoz company, leader in additive manufacturing in ceramic materials (production of 3D print machines and component manufacturing).
Within CERN EP R&D alternative ceramic AM technologies are being investigated (Xjet, Fabrica Group, Kyocera, Adamant, …).
**Smart wall pipes and ducts, link
Material: Al alloys (AlSi12, EN AC-44300), nickel-iron alloys (Invar and Kovar)
Material: Aluminum oxide (Al2O3), Aluminum nitride (AlN), polymeric-ceramic composite*
*Polymerised light-sensitive organic matrix in which high-purity ceramic powder is dispersed. (Green part, before de-binding and sintering)

## Slide 9: 3D-printed structures with integrated cooling
2021 Highlights
Preliminary ceramic AM process characterization
CERN EP R&D WP4
Printable ceramic
(Al2O3, Zr, SiC, AlN)
D 0.4mm
15x30mm2
Height measurement accuracy of +- 3 um and a repeatability of 0.4 um
Keyence VR5200
Substrate roughness, flatness (3D scan)
Wide-Area 3D measurement system
Sa (arithmetical mean height) = 6 µm
Height magnification 1200%
Substrate defects and channel obstructions (x-ray computed tomography)
>90°
Tomography resolution 7 um
Zeiss METROTOM 1500 CT scanner
@CERN EN MME-MA
LCM, Alumina, flat orientation D=0.7mm
Ra=14.6 µm
Channel roughness measurements (Profilometer)
@CERN EN MME-MA
D=0.7mm
D=0.5 mm
D=1 mm
  Performed in the framework of a modular cooling substrate investigation (EP R&D subject)
Different sample orientation

## Slide 10: 3D-printed structures with integrated cooling
NEXT: CERN, CSEM and Lithoz will work to explore
Geometrical limits (substrate flatness, minimum wall thickness, channel leak-tightness, inner wall roughness, dimensional manufact accuracy…)
For polymeric-ceramic composite: Define and optimise polymeric matrix (acrylate-based or epoxy based) producing parts with good mechanical properties and investigation of tolerance to the ionizing radiations
Planning:
2022 |  |  |  |  |  |  |  |  | 
Mar | Apr | May | June | July | Aug | Sept | Oct | Nov | Dec
 |  | Samples production (Ceramic & Metal) |  |  |  |  |  |  | 
 |  |  | Characterization test at CERN and INFN |  |  |  |  |  | 
Future collaboration TASK 10.3 (CNRS-LNPHE Paris and INFN) substrate-substrate interconnection. Interconnection solution developed in EP R&D WP4: https://indico.cern.ch/event/1063927/ ,
Publication: https://doi.org/10.1016/j.mee.2022.111707
WT= 0.2 – 0.6 mm

## Slide 11: THIS IS THE END…
Thank you
for your attention