## Slide 1
The PIN structured Si sensor for the ALICE FoCal / APD structure into the pixels for the LS3 upgrade
YOUNG HOON HAN

## Slide 2
The PIN structured Si sensor for the ALICE FoCal

## Slide 3
Processed Submission
As a plan we announced at previous workshop, we proceed submission with design considered
Fixed version of Mask design
Fabricated sensor
With various types of test patterns

## Slide 4
Characteristic of fabricated sensor
Device’s ideality factor was measured as 1.21, so we could confirm device show enough quality of being diode
Device show turn on at 0.2V, general forward characteristic of diode

## Slide 5
Characteristic of fabricated sensor
There exist some variation at leakage level, but nearly all pattern show leakage level under 1A, which was our limitation to use for detector
By measuring capacitance, we find that full depletion is achieved at under the half of breakdown voltage, so we concluded it can be operated for ALICE E-FoCal

## Slide 6
GR structure study using test pattern
Tertiary guardrings
Patterns
Main guardring
Oxide
Intrinsic P- Wafer
P+
P+
N+
N+
N+
N+
N+
GR structure
Give some variances at GR
structures using test pattern
GR numbers, width, rounding.. etc

## Slide 7
Radiation test
In order to study radiation hardness issues, we perform experiments at KOMAC.
We use two beam line to do research about type-inversion
and leakage current variations due to irradiation

## Slide 8
Radiation test
Proton flux injected was choosed by ALICE FoCal radiation criteria
IV Plot
1E+13 neq/cm2
We check type inversion and increased leakage current

## Slide 9
Dicing study
Dicing improved leakage current of sensor

## Slide 10
APD structure into the pixels for the LS3 upgrade

## Slide 11
Considered APD structure
gain layer
gain layer
Avalanche region ~ 1um
layer
blancket

## Slide 12
Considered technology of ‘Epitaxial growth’
Dopant: P, As, B
with thickness
Claim for commercial service: https://svmi.com/service/epitaxial-wafer-service/
Typical growth rate:

## Slide 13
Key features of design
As a reverse bias is applied to P sub, avalanche PN junction region start to be depleted
Full depletion is achieved at 23V with gain of near 93 and we have margin about 3V
As shown at Dark current feature, Light current characteristic follow avalanche behavior due to depletion at junction

## Slide 14
Hands estimation of APD gain
Avalanche region
REF: IMPACT IONIZATION IN SILICON: A REVIEW AND UPDATE W. MAES, K. DE MEYER* and R. VAN OVERSTRAETEN IMEC vzw, Kapeldreef 75, 3030 Hevedee, Belgium Solid-State Electronics Vol. 33, No. 6, pp. 705-718, 1990
Use k-factor (ratio between electron and hole ionization coefficients) to estimate formula

## Slide 15
APD into the pixel
Reverse bias of 1.2V is applied at each deep P-well region
Insert previous APD structure into ALPIDE pixel

## Slide 16
Key features persist!
There were no big differences at current feature when we implant APD structure into the ALPIDE pixel structure
No punch through until system breakdown occur

## Slide 17
As a plan, We processed submission and check characteristics of sensor
  Sensor’s characteristic was concluded enough to be used for ALICE E-FoCal
  Guardring structure study through test pattern
  Radiation hardness test was processed
APD structure study using Tcad was processed
  Inserting APD structure into the pixel doesn’t make change at avalanche behavior
Summary
17

## Slide 18
Thank you for attention