## Slide 1: Time-of-flight methods in ion beam analysis
MARKO BRAJKOVIĆ, ZDRAVKO SIKETIĆ, MARKO BARAC, IVANČICA BOGDANOVIĆ RADOVIĆ
RUĐER BOŠKOVIĆ INSTITUTE, ZAGReB, CROATIA
EUnpc22, SANTIAGO DE COMPOSTELA, OCTOBER 2022

## Slide 2
1.0 MV HVE Tandetron accelerator
6.0 MV EN Tandem Van de Graaff accelerator
TOF-ERDA
PIXE/RBS
Ion microprobe
Nuclear reactions
In-air PIXE
Dual beam,DiFu
Channeling
Dual µ-beam
Collimated beam MeV TOF-SIMS
RBI ACCELERATOR FACILITY
Currenty: protons up to 8 MeV, and heavy ions up to 30 MeV from the VDG accelerator

## Slide 3
TOF ERDA
Time-of-Flight Elastic Recoil Detection Analysis
MeV TOF SIMS
Time-of-Flight Secondary Ion Mass Spectrometry
HEAVY ION BEAM TECHNIQUES
Most IBA techniques use protons: PIXE, RBS, PIGE, IBIC.
Heavy ions vs protons:
Production of recoils and secondary particles
High stopping power
organic samples
inorganic films

## Slide 4
TOF ERDA
Time-of-Flight Elastic Recoil Detection Analysis

## Slide 5
Chamber
Target
Ion beam (Cl, I, Au.., E~0.2 MeV/A)
Collimator
Recoiled atoms
Depth profiling of few 100 nm thick samples
Depth resolution up to ~1 nm at the surface
Heavy ion beam – e.g. 23 MeV Iodine ions
sensitivity 1015 /cm2
2 nm depth resolution, up to 500 nm probe depth
all elements are resolved
Resolution < 1 amu for m < 40 amu
SEPARATION OF ELEMENTS BY MASS
E and TOF measured
cross sections, stopping powers known

## Slide 6
x,y,z,
manipulator
L=523.4 mm
Chamber
TOF ERDA: SETUP
GID: better energy resolution than particle silicon detectors + radiation hardness
Z. Siketić, N. Skukan and I. Bogdanović Radović "A gas ionisation detector in the axial (Bragg) geometry used for the time-of-flight elastic recoil detection analysis", Review of Scientific Instruments 86, 083301 (2015)

## Slide 7
T1
T2
CFD
TAC
Electrostatic mirror
Incoming ion
Foil:
Accelerating grid
MCP-in
MCP-out
Anode
Coaxial cable
TOF ERDA: SETUP – TIMING GATES
Timing signal: detection of secondary electrons from the diamond-like carbon foil coated with LiF

## Slide 8
TOF-ERDA applications – industrial partners
H
C
N
O
F
Si
Ti
Ni
Ta
Ir
Element | Total Number of 1015 at/cm2
H | 15.2
C | 6.6
O | 158.7
F | 33.5
Ni | 141.8
Flourine contamination found
TOF ERDA APPLICATION – Quality control of production proces
NiO film

## Slide 9
Sample: TiN
Beam: 20 MeV 81Br5+
TOF ERDA APPLICATION – Thin film analysis

## Slide 10
Beam: 25 MeV 127I, θin = 5°, θscatt. = 37.5°
Target: 5x AlN/TiN 20 nm layers
E (Channel)
TOF (Channel)
Al layers
TOF (Channel)
Counts
TOF ERDA APPLICATION – Multilayer samples
Time spectra of the Al events
Result of the analysis:
Al:N=1:1, d = 24 nm
Ti:N=1:1, d = 40 nm
Resolution detoriaties with a depth!

## Slide 11
TOF ERDA promoted by argon sputtering (lines + symbols) and TOF-ERDA (lines) depth profile for a 15-nm-thick Cu layer evaporated onto the Si substrate.
TOF ERDA + Ar SPUTTERING
TOF-ERDA used to measure the surface elemental composition, Ar sputtering to extract the depth information
best achievable (surface) resolution of 2 nm for the entire layer
Siketić, Z., Bogdanović Radović, I., Sudić, I. et al. Surface analysis and depth profiling using time-of-flight elastic recoil detection analysis with argon sputtering. Sci Rep 8, 10392 (2018).

## Slide 12
MeV TOF-SIMS
Time-of-Flight Secondary Ion Mass Spectrometry

## Slide 13
= mass spectrometry technique used for identification of atomic and molecular species by measuring time-of-flight of the secondary ions sputtered from the sample surface
Primary
ion beam
Target
Secondary ions
Extractor
TOF analyzer
Spektar pozitivnih iona
TOF spectrum
Mass spectrum
Scanning over the sample
Imaging (2D spatial molecular distribution)
= 2V
(E0 few eV)
MeV SIMS

## Slide 14
Silicon beam on a leucine target:
electronic stopping dominates for MeV energies
Higher SI yield for heavier molecules, and less fragmentation, than for keV counterpart
TOF mass spectrometry techniques comparison
lateral resolution (µm)
mass resolution (Da)
commercially available,
mostly inorganic samples
MV accelerators required,
organic samples

## Slide 15
Since 2014 we published 16 papers in high IF journals on application of MeV SIMS analysis:
  Biology (identification of lipids and fatty acids in various tissues and single cells, 2 papers published)
  Cultural heritage (identification of pigments and binders of modern paint materials, 3 papers published)
  Forensics (study of deposition order of crossing lines of different writing tools, 3 papers published)
  Simultaneously analysis of organic and inorganic materials (2 papers published)
  Development of MeV SIMS and measurements of fundamental parameters (6 papers published)
MeV SIMS APPLICATIONS @ RBI

## Slide 16
Example #1: Molecular imaging of single CaCo-2 cancer cell
Beam: 9 MeV O4+
Scan size: 85x85 µm2 (≈300 nm/pixel)
STIM
Na+
K+
Lipid
Optical photo
Positive ion spectrum
Siketić, Z., Bogdanović Radović, I., Jakšić, M., Popović Hadžija, M., & Hadžija, M. (2015) Applied Physics Letters, 107(9), 093702.
MeV SIMS: APPLICATIONS

## Slide 17
Exampple #2: Forensics: determination of depositioning order of inks/toners
Ink crossing imaging + PCA analysis
Moore, K. L., Barac, M., Brajković, M., Bailey, M. J., Siketić, Z., & Bogdanović Radović, I. (2019) Analytical chemistry, 91(20), 12997-13005.
MeV SIMS: APPLICATIONS

## Slide 18
Timing filter amplifier
Timing filter amplifier
MeV SIMS: OLD SETUP
TOF START: Primary beam pulsing
TOF STOP: MCP detector
FOCUSING: magnetic lenses
IMAGING: Primary beam scanning over the sample
Cannot use ions heavier than Silicon!
upper limit: m·E/q2 < 14 MeV amu

## Slide 19
ALTERNATIVE: COLLIMATED BEAM
cheap alternative for magnetic focusing for small current (fA) application
collimation independent on ion mass and energy = heavy, high energy ion can be used
in principle, in-air extraction possible
TOF START: Primary beam pulsing ?
TOF STOP: MCP detector (upgraded with 10 kV postacceleration)
FOCUSING: COLLIMATION with micro-capillary/micro-aperture
IMAGING: sample placed on piezo-stage in front of fixed collimator
COLLIMATED BEAM:

## Slide 20
MICROCAPILLARY: TRANSMISSION
energy spectra of transmitted beams
spatial distribution of transmitted beam
conically-shaped glass capillary
(5 µm exit diameter)
M. Brajković, M. Barac, D. Cosic, I. Bogdanović Radović, Z. Siketić, Development of MeV TOF-SIMS capillary microprobe at the Ruđer Bošković Institute in Zagreb, Nucl. Instr. and Meth. B 461 (2019) 237-242.

## Slide 21
MICROCAPILLARY: IMAGING
lateral resolution: leucine-evaporated copper mesh
Imaging: ink crossing on a paper
CONS: halo and low contrast
M. Brajković, I. Bogdanović Radović, M. Barac, D. D. Cosic, Z. Siketić, Imaging of Organic Samples with Megaelectron Volt Time-of-Flight Secondary Ion Mass Spectrometry Capillary Microprobe, J. Am. Soc. Mass Spectrom. 2021, 32, 10, 2567–2572.

## Slide 22
0.1 mm
steel, thickness 12.7 µm, aluminum frame
5, 10 µm aperture opening
beam through the aperture on Gafchromic EBT3 film
5 µm APERTURE

## Slide 23
transmission: mesh with 127 µm pitch
Leucine map, 250 x 250 µm2
Phthalocyanine map, 1 x 0.9 mm2
electron start: mesh with 440 µm pitch
lateral resolution ≈ 10 µm (for 5 µm aperture)
IMAGING #1: MESH
MUCH BETTER CONTRAST COMPARED TO THE CAPILLARY!

## Slide 24
Primary ion detection (by a PIN diode)
simple setup, good mass resolution
thin targets only, radiation damage
Detection of secondary electrons
thick targets, radiation hard
complicated setup
TWO TOF START TRIGGER OPTIONS
?
Kore detector with 10 kV postacceleration
STOP signal

## Slide 25
thin carbon foil (5 nm thickness) over the aperture = the production of secondary electrons sample-independent (for example, 7 kHz from a silicon plate but only 1 kHz from a paper
THE SETUP
schematics of secondary ion detection

## Slide 26
THICK TARGET SETUP:
DETECTION OF ELECTRONS
electric potential distribution and electron detection with the target at zero potential
electric potential and electron trajectories with the target at the extraction potential
COMSOL simulations
TARGET CANNOT BE HELD AT CONSTANT (EXTRACTION) VOLTAGE!

## Slide 27
+target voltage
extractor
+
+
+HV
+
+
electron
multiplier
C foil over aperture
target voltage switch
+
+
+HV
+
+
Trigger
SHEMATIC OVERVIEW OF THE THICK-TARGET SETUP: DETECTION OF SECONDARY ELECTRONS
target voltage applied only for 2 µs
delayed extraction
extraction blocked for the remaining part of the acquisiton window(98 µs)
M. Brajković, I. Bogdanović Radović, M. Barac, D. D. Cosic, Z. Siketić, Imaging of Organic Samples with Megaelectron Volt Time-of-Flight Secondary Ion Mass Spectrometry Capillary Microprobe, J. Am. Soc. Mass Spectrom. 2021, 32, 10, 2567–2572.

## Slide 28
leucine, +3 kV extraction
Phthalocyanine blue (m = 576.1 Da) mass spectrum with 10 kV postacc. detector
Mass resolution (for m = 576.1 Da):
2500 in the transmission mode
1400 in the electron start mode
but S/N ration 2 – 5 times better in electron start mode
(random coincidences minimized)
MASS SPECTRUM: TWO MODES
Comparison of two modes of operation

## Slide 29
map of signature ink molecules (358-372 Da),
ink crossing on a paper, 1 x 1 mm2
optical photo of ink crossing on a paper
mass spectrum from the ink crossing area
IMAGING #2: INK CROSSING ON A PAPER

## Slide 30
total map, fingermark on a silicon plate, 5 x 5 mm2
fingermark on a silicon plate under optical microscope
IMAGING #3: FINGERMARK

## Slide 31
lipid fragment
184.1 Da
medium 228.4 Da
cholesterol 369.4 Da
2 x 2 mm2 scan, t = 3.5 hours
primary beam 14 MeV Cu4+
IMAGING #4: MOUSE TISSUE

## Slide 32
lipid fragment (m = 184.1 Da)
cholesterol (m = 369.4 Da)
medium (m = 228.4 Da)
sample photo on an optical microscope
total map
IMAGING #4: MOUSE TISSUE

## Slide 33
CONCLUSIONS
Acknowledgments
THANK YOU FOR LISTENING!
Two techniques (heavy MeV ions + TOF measurements): inorganic films and organic samples
Different applications: thin film analysis, biomedicine, forensics, ...