## Slide 1: Keys an bladders cross sections
Proposal for FalconD

## Slide 2
From the previous experience on Nb3Sn magnets two axes of work:
  Quality of coils – Winding, thermal treatment tools.
  Stress management in the structure – limit peaks of compression in the coils.
Take the time to carry out winding tests – Check if tools can be improved.
Design ‘intrinsically safe’ structures. Identify and manage effect of tolerances on coil compression.

## Slide 3
A Sum of Gaussian Random Variables is a Gaussian Random Variable
Sn sum of n statistically independent random variables xi
The mean value of the sum is the sum of the individual means.
The variance of the sum is the sum of the individual variances.
If all the individuals xi have the same probability density we have:
The width of the Gaussian Sn grows as while the mean of Sn grows as n (in our case n is the number of pieces of the dipole cross section).
Reduce the number of pieces to be less sensitive to tolerances

## Slide 4
Intrinsically safe structure
Work with closed cavities (whenever possible)
  To protect the coils from over stresses.
  To control unbalanced stresses. The alignment precision of long presses or long ‘force’ tools is limited.
Rigid material. Collars or paddles.
Soft material. Coils.

## Slide 5
F
F
Compression
Traction
Effect of horizontal interference
Compression is added at the top inner corner of the coil. This is the first place to loose the contact with the collars at energization.
Traction is added at the coil midplane inner radius. This is the place where the compression is maximal at energization.
A moderate horizontal interference can help to control stresses in the coils.
In the past some dipoles were built and tested using this principle but with large interference. Good and less good results.
1992

## Slide 6
Cross section presented in FalconD TDR
INFN/Code-19/001
Reduce no of pieces
Prevent coil over stresses

## Slide 7
Horizontal alignment of the paddles. 0.0 – 0.1 mm clearance of undeformed parts for assembly.
Clearance absorbed by the horizontal pushing key.
Horizontal gap closed after cool down. Closed cavity.
Tight tolerances for the cavity but coil shims. Angles are important.
Horizontal gap always open.
Large tolerances.
Horizontal alignment of the iron yoke halves. 0.0 – 0.1 mm clearance of undeformed parts for assembly.
Clearance absorbed by the horizontal pushing key.
Fix line. Longitudinally free key. Horizontal clearance just to insert it (0.05 – 0.1 mm).
Pushing key. Horizontal clearance just to insert it (0.05 – 0.1 mm)
Pushing key. Large horizontal clearance (0.2 – 0.3 mm)
Aluminium insert. Longer than in the picture. Just to easy the assembly. Aluminium cylinder heated and slightly forced on the two half yokes kept at the right position by the inserts.
Proposed cross section
Moderate coil prestress at room temperature (50-60 MPa). Higher compression at the end of cool down (70-80 MPa).

## Slide 8
Do we need the inside tie rods? Or tie rods in general?
They weaken the pads where there is the need of space for the bladders.
  Suppress the tie rods in the pads.
  Fix the end plate to the outside aluminium cylinder with sector inserts.
  Use an end cage to load the first turns of the ends and not only the last (as it would happen with tie rods and friction).
Proposed longitudinal section
Tie rods
Aluminium cylinder
Iron yoke
Pads
End plate
End cage
Inserts
FalconD TDR
Proposed modifications

## Slide 9
Iron laminations
End cage working principle – longitudinal compression of first turns.
F’ +
Collar laminations or pads
Coil end 2nd layer
Coil end 1st layer
Surfaces with friction
Load from bullet gages
F
F’
Iron laminations
Collar laminations or pads
Load from bullet gages
F’’
F’’’
Preloaded bolts to compress longitudinally the coil ends in a controlled way.
Iron laminations

## Slide 10
Programm of the FEM computations (FalconD and more).
Study of the nominal configuration.
  Linear coils.
  Non linear coils.
  Austenitic stainless steel pads (contraction 3 mm/m).
  High manganese steel pads (contraction 1.9 mm/m).
Effect of tolerances.
  Variation of one parameter per time.
  Montecarlo approach.
Study of an alternative, low number of pieces cross section.
Compute a ‘12 T coil configuration’, double aperture, in view of the construction of an instrumented mock-up.

## Slide 11
Single iron lamination, large tolerances.
Invar inserts.