## Slide 1: A novel two-dimensional microstrip sensor for charge division readout
D. Bassignana, M. Lozano, G. Pellegrini
CNM-IMB (CSIC)
M. Fernández, R. Jaramillo, F.J. Muñoz, I. Vila
IFCA (CSIC-UC)
17th RD50 Workshop, CERN Nov 18th 2010

## Slide 2: _Outline
Sensor’s working principle.
Prototype manufacturing.
Electrical characteristics.
Laser and radioactive source characterization.
Test beam @ SPS.
Conclusions and outlook.

## Slide 3: _Charge division concept
Charge division used in wire chambers to determine the coordinate along the sensing wire.
Same concept with conventional microstrips with slightly resistive electrodes
L2a
L3a
L4a
L5a
L6a
L1a
X
Y
P1
P2
P3
P4
1
P5
P6
L2b
L3b
L4b
L5b
L6b
L1b
Al
Resistive material
t
t
t1
t2
V
Particle
P4
S1
S2
Ampl1
Ampl2
S1=f(y)
S2=f(L-y)

## Slide 4: _Concept Demonstrator: P-Si sensor
Designed and produced at IMB-CNM.
strip length= 14 mm.
Two different prototypes with different strip widths:
20 μm and 40 μm.
metal guides to drive the contact pads at the same edge of the detector.
implant pitch= 160 μm
read out pitch= 80 μm
Multiple guard rings.
standard technology
of silicon microstrip detectors.
P-on-n, 300 μm thick detectors.
Only one chip
to read out
the detector
Resistive material = highly doped polysilicon.

## Slide 5: _Electrical Characterization
Strip Width | Vdepl | Vbd | Rbias | Rint | Cint | Ccoupl | Relectrode/ □ | Relectrode/μm
20μm | 40 V | > 400 V | 1,31 MΩ | > GΩ | 1,32 pF | 248 pF | 400 Ω/□ | 20 Ω/μm
40μm | 40 V | > 200V | 1,37 MΩ | > GΩ | 1, 60 pF | 487 pF | 400 Ω/□ | 10 Ω/μm

## Slide 6: _Readout Electronics
ALIBAVA SYSTEM – Sensors P20 & P40 bonded at IFIC

## Slide 7: FE chip calibration
Chip 1 did not perform calibration
P20 channels
68
400 electrons/ADU

## Slide 8: Laser characterization: test stand
Laser head on 3D platform ( 5 um accuracy):
  Gaussian profile with microspot width 2s < 10um
  Wavelength 1080 nm
  Pulse duration < 1ns
  Pulse energy  10% gaussian fluctuation.

## Slide 9: Laser Longitudinal scan
. Laser scanned along the polysilicon electrode
(S1L S1 S1R )
(S2L S2 S2R)
. Poly-Si Electrode
Near Side
. Al via
Far Side

## Slide 10: Longitudinal coordinate from Qdiv
Naïve computation of position along the strip:
Fit residuals within ± 50 um band !!!
[mm]

## Slide 11: Longitudinal coordinate: Simulation vs. measurement
Spice simulation using electrical parameters
five strips (Rstr, Ccou, Rmet).
interstrip circuital elements (Cint, Rint, Cm, Cp).
bulk representation (Rsub, Csub).
Overall shape reproduced.
Bias introduced by direct coupling of the pulse to the Al via.

## Slide 12: SNR determination
Laser characterization demonstrated the soundness of the charge division method for strip sensors.
Increased level of noise but not much (900 ENC)
In the real world:
  What signal/noise ratio we should expect for a MIP particle ?
  ↓
  Sr90 beta source
  120 GeV Pion test beam at SPS.

## Slide 13: Sr90 Beta source
Collimated (1mm) b-source, at the strip center
Signal / Noise  15
15000 Electrons
14000 Electrons

## Slide 14: Test Beam @ SPS
During the first week of October testing at SPS pion beam in parasitic mode:
  Standalone Testing (ALIBAVA daq) around 800Kevt.
  Inside the EUDET mimosa telescope (APV25 daq)

## Slide 15: Test Beam @ SPS (2)
SPS beam very stigmatic along the longitudinal (strip) direction.
Last run with ALIBAVA as DUT inside EUDET telescope (BUT TLU too long trigger delay)

## Slide 16: Test Beam @ SPS (3)
Signal Spectrum
& pulse shapes

## Slide 17: Short term plans
Almost all the data to be analyzed from the test beam: ALIBAVA & AVP25 (Including EUDET telescope tracking).
New 2D strip sensor of larger dimensions (3 cm) already produced at CNM.
Designed with contacts at both strip ends to be read out by two independent FE chips.

## Slide 18: A longer desmostrator
Each wafer: one reference sensor, poly sensor and two DML integrated PA sensors
Reduced polysilicon resistivity (366 and 84 Ohm/□)
Modified ALIBAVA daughter board to boh side read out

## Slide 19: Conclusions
We have demonstrated the feasibility of the charge division method in microstrip sensors to determine the coordinate along the strip.
Resolution in the determination of the strip coordinate about few tens of micron.
We have used the standard (cheap) technology to produce this genuine 2D single sided strip detector.
Possible application targets:
  Future detector outer trackers (trigger capable modules)
  Ion tracking systems.
  Neutron imaging (+ conversion element).
  Space applications.
New few cm long demonstrator under preparation

## Slide 20
THANK YOU

## Slide 21
BACK-UP

## Slide 22: Signal directly induced in the metal via from sensor far side (1)

## Slide 23: Signal directly induced in the metal via from sensor far side (2)

## Slide 24: Signal directly induced in the metal via from sensor far side (3)

## Slide 25: Signal directly induced in the metal via from sensor far side (4)