## Slide 1: Annealing in n and p-side readout of silicon microstrip detectors after irradiation to LHC and sLHC doses
G. Casse, A. Affolder, P. P. Allport, V. Chmill, P. Dervan, A. Greenall, I. Tsurin, T. Huse, C. Wigglesworth, J. Vossebeld

## Slide 2: CONTEXT:
Two rather recent results from studies performed for preparing high resolution sensors for the future supercolliders (sLHC at CERN) have proven that silicon detectors can be used for tracking minimum ionising particles (mip’s) after doses above 2x1016 neq cm-2. These are the discovery of the charge multiplication mechanism taking place in irradiated n-in-p silicon detectors and the suppression of the reverse annealing. A discussion of this last feature is here presented with the implications for the running scenario in the actual experiments.

## Slide 3
Evolution of Sensor Properties After Irradiation
Evolution of VDEP shows dependence on both temperature and time
spent after irradiation.
Require full depletion (and some) of sensor in order to optimise CCE.
ILEAK Shows strong temperature.
(Typical behaviour for a silicon microstrip sensor).
Sensor leakage current (ILEAK), depletion voltage (VDEP) and charge collection efficiency (CCE) are all affected by irradiation.
Need to avoid the sensors being warm (> 0 oC) for long periods of time!

## Slide 4
The Hamburg parameterisation is believed to best fit the available data to predict VDEP.
However, large differences observed between the predictions of the TDR model and the Hamburg model.
Origin is in reverse annealing contribution DNY to the predicted change in effective doping concentration DNEFF:
Comparison of Hamburg Model and ATLAS TDR Parameterisation
TDR model parameterised reverse annealing as a second order process
(dNY=-k·dNX2·dt) NY(t)=NX,0(1-(1+k·NX,0 ·t)-1).
Hamburg model parameterises reverse annealing as a modified first order process.
(dNY=-1/t·dNX·dt) NY(t)=NX,0(1-exp(-t/t))
Need high fluence + long annealing data to compare to predictions of both models.

## Slide 5
Re-Evaluating the Evolution of VDEP and ILEAK in the SCT
Paul Dervan, Joost Vossebeld, Tim Jones (Liverpool), Taka Kondo (KEK), Graham Beck (QMUL), Georg Viehhauser (Oxford), Steve McMahon (RAL), Koichi Nagai (Brookhaven), Kirill Egorov (Indiana), Richard Bates, Alexander Bitadze (Glasgow).
An updated LHC luminosity profile now exists.
Maintenance/shutdown time and cooling temperatures reviewed in line with:
Achievable coolant temperatures.
Insertable B-Layer installation.
Possibly longer maintenance.
VDEP predictions suggest 450 V (max for SCT) is sufficient for at least 10 years operation.

## Slide 6
Sensor performance traditionally studied by determining VDEP from CV measurements.
The rate of annealing is a function of temperature, therefore it is possible to slow it down or accelerate it relatively to a given temperature. Previous studies have found an Arrhenius relation for temperature dependence of the reverse annealing of VDEP with an activation energy Ea = 1.31 eV. With a reference temperature of 20oC, the acceleration factors are about 540 at 60oC and 7350 at 80 oC.
In Liverpool the focus has been on measuring the annealing of CCE
The p-in-n case.
Manufacturer | HPK
Wafer Tech. | FZ
Structure | p-in-n
Size | 1 cm x 1 cm
Thickness | 285 µm
Programme of Accelerated Annealing Measurements
New programme of accelerated annealing measurements on ATLAS mini sensors.
Pair of sensors irradiated with neutrons at Ljublijana (V. Cindro et al) to 2x1014 1 MeV neq cm-2
(new prediction for SCT = 1.6x1014 1 MeV neq cm-2).
One sensor used for CCE measurements and one sensor used for VDEP measurements.
Both sensors annealed together at same temperature for same length of time.

## Slide 7
Charge Collection Measurements
90Sr fast electron source used to generate signal.
Readout triggered by scintillator.
Charge collection measured using
analogue electronics chip (SCT128A or Beetle) clocked at LHC speed (40 MHz clock, 25 ns shaping time).
System calibrated to most probable value of MIP energy loss in non-irradiated 300 m thick sensor (~ 23000 e).
Experimental Setup and Analysis Procedure
Depletion Voltage Measurements
VDEP Determined by standard method of measuring the VBIAS at which 1/C2 saturates.
Both sets of measurements performed in freezer at temperature of ~-25 oC with N2 flush.
@ 1 kHz

## Slide 8
Smooth fall off after ~ 100 days @ 20 oC
Results of Charge Collection Measurements
SCT Default threshold 1 fC (~ 6.2 ke)
No sharp drop in the collected charge
Above ~ 500 V collected charge remains almost constant in time

## Slide 9
Comparison of Predicted VDEP and Measured VDEP
Data shows a slower annealing effect than the two models

## Slide 10
This discussion is relevant to the present tracker sensors in the LHC experiments. The future experiments on sLHC will make large use of n-side readout sensors, possibly n-in-p.
The annealing of n-in-p sensors is different again: the reason is that the effect of charge multiplication plays a role.

## Slide 11
Evidence of a charge multiplication effect: not only the whole charge is recovered, but increased by f = 1.75/2.1
140 and 300 mm n-in-p Micron microstrip sensors after 5x1015 neq 26MeV p
11

## Slide 12
Accelerated Annealing of the collected charge, case of n-in-p sensors. HPK FZ n-in-p, 1E15 neq cm-2
Neutron irradiations in Ljubljana, neutrons are dominating the radiation damage > 25 cm radius.

## Slide 13
Annealing of the colleted charge, Micron FZ n-in-p, 1E15 n cm-2 (26MeV p irradiation)

## Slide 14
Accelerated CCE Annealing 1.5E16 neq cm-2 (Micron sensors)
Irradiated with 26MeV protons (Karlsruhe).

## Slide 15
Annealing of the reverse current, n-in-p sensors, 1E15 and 1.5E16 n cm-2

## Slide 16
Room Temperature Annealing of the collected charge, HPK FZ n-in-p, 2E15 n cm-2 ( 26MeV p irradiation)
We make large use of accelerating annealing: is this a safe and correct approach?

## Slide 17
Room Temperature Annealing of the collected charge, HPK FZ n-in-p, 1E16 n cm-2 (26MeV p irradiation)
We make large use of accelerating annealing: is this a safe and correct approach?

## Slide 18
Room Temperature Annealing of the reverse current, n-in-p sensors, 2 and 1E16 n cm-2 (26MeV p irradiation)
NOISE

## Slide 19
Comparison of the Accelerated and Room Temperature Annealing of the reverse current, HPK FZ n-in-p, 2E15 and 1E16 neq cm-2

## Slide 20: CONCLUSIONS
The CCE measurements with both p-in-n and n-in-p sensors show discrepancies with accepted annealing features as measured with CV methods and as predicted by widely accepted parameterisations. In practical terms, the changes with annealing of the CCE sensors after LHC doses (microstrip sensors) are less severe than anticipated.
With n-in-p sensors the reverse annealing seems suppressed when the study is performed by accelerating the annealing at 60 and 80 oC (maximum voltage 1100V). Nonetheless the rescaling of the accelerated annealing to RT could be wrong at least when applied to the CCE. The reason could be the rescaling criterion itself, or a different evolution of the effective space charge triggered by temperatures between 20 and 60-80 oC.
Controlled annealing (at 200C) is still a very useful tool to reduce power dissipation and recover fraction of S/N in heavily irradiated silicon detectors. The discrepancies between the accelerated and RT annealing need to be studied to base the prediction for the changes of CCE with time according to the real operation and maintenance temperatures in the experiments.