## Slide 1: Cable splices and instrumentation for DFM system
J. Fleiter and A. Ballarino with contributions from WP6a members
DDR DFM meeting 18th of January 2022

## Slide 2: Outline
Cable splices of DFM
List of Instrumentation of DFM
    Electrical Protection
    Cryogenic operation
    Vacuum instrumentation
Instrumentation feedthroughs of DFM

## Slide 3: Overview of electrical circuits of MS
5 circuits per MS SC Link
    D2: 2 cables rated for 18 kA
    MCBRD : 8 cables rated for 0.6 kA
Current rating, Circuit Time Constants, Protection and electric insulation tests levels defined in EDMS 2659857

## Slide 4: Description of branch of circuit of SC Link
Each branch of circuit of SC Link in DFM consists of:
NbTi/NbTi
Splice
MgB2/Nb-Ti
Splice
NbTi
cables
Plug
NbTi
cables
MgB2
  Sc cables
    Nb-Ti bus bars
    MgB2 cable
  Splices
    Nb-Ti/Nb-Ti
    MgB2/Nb-Ti
WP3

## Slide 5: Sc Cables
MgB2 cable
Nb-Ti cable
Bus bar review April 2021 indico 1021628
Copper core
Nb-Ti wire, Type 01, 1.07 mm OD
Nb-Ti wire, Type 02, 0.825 mm OD
18 kA cable
0.6 kA cable

## Slide 6: Nb-Ti/Nb-Ti cables splices
Geometry of splices identical to the one defined in Internal review of busbars and splices Apr-14..16, 2021 EDMS@2544721
18 kA splice
  Sn96Ag4 with Pre-tinning (221°C)
  Soldering length 150 mm
  Cu OFE
  Flux MOB39
0.6 kA splice
  Sn96Ag4 with Pre-tinning (221°C)
  Soldering length 100 mm
  Cu OFE
  Flux MOB39

## Slide 7: MgB2/Nb-Ti cables splices
MgB2/Nb-Ti splices of DFM with same geometry as the one of DFX
18 kA splice
  Sn-Pb (183°C)
  Soldering length 200 mm
  Cu OFE
  Flux MOB39
0.6 kA splice
  Sn-Pb (183°C)
  Soldering length 200 mm
  Cu OFE
  Flux MOB39
MgB2
NbTi
NbTi
Insulation of splice
Cu OFE

## Slide 8: Splices assemblies
Nb-Ti/Nb-Ti splices
  splices maintained together via insulating structure
  Splice assembly is a fix point vs cryostat
MgB2/Nb-Ti splices
  splices maintained together via insulating structure
  Splice assembly is a sliding point vs cryostat (free to rotate and to slide with amplitude of +/-20 mm)
insulating structure not shown
Assembly of splice inspired from the DFX, exact arrangement under finalization

## Slide 9: SC Link electrical instrumentation
Each branch of circuits equipped with 14 Vtaps for the protection of:
  Current lead heat exchanger
  SC cables (HTS, MgB2, NbTi)
  Splices (HTS/MgB2, MgB2/NbTi and NbTi/NbTi)
Same layout for all branches of circuits (0.6-18 kA) IT and MS
Requirements for the protection of the SC-Links components presented by A. Ballarino in cold powering review July 2017 (Indico/643197)
4 Vtaps placed in the DFM will be routed out at the level of DFM
HL-LHC Circuit Voltage Taps Layout of SC Link (EDMS 2411822 )
Engineering Specification: Instrumentation of the Cold Powering System EDMS 2512704 and 2591698

## Slide 10: Cryogenic instrumentation of DFM
Cryogenic instrumentation of DFM :
8 Thermal transducers (TT)
  Two in vacuum attached to He vessel (Cernox)
  4 in the splice box (He vessel) (Cernox)
  2 temperature sensors attached to the resistive heaters (PT100)
5 Heaters
  1 GHe/LHe Heat exchanger
  2x100 W resistive Heaters in external bath (includes 1 spare)
  2x100W resistive heater in the lower bath (includes 1 spare)
1 He pressure gage
Two LHe level transducers
Cryo control valves are part of cryo jumper
For a safe operation of SC Link system, during nominal operation but also during transients, dedicated cryo instrumentation is required.
PID LHCLSQRG0042-V0
Engineering Specification: Instrumentation of the Cold Powering System EDMS 2512704 and 2591698

## Slide 11: Vacuum instrumentation
Each SC Link system made of three vacuum volumes DFM, DSHM and DFHM (EDMS1824906)
DFM equipped with vacuum ports to plug pumping units and/or vacuum instrumentation
=> no wiring in the vacuum vessel
EDMS 1824906

## Slide 12: Feedthrough for instrumentation of SC-Link
DFM equipped with four feedthroughs:
  Type 1 vac. temp probes DN ISO-K-SubD connector
  Type 2 LHe level gage DN ISO-K-SubD connector
  Type 3 40 Vtaps IFS L-Type
  Type 4 Heaters and TT DN ISO-K-SubD connector
12
Type 1
Type 3
Type 2
Type 4

## Slide 13
Conclusions
  Geometry of splices (including insulation) finalized
  Splices arranged in assemblies per type (NbTi/NbTi and NbTi/MgB2)
  List of instrumentation for cryo and electric protection defined
  Feedthroughs of instrumentation defined, type of connector to be confirmed together with CRG and MPE