## Slide 1: Results from Single Event Effect Tests with MIMOSIS-1
Benedict Arnoldi-Meadows
for the CBM-MVD Collaboration
IWORID2022, June 28th, 2022.

## Slide 2: The CBM Micro Vertex Detector (MVD)
CBM
CBM-MVD
The CBM – MVD will operate at:
100 kHz Au+Au collisions (10 MHz beam)
10 MHz p + Au collisions
Beam hole: 11mm
Todays topics:
What if the beam ions miss the hole?

## Slide 3: Requirements on the MIMOSIS sensors
 | Requirement
Spatial / time resolution | ~5 µm / 5 µs
Sensor thickness | ~50 µm
Radiation doses (non-ionizing) | ~ 7 x 1013 neq/cm²
Radiation doses (ionizing) | ~ 5 MRad
Rate capability (mean/peak) | (20/80) MHz/cm²
Readout mode | Continuous
Established by ALPIDE
(Sensor of ALICE ITS2 upgrade)
~10 x ALPIDE
Incompatible with ALPIDE
> 20x internal bandwidth needed
Idea:
Get inspiration from ALPIDE:
Re-use pixel analog front-end.
Re-use priority encoder.
Complement design with:
High bandwidth internal DAQ.
Fully depleted pixels ( > 20 V top bias).
…
MIMOSIS-0 (2018)
Confirm (depleted) pixels and priority encoder
MIMOSIS-1 (2020)
Full size prototype, this work
MIMOSIS-2 (2022)
Advanced rad. hardening, data compression…
MIMOSIS-3 (2023/24)
Final sensor

## Slide 4: Origin of heavy ion impacts
Beam
Beam hole: 11 mm
Beam halo
Origin: Limited focus - few ions miss hole all the time.
Our assumptions:
  Geometry still (measured at SPS – NA61/SHINE)
  Assume 1 kHz/cm² thanks to collimators.
1 cm
M. Deveaux for NA61/SHINE, SQM 2017
SPS Pb beam halo @ NA61/SHINE
as seen with MIMOSA-26
Beam loss
Direct beam impact to MVD due to steering fail.
Highest rate: ~300 MHz/cm² Au ions in MVD
Target fragments
Nuclear fragments kicked out of target by beam.
Very slow: Absorbed by first station.
Highest energy transfer: 35 MeV cm²/mg
More information on simulation:
H. Darwish, CBM Progress Report 2020
MIP (proton)
~2 fired pixels
~2x2 mm
Heavy ion:
~200 fired pixels

## Slide 5: Effect of heavy ion hits on electronics
Heavy ions show high dE/dx or LET:
Scales with z² of the projectile => Au = 6200 M.I.P
Bethe Bloch: "Slow" ions create higher LET than relativistic ions.
Minority charge carriers excited by ions may:
Break transistor gates => Gate rupture
Switch digital electronics => Bit flip
Open unwanted conduction paths => Latch-up
(like short cut, extinguish by power cycle)
Macroscopic damage by individual ion: Single Event Effect.
Irreversible destruction
Thermal destruction if ignored
Malfunction if ignored
Latch-up: Vulnerable structure
Unwanted current
SEE cross section: (JESD57A standard)
SEE probability: size independent.

## Slide 6: What do we know?
Data: ALPIDE measured
(may not represent final sensor)
CBM - MVD | Requirement | Remark
LET tolerance (gate rupture) | > 35 MeV cm²/mg | Fulfilled by ALPIDE (same process)
Flux tolerance @ 12 MeV cm²/mg | ~ 300 MHz/cm² | no damage for > 150 µs (until beam stop)
SEE per sensor @ 12 MeV cm²/mg | < 3 x 10-7cm² | < 1 SEE/h (in 1 kHz Au beam halo)
CBM - MVD | Requirement | Remark
LET tolerance (gate rupture) | > 35 MeV cm²/mg | Fulfilled by ALPIDE (same process)
Flux tolerance @ 12 MeV cm²/mg | ~ 300 MHz/cm² | no damage for > 150 µs (until beam stop)
 | < 3 x 10-7cm² | < 1 SEE/h (in 1 kHz Au beam halo)
ULTIMATE for STAR PXL detector
Latch-ups for particles with LET > 3 MeV cm²/mg.
Sensor destruction during experiment observed.
Old AMS 0.35 µm process
H. Hillemanns, https://tinyurl.com/23dn8pdy, retrieved 10.06.2022
CBM: Max
CBM: Min LET
Latch-ups in digital part only
Tower Jazz 180 nm
ALPIDE for ALICE-ITS2
ALPIDE: Valuable guideline (same Tower Jazz 180 nm process as MIMOSIS).
But: MIMOSIS has different digital electronics => Must remeasure.

## Slide 7: The sensor under test: MIMOSIS-1
produced in TowerJazz CIS 180nm process
MIMOSIS-1, 60µm thick
Hardening strategy for MIMOSIS:
"Latch up" protective design rules.
Bit error correction for important status registers (Hamming encoding).
Triple retundancy of important state machines (future MIMOSIS-2).
Data registers remain unprotected.
Dark rate: < 1e-6
More Details: H. Darwish, poster 137, this conference.
 | MIMOSIS - 1
Spatial/time resolution | ~5 µm/5 µs
Thickness | 60 µm
Rate (average/peak) | 20 / 80 MHz/cm²
Pixel | > 20V top bias fully depleted
MIMOSIS – 1 in-beam performance

## Slide 8: Initial experimental strategy
PC
Oscilloscope
Information available to experimenters
Current [a.u.]
Time [2s/div]
Dosimetry foil
Approx.
Beam spot
Latch-up detection/protection:
Over-current detection.
Automatic shut down, manual counting.
Bit flip detection:
No/few bit flips expected.
Manual read-back of slow control data.
IAnalog
Latch-up protection PCB
Slow control
IDigital
Voltage signal proportional to currents
Beam line | Beam | LET
GSI (mCBM) | Pb, 1.05 A GeV | 12 MeV cm² / mg
GSI (mCBM) | Xe, 1.3 A GeV | 5 MeV cm² / mg
Beam intensity up to 20 MHz/cm²
Dosimetry: Beam instrumentation, foil (both not really accurate)
Few hours in
Parasitic mode

## Slide 9: Observations (~ 1 A GeV ions)
I
t
10s
 | Pb, 12 MeV cm² / mg | Xe, 5 MeV cm² / mg
LU |  | 17
Bit flip |  | 149
Ions on sensor | ~ 3 x 109 | ~ 1011
per 5.3cm² sensor | 1.2 x 10-7 cm² | LU: 9 x 10-10 cm² BF: 8 x 10- 9 cm²
 | Pb, 12 MeV cm² / mg | Xe, 5 MeV cm² / mg
LU |  | 17
Bit flip |  | 149
Ions on sensor | ~ 3 x 109 | ~ 1011
 | 1.2 x 10-7 cm² | LU: 9 x 10-10 cm² BF: 8 x 10- 9 cm²
Uncertainty rough factor 3 (dosimetry)
Expected:
"Latch-ups"
Not expected:
Bit flips exist and modify currents.
=> False LU – signatures?
LU cross section seems in acceptable range.
High bit flip cross-section.
Bug in Hamming Code implementation. Fixed in MIMOSIS-2.
Recovery may require hard reset…
BF if recoverable with soft reset.
71
LU if not recoverable with soft reset.
Results match requirements. Sensor bug spotted and fixed.
Hard to distinguish BF and LU, major bias possible.
preliminary

## Slide 10: Test at GSI - M3 beam line
LET [eV/Å]
500
0
3.3 AMeV Ca
on Si (SRIM)
Not fully to scale
Substrate
ROI
 | M3 @ GSI UNILAC
Energy / ion type | 3.2 A MeV Ca
Beam spot | 1.5 x 1.5 cm² mostly uniform
Beam time structure | 5 Hz pulses of 6 ms
Beam intensity (mean) | ~ 107 Hz/cm²
Beam intensity (pulse) | 400 MHz/cm²
Dosimetry | Dedicated installation
Low beam energy: Sufficient to reach vulnerable structures?
OK
New strategy:
Use masks to isolate building blocks (most sensitive and representative as chosen by the designers)

## Slide 11: Results
 | 3.2 A MeV Ca 20 MeV cm² / mg
Latch - ups | 0
ROI (all except DAC) | 3.2 cm²
Ions on ROI [1/cm²] | > 3 x 1010 / cm²
per 5.3cm² sensor | 1.5 x 10-10 cm²
 | 3.2 A MeV Ca 20 MeV cm² / mg
Latch - ups | 0
ROI (all except DAC) | 3.2 cm²
Ions on ROI [1/cm²] | > 3 x 1010 / cm²
 | 1.5 x 10-10 cm²
Observation on DAC:
Bit flips in DAC generate current fluctuation.
  will shrink after Hamming code bug fix.
Cross-section not acceptable
  will shrink after Hamming code bug fix.
System instable, no detailed study possible.
Latch-up:
Previous observed latch-ups likely falsely interpreted bit flips in DAC.
Latch-up cross-section orders of magnitude better than required (all structurs except DAC) .
No latch-ups observed (but sensor senses ions).
=> Why discrepancy with previous results?
Pulses: Few 106/cm²
No beam
MIMOSIS-1
ROI = DAC
preliminary

## Slide 12: Outlook: Bit flip cross-sections
ca. 30 µm
Micro-Beam: Microscope view of the pixel area
Block | Window size | Ions | Bit flips to (1/0) | p [1]
DAC digital part | 320 x 40 µm² | 148/µm² | 1140/902 | 1 x 10-4
RAM | 50 x 80 µm² | 528/µm² | 3030/4278 | 6 x 10-3
Result depends on good choice of window. => Numbers subject to update.
Reminder:
Should be 5x10-8 over full sensor.
Beam diameter (500 nm)
Further data analysis needed (e.g. consider surface of RAM cells, beam to device alignment etc.)
Preliminary conclusion:
Protection of status registers indeed required.
Expect <200 data errors /s and sensor in the MVD.
Beamline: GSI UNILAC X0
Beam: 4.8 A MeV Ca
Beam intensity: ~120 Hz
Beam diameter: 500 nm, raster scan possible.
Mode: Write and read back RAM.
Work in progress

## Slide 13: Summary
MIMOSIS will be the sensor of the CBM-MVD.
5 µs, 5µm resolution, 80 MHz/cm² peak rate, continuous readout.
1024 x 504 pixels of 27x30 µm² pixels (fully depleted).
MIMOSIS-1 was tested for its tolerance to heavy ion impacts at GSI.
Latch-up cross section <1.5 x 10-10 cm² at LET 20 MeV cm²/mg
Beam intensity similar to beam loss scenario => successfully tested
Unexpectedly many bit flips:
  Bug in the Hamming code protection of status registers found and fixed.
  Expect problem solved for MIMOSIS-2
Data for measuring bit flip cross-sections was taken, analysis under progress.
So far: MIMOSIS-1 matches the requirements of the CBM-MVD.

## Slide 14: CBM-MVD collaboration members
Julio Andary1, Benedict Arnoldi-Meadows1, Ole Artz1, Jérôme Baudot2, Grégory Bertolone2, Auguste Besson2, Norbert Bialas1, Roma Bugiel2, Gilles Claus2, Claude Colledani2, Hasan Darwish1,2,3, Michael Deveaux3, Andrei Dorokhov2, Guy Dozière2, Ziad El Bitar2, Ingo Fröhlich1,3, Mathieu Goffe2, Fabian Hebermehl1, Abdelkader Himmi2, Christine Hu-Guo2, Kimmo Jaaskelainen2, Oliver Michael Keller6, Michal Koziel1, Franz Matejcek1, Jan Michel1, Frédéric Morel2, Christian Müntz1, Hung Pham2, Christian Joachim Schmidt3, Stefan Schreiber1, Matthieu Specht2, Dennis Spicker1, Joachim Stroth1,3,4, Isabelle Valin2, Yue Zhao2, Roland Weirich1 and Marc Winter2,5 1Goethe-Universität Frankfurt, Germany 2Université de Strasbourg, CNRS, IPHC UMR 7178, Strasbourg, France 3GSI Helmholtzzentrum für Schwerionenforschung GmbH, Germany 4Helmholtz Forschungsakademie Hessen für FAIR, Germany 5IJCLab, UMR9012 – CNRS / Université Paris-Saclay / Université de Paris, France 6Facility for Antiproton and Ion Research in Europe GmbH,Germany
Supported by:
(05P19RFFC1)