## Slide 1
System development of Silicon Photonics links for CERN Experiments and Accelerators
Carmelo Scarcella, S. Detraz, M. Lalovic, L. Marcon, L. Olantera,
T. Prousalidi, U. Sandven, C. Sigaud, C. Soos, J. Troska
CERN EP-ESE-BE
22nd September 2022
TWEPP 2022
carmelo.scarcella@cern.ch

## Slide 2
Future high-speed links for High Energy Physics at CERN
Silicon Photonics as promising technology
Experimental results on µ-ring optical modulators
Future activity
TWEPP 2022
2
carmelo.scarcella@cern.ch

## Slide 3
Particle sensor
PIC
>> 100 m Single-mode fiber
Future HEP link architecture
Photonic Integrated Circuits (PICs)
Wavelength division multiplexing:
  Lane: 25 Gbps NRZ
  Fibre: 100 Gbps
Laser sits outside of radiation environment
Low power / Low mass
  Depending on the level of integration
RadHard “promise”
System concept
TWEPP 2022
carmelo.scarcella@cern.ch
3
CERN EP R&D programme WP6

## Slide 4
Particle sensor
PIC
>> 100 m Single-mode fiber
Future HEP link architecture
Photonic Integrated Circuits (PICs)
Wavelength division multiplexing:
  Lane: 25 Gbps NRZ
  Fibre: 100 Gbps
Laser sits outside of radiation environment
Low power / Low mass
  Depending on the level of integration
RadHard “promise”
System concept
TWEPP 2022
carmelo.scarcella@cern.ch
4
CERN EP R&D programme WP6

## Slide 5
PIC
DC Lasers
Rx channel
Tx channel
Photodiode
Modulator
Particle sensor
Single-mode fiber
Front-end optical transceiver
TWEPP 2022
carmelo.scarcella@cern.ch
5
Silicon Photonics Integrated Circuits (PICs)
CMOS technology
  Fiber couplers
  Silicon waveguides
  Optical modulators
  Germanium photodiodes
Second iteration of PIC designed at CERN
  Radiation tolerance study
  Data link development
5 mm
Silicon Photonics test chip (PIC)
450 nm

## Slide 6
PIC
Single-mode fibers
2.92 mm coaxial connector
TWEPP 2022
carmelo.scarcella@cern.ch
6
High-speed “driverless” test board
PIC mounted onto a test board with access to electrical and optical ports
Wide open eye diagram at 25 Gb/s
Electro-optical response shows ~ 20 GHz bandwidth
Moderate return loss |S11|
25 Gb/s optical eye diagram

## Slide 7
TWEPP 2022
carmelo.scarcella@cern.ch
7
Ring modulator coupled to a commercial driver
Driverless test board connected to commercial driver evaluation board
  1 V peak-to-peak driving strength
  wide open optical eye diagrams, 26.5 Gb/s NRZ and 26.5 Gbd PAM4
PAM4 modulation involves trade-oﬀ between optical SNR and electrical driver speed
NRZ 26.5 Gb/s
PAM4 26.5 Gbd (53 Gb/s)

## Slide 8
TWEPP 2022
carmelo.scarcella@cern.ch
8
Resonance wavelength tuning
Ring modulators are highly selective wavelength filters
Resonance wavelength (λres) depends on environmental and fabrication parameters
λres needs to be aligned to the input laser
Thermo-optic effect in Silicon to adjust λres (Δλres ~70 pm/°C)
Tungsten µ-heater on top of the ring waveguide for local and active tuning of λres
λres
input
laser
SiO2
µ-heater
Si waveguide
10 µm
input laser
20 µm
Temperature
300 K
400 K
From 17 °C to 34 °C

## Slide 9
TWEPP 2022
carmelo.scarcella@cern.ch
9
Control system for wavelength stabilisation
System that automatically locks the ring to the input laser wavelength
Measurement of photodiode current and steering of heater current
Change in steps the input wavelength (): equivalent to changing device temperature
OMA
Electrical
Data in
µ-heater
Optical data out
Input laser
Δλ(V)
Photodiode
PID controller
Δλ(T)
Drop port
+
-
error
setpoint

## Slide 10
TWEPP 2022
carmelo.scarcella@cern.ch
10
4 channel WDM demonstration block diagram
Wavelength division multiplexing (WDM)
4-channel external laser COMB with ~ 5 nm wavelength grid spacing
Ring modulators driven by a 2-channel pattern generator
4 wavelengths separated using DEMUX and measured using oscilloscope
Single-mode fiber
1545 nm laser
1550 nm laser
1555 nm laser
1560 nm laser
MUX
PIC
SCOPE
Amplifier
pattern generator
MUX
DEMUX
DC laser COMB
Modulated outputs
Notes: 10

## Slide 11
TWEPP 2022
11
4-channel WDM transmitter - Measurement results
carmelo.scarcella@cern.ch
500 µm
Bond pad
Optical waveguide
DC laser COMB
Modulated outputs
Notes: 11

## Slide 12
TWEPP 2022
12
4-channel WDM transmitter - Measurement results
Wide open 4x25 Gb/s NRZ optical eye diagrams
Good channel uniformity
carmelo.scarcella@cern.ch
DC laser COMB
Modulated outputs
Electrical data in
Notes: 12

## Slide 13
carmelo.scarcella@cern.ch
13
TWEPP 2022
carmelo.scarcella@cern.ch
13
Conclusions
Presented the progress on the system development on Silicon Photonics links for HEP
Uplink
  25 Gb/s NRZ and 25 Gbaud PAM4 operation of ring modulators integrated on CERN PIC
  Compensation of slow temperature changes by thermally tuning the ring modulator resonance wavelength
  First demonstration of 4x25 Gb/s Wavelength Division Multiplexing (WDM) transmitter
Downlink
  Demonstration of radiation tolerant receiver based on Silicon Photonics presented during TWEPP 2021

## Slide 14
  New PIC design iteration
  Tape out on the 5th October 2022
  Turn around time 12 months!
TWEPP 2022
carmelo.scarcella@cern.ch
14
Next photonic test chip
  Radiation tolerance
    Modelling radiation damage
    Radiation tolerance enhancement by design
  Data link design
    Thermal control of ring modulators
    Integration of modulators with electrical drivers
    Wavelength Division Multiplexing
    Aligning with industry emerging standards for COTS components

## Slide 15
TWEPP 2022
carmelo.scarcella@cern.ch
15
Back-up slides

## Slide 16
Selective wavelength filters
Small footprint (radius ~ 5µm)
Small driving voltage amplitude (down to 1 Vpp)
Optically narrowband (< 1nm)
Thermally sensitive (< 1 K)
carmelo.scarcella@cern.ch
16
Si µ-ring modulator
TWEPP 2022
Input
laser
CERN custom design
10 µm
V
Waveguide cross-section
Reverse biased pn Junction
+
-
Electrical contacts
Waveguide
V0
V1
Electrical
data
Optical data
Input laser
Δλ(V)
p-n junction

## Slide 17
TWEPP 2022
carmelo.scarcella@cern.ch
17
4 channel WDM transmitter
Wavelength division multiplexing (WDM)
Four ring modulators coupled to the same waveguide
Ring radius difference induces uniformly spaced resonance notches
4-channel external laser COMB with ~ 5 nm wavelength grid spacing
Resonance wavelength of each modulator aligned to the corresponding laser using thermal tuning
CW laser COMB
Modulated outputs
r r+∆L r+2∆L r+3∆L
r = radius

## Slide 18
Radiation tolerant receiver based on on-chip Ge photodiode and transimpedance amplifier (TIA)
Downstream requires relatively low data rate (2.56 / 5.12 Gbps)
First demo using GBTIA (5 Gbps radiation-hard optical receiver)
Open eye diagram at the output of the receiver board
Receiver sensitivity ~ - 10 dBm
Ge PD
Downstream
GBTIA
PIC
Digital Data out
TWEPP 2022
carmelo.scarcella@cern.ch
18
SiPh radiation tolerant receiver demonstration
Presented to TWEPP 2021, T. Prousalidi et al., “Towards Optical Data Transmission for High Energy Physics using Silicon Photonics”