## Slide 1: Measuring charged-particles with 10ps time resolution using innovative 3D trench-type silicon pixel sensors
Alessandro Cardini, INFN Cagliari
on behalf of the TimeSPOT Team

## Slide 2: Outline
Challenges in tracking at high luminosities
The development of the TimeSPOT 3D trench pixels
Experimental results
Conclusions and outlook
TimeSPOT 3D-trench pixels in a strip-like configuration
55µm x 55 µm

## Slide 3: Present and future challenges in tracking
Future and today’s upgraded colliders will operate at extremely high instantaneous luminosities
  Very important radiation damage to tracking detectors
  Extremely difficult event reconstruction due to large pile-up  adding the time information (at the track or hit level) will help recovering tracking and vertexing capabilities
ATLAS & CMS Phase-II upgrades (2026): mostly “traditional” tracker + single timing layer
  𝜎t ≈ 30 ps, 𝜎s ≈ 100-300 µm, F ≈ 1015 1 MeV neq/cm2
LHCb Upgrade-2 (2030s): time information on each pixel
  𝜎t = 30-50 ps, 𝜎s ≈ 10 µm, F = 1016 to 1017 1 MeV neq/cm2
FCC-hh (2040s ?): further improve the radiation hardness
  𝜎t = 10-20 ps, 𝜎s ≈ 10 µm, F = 1017 to 1018 1 MeV neq/cm2
LHCb upgrade-2 Workshop, March 2020
Adding time information
LHCb
Adding the track time information
Spatial resolution, time precision and radiation hardness are required at the same time!  4D tracking detectors

## Slide 4: Requirements for (some) future upgrades
Possible users of 4D tracking detectors: LHCb Run5, NA62(x4), CMS-PPS & ATLAS-AFP Run4, FCC-hh, …
  O(10µm) spatial resolution, requiring a pixel pitch of O(50µm)
  Hit time stamping better than 50 ps (sigma) on the full chain (sensor + FEE + digitization)
  Radiation hardness to high fluences for sensors: 1016 ÷ 1017 1 MeV neq/cm2
  Radiation hardness to high doses for electronics: >1 Grad
  A detection efficiency of 99% per layer is usually needed (this also requires a high fill factor)
  The material budget must be kept below 0.5÷1.0 % X0 per layer
  The FEE should provide the required time resolution at O(10 µW/pixel) and should be capable of handling a huge data amount of data O(100 Gbps/cm2)

## Slide 5: Why 3D sensors?
Original idea: S. Parker, 1997
Key points
  Short inter-electrode drift distance (tens of µm) give rise to extremely fast signals (d<<L)
  Active volume and electrode shape can be designed for maximum performance
  Unmatched radiation hardness (> 1017 1MeV neq/cm2, NIMA, 979 (2020) 164458)
  3D columnar geometry is a production-ready technology (ATLAS IBL, ATLAS-P2)
p+
n+
n
h
e
p+
n+
n
h
e
d
Planar sensor
3D sensor
L

## Slide 6: Limits to the time resolution of a 3D sensor
𝜎tw : the time-walk effect can be eliminated by triggering at a constant fraction of the signal amplitude
𝜎dr : jitter due to delta-rays - negligible in a 3D sensor since all the charge deposits created at various depths contribute in the same way at the total signal because the charge collection occurs in a direction which is perpendicular to the charged particle path (and in general to the delta-rays produced)
𝜎un : non-uniformities in the weighting field and charge carrier velocities inside the detector sensitive unit give the ultimate limit on the time resolution that can be achieved with a 3D sensor
𝜎ej : the analog noise of the preamplifier limits the sensor’s time resolution and scales as
𝜎TDC : an adequate TDC will make this term negligible
X
X
X
physics
detector
electronics

## Slide 7: Toward an optimized 3D sensor design
𝜎un
  The detector signal is produced by the drift of the charge carriers created along the path of the (charged) particle across the pixel volume, which creates an instantaneous current defined as
  where is the weighting field and is the carrier’s drift velocity. To have signals that do not depend on where the charged particle has crossed the detector 
  (1) make uniform by design and (2) work in a velocity saturation regime
𝜎ej
  To fully exploit the sensor capabilities, one needs to reduce the front-end amplifier noise (increasing the sensor’s thickness is usually not an option)
 TimeSPOT 3D trench-type silicon pixel detectors

## Slide 8: A custom full sensor simulation: TCoDE
The carrier motion is calculated using a 4th order Runge-Kutta algorithm and the thermal diffusion equation
The contribution of each carrier to the current induced on the readout electrode is determined with the Ramo theorem
TCoDE usess a multi-threaded approach (based on the Hydra libraries): each carrier is followed in separate threads, either in CPU or GPU
https://github.com/MultithreadCorner/Tcode
TCAD

## Slide 9: Why another custom simulation?
Example: simulating 50 charged 10 GeV pions crossing a TimeSPOT pixel with GEANT4 and reconstructing the induced signals with TCoDE:
1h40’ in single-thread on an Intel®Xeon®CPU X5450 (10 GB RAM)
Estimated that a similar simulation would take 2-3 months using TCAD on the same hardware
About 2’ in multi-thread on a gaming laptop

## Slide 10: Comparison between 3D geometries
Simulated weighting field and velocity maps are much more uniform in the trench geometry - both in magnitude and direction
This is essential to guarantee, via Ramo theorem, signals which are largely independent on where the charged particles crossed the detector
5 columns
3D trench
TCAD simulations, Vbias = – 100 V

## Slide 11: Comparison between 3D geometries
Charge collection curves (top) and total charge collection vs. impact point 2D maps (bottom) obtained with 3000 simulated MIPs uniformly crossing a 3D pixel over its active area, in three different pixel geometries (5 and 9 columns, trench)
 Shorter and much more uniform charge collection time for the 3D trench geometry
TCAD+TCoDE simulations, Vbias = – 100 V

## Slide 12: The trench-type TimeSPOT 3D pixels
55 µm x 55 µm pixels (to be compatible with existing FEE, for example the Timepix family ASICs)
In each pixel a 40 µm long n++ trench is placed between continuous p++ trenches used for the bias
150 µm-thick active thickness, on a 350 µm-thick support wafer
The collection electrode is 135 µm deep

## Slide 13: The TimeSPOT 3D sensors fabrication
Single sided (Si-Si) process with a support wafer
Two batches were produced in 2019 and 2021 at Fondazione Bruno Kessler (FBK, Trento, Italy) using the Deep Reactive Ion Etching Technique (DRIE) Bosch process, 6” wafers
High aspect ratios (30:1) and good dimensional uniformity
Photolithography performed with a stepper machine (min. feature size 350 nm, alignment accuracy 80 nm, max. exposure area 2x2 cm2)
Many devices were designed and fabricated (single, double pixels, 10 pixel-strips, various pixel matrices, …)

## Slide 14: Characterization of 3D trench pixels with custom FEE
We have characterized single-pixels and various pixel-strips (10-30 pixels) test structures, connected to home-made custom front-end electronics boards featuring a two-stage transimpedence amplifier made with fast SiGe BJTs - to fully exploit the sensor speed one needs to readout the sensor’s current
1 pixel
1 pixel-strip
3 pixel-strip

## Slide 15: Testing 3D pixels in the lab
The complete characterization of these very high-performance sensors also needs to be performed in the laboratory with a dedicated setup – to verify that the whole pixel area is active and how it performs from the timing perspective
At INFN Cagliari we developed a new testing station
  1030 nm, 100 fs, 2 nJ per pulse, 40 MHz laser
  Pulse-picker to select pulses down to O(kHz)
  Mono-mode fiber to the microscope laser port
  Pin-hole to collimate laser spot on microscope image plane
  IR camera to verify sensor position and laser focusing depth
  XY 3D sensor moving system for automatic sensors’ scans
  4 ch. 20 Gs/s 8 GHz oscilloscope for waveform readout

## Slide 16
At 1030 nm, ~1/3 of the laser pulse energy is absorbed in 150 µm of Si
Both optics provide a quasi-cilindrical energy deposit in the sensor; this emulates a MIP crossing the sensor
150 µm
5x
20x
Camera
Objective (5X, 10X or 20X)
Fiber port with pinhole
20x

## Slide 17: Measurements with IR laser
We measure, over the full pixel area:
  DUT amplitude response vs. position
  DUT timing performance vs. position
Calibration of deposited energy based on test beam data
To precisely characterize the DUT time response, we require an accurate (~ 1 ps) time reference:
  Use previous laser pulse (40 MHz laser jitters <<1ps)
  Measure the same laser pulse with another sensor providing the required time stamping accuracy
pixel
Averaged DUT signal
Averaged REF signal

## Slide 18: Time reference accuracy
Laser reflection from a mirror (unfocused)
t
New FEE board with 3D sensor
Vbias = -50V
~10 MIP deposit
Sub-ps timing accuracy can be obtained with a TimeSPOT 3D multi-pixel sensor with custom FEE using a laser intensity providing an energy deposit equivalent to ~10 MIPs

## Slide 19: Amplitude and ToA maps
Amplitude map: in yellow where the laser could properly excite the pixel, i.e. no metal on top
Time of Arrival map: for this particular pixel @50V bias, the max. timing spread is less than 20ps
x (µm)
y (µm)
Average Time of Signal Arrival (ns)
y (µm)
x (µm)
pixel

## Slide 20: Example: Trench vs Hexagonal geometries
(Half) 3D trench pixel
3 ps
130 ps
Hexagonal pixel
100 V
100 V
x (µm)
y (µm)
y (µm)
x (µm)
ToA (ns)
ToA (ns)
200 ps
20 ps
For excellent timing performance, ToA uniformity is the key element

## Slide 21: 2022 SPS/H8 beam test measurements
180 GeV/C π+ beam
106 pions per spill (4 sec.) on a beam spot of 8mm RMS transverse size
2 MCP-PMTs on the beam line to time-stamp the arriving particle (σavg = 5 ps)
One fixed sensor (DUT). Another sensor, used as trigger, is mounted on piezoelectric slides to precisely align the two 3D sensors with beam. All is mounted in a RF-shielded box
Readout with 8 GHz bandwidth 20 GS/s scope, trigger on the AND of one 3D sensor and one MCP-PMT
Possibility of operating the fixed sensor down to -40°C using dry ice to test irradiated sensors
π+ beam
MCP1 (trigger)
Sensor 1 on piezo
(trigger)
Sensor 2
(DUT)
MCP2
MCP1
MCP2
Sensor1
Sensor2 (DUT)

## Slide 22
π+ beam
π+ beam
Pt100

## Slide 23: Pixel waveforms data analysis
For each sensor’s waveform:
  Signal baseline (red-dashed line) is evaluated on an event-by-event basis
  The signal amplitude A is measured (w.r.t. to the event baseline)
  Signal time of arrival evaluated with various methods:
    Leading-edge: time at 20mV signal amplitude, linear interpolation around threshold
    Spline: a traditional CFD at 35% with rising edge interpolated with a spline
    Reference: subtract each waveform from a delayed (by half of the signal rise time) copy of itself, then on the resulting signal we trigger at X/2 height

## Slide 24: Single 3D pixel - amplitude
Non-irradiated pixel
Normal pion incidence
Unbiased trigger – i.e. not triggering on DUT
The shape of the Landau distributions as a function of Vbias indicate a very good sensor performance even at low Vbias
Preliminary

## Slide 25: Single 3D pixel – timing performances
3D pixel time distribution w.r.t. MCP-PMTs: symmetric with only a small tail due to late signals
Time distribution fitted with two gaussians, slightly time shifted, to include late signal contributions
Excellent timing performances with CFD-based methods, but also using a leading edge algorithm
𝜎eff = 11.5 ps
@ 100V
Preliminary
Preliminary

## Slide 26: Efficiency: setup
Trenches (5 µm wide) are non-active volumes, channeled particles will not be seen
Tilt the sensors with respect to normal incidence to recover geometrical efficiency
Efficiency is measured by triggering on the single pixel (55 µm x 55 µm, on piezos) centered on the triple strip (165 µm x 550 µm, the DUT) and counting the fraction of signals seen by the DUT (reaodut by a single FE channel)
Rotate the DUT around the trench direction
π+ beam
Single pixel (trigger)
Triple strip (DUT) @ 20°
π+ beam

## Slide 27: Efficiency: the method
Plot the time distribution of all triple-strip signals w.r.t. MCP-PMTs and count as ‘seen’ the ones under the peak
3D pixel detection (geometrical) efficiency at normal incidence is in agreement with calculated fraction of active area
𝜀 = seen/all
At normal incidence
Preliminary
Preliminary
(red line includes noise contribution)

## Slide 28: Efficiency: results
π+ beam
The inefficiency (at normal incidence) due to the 3D pixel dead-area of the trenches is fully recovered by tilting the sensors around the trench axis at angles larger than 10°
@100V Vbias
Total signal amplitude on triple strip
Preliminary
Preliminary

## Slide 29: Tilted sensors: timing performances
Rotation 1
Rotation 2
Preliminary
Single Pixel @ 50V
Rotation 2
Rotation 1
π+ beam

## Slide 30: Tilted sensors - time distributions
In a tilted sensor, every charged track crosses both fast and less-fast regions of the pixels, thus providing a more uniform timing response
Note that 3D detectors are required to be operated titled w.r.t normal incidence to recover the detection efficiency
@ 0°
@ 10°
@ 20°
Single Pixel
Single Pixel
Single Pixel
Preliminary
Preliminary
Preliminary

## Slide 31: Charge sharing
A 4-channels analog FEE board was used to measure the charge sharing between two adjacent pixels (DUT)
A single pixel, used as trigger, defines where the beam impacts on the DUT
The two adjacent pixels, the single pixels used as trigger and one of the two MCP-PMTs were acquired with the oscilloscope
π+ beam
Single pixel (trigger)
DUT

## Slide 32: Charge sharing: results
When a particle crosses two pixels we define a cluster:
  the cluster amplitude is the sum of the two pixels individual amplitudes
  the cluster time of arrival (ToA) is the average of the two pixels ToAs weighted with their amplitudes
The cluster total amplitude follows the expected Landau distribution
The cluster ToA is more accurate than the ToA from each of the two individual pixels
@ 20° tilt angle
Preliminary
Preliminary
1
2

## Slide 33: Irradiated sensors – the setup
3D sensors were irradiated at the Triga Mark II reactor at the Jožef Stefan Institute in Lubjiana, Slovenjia
Fluences: 1015, 1016 and 2.5·1016 1MeV neq, sensors not annehaled
2.5·1016 1MeV neq is what one would expect on LHCb vertex detector after LHC Run5 on innermost sensors
Irradiated sensors were tested below -20°C to reduce leakage current
Characterization of irradiated single pixels and triple-pixel-strips structures
π+ beam
Single pixel (trigger)
DUT
Dry ice
Dry ice

## Slide 34: Irradiated sensors – working point
With a slightly larger bias voltage (w.r.t. non-irradiated pixel working point ) the signal amplitude of irradiated sensors is recovered!
Single pixel non irradiated – 0°
Increasing HV
Preliminary
Preliminary
1

## Slide 35: 3D irradiated pixel – timing performance
Excellent time resolution (𝜎eff = 10.3 ps) measured at 150V on a single pixel irradiated with fluences of 2.5·1016 1-MeV neutron equivalent
@150V, 0°
𝜎eff = 10.3 ps
Preliminary
Preliminary
1

## Slide 36: Irradiated sensors – efficiency
π+ beam
The inefficiency (at normal incidence) due to the dead-area of the trenches is fully recovered by tilting the sensors around the trench axis also for sensors irradiated with fluences of 2.5·1016 1-MeV neutron equivalent
@130V Vbias
Preliminary
Preliminary
(100V)
1
Triple pixel-strip

## Slide 37: Conclusions
Unprecedented results on trench 3D trend silicon pixels timing performances have been presented
The time resolution of a single 3D trench pixel sensor was measured at SPS/H8 with a 180 GeV/c π+ beam and found to be of about 11ps @ Vbias = 100V (dominated by FEE noise)
The sensor detection efficiency is fully recovered for incident angles larger than 10° with respect to normal incidence
Sensors irradiated at a fluence of 2.5·1016 1-MeV neq at Vbias exceeding 100V perform as the non-irradiated sensors, both in timing performances and in efficiency
3D devices confirm their expected theoretical performance in timing and the trench geometry appears to be the right direction to go
VERY IMPORTANT: The front-end electronics is the limiting factor to the system performance

## Slide 38: … and Outlook
The TimeSPOT collaboration has developed and produced an ASIC (CMOS 28nm) to read a small pixel matrix
3D pixel matrices has just been bump-bonded to ASICs and the assemblies are being tested in the laboratory with laser and radioactive sources
 see Adriano Lai’s talk

## Slide 39: Thank you very much!
Publications by the TimeSPOT Collaboration
  3D trenched-electrode sensors for charged particle tracking and timing, NIM A, (2019)
  Simulation of 3D-Silicon sensors for the TIMESPOT project NIMA, 936-, (2019)
  Development of 3D trenched-electrode pixel sensors with improved timing performance JINST, 14-, C07011 (2019)
  Sensors, electronics and algorithms for tracking at the next generation of colliders NIMA, 927-, (2019)
  Combined TCAD and Geant4 simulations of diamond detectors for timing applications NIMA, 936-, (2019)
  A Timing Pixel Front-End Design for HEP Experiments in 28 nm CMOS Technology, 15th Conference on Ph.D. Research in Microelectronics and Electronics, 2019
  First results of the TIMESPOT project on developments on fast sensors for future vertex detectors, NIMA, 2020
  Timing characterisation of 3D-trench silicon sensors, JINST, 2020
  Intrinsic time resolution of 3D-trench silicon pixels for charged particle detection, arXiv:2004.10881, JINST, 2020
  High-resolution timing electronics for fast pixel sensors, arXiv:2008.09867, to appear in JINST
  A. Loi et al., Timing Optimisation and Analysis in the Design of 3D silicon sensors: the TCoDe Simulator, JINST (2021) 16:P02011
  D. Brundu et al., Accurate modelling of 3D-trench silicon sensor with enhanced timing performance and comparison with test beam measurements, JINST 16 (2021) 09, P09028.
  L. Piccolo et al., First Measurements on the Timespot1 ASIC: a Fast-Timing, High-Rate Pixel-Matrix Front-End, arXiv:2201.13138
  Brundu D, et al. (2022) Modeling of Solid-State Detectors Using Advanced Multi-Threading: The TCoDe and TFBoost Simulation Packages. Front. Phys. 10:804752. doi: 10.3389/fphy.2022.804752

## Slide 40: Backup Slides

## Slide 41: Simulating energy deposits in silicon pixels
The charge deposits in simulation are obtained using GEANT4 (for MIPs) or analytically (for IR and red laser beams)
MIP
IR laser
X10 obj.
Red laser
X10 obj.
IR laser
X5 obj.

## Slide 42: DC electrical characterization of 3D trench pixels
IV-curves on 18x18 pixel matrices (pixels connected with temporary metal): ~10 pA/pixel – good!
Measured pixel capacitance ~100 fF/pixel in agreement with simulation
Full depletion @ ~7V
MOS capacitor effect

## Slide 43: Fitting the time distribution: 𝜎eff
where f1 is the fraction of the Gaussian core and μ is defined as
𝜎eff takes into account the two-Gaussian behaviour