## Slide 1: 12 T Robust CERN Models: Nb3Sn Wire and Cable
Simon C. Hopkins

## Slide 2: Similar Cable/Strand Experience (1)
Baseline: 40-strand cable of 1 mm diameter strands
  FalconD Cable Spec: EDMS 2663170
  cf. HL-LHC, 108/127
Ref | Name | Keystone | Width (mm)* | Strand Types
C01 | FalconD | 0.5° | 20.95 | 162/169, R&D (TVEL, KAT)
H11 | FRESCA2 | 0° | 20.95 | 132/169, PIT
H19 | ERMC | 0° | 20.95 | 150/169, 120/127
* width spec for FalconD set to 20.95 mm to match production experience for ERMC, FRESCA2

## Slide 3: Similar Cable/Strand Experience (2)
RRP layouts with relevant cabling experience at CERN:
 | 108/127 | 132/169 | 150/169 | 162/169
Layout |  |  |  | 
Cu/non-Cu | 1.15-1.2 | 1.25 | 1 | 0.9
deff (µm) | 60 | 52 | 52 | 52

## Slide 4: Current Density
For strand, can anticipate:
  specified non-Cu Jc 2450 A/mm2 (4.2 K, 12 T)
  typical non-Cu Jc ~2800 A/mm2 (4.2 K, 12 T), and Je ~ 1250–1400 A/mm2, depending on chosen Cu/non-Cu, Sn stoichiometry and heat treatment
    Conservative optimisation might suggest reduced Sn (cf. HL-LHC), deff < 60 µm, Cu/non-Cu > 1, RRR >> 100 as cabled; but available data (axial strain, transverse stress, stability…) to be reviewed

## Slide 5: Jc (DEM-1.1 & ERMC-1)
Jc distribution as measured by the supplier (nominally 4.2 K) and CERN (mean 4.26 K) Standard heat treatment; supplier Cu/non-Cu values used for consistency.
DEM-1.1 665 °C
ERMC-1 650 °C