## Slide 1
Stability Studies of High-Quality Concrete Slab Floors at the ESRF
IWAA2022 CERN
David Martin ESRF

## Slide 2: Outline
The ESRF
ESRF site movement signatures
Behavior of concrete slabs

## Slide 3: The ESRF
13 Member states:
France 27.5 %
Germany 24 %
Italy 13.2 %
United Kingdom 10,5 %
Russia 6 %
Benesync 5,8 %
(Belgium, The Netherlands)
Nordsync 5 %
(Denmark, Finland, Norway, Sweden)
Spain 4 %
Switzerland 4 %
8 Associate countries:
Austria 1.75 %
Israel 1.75 %
Poland 1 %
Portugal 1 %
India 0.66 %
Czech Republic 0.6 %
South Africa 0.3 %
Hungary 0.25 %
21 partner nations
Annual budget: ~115 million euros
Members of staff: 630 of 40 different nationalities
Legal status: Private civil company subject to French law
Contribution to the budget in %

## Slide 4: The ESRF
A ESRF is composed of two main elements:
A particle accelerator that generates synchrotron radiation – the source,
Beamline(s) that use the synchrotron radiation generated by the accelerator to study matter.
The linear accelerator (linac) accelerates the electrons from rest mass to 100 MeV
The booster accelerates the electrons from 100MeV to 6GeV
The storage ring keeps the electrons circulating at 6GeV for many hours
The 6GeV electrons produce synchrotron radiation in a tangential direction to the beam travel

## Slide 5: The ESRF X-rays for science
Scientists use the ESRF to explore everything from exotic states of matter to snake fossils to the reason why chocolate sometimes develops a white film when it melts …

## Slide 6: ESRF Upgrade programme
- Construction of 19 new-generation experimental stations to explore the nanoworld
- Creation of a new ultra-stable experimental hall
- Improvement and refurbishment of most of the cutting-edge scientific equipment and accelerator infrastructure
2009
2015
Upgrade PHASE I – 160 M€
In time and within budget
- Construction of a new storage ring –the EBS, inside the existing structure, with performance increased by a factor of 100
- Construction of new state-of-the-art beamlines
- Ambitious instrumentation programme (optics, high-performance detectors)
- Intensified big data strategy
2015
2022
ESRF-EBS – 150 M€
Launched in June 2015

## Slide 7: Alignment – one of the defining characteristics of the UP1 and EBS
Loading case of long term movements | Response performance to loading
Slab thermal stability with respect to the inside hall temperature set point and the external temperature variation over a 12 hour period | Anywhere within a solid disk of 5 metres radius over a 12 h period ▪ Vertical deflections < 2 µm ▪ Rotation angle < 200 nrad
Daily external ambient temperature changes ΔT=20 C | Anywhere within a solid disk of 5 metres radius over a 24 h period vertical differential movement of ▪ < 1 µm ▪ < 100 nrad Anywhere on the Golden Slab except at distances closer than 1.5 m from the edge.
Vertical deformation due to medium term settlement | ≤ 250 µm peak to peak displacements anywhere in a disk of 60 diameter over a period of 12 months starting one year after building completion.
Golden Slab deformation due to settlement: Long term | Differential movement ≤ 5 mm peak-to-peak anywhere in a circle of 200 m diameter, measured on the EXPH2 slabs over a period of 10 years
Upgrade Programme Phase I
EBS - UP Phase II
Note EBS will be discussed in detail :
03 November 2022, 09:45 AM (Machine)
04 November 2022, 11:05 AM (Beamlines)

## Slide 8: Context - ESRF Site Movement signatures
At the ESRF, there are several well known site movement signatures …
The ESRF is located:
between the Chartreuse and Vercors mountain ranges so there are geological influences.
between the Drac and Isère rivers so there are geomorphological influences.
upriver of the Saint-Égrève dam which is emptied periodically changing the level of water in the rivers and ground water.
on an old glacial lake bed – the underlying soil profile is relatively homogeneous clay overlaid by alluvial material.

## Slide 9: Grenoble Basin
A study based on levelling of the Grenoble basin between 1880 and 2001 shows …
Several things appear to be happening:
The center of the Grenoble basin is sinking (48 mm between 1989 and 2001, > 40cm since 1880).
The Chartreuse range is slowly separating from the Vercors.
These observations indicate the ESRF has tilted ~ 5 mm towards the Vercors over 11 years or so.
Movements 1989 to 2001*
*Mesure de l’affaissement actuel de la cuvette grenobloise par comparaisons de nivellements, Menard G., Pôle Grenoblois Risques Naturels

## Slide 10: ESRF vertical movements in the Grenoble basin context
It is difficult to confirm this tilt across the site with our observations.
If the whole site is sinking it is not very important…
However, several things are happening:
The center of the site is sinking,
The area at the confluence of and along the two rivers is sinking,
The central office building is sinking,
The SR is relatively stable.
c)
a)
b)
d)

## Slide 11: Long term horizontal deformation
C01
C17
0 mm
+2.5 mm
-3.5 mm
The ESRF site, and machine are stretching along the valley and river axes…

## Slide 12: Long term Vertical deformation
C01
C17
0 mm
+2.5 mm
-3.5 mm
The ESRF site, and machine are tilting across the valley as we have already observed…

## Slide 13: Deformation due to dam purging
C01
C17
0 mm
+0.4 mm
-0.4 mm
The ESRF site, and machine bend up towards the adjacent rivers…

## Slide 14: Movements at the slab joints
Joint
Crack
January to August
August to January
There are movements between girders of the old SR of ±150 µm per year.

## Slide 15: Horizontal Movements at the slab joints
Interestingly WPS observations show even larger horizontal movements across the slabs joints …

## Slide 16: BM18 tests July 2009 to September 2011
This HLS was installed to determine the deformation of the slab under a charge of 5T.
However, it was also observed that the slab was bending – apparently as a function of temperature change

## Slide 17: BM18 slab bending as a function of temperature change
This discovery was made at the start of the Upgrade Programme High Quality Slab (HQS) study. It led to more detailed studies of slab bending…

## Slide 18: Briefly what is a beamline?
A beamline can be thought of in three ways:
  It’s a physical space within the experimental hall.
  It’s also a set of equipment that brings the X-ray beam to the material being studied and records what happens.
  And most importantly, it’s a dynamic meeting place, where scientists and staff collaborate to answer leading-edge research questions.
X-ray source
X-ray optics
Sample and detector

## Slide 19: Alignment – one of the defining characteristics of the UP1 and EBS
Loading case of long term movements | Response performance to loading
Slab thermal stability with respect to the inside hall temperature set point and the external temperature variation over a 12 hour period | Anywhere within a solid disk of 5 metres radius over a 12 h period ▪ Vertical deflections < 2 µm ▪ Rotation angle < 200 nrad
Daily external ambient temperature changes ΔT=20 C | Anywhere within a solid disk of 5 metres radius over a 24 h period vertical differential movement of ▪ < 1 µm ▪ < 100 nrad Anywhere on the Golden Slab except at distances closer than 1.5 m from the edge.
Vertical deformation due to medium term settlement | ≤ 250 µm peak to peak displacements anywhere in a disk of 60 diameter over a period of 12 months starting one year after building completion.
Golden Slab deformation due to settlement: Long term | Differential movement ≤ 5 mm peak-to-peak anywhere in a circle of 200 m diameter, measured on the EXPH2 slabs over a period of 10 years

## Slide 20: ESRF long beamlines alignment tolerances
To respect tolerances we must know the stability characteristics of the ground and the floor that everything is built on - and influence they have.
The size of the focused x-ray probe spot depends on:
  the source size,
  the distance between the source and the focusing optics p, and
  the working distance between optics and the experimental sample q.
  At the ESRF p=150 m and q=0.05 m so q/p=3000-1 → theoretical probe size ~10 nm

## Slide 21: Long Beamline Translation tolerance
Tolerance is 10% of 50 nm probe size e = 5 nm

## Slide 22: Long Beamline Rotation tolerance
Tolerance is 10% of 50 nm probe size e = 5 nm

## Slide 23: Alignment – one of the defining characteristics of the UP1 and EBS
Machine | U(L) [μm] | U(R) [μm] | U(Z) [μm]
Long. Varying field dipoles | 1000 | >100 | >100
High gradient quadrupoles, Combined function dipoles | 500 | 60 | 60
Medium gradient quads | 500 | 100 | 85
Sextupoles | 500 | 70 | 50
Octupoles | 500 | 100 | 100
Maximum permissible error 2.5σ
There were two key constraints for EBS
first respect the magnet (and other) alignment tolerances
… and second ensure the new machine was in the same place as the old machine to minimize disturbance to the functioning beamlines.

## Slide 24: Movements at the slab joints
Joint
Crack
Movements at the slab joints were directly observed in the orbit of the old SR machine.

## Slide 25: EBS machine tolerances
Before the construction of EBS we discussed extensively what these tolerances mean and how they could be interpreted to the machine as a whole.
Error “waves” applied to the lattice: DX, DY, Rotations for quad and sext.
Correction performed for each frequency and amplitude.
This is an exercise to verify large errors at long wavelengths are unimportant (next slide).
Simulations were made based on the old SR measured position (below).
Real survey data was used to define the tolerances interpolated to the new EBS machine positions.
Random Gaussian DX DY to represent fiducialisation and local alignment errors in quadrupoles and sextupoles were added on top of the survey errors.
In the definition of tolerances girders are unnecessary – they are replaced by the simulated machine survey.
Alignment meeting | SOLEIL-ESRF Zoom | April 2022 | S.M.Liuzzo
Nominal Position
+1.1 mm
-2.1mm
Horizontal
Nominal Position
+0.8 mm
Vertical
-1.2 mm

## Slide 26: Long range errors: error envelope function
Impact of error “waves” on horizontal orbit
At a wavelength of L/128~6m 30 um errors amplitude give 30 um residual orbit distortion.
At a wavelength of L/2~422m 7mm errors amplitude give 30 um residual orbit distortion.
Slow, large variations have limited impact on the optics!
Alignment meeting | SOLEIL-ESRF Zoom | April 2022 | S.M.Liuzzo
Residual orbit after closed orbit correction

## Slide 27: Characteristic Thermally induced slab bending
NECS (Numerical Engineering & Consulting Services SAS), “«Etudes de Stabilité du Golden Slab»- Comportement Thermomécanique Tenant Compte des Charges Statiques, et des Déformations Différées Dues au Séchage du Béton, Note Technique - Rapport d’Etudes Paramétriques”, N001_A143_2010_ESRF_A,26 May 2010
It is assumed bending results from thermal gradient variations through the slab.

## Slide 28: Chartreuse (Belledonne, ID16) HQS HLS studies
ID27
ID28

## Slide 29: Id27 AND id28 MAX AND MIN BENDING OVER TWO YEARS

## Slide 30: BM19 HLS
To study carefully slab thermal bending an extensive HLS was installed on BM19 Slab1a and Slab1b in November 2021.
Recall, when the EXPH floor was build in 1990-91, four steel reinforced slabs were poured along each beamline from the port end to the freeway. A surface joint was then cut at the middle of each slab. In reality, these surface joints run through the depth of the slab, and despite reinforcement between slab parts, they act independently. So there are actually 8 slabs along a given beamline between the port end and the freeway.

## Slide 31: BM19 HLS
11/2014 to 05/2015 6 months
Recall ID27
Observations on BM19 for roughly 6 months between November 2021 and May 2022 show movements that are qualitatively similar to those observed on ID27 in 2014-15.
The bending between the start and the maximum in March is highly characteristic.
maximum

## Slide 32: BM19 HLS floor Tilt
Tilt along the beam
Tilt across the beam

## Slide 33: BM19 HLS floor Movements as a function of time
Range of movement
Standard Deviation of movement
Some key points:
  Peak at 8 to 12 hours,
  SD greater than 10 um after 24 hours, and greater than 100 um after 4 weeks,
  Range greater than 10 um after 2 hours, and greater than 100 um after 2 to 3 days.
Note these graphs are created using 1000 samples of each specified period (e.g. 24 hours) over the entire period November 2021 to May 2022

## Slide 34: BM19 HLS floor Tilt on beam axis for different time periods
Note these graphs are created using 1000 samples of each specified period (e.g. 24 hours) over the entire period November 2021 to May 2022
A key point:
  Tilts near and on the beam axis are less variable on slab1b than slab1a. This is because the beam axis is much closer to the edge of the slab1a.

## Slide 35: Variable Movements for a change in temperature of 1°C
ID03
ID14
BM18
A study was made that shows variations in thermally induced movements between different parts of the EXPH.
ESRF-TS-ALGE/2202DM, Final ID03 HLS slab study and a detailed slab thermal bending study for ID03, ID14 and BM18, 23/09/2021

## Slide 36: Conclusion
In summary and ignoring vibration:
  Dam purging and associated ground water variations produce a smooth deformation over the entire ESRF site. Movements typically last less than a week.
  Movements due to the adjacent rivers, geomorphology and geology are also smooth but take place over years to decades.
  Slab movements occur on 12 hour and 6 month cycles. They can produce sharp discontinuities at the joints between adjacent slabs.
  Slab bending produces both vertical and horizontal displacements and tilts that can have an adverse effect on both machine and beamline performance.
Slab Diurnal
Geologic
Slab Semi-annual
Dam Purging/Ground Water
Vibration
6 months
12 hours
Years
Decades
Days
< 1 second
Magnitude
Geomorphologic - Rivers
All slabs bend, and their movements can impose an upper limit on alignment if their behavior is not properly considered!